NAMIBIA UNIVERSITY OF SCIENCE AND TECHNOLOGY

FACULTY OF ENGINEERING

DEPARTMENT OF CIVIL AND ENVIRONMENTAL ENGINEERING COMPREHENSIVE STUDY ON THE IMPACT OF USING AGRICULTURAL

RESIDUES FOR ENHANCING BUILDING ENERGY PERFORMANCE IN NAMIBIA

By

Onjefu Leonard Agbo

216104017

A final thesis submitted to the Department of Civil and Environmental Engineering in the Faculty of Engineering at the Namibia University of Science and Technology in partial fulfillment of the requirements for the award of a Ph.D. in Structural/Material Engineering

degree

November 2020

ATTESTATION

I, Onjefu Leonard Agbo, declare that this is my work. The work has not been previously submitted to any other University or similar Institution for any degree. I also declare that as required by the Namibia University of  Science  and  Technology  (NUST)  academic  honesty  and  integrity, I  have  cited  and

referenced all information that is not my work.

Onjefu Leonard Agbo	Date

Copyright © 2020 Namibia University of Science and Technology

All rights reserved

RETENTION AND USE OF THESIS

I, Onjefu Leonard Agbo being a candidate for the degree of Ph. D (Structural Engineering specialisation) in the Department of Civil and Environmental Engineering accept the requirements of the Namibia University of Science and Technology relating to the retention and use of the thesis deposited in the Library and Information Services.

About this condition, I agree that the original copy of my thesis deposited in the Library and other Information Services will be accessible for study and research purposes, following the normal conditions documented by the Librarian for the care, loan, or reproduction of these.

Signature: .................................................                                                         Date: ...................................

DECLARATION OF SUPERVISION

We the undersigned hereby declare that we have thoroughly monitored and supervised all components of this thesis work with a high level of professionalism. We are confident that all results and statements are from the authors and those from other authors are adequately cited.

…………………………………………….                                               Date: ………………………………

Prof. Victor Kamara

Main Supervisor

……………………………………….                                                                 Date: ………………………………..

Prof. Paul Chisale

Co-Supervisor

ACKNOWLEDGEMENTS

My profound gratitude goes to the Almighty God who in His infinite mercy has allowed me to

share in His abundant love and mercy. “TO GOD BE THE GLORY”.

I am sincerely grateful to my supervisors Prof. Victor Sorie Kamara and Prof. Paul Chisale who despite their very tight schedule patiently saw me through to earn my Ph.D. degree in Civil Engineering. Moreover, I owe a debt of gratitude to the Staff of the Namibia Energy Institute, especially Mr. Penti Isaiah for helping with the data logger and Mrs. Iileka Helvi for her assistance in providing space and financing the prototype design Rigs building at the Energy Efficient Building Namibia (EEBN). Also, not left out are the staff members of the Civil and environmental engineering who contributed to making this work a reality.

I am deeply indebted to my wife Josephine Onjefu for her patience and prayers and my children Favour Onjefu, Redeemer Onjefu, and Treasure Onjefu are known for their support and love throughout my study. Posterity will judge me if I fail to acknowledge my parents, Sir Emmanuel Onjefu and Lady Veronica Onjefu for their motivations and encouragement. Also to my brothers and sisters, I say thank you for your encouragement.

I offer my deep appreciation to my Patrons Deeper Life Campus Fellowship Prof. Sunday Reju, Mr. Kenda, and my National Overseer deeper Christian Life Ministry Namibia Pastor Paulus Shilongo who supported me with prayers and encouragement.

Lastly, I offer my deep appreciation to Prof. Nnenesi Kgabi who motivated me to apply for funding. Again, this work would not have run smoothly without the financial support of the National Commission on Research, Science, and Technology (NCRST), I appreciate it.

ABSTRACT

This research work aimed at an understanding of the impact of using local agricultural residues to enhance building performance in Namibia. As human lifestyles improved with the emergence of high economic growth and technologies, the increasing demand for energy in Namibia as a developing country is posing a serious challenge to government and lawmakers in the allocation of funds for appropriate researches and technologies. One such appropriate kinds of research involve developing appropriate material technologies that will improve energy efficiency in the form of using agricultural residues/wastes readily available in Namibia.

Like other developing countries, the building sector accounts for approximately 40% of total energy

usage in Namibia. For that purpose, the efficient use of energy within buildings is a needed requisite to alienate against rising energy costs and contribute towards decreasing global greenhouse gas emissions. Namibia´s energy usage of buildings closely reflects these global trends and this research therefore aimed at validating its results through the construction of rigs following the design concept of the prototype of the EEBN (Energy Efficient Building in Namibia) research project at the Namibia University of Science and Technology campus that was designed, constructed and equipped through funding from EEP (Energy Efficiency Programme), in partnership between NUST and Carinthia University of Applied Sciences Austria.

Through appropriate mixed designs of well-selected locally available agricultural residues, insulating boards and bricks of standard sizes were developed, and results validated through the construction of rigs. Thermal conductivities and transmissibility of the insulating boards together with compressive strength, water absorption were also measured for bricks to measure the degree of thermal effectiveness/efficiency of a standard residential building.     This is to establish how the use of affordable and readily available local materials can be used to develop high-quality and energy- efficient building materials which when used in building construction will improve the comfort level of occupants without the use of conventional heating and cooling devices.

Vary mixed percentages of residues of maize, millet, rice, and cow dung were designed to develop eleven 220cm by 110 cm by 40 cm board samples (labelled AK) from residues of maize, millet, rice, and cow dung. The samples were compacted, sun-dried for 7 days, and tested for thermal conductivity and thermal resistivity using a thermal conductivity test machine EP500e. Results from the eleven samples tested revealed that sample C (composed of 10% maize, 10% millet, 30% rice, and 40% cow dung) gives the lowest thermal conductivity (i.e.

of 54.65 mW/(m*K)) and the highest thermal resistivity (i.e. 0.6935 m2K/W), hence a very good thermal efficiency as compared with sample A (composed of 40% maize, 30% millet, 10% rice and 20% cow dung) that gave the highest thermal conductivity and lowest thermal resistivity, hence considered poor thermal efficiency. Regression analyses conducted between the best (i.e. sample C) and the worst (i.e. sample A) revealed an R2 value of 95% and 91% respectively

Test rigs were constructed and equipped with appropriate devices both inside and outside. Wide- ranging measurements were conducted, and results related to thermal behaviour of the interior at fluctuating changes in temperature at the exterior especially at extreme summer and winter periods were obtained.

The three prototype Rigs, with varying compositions, were designed and built using standard building procedures. Rig A (TAR 1) with 150 mm thick internal and external walls; made of standard bricks of 7 MPa, insulated with a compacted mixture containing 20% (wt.) Maize, 10 % (wt.) Millet, 30% (wt.) Rice and 40% (wt.),

30% (wt.) Cow dung; Rig B (Tamb2) 40% (wt.) with Maize, 30% (wt.), Millet, 10% (wt.), 20% (wt.), 20%wt. Marble dust and C (TNo3) that serve as control rig. Outside and inside temperatures of the Rigs were monitored during the warm (September 2017 - March 2018) and cold (April to August – 2018) seasons. Temperature and humidity sensors installed at critical positions in the interior of the building were connected to the symmetron data logger. Results of the three design concepts revealed that TAR 1 (Rig A) attained maximum and minimum temperatures of 24.40C and 14.80C, and humidity of 26.4% during winter and 29.60C and 19.30C during summer with an average humidity of 21.1%. Tamb2 (Rig B) recorded a maximum and minimum temperature of 31.220C and 18.70C during summer with a relative humidity of 20.3%. During winter Rig B attained an average temperature of 22.600C. Furthermore, Rig C (TN03) recorded 32.220C and 21.700C in summer and winter respectively. From the results, it can be deduced that Rig A (TAR 1) with compositions of 20% (wt.) Maize, 10 % (wt.) Millet, 30% (wt.) Rice and 40% (wt.), 30% (wt.) Cow dung; had the best performance.

Simulation on results obtained from the rigs was also done using Ansys software.

This research showed that results from both software and measured are approximately the same.

vii

LIST OF ABBREVIATIONS

A	Area of heat transfer

A1	Percentage composition of 20% Rice brick husk

CFD	Computational Fluid Dynamics

CH4	Methane

CO2	Carbon dioxide

dEwall	Change in Energy in the wall

DIN	Deutsches Institut für Normung

EE	Energy Efficiency

EEA	 European Environmental Agency EEBN	Energy Efficiency Building of Namibia EEP	Energy Efficiency Programme

EN	European Norms

EPS	 Expanded Polystyrene Ext.AT	 External air temperature EXT.19 External temperature for 2019 g	Gram

GHG	Greenhouse Gas

h	Hour

HVAC	Heating, ventilation, and air conditioning

IEA	International Energy Agency

ISO	International Standards Organisation

K	Kelvin

Kg	Kilo-gram

Ko	 Thermal Conductivity at 0o C K	Thermal Conductivity

MME	Ministry of Mines and Energy

MPa	Mega Pascal

NEEP	National Energy Efficiency Programme

NEI	Namibia Energy Institute N/mm2 Newton per millimetre squared NMSE	 Normalized mean square error NSI	 Namibian Standards Institute

NUST	Namibia University of Science and Technology

βt	Temperature Coefficient of thermal Conductivity

%	Percentage

0C	Degree Celsius kJ	 kilojoule

NH3	Ammonia

NiCr	Ni Nickel Chromium-Nickel q•	Heat flux

Q	Total amount of heat transfer

Q•

in	Heat transfer inside the wall

Q•

out	Heat transfer outside the wall

R	Thermal Resistivity

REEEI	Renewable Energy and Energy Efficiency Institute

RHA1	Relative humidity for rig A RHExt.	External Relative humidity

RHMB2 Relative humidity for rig B containing Marble dust

RHNo3  Relative humidity for rig C with no insulation

SO2	Sulphur dioxide

STAR1	summer temperature of agricultural residue for rig A

ΔT	Temperature difference at the wall

TAR1	Temperature of agricultural residue for rig A

TMAB2 Temperature of agricultural residue and marble dust for rig B TNO3	Temperature for rig C without insulation

TAR1, 19 Temperature of agricultural residue for rig A for data collection in 2019

TMAB,19 Temperature of agricultural residue and marble dust for rig B for data in 2019

TAN19 Temperature for rig C without insulation for data collection in 2019

TIASA	Thermal Insulation Association of South Africa

TRNSYS  Transient system simulation tool

VIP	Vacuum insulation panels

W	Watt

WA	Water Absorption

W/Ft2	Watt per Square feet

WHO	World Health Organization

W/ m2	Watt per square meter

W/ mK	Watt per meter Kelvin

Wt.	Weight

WTO/TBT  World Trade Organization/Technical Barriers to Trade

Δx	Thickness of layer

XPS	Extruded Polystyrene

TABLE OF CONTENTS

ATTESTATION……………………………………………………………………………......................................................….ii

ATTESTATION AND USE OF THESIS…......................................................................................................iii

ACKNOWLEDGEMENTS…………………………………………………………………………………………………………………...iv ABSTRACT………………………………………………………………………………………………………………………...................v LIST OF ABBREVIATIONS…...................................................................................................................viii CHAPTER ONE……………………………………………………………………………………………………………………………...1

1. INTRODUCTION…......................................................................................................................1

1.1 Overview……………………………………………………………………………………..….…………………………………………1

1.2 Key Information about Namibia.……………..………………………………………………………………………………...3

1.3 Climate……………………………………………………………………………………………………………………………………….4

1.3.1 Introduction…………………………………………………………………………………………………………………………….4

1.3.2 Temperature………………………………………………………………………………………………………………………..….5

1.3.3 Precipitation……………………………………………………………………………………………………………………….……7

1.4 Statement Problem ………….………………………………………………….…………………………….………………………8

1.5  Objectives of the Research…………………………………………………………………………………………………………9

1.6. Research hypothesis…………………………………………………………………………………….………………………….10

1.7 Significance / Contribution of Research …………………………………………………………………………..……….10

1.8 Structure of thesis ……………………………..……………………………………..................................................11

CHAPTER TWO……………………………………………………………………………………………………………………….….13

2. Literature Review……………………………………………………………………………………………………………………13

2.1 Overview…………………………………………………………………………………………………………………………………..13

2.2. Agriculture in Namibia……………………………………………………………………………………………………………..15

2.2.1 Importance of Agriculture in Namibia……………………………………………………………………………………16

2.3 Key Agricultural Wastes/Residues: Types, behaviour, usefulness, environmental impact………..16

2.3.1 Pearl millet (Pennisetum glaucum) husk………………………………………………………………………………..17

2.3.2 Rice husks……………………………………………………………………………………………………………………………..18

2.3.3 Maize husks (Zea mays)…………………………………………………………………………………………………………18

2.3.4 Cow dungs……………………………………………………………………………………………………………………………..20

2.3.5 Marble dust…………………………………………………………………………………………………….…………………….20

2.4 Current Building Regulations and Standard ..................................................................................21

2.4.1 Namibia Building Regulations and Standards.............................................................................21

2.4.2 Namibia Energy Efficiency Programme in Buildings (NEEP) ......................................................22

2.4.3 NEEP Baseline Study..................................................................................................................22

2.5 Forms of solar heating and cooling…………......................……………………………………………………………23

2.5.1 Passive solar home system……………………...................………………………………………………………….…23

2.5.2 Building Orientation…………………………………………....................…………………………………………………24

2.6 Energy efficient building in Namibia (EEBN)………………….................………………………………………….24

2.6.1 Energy Efficient Building/House….................………………………………………………………………………….25

2.6.2 Energy analysis of buildings………………………................…………………………………………………………..27

2.6.3.1 Heating and Cooling Load…………………………………................………………………………………………..27

2.6.3.2 Thermal Transmission……………………………………………................……………………………………………28

2.6.3.3 Solar………………………………………………………………………………................……………………………………28

2.6.3.4 Infiltrations……………………………………………………………………………………………….............…………….29

2.6.3.5 Internal loads………………………………………………………………………………………………................………29

2.7 Ventilation systems………………………………………………………………………………………………...............….. 30

2.7.1 Types of Ventilation systems……………………………………………………………………………...............……  30

2.8 Low-energy ventilation systems…………………........................……………………………………………..........30

2.8.1 Air quality……………………………………………………………………………………............................................31

2.9 Psychometrics………………………………………………………………………………………………........................……32

2.9.1 State of air………………………………………………………………………………………………….......................……32

2.10 Thermal comfort…………………………………………………………………………..........................…………………33

2.10.1 Measurement of thermal comfort……………………………………………………..........................…………34

2.10.2 The comfort equation…………………………………………………………………………..................………………34

2.10.3 Heat balance……………………………………………………………………………………………..............…………….34

2.11 Computational fluid dynamics………………………………………………………………………….................……..36

2.12 Mesh…………………………………………………………………………………………………………………......................36

2.13 Mathematical model for heat simulation…………………………………………………………...................…..37

2.13.1 Momentum equations…………………………………………………………………………………...................……38

2.13.2 Energy equation……………………………………………………………………………………………….....................39

2.13.3 Dimensional numbers………………………………………………………………………………………....................39

2.13.4 Nusselt number………………………………………………………………………………………………......................39

2.13.5 Reynolds number…………………………………………………………………………………………......................…40

2.13.6 Grashof number…………………………………………………………………………………................………………..40

2.13.7 Dimensionless temperature…………………………………………………………………...................……………41

2.14 Approximating the differential equation by a numerical equation………………................………….41

2.14.1 The Finite-Volume Methodology…………………………………………………………………................……….41

2.14.2 Discretisation…………………………………………………………………………………………………................…….42

2.15 Building materials………………………………………………………………………………………………................……43

2.16 Insulation materials………………………………………………………………………………………………..................43

2.17 Building thermal system………………………………………………………………………………………....................44

2.18 Building elements and materials………………………………………………………………………….................….45

2.19 Basic Theoretical Information……………………………………………………………………………….................…47

2.19.1   Conduction heat transfer…………………………………………………………………………………................…47

2.19.2 Heat Conduction in Plane Wall………………………………………………………………………….................….48

2.19.3 Heat transfer by convection……………………………………………………………………………...................…48

2.19.4   Heat transfer by radiation……………………………………………………………………………...................….49

2.19.5 Solar Radiation…………………………………………………………………………………………………....................49

CHAPTER THREE………………………………………………………………………………………………………………………...52

3. LABORATORY SETUP, TEST AND MEASUREMENT……………………………………………………………………52

3.1 Overview………………………………………………………………………………………………………………………………….52

3.2 Sample collection…………………………………………………………………………………………………………. 52

3.3 Sample preparation of Particleboard……………………………………………….……………………………..54

3.3.1 Overview……………………………………………………………………………………………………………………54

3.3.2 Preparation of Particleboard/Isolating Material………………………………………………………….54

3.3.3 Preparation and Production of Bricks………………………………………………………………………….59

3.3.4 Preparation of experimental rigs…………………………………………………………………………………61

3.4 Laboratory Tests: Tools, Procedures, and Measurements………………………………………………...62

3.4.1 Overview……………………………………………………………………………………………………………………62

3.4.1.1 Thermal Conductivity Test Tool (EP500)…………………..…………...…………………………………62

3.4.1.2 Water Absorption Test……………………………………………………………………………………………..64

3.4.1.3 Compressive Test…………………………………………………………………………………………………….64

3.4.1.4 Density...................................................................................................................... ............................................64

3.4.1.5 Experimental Rigs……………………………………………………………………………………………………65

3.4.2 Sensors: Types, application, and measurement……………………………………………………………..66

3.4.2.1 Temperature sensors……………………………………………………………………………………………….66

3.4.2.2 Digital humidity and temperature sensors………………………………………………………………...67

3.4.2.3 Meteorological Station……………………………………………………………………………………………..68

3.4.2.4 Symmetron stylitis 101……………………………………………………………………………………………69

3.4.2.5 Data measurement and data collection methods………………………………………………………..70

CHAPTER FOUR………………………………………………………………………………………………………………………….71

EXPERIMENTAL RESULTS……………………………………………………………………………………………………………….71

4.1 Overview………………………………………………………………………………………………………………………………….71

4.2 Results...........................................................................................................................................71

4.2.1 Thermal Conductivity and Resistivity of Insulation / Particleboards..........................................71

4.2.2 Thermal Conductivity of Samples Mixed with Marble Dust.......................................................73

4.2.3 Thermal conductivity of the brick types.....................................................................................74

4.2.4 Physical and mechanical properties of the brick types..............................................................78

4.2.4.1 Water Absorption Results of Bricks.........................................................................................78

4.2.4.2 Compressive Strength Results of Bricks..................................................................................80

4.2.5 Results on Experimental Rigs......................................................................................................82

CHAPTER FIVE…………………………………………………………………………………………………………………………..107

ANALYSIS AND DISCUSSION OF RESULTS………………………………………………………………………………….…107

5.1 Overview......................................................................................................................................107

5.2 Analysis and Discussion of Results...............................................................................................107

5.2.1 Results of Thermal Conductivity of Insulating Board...............................................................107

5.2.2 Results of Thermal Conductivity of Bricks................................................................................110

5.2.3 Results of Marble Dust mixed with Agricultural Residues........................................................112

5.2.4 Results on Physical and Mechanical Properties of Brick Type..................................................112

5.2.5 Results of Experimental Rigs....................................................................................................113

5.2.5.1 Winter period........................................................................................................................113

5.2.5.2 Summer period......................................................................................................................114

5.3 Thermal performance on experimental rig.................................................................................116

5.3.1 Winter condition......................................................................................................................116

5.3.2 Summer condition....................................................................................................................117

5.4 Summary of Key Results..............................................................................................................117

CHAPTER SIX…………………………………………………………………………………………………………………………….119

VALIDATION OF RESULTS…………………………………………………………………………………………………………….119

6.1 Overview…………………………………………………………………………………………………............................…..119

6.2 Validation Tools Used for thermal conductivity……………………………………............................……..119

6.3 Validation Tools Used for Experimental Rigs………………………………………..............................……..120

6.4 Validation Model for thermal conductivity of particle board…………………...........................……..124

6.5 Validation Model for Bricks ……………………………………………………………….................................……125

6.6 Validation Model for Experimental Rig………………………………………………............................………..126

6.6.1 Validation of CFD data for winter and summer in 2019...........................................................127

CHAPTER SEVEN……………………………………………………………………………………………………………………….130

CONCLUSION AND RECOMMENDATION………………………………………………………………………………………130

7.1 Overview………………………………………………………………………………………………………………...................130

7.2 Key Research Findings…………………………………………………………………………………………................….130

7.2.1 Thermal Conductivity Test of Insulating Board…………………………………………………....................130

7.2.2 Thermal Conductivity Test of Bricks………………………………………………………………….....................131

7.2.3 Marble Dust mixed with Agricultural Residues………………………………………………...................….131

7.2.4 Physical and Mechanical Properties of Brick Type…………………………………………........................131

7.2.5 Experimental Rigs…………………………………………………………………………………………..…...................132

7.3 Key Recommendations………………………………………………………………………………………......................133

7.3.1 Recommendations of Thermal Conductivity Tests for particle Board……………........................133

7.3.2 Recommendations Thermal Conductivity Test of Bricks……………………………….....................….133

7.3.3 Recommendations Marble Dust mixed with Agricultural Residues………………......................…133

7.3.4 Recommendations Physical and Mechanical Properties of Brick Type………………....................133

7.2.5 Recommendations Experimental Rigs…………………………………………………………….......................134

LIST OF REFERENCES……………………………………………………………………………………………..........................135

LIST OF PUBLICATIONS…………………………………………………………………………………………………………………148

LIST OF PUBLICATIONS……………………………………………………………………………..............................………151

APPENDICES...............................................................................................…………..................………..152

A.1 Acceptance and editors report from publications......................................................................152

A1.1 Thermal conductivity raw data for sample A……………………………………………..............................158

A1.2. Thermal conductivity raw data for sample C………………………………….………...............................168

A1.3. Thermal conductivity raw data for marble mix at 20 %...........................................................178

A1.4. Thermal conductivity raw data for 60 % maize husk……………………………….........................……188

A1.5. Thermal conductivity raw data for 60 % cow dung…………………………………………......................198

A1.6. Thermal conductivity raw data for 60 % millet……………………………………………….......................208

A2.1 Thermal conductivity of raw data for 30% Marble dust for Sample A…………………...................218

A2.2 Raw data of Marble dust at 30% for Sample C……………………………………………….….....................225

B.1 Welcome to ANSYS Fluent Release 18.2………………………………………………………………....................232

Turn it in Originality Report..............................................................................................................263

Test report.........................................................................................................................................264

Candidate’s responses to questions from Examiners during oral presentation................................271

LIST OF FIGURES

Figure 1.1: Map of Namibia (Bahrami, 2008)……………………………………………………………………………………4

Figure 1.2 Namibia map of Climate Classification…………………………………………………………………..…………5

Figure 1.3: Annual yearly temperature of Namibia (Zalaudek, 2013)……………………..…………………………6

Figure 1.4: Average annual Temperatures in Namibia (Kamara, 2018)……………………………………………..6

Figure 1.5: Average min. and max. Temperatures in Windhoek, Namibia (Zalaudek, 2013)……….…….7

Figure1.6: Precipitation Namibia (Zalaudek, 2013)……………………………………………………………………….….8

Figure 1.7: Precipitation chart for Windhoek, Namibia (METEOTEST, Meteonorm, Version 7.0)………8

Figure 2.1 Passive solar space heating design (Irace, et. al. 2017)….......................……………………....…23

Figure 2.2: Energy-efficient Building of Namibia: Kamara, (2018)……………………………………………………25

Figure 2.3: Model computational mesh………………………………………………………………………………………….37

Figure 2.4: Flow domain of interest………………………………………………………………………………………………..38

Figure 2.5- Two-dimensional control volumes in an orthogonal grid. (a) General grid…………………….42

Figure2.6 Outline of parts in the building heat balance (Risberg, 2018)………………………………………….45

Figure 2.7 Thermal bridges at junction……………………………………………………………………………………………47

Figure 2.8: Solar Radiation across regions in Namibia (SolarGIS-Solar-map-Namibia, 2017)……………50

Figure 2.9: Monthly solar radiation of Windhoek, Namibia (Zalaudek, 2013)………………………………….51

Figure 3.1 - Regions and Towns Samples Collected…………………………………………………………………………53

Figure 3.2 – Sample of Cow dung……………………………………………………………………………………………………56

Figure 3.3 – Sample of marble dust…………………………………………………………………………………………………56

Figure 3.4 – Sample of ground rice husk………………………………………………………………………………………..57

Figure 3.5 – Sample of ground maize husk………………………………………………………………………………….…57

Figure 3.6 – Sample of ground millet husk……………………………………………………………………………………..58

Figure 3.7 - Sample mixture for particleboard…………………………………………………………….………………….58

Figure 3.8 Retsch SK 100 hammer mill……………………………………………………………………………………………59

Figure 3.9 The Brick Making Mould..….……………………………………………………………………………...............60

Figure 3.10 The brick test sample…………………………………………………………………………………………………..60

Figure 3.11 Three experimental used in the research……………………………………………………………………..62

Figure 3.12:  EP500 lambda machine………………………………………………………………………………………………63

Fig.3.13 Set up for Thermal Conductivity Measurement ………..........................……………………………….63

Figure 3.14: Uniaxial Compressive Test Machine Used………………………………………………………………….65

Fig. 3.15: Thermowire NiCr-Ni…………………………………………………………………………………………………………67

Fig. 3.16: Digital humidity and temperature sensors……………………………………………………………………….68

Fig. 3.17: Weather Station and Symmetron data logger………………………………………………………………..68

Figure 3.18 Symmetron stylitis 101……………………………………...…………………………………………………………69

Figure 3.19 Symmetron data logger connected with sensors………………………………………………………….70

Figure 4.1: Bar Chart of Sample Thermal Conductivity of Samples Considered..................................72

Figure 4.2: Bar Chart of Thermal Resistivity of Samples Considered...................................................73

Figure 4.3: Thermal Conductivity versus Time for 60% Maize husk brick...........................................74

Figure4.4: Thermal Conductivity versus Time for 60% Rice husk brick...............................................75

Figure 4.5: Thermal Conductivity versus Time for 60% Cow dung brick.............................................76

Figure 4.6: Thermal Conductivity versus Time for 60% Millet husk bricks..........................................77

Figure 4.7: Water absorption of Maize Husk Bricks............................................................................78

Figure 4.8: Water absorption of Rice Husk Bricks...............................................................................79

Figure 4.9: Water absorption of Millet Husk Bricks.............................................................................79

Figure 4.10: Water absorption of Cow Dung Bricks............................................................................80

Figure 4.11: Compressive Strength of Maize Brick..............................................................................80

Figure 4.12: Compressive Strength of Rice Brick.................................................................................81

Figure 4.13: Compressive Strength of Millet Brick..............................................................................81

Figure 4.14: Compressive Strength of Cow Dung Brick.......................................................................81

Figure 4.15: Temperature quarterly Profile on 03-07-2018................................................................85

Figure 4.16: Temperature profile for July 2018...................................................................................87

Figure 4.17: Humidity profile for July 2018.........................................................................................88

Figure 4.18 Summer Temperature Profile for October 2018..............................................................92

Figure 4.19 Hourly Summer Humidity Profile 15th October 2018.......................................................95

Figure 4.20 Winter quarterly Temperature Profile for 1st June 2019..................................................98

Figure 4.21 Winter Temperature Profile for June 2019....................................................................100

Figure 4.22 Winter Humidity Profile for June 2019...........................................................................101

Figure 4.23 Summer quarterly Temperature Profile for 17th September 2019.................................104

Figure 4.24 Summer daily Temperature Profile for September 2019...............................................105

Figure 4.25 Summer daily Humidity Profile for September 2019......................................................106

Figure 5.1: Sample A Thermal Conductivity versus Time..................................................................109

Figure 5.2: Sample C Thermal Conductivity versus Time...................................................................109

Fig. 5.3. Thermal conductivity versus percentage mix of Agricultural residues................................111

Figure 6.1 fluent simulation convergences.......................................................................................119

Figure 6.2 Temperature (in Kelvin) plot............................................................................................121

Figure 6.3 Velocity plot......................................................................................................................121

Figure6.4 Temperature (in Kelvin) plot winter..................................................................................121

Figure 6.5 Velocity plot for winter.....................................................................................................122

Figure6.6 Temperature (in Kelvin) plot summer...............................................................................123

Figure 6.7 Fourier Law with constant thermal conductivity..............................................................124

Figure 6.8 Validation of CFD Simulation for Rig A..............................................................................127

Figure 6.9 Validation of CFD Simulation for Rig A.............................................................................127

LIST OF TABLES

Table 2.1: Annual Production of Millet from 2007 – 2017.................................................................................18

Table 2.2: Annual Production of Maize from 2009 – 2019..................................................................19

Table 2.3: National livestock census 1998 (Source: Schneiderat, 2011)………………........………………….20

Table 2.4 Terms used in the predicted mean vote (PMV) Source: Comfort equation

of Fanger (1970)…………………………………………………………………………………………………………………………….35

Table 2.5 Equations for components of the heat balance equation used by Fanger (1970)

in determining the PMV thermal comfort equations (see Table 2.2 for terms) ...………………………....35

Table 3.1: Percentage composition of samples……………………………………………………………………………….55

Table 3.2 Percentage composition of samples A and C with Marble dust..........................................55

Table 3.3 Composition of Maize Husk Mix with Sand.........................................................................60

Table3.4 Composition of Rice Husk Mix with Sand.............................................................................60

Table 3.5 Composition of Cow Dung Mix with Sand...........................................................................61

Table 3.6 Composition of Millet Mix with Sand..................................................................................61

Table 3.7: Technical data of thermo wires..........................................................................................66

Table 3.8: Technical data of digital humidity and temperature sensors.............................................68

Table 4.1: Thermal Conductivity and Resistivity of insulation boards of Samples considered.........  71

Table 4.2: Results of Thermal Conductivities of Samples from Table 3.2 when varying

percentage of Marble Dust.................................................................................................................73

Table 4.3: Bricks Thermal conductivity and resistivity results for Maize Husk Bricks.........................74

Table 4.4: Results of thermal conductivity and resistivity for Rice Husk's brick...................................75

Table 4.5: Results of thermal conductivity and resistivity for Cow dung brick....................................76

Table 4.6: Results of thermal conductivity and resistivity for Millet Husk's bricks.............................77

Table 4.7: Water Absorption of Bricks with varying percentage mixes..............................................78

Table 4.8:  Compressive Strength of Bricks.........................................................................................80

Table 4.9: Average quarterly indoor air temperature in rig TAR1, TAMB2,

TNo3 and outdoor temperature for July 2018....................................................................................82

Table 4.10: Average monthly indoor air temperature in rig TAR1,

TAMB2, TNo3 and outdoor temperature in July 2018........................................................................86

Table 4.11: Average monthly indoor humidity in rig TAR1, TAMB2, TNo3 and

outdoor humidity in July 2018.............................................................................................................87

Table 4.12: Average quarterly indoor air temperature in rig TAR1,

TAMB2, TNo3 and outdoor temperature for October 2018...............................................................89

Table 4.13: Average quarterly indoor air humidity in rig TAR1, TAMB2,

TNo3 and outdoor humidity for 15th October 2018............................................................................92

Table 4.14: Average quarterly indoor air temperature in rig TAR1,19,

TAMB19, TAN19 and outdoor temperature for June 2019.................................................................96

Table 4.15: Average monthly indoor air temperature in rig

TAR1,19 TAMB19, TAN19 and outdoor temperature in June 2019..................................................100

Table 4.16: Average monthly indoor humidity in rig TAR1, TAMB2,

TNo3 and outdoor humidity in June 2019.........................................................................................101

Table 4.17: Average quarterly Temperature in rig A, B, C and outdoor

The temperature on 17th September 2019.......................................................................................102

Table 4.18: Average daily Temperature in rig A, B, C and outdoor

The temperature in September 2019...............................................................................................104

Table 4.19: Average daily Humidity in rig A, B, C and outdoor humidity in September 2019...........105

Table 6.1 Specifications for thermal conductivity equipment. Source (Ashour, 2010)....................119

Table 6.2:  Normalized Mean Square Error (NMSE) between the winter

temperature values obtained in the simulation and experimentally................................................125

Table 6.3:  Normalized Mean Square Error (NMSE) between the

summer temperature values obtained in the simulation and experimentally.................................126

Table 6.4: Measured and Simulated data for June 2019..................................................................126

Table 6.5: Measured and Simulated data for September 2019.......................................................127

CHAPTER ONE

1.1	Overview

INTRODUCTION

Due to exponential growth in population in recent times as a result of the emerging industrial revolution, there is an increase in energy use in all spheres of life. In recent years, the method of energy generation and conservation has and continues to be a global issue. The energy in buildings can be consumed in many ways. In Europe for example, it was found that 52% of energy is consumed in buildings (Sanoussi, 2012). Similarly, Nina (2006) has shown five ways in which buildings consume energy, namely: embodied energy that is consumed in the manufacture of construction materials; grey energy that is consumed in the distribution and transportation of the materials to the construction site; induced energy that is used up all through the construction of the materials; operating energy that is consumed in succession the building and its equipment and appliances; and energy that is consumed during the maintenance, alteration, and demolition of the buildings(Nina, 2006).

The consumption of energy in any building is a function of the building’s orientation, design, material

type, and usage. To maintain good and comfortable indoor building conditions, the use of thermal insulation is a key parameter that measures a building's energy efficiency. By appropriately insulating buildings one can reduce operational costs, dependence on external primary energy supplies, and other environmental challenges such as CO2 emissions. Additionally, from a broader perspective, the building sector accounts for 40% of CO2 emissions (Castell et al., 2009).

The need to lessen energy usage and the associated carbon emissions on a global level is commonly known and varying techniques are widely being invented and used in most developed and developing countries in recent times. In Namibia, since over 10278 houses are built every year (Sweeney, 2011), there are growing energy needs and consumption in the country that has a tremendous impact on emission levels during the building’s life cycle.   Reducing energy consumption therefore reduces carbon emissions that are associated with energy generation for Namibia.

Moreover, moving away from the conventional methods of building construction and introducing new, efficient, and affordable building techniques will mitigate the current situation (Onjefu et al., 2019). Techniques like producing materials that require less energy to manufacture but demonstrate better

thermal efficiency at reduced energy requirements in ensuring ambient indoor temperatures at both hotter and cooler seasons.

Thermal insulator materials are those that resist the flow of heat to a great level. The efficient use of this property of materials to conserve heat energy depends on the material type which in turn, brings in the cost factor (Ekoja et al., 2016). Hence, the need for materials with the most economic advantage is at hand.

Insulating materials used in buildings in Namibia and most developing countries are imported hence very expensive and inaccessible to many due to their income levels. Thus there is a need to develop new and affordable techniques of producing insulating materials that ensure high building performance in terms of energy efficiency i.e. using less or no externally driven energy to ensure ambient indoor temperature regardless of fluctuating outdoor temperatures throughout a year. Affordability comes into play when materials that are locally and abundantly available are used to produce energy-efficient materials that replaced imported ones.

To ensure the above-mentioned output, this research aimed at conducting a comprehensive study of

the impact of using locally available agricultural residues/wastes in building developing materials that will ensure high building performance in terms of energy efficiency in Namibia.

The agricultural residue is a biological material (biomass), it is biodegradable and can be used for

insulation purposes (Zulkifli et al., 2009; Panyakaew and Fotios, 2008).

Furthermore, renewable biodegradable building thermal insulation can have a net reduction in CO2 emissions during the building’s life cycle. An economical, reliable, and abundant supply of biodegradable fibrous materials can be obtained as waste by-products from many commercial agricultural processing industries (Rodriguez et al., 2011). Materials such as coconut fibre, sugarcane fibre, cotton, wheat straw, date palm leaves, oil palm fibre, and others which consist of lignocelluloses fibres are promising alternatives for use as biodegradable, renewable, environmentally friendly building thermal insulation (Zhou et al., 2010; Al-Juruf et al., 1988). Though the main pointer of the quality of insulating material is based on the thermal conductivity of the materials, accurate findings of the thermal conductivity require special tools (Khomenko, 1974; Laser Comp, 2006).

In this research, agricultural residues in the form of millet husk, rice husk, maize husk, cow dung, and

marble dust that are abundant in many parts of Namibia were chosen and used. Been the first in Namibia, the results obtained in this research provides a strong foundation for further researches in the development and mass production of appropriate, affordable, and easy-to-produce wide-ranging

energy-efficient building materials locally. This will not only reduce the over-reliance of such materials from high technologically advanced countries that continue to put tremendous stress in our local economy due to the importation of conventional heating and cooling devices but also increase the development of non-affordable and non-energy efficient housing in Namibia and other countries of similar situations.

1.2 Key Information about Namibia

Namibia, which became an independent and Republic in March 1990 is located in southwest Africa with its capital city Windhoek. It has an area of 824.292 km² with a Population of 2.2 million according to the national census conducted in 2011. However, the current population has increased to 2.55 million in 2020. In the west, the country borders the Atlantic Ocean, to northern Angola, Botswana to the east, and the Republic of South Africa to the south as shown in Fig. 1.1. The name of the country is derived from the Namib Desert, which nearly occupies the entire coastal area of the country (Zalaudek,

2013). The climate is arid, generally dry, and extremely hot with temperatures in the range of above

40°C during summer to -5°C in mid-winter in some parts of the country. The average yearly temperatures of Namibia range between 13°C and 22°C.

The country’s capital is Windhoek situated at Latitude [°N] 22, 57° (22°33‘36‘S) and longitude [°E] +17,

10° (17°05‘24‘‘E). Covering an area of 37.007 km² and a population of close to 300,000 inhabitants, Windhoek is the economic and political centre of the State. It is the geographic centre of the country, amid the Eros Mountains in the east, Auas Mountains to the south, and Khomas Highland in the west and north as in Fig. 1.1. It was founded in 1890 as a modern city and holds approximately 40% of the total population of Namibia (Rosenlund, 2000).

Figure 1.1: Map of Namibia (Bahrami, 2008)

1.3 Climate

1.3.1 Introduction

According to the Namibia Meteorological Service, (2008), Namibia extends from 17°S to 25°S latitude: climatically the range of the Sub-Tropical High-Pressure Belt. The overall climate report is arid, descending from the Sub-Humid (mean rain above 500 mm) through Semi-Arid between 300 and

500 mm and Arid from 150 to 300 mm. Temperature maxima are limited by the overall elevation of the entire region: only in the far south, Warm bad for instance, are mid-40 °C maxima recorded as shown in Fig. 1.2.

Namibia has more than 300 days of sunshine per year due to its Sub - Tropical High-Pressure Belt and clear skies. It is located at the southern edge of the tropics; which cuts about half the Tropic of Capricorn. The winter period is from (June–August) and is generally dry; both rainy seasons occur in summer, the small rainy season between September and November, while there is more rainfall between February and April. Humidity is low, and the average rainfall varies from almost zero in

the coastal desert to more than 600 mm in the Caprivi Strip. Due to the dry winters’ snowfall has a very rare occurrence and prompts media coverage whenever it happens.

Figure 1.2 Namibia map of Climate Classification

1.3.2 Temperature

During the hot winter months (summer in the northern hemisphere), from late September to early April, the average values of the temperature are between 20°C and 26°C (Radhi, 2009). According to Radhi, (2009), during the winter period i.e. April - September, the monthly average temperature drops to 13°C. This leads to indoor heating demand either by using external conventional sources or by using other emerging forms like geothermic energy and passive sun-radiation.

Annual distribution of Namibia’s yearly temperatures and periods of annual minimum and maximum

temperatures are as shown in Figs. 1.3 – 1.5

Figure 1.3: Annual yearly temperature of Namibia (Zalaudek, 2013)

Figure 1.4: Average annual Temperatures in Namibia (Kamara, 2018).

Figure 1.5: Average min. and max. Temperatures in Windhoek, Namibia (Zalaudek, 2013).

1.3.3 Precipitation

Namibia is considered by a complex earth-atmospheric interactions system of low precipitation and moist air at the Atlantic coast (Namib Desert). Precipitation forms as water vapour condense, usually in rising air that expands and therefore cools (Kagbi et al., 2016). Also, the upward motion arises from air rising above mountains, warm air riding over cooler air (warm front), colder air pushing under warmer air (cold front), convection from local heating of the surface, and other weather and cloud systems (Trenberth, 2011). Trenberth further reported that precipitation characteristics significantly depend on temperature and other atmospheric conditions.

Windhoek in Namibia has an arid climate. The rainy season in 2010/2011 for instance witnessed more than 1,100 millimetres of rainfall, the rainiest in the 120-year history of the Namibian climate records. Normally the total precipitation is 370 mm (Zalaudek, 2013) as shown in Figs.1.6 and 1.7.

Figure1.6: Precipitation Namibia (Zalaudek, 2013)

Figure 1.7: Precipitation chart for Windhoek, Namibia (METEOTEST, Meteonorm, Version 7.0)

1.4 Statement of the problem

Due to the tremendous growth in the complexity of the human lifestyle in Namibia and globally, new technologies that require the use of appropriate energy sources and usage have emerged in the 21st century. According to recent findings, buildings, which are the leading energy users, constitute 40% of the total energy consumption in developed and developing countries, resulting in to increase in energy demand. In underdeveloped countries, the increasing energy demand in buildings and energy- dependent new technologies is gradually reaching a crisis level.

To control this growing energy demand, appropriate building technologies, and materials that will ensure high comfort levels with minimal energy consumption and low carbon emissions should be developed. Waste generation and unsafe disposal of agricultural residues can in most cases lead to environmental pollution and the depletion of the ozone layer, thereby leading to climate variability (Liang & Ho, 2007) , the development of technologies (through research) using such wastes in designing an energy-efficient building is thus becoming an absolute necessity in modern times.

Due to its growing focus on agriculture and the low utilisation of agricultural wastes/residues, the study focused on the use of wastes from millet (Pennisetum glaucum) husks, rice hulls, maize husks, and cow dung to develop an environmentally friendly and energy-efficient /thermal insulation building materials for building construction in Namibia. Wide-ranging investigations including laboratory tests were performed and appropriate isolation material was produced. The physical, mechanical, and thermal properties of the developed material were compared with internationally accepted building isolation materials.

1.5 Objectives of the Research

This study aims to carry out a comprehensive study of the impact of using locally available agricultural wastes/residues in the development of appropriate and highly rated energy-efficient building materials to be used in the design of affordable energy-efficient buildings in Namibia. Using such materials, building energy performance was measured to ascertain the extent of energy usage, degree of carbon capture / saved, and level of indoor comfort on building occupants/inhabitants with minimal use of conventional heating and cooling devices that use electricity from the general grid. The specific objectives are to:

1.   Develop affordable and highly thermal efficient insulating materials from millet (Pennisetum glaucum) husks, rice hulls, maize husks, and cow dung wastes/residue for the design of energy- efficient buildings.

2.   Carry out laboratory tests to determine the appropriateness of the physical, mechanical and thermal properties/behaviours of developed insulating materials to be used in energy-efficient buildings.

3.   Design the experimental test rig.

4.   Conduct a comparative thermal behaviour assessment with conventional insulating materials.

5. Measure and simulate possible energy savings and CO2 emission reductions between conventional and energy-efficient buildings using the developed energy-efficient construction materials.

6.   Validate experimental results using readily available simulation tools and techniques.

1.6 Research hypothesis

The hypotheses for this research are as follow:

1.  Agricultural wastes/residues produced from millet (Pennisetum glaucum) husks, rice hulls, maize husks, and cow dung results in a very good insulating material.

2.   The  development  and  implementation  of  thermal  insulated  structural  members  from

agricultural  wastes/residues will  help  to  lower energy consumption  in  buildings, thereby producing a highly energy-efficient building.

3.  The physical, mechanical, and thermal properties of the developed insulating material will perform the same or even have higher design values as compared with those internationally recognised and currently used in Namibia.

4.   The test rig designed using local materials and techniques in this research gives a higher thermal

efficiency and energy efficiency properties than those internationally recognised and used in

Namibia.

5.   Thermal and other energy efficiency components/parameters and results obtained to comply with internationally recognised design models that define an effective energy efficiency building.

6.   The design rig developed from materials used in the research contributes to new indigenous knowledge and has resulted in the development and design of affordable and energy-efficient buildings that reduce carbon footprint and ensure appropriate energy-saving measures.

1.7     Significance / Contribution of Research

Within the limits of my feasibility studies, even though Namibia produces a large volume of agricultural wastes/residues annually, not much has been done to fully utilise wastes/residues from Pennisetum glaucum husks, maize husks, and rice husks mixed with cow dung. With the quest for affordable

housing at all levels of society especially the low-income group, research on the utilisation of such wastes/residues to produce affordable and locally produced insulating materials will be of great necessity that will meet the new Namibia vision of producing affordable energy-efficient housing for all using indigenous techniques and materials.

The effect of hot weather patterns on the living conditions and comfort level of occupants in most buildings especially those of low-income Namibians are worth considering. Findings on appropriate and effective heat efficient isolating building materials using locally produced agricultural wastes/residues are necessary. This will pave the way for producing affordable and low heat transmissibility housing from local /indigenous materials in Namibia.

Due to its uniqueness and originality, findings from this research will do more than just adding to new knowledge in the development of affordable materials that can be used towards designing heat/energy-efficient green buildings. It will also open opportunities to wide-ranging investigations on other readily available agricultural wastes/residues like Pennisetum glaucum husk (also known as pearl millet) widely produced in Namibia and SADC region. The output from the research will also contribute to the development of appropriate local/ regional building codes/standards that will lead to the limitation of the importation of isolating building materials that have been limiting the design of affordable and energy-efficient housing.

1.8 Structure of the thesis

This Ph.D. research thesis will be developed to contain seven chapters. What is contained in each chapter is as summarised below:

Chapter One – Introduction

Gives an overall view on the relationship between building energy performance and material use, Namibia, climatic/weather distribution pattern across Namibia, need of such research, objectives of the research, research hypothesis, contribution of the research, and proposed structure of research findings.

Chapter Two – Literature Review

The chapter will show details of in-depth information on the state of agriculture in Namibia, the extent of agricultural Wastes/Residues considered in the research in terms of types, behaviour, usefulness, and their environmental impacts. Summary of local, regional, and international researches has been carried on similar topics in terms of extent, key findings, limitations/gaps will be presented.

Chapter Three- Methodology and Procedure

The chapter will detail the various sample collection, the formation of particle board from the mix ratio of the various samples collected, and the production of bricks, preparation of the different rigs type is also depicted in this chapter. Also, the different apparatus/ equipment used in this research will be explained in the chapter.

Chapter Four: Experimental results

The results obtained from the laboratory testing of particleboard, bricks, and experimental rigs will be presented in this chapter.

Chapter Five: Analysis and discussion of Results

This chapter will discuss the results and simulation of the experimental results obtained from the previous Chapter.

Chapter Six: Validation of results

The Chapter will show details of the validation of measurement and simulated results.

Chapter Seven: Conclusions and Recommendations

This chapter gives a summary of the key findings along with important conclusions, future recommendations of work will be present in this Chapter as well.

CHAPTER TWO

LITERATURE REVIEW

2.1 Overview

According to existing literature, many works have been done globally using locally available materials in the design of affordable, sustainable, and energy-efficient housing. In Thailand, Satta and Steve (2008) used wastes from bagasse, rice hulls, coconut husks, corn stalk durian peels, and palm oil leaves to design particle boards. Results revealed that these wastes have reasonable insulating properties that can be used in any energy efficiency building. Binici (2015) in Turkey looked at the production of thermal insulation from animal wastes and vegetable/organic fibres. His results revealed that such wastes produced very good insulating materials that can be used in energy-efficient buildings. Also, in Turkey, Eskin (2008) looked at energy building in four major climatic zones and illustrated that the annual cooling energy requirement and annual total energy requirement of the energy buildings increase with high quantities of glazing, both in hot and humid climate zones. His results revealed the following: up to 10% of energy can be saved if light colours are chosen on external walls of buildings; maximum annual of 19.67% and 34.4% of energy are required for both cooling and heating respectively when 75mm insulation is provided in the interior walls in mild climates/environments.

In Europe, Manohar (2003) in Spain carried out an experimental investigation on building thermal insulation from oil palm fibre, sugar cane, and coconut fibres. Results revealed that sugarcane fibre with the lowest solid fibre density of 686 kg/m3 exhibited the lowest apparent thermal conductivity of

0.04610 W/m K and an increase in trend of solid fibre density of the material showed a rise in the

minimum thermal conductivity of the fibrous. Luamkanchanaphan, et. al., (2012) on the other hand looked at the physical, mechanical and thermal insulation from narrow-leafed cattail fibres. Results revealed that thermal conductivity values between 0.0438 – 0.0606 W/ m K were obtained for boards of density between 200 – 400kg/m3 when measured to ASTM C518 standards. Elias et. al., (2006) also conducted a comparative study on the thermal performance of building materials made from mud bricks and straw bales. Results revealed that straw bales have better thermal insulation properties.

Additionally, Sun and Xiao (2014) in China showed that energy-efficient building materials refer to the building materials with low energy consumption. On the other hand, Anas, (2010)  stated that for an enclosed boundary spaced building, the building insulation is used for the need of thermal transfer value. These findings showed that to achieve the target thermal transfer value the space building is designed to reduce the absorption of external heat and to minimize the cooling load system.

Patnaik et. al., (2015) in South Africa carried out a study on thermal and insulation from waste materials from wool and recycled polyester fibres. The study examined the thermal insulation properties concerning thermal conductivities and revealed that these materials had lower thermal conductivities; hence good building insulators.

In Chad, Mahamat et. al., (2008) evaluated the thermophysical characteristics of clay bricks mixed with

agricultural wastes. The study examined the thermal conductivity and thermal diffusivity of the materials and revealed that clay bricks mixed with millet pods have a good thermal performance and good energy-saving properties. Kyauta, et. al., (2014) investigated the thermal properties of composites of rice husks, corncob, and bagasse for building thermal insulation. Results revealed that the thermal conductivity and resistivity fall within the same range as the conventional materials, thereby making them suitable insulation materials.

In Uganda, Bwayo, et.al., (2014) used locally produced insulation bricks from sawdust mixed with local

clay. Results revealed that thermal conductivity increases with a decrease in particle size of kaolin and ball clay, but decreases with increases in particle sizes of sawdust

In Namibia, even though not much has been done, Domingue, (2012) researched producing sustainable paper insulation for structures built from corrugated iron sheets commonly known as ‘’Kambashus’’ mostly used in informal settlements. The study examined the thermal behaviour in terms of resistance, flammability, and efficiency of recycled waste materials to be used as insulators in such structures. Results revealed that a proportionate mixture of paper and sawdust under a well-controlled environment gives materials with good thermal behaviour that is ideal in such structures.

From the well-selected publications mentioned above, a reasonable number of researches have been

done and published in the area of construction materials developed from varying forms of wastes. However, based on works of literature at the disposal of this research, not much has been done in Namibia and across the SADC region in the use of locally available agricultural waste/residues in the development of energy-efficient materials as was done in this research.

considering the high volume of agricultural and animal wastes/residues like maize, rice, and Pennisetum glaucum, and cow dung produced in Namibia annually, there is a need to research how these wastes/residues can be used to produce thermal insulating materials that can be used to produce a low energy consumption building with very high comfort levels in Namibia. This will not only greatly contribute to the country’s diversified approach to energy supply and distribution, but also contribute to the “Green Building Initiatives” in the country.

2.2. Agriculture in Namibia

According to FAO, (2012), agriculture in Namibia contributes around 5% of the national Gross Domestic Product. However, between 25% and 40% of Namibians lived on subsistence agriculture and herding. The country produces primary products like livestock and meat products, crop farming, and forestry (United States Department of State, 2016). Due to its geographical location, only 2% of Namibia's land receives sufficient rainfall to grow crops. Also, all inland rivers are ephemeral making irrigation possible in valleys of the border of rivers Oranje, Kunene, and Okavango (Hoffmann, 2012).

Although Namibian agriculture (excluding fishing) contributes between 5% and 6% of Namibia's GDP from 2004-2009, a large percentage of the Namibian population depends on agricultural activities for livelihood, mostly in the subsistence sector. Animals and their products, and crop exports constituted roughly 10.7% of total Namibian exports. Due to emerging government regulations, retailers of fruits, vegetables, and other crop products must purchase 27.5% of local agriculture products hereby encouraging Namibians to purchase such products to avoid fluctuating importation costs, hence boost the local economy.

According to Weidlich, Brigitte (2010), in the largely white-dominated commercial sector, agriculture consists primarily of livestock ranching. The same applies to Namibia where a large percentage of large- scale farmers are white. According to recent statistics, there are about 4,000 commercial farms in Namibia in which 3,000 are owned by whites. Moreover, cattle raising is key in the central and northern regions, whereas karakul sheep and goat farming are intense in the more arid southern regions. Subsistence farming is mainly confined to the "communal lands" of the Country's populous north, where roaming cattle herds are prevalent, and the main crops generally grown are millet, sorghum, corn, and peanuts. Table grapes, grown mostly along the Orange River in the Country's arid south, are

becoming a progressively important commercial crop and a significant source of employment for seasonal labour. In Namibia, rain-fed white maize is produced by farmers mainly in the maize triangle situated between Tsumeb, Otavi, and Grootfontein (BoN and IMF, 2018).

2.2.1 Importance of Agriculture in Namibia

According to the Namibia Statistics Agency, agriculture and forestry are projected to a progressive rise of 1.6% in real value during the 3rd quarter Gross Domestic Product (GDP) review of 2016, compared to a decline of 15.5% during the 3rd quarter of 2015 (Meatco, 2017).

The performance in these sectors can be attributed to an increase in the number of slaughtered livestock at export abattoirs and butchers. The question is whether the negative growth was a result of considering a decrease in stock numbers.

According to recent statistics, a third of the Namibian workforce is involved in the agricultural sector. It is good to ensure an increase in agricultural production to avoid heavy reliance on imports. To continue developing the farming tradition in Namibia and to ensure long-time sustainability, education in the field of agriculture must take place at all levels of society.

Agriculture is a dynamic sector that is part of Namibia's development programmes; it is also the first link in the value chain for the 'Growth at Home' strategy. It, therefore, forms a critical component in the newly introduced Fifth National Development Plan (NDP5) that gears towards Namibia’s economic growth in the next five years i.e. 2018-2023.

2.3 Key Agricultural Wastes/Residues: Types, behaviour, usefulness, environmental impact

Agriculture is the main backbone of the Namibia economy, thereby leading to the availability of a wide

range of agricultural wastes/residues that are most adequately used/utilised.

Results of Shifiona, et al. (2016) showed that cereals are the most important food widely produced in developing African countries, especially the southern and Eastern countries. The research looked at the crop production rate of Maize and Mahangu (also known as Millet pearl) in Namibia. The findings showed that the production of Maize and Mahangu has tremendously increased over the years due to the high yield per hectare harvested. According to EEA, (2006), these waste materials generated from agricultural products during harvesting and post-harvesting in Namibia are usually disposed of by

burning or being dumped in landfills. The finding also revealed that such wastes/residues produced can be problematic due to the level of emission of Ammonia (NH3) and Methane (CH4) that can lead to acidification thereby contributing to greenhouse gas emissions.

According to the findings of Rowell et al. (1996), the degree of fibrous content in some of the agricultural waste like corncob, oil palm, sugar cane husks, straw, rice husks, are suitable for making good insulating panels/boards that can be used in the construction of energy-efficient buildings.

Also, Satta et al. (2008) considered the potential of using agricultural wastes to develop thermal

insulating materials. They outlined the following pre-requisites: availability of the agricultural waste materials; physical and thermal properties determination of materials; environmental and health impact; and transformation of the materials into useful construction materials.

This research, therefore, follows the same approach in producing energy-efficient building materials

from appropriate combinations of agricultural wastes/residues.

2.3.1   Pearl millet (Pennisetum glaucum) husks

Pennisetum glaucum husks are the fibrous by-product left after the grains have been removed. Pennisetum glaucum (Pearl Millet) also known as “Mahangu” is a cereal that more than half of the Namibia population is considered as a staple food when combining with other sauces (NAB, 2008). It’s generally grown in climates having rainfall ranging between 150 and 800 millimetres per annum. The plant is commonly produced in the Northern region of Namibia; Zambezi, Kavango, Ohangwena, Omusati, Oshana, Oshikoto, and Otjozondjupa Regions. This crop is highly adapted to low rainfall and predominant in soil conditions in the North Central Regions and the Kavango. For many years, small- scale farmers have survived on the low yields obtained from “mahangu” (Pennisetum glaucum), especially during low rainfall seasons. “Mahangu” farmers in Namibia are amongst the few peoples in Africa who have successfully developed an integrated food storage system where they can store their grain in storage baskets made of wood strips for up to five years.

According to Namibian Agronomic Board, NAB, (2008) the average annual production of Pearl Millet,

(i.e. Mahangu), was over 40 tonnes for the past ten years (2007-2017) as shown in Table 2.1. However, in Sahel regions/countries, particularly in Senegal the Pennisetum glaucum Husks are used in the development of construction materials as an adjuvant (Bal et al., 2012). However, in Namibia no extensive works have been done regardless of the abundance production of Pennisetum glaucum Husks annually especially during normal rainy seasons, hence the need for this research.

Table 2.1: Annual Production of Millet from 2007 - 2017

| Year | Annual Production (Tons) |
| --- | --- |
| 2007 | 44,450 |
| 2008 | 35,512 |
| 2009 | 37,301 |
| 2010 | 45,836 |
| 2011 | 42,000 |
| 2012 | 56,000 |
| 2013 | 25,000 |
| 2014 | 37,000 |
| 2015 | 45,593 |
| 2016 | 45,691 |
| 2017 | 44,377 |

Source: (Namibian Agronomic Board, 2008)

2.3.2 Rice husks

Rice husks are the hard coverings of the rice grains. In wide-ranging traditional norms, traditional houses are constructed using rice husks as the main constituent in varying building elements in most African countries. According to the FAO (2004) statistics division, more than 100 million tons of rice is produced every year around the world. In Namibia, the Zambezi Region is where rice is produced in abundance. According to Mutorwa (2015), more than 70 metric tons of rice are released into the market annually from Katima Mulilo. According to Piva et al. (2004) rice husks are a great challenge to farmers due to their resistance to decomposition in the ground and their low nutritional value to animals since they can hard/difficult be digested.

Choi, et al., (2006) showed that rice husk as an Agricultural waste has a very good potential for building

insulation purposes because its thermal conductivity is very low. Similarly, Yarbrough et al. (2005) compared the thermal behaviour of rice husks with conventional materials and found that rice husks exhibit similar properties with most conventional insolating materials.

2.3.3 Maize husks (Zea mays)

Maize, like pearl millet, fits the class of grass family Graminae. it is an annual summer crop with many cultivars including dented maize, flint maize, sweet corn, popcorn bread maize, and pod maize. Maize

in its mature stage consists of three main parts: the teats (or pericarp), the starchy endosperm, and the embryo (germ) that gives rise to the new plant.

Maize husk is the outer shell of the maize seed. It often refers to the leafy outer covering of the maize as it grows in the plants.

A study carried out by the FAO (2012) showed the world most production of maize is in the United State of America with about 274 Million tons produced per year, while in China it was 208 Million tons, Brazil 71 Million tons and South Africa 12 Million tons.

In 2019, maize production for Namibia was 44 thousand tonnes. Though Namibia maize production

fluctuated substantially in recent years, it tended to increase through the 2000 - 2019 period ending at 44 thousand tonnes in 2019 as shown in Table 2.2.

Maize is the most staple food consumed in Sub – Sahara Africa (NAB, 2008). White Maize is also usually consumed in Namibia. A study carried out by Ranum, et al. (2014) showed the consumption rate of maize in 2009 in Namibia was 127g /person/ day. Correspondingly, Chow, (1974) showed that maize waste can be formed into fibreboard which is very good for insulation purposes.

Table 2.2: Annual Production of Maize from 2009 - 2019

| Year | Annual Production (Tons) |
| --- | --- |
| 2009 | 57,320 |
| 2010 | 53,071 |
| 2011 | 53, 800 |
| 2012 | 87,600 |
| 2013 | 40000 |
| 2014 | 55,985 |
| 2015 | 60,431 |
| 2016 | 64,210 |
| 2017 | 62,604 |
| 2018 | 59,000 |
| 2019 | 44,000 |

Source: (Namibian Agronomic Board, 2019)

2.3.4 Cow dungs

Cow dung is the undigested residue of plant matter that has passed through the animal's gut. The resultant faecal matter is rich in minerals. Colour ranges from greenish to blackish, and often darkening soon after exposure to air. The main components of cow-dung are plant fibres (essentially composed of cellulose, hemicelluloses, and lignin), amine organic compounds, and fragments of intestinal tissues (Millogo, et. al., 2014).

According to Schneiderat (2011), in 1998, in addition to smaller numbers of pigs, poultry, and farmed ostriches, about 2.2 million cattle, 2.1 million sheep, and 1.7 million goats were recorded in Namibia. Conversely, the numbers of livestock vary because of the changing effect of rainfall patterns. The 1998 census data shows the distribution between the communal and commercial sectors, as presented in Table 2.3

Table 2.3: National livestock census 1998 (Source: Schneiderat, 2011)

Cattle	Sheep	Goat

Communal	1,368,152	1,368,152	1,230,260

Commercial	824,207	1,727,210	479,930

Total	2,192,359	2,086,434	1,710,190

According to Table 2.3, livestock farmers in communal areas hold approximately 62% of the total cattle population, 72% of the goats, and 17% of the sheep. This is mainly confined to the northern part of Namibia where there are high deposits of animal dung on grazing sites due to the high animal population.   Usually, cow-dung is mainly used to fertilize agricultural soils due to its high nitrogen content that is good for the growth of plants. Apart from its usage as manure for plants growth, cow dung can also be used as a key constituent in producing thermal insulating building materials (Onjefu et al., 2019).

2.3.5 Marble dust

According to the survey and evaluation of geo-resources, since the last century, Namibia was considered as one of the favourable mining environments. From 1990 to 2000, the production of marble and granite was about 20,000 tons per year in Namibia according to (Ministry of Mines and Energy,2019). Since 2004, due to modern technological advancement, there has been an increase in

production of more than the threshold of 50,000 tons/year according to Punturo, et al., (2019). The geo-mining industry of Namibia includes several ornamental stones such as marbles (calcite and/or dolomite-bearing metal carbonate rocks); magmatic rocks such as granites, granodiorites, and gabbros; serpentinites; and onyxes and alabasters. Firms linked to the ornamental stone are situated in locations around the town of Karibib and have been producing high quantity and quality of marble over the years. In the Karibib district, the most important marble and granite reserves are in the Karibib quarry area of the northwest sector of town.

Marble dust is a product of the quarrying process from the parent marble rock. It contains high calcium

oxide content of more than 50%. It has various industrial uses due to the high percentage of fines and a low percentage of metallic oxides. These include agricultural soil amendment, manufacture of cement (Misra  &  Gupta,  2008), filler  in  the manufacture of  various  types of  paper, paint,  and polypropylene, production of soda, blast furnace flux, acid neutralizer for industrial effluents, and heavy metal sorption (Pincomb & Shapiro, 1994). Others are flue gas desulphuration in electric power stations (Fraes, 1994); manufacture of lime; resin conglomerates for flooring and coatings in the building industry; and production of a multitude of chemical applications, including cosmetics and pharmaceuticals. It is also used as filler in concrete and paving materials.  Due to its abundance in Namibia, this research considered it as a constituent in design mixes considered in the production of energy-efficient building materials that will ensure improvement in energy performance in buildings. Partially, this work was suggested by the manufacturer of the marble industry in Karibib for a scientific study to be done on marble dust to ascertain the viability of marble dust to be used for energy efficiency on building performance in Namibia for commercialisation purpose.

2.4 Current Building Regulations and Standard

2.4.1 Namibia Building Regulations and Standards

In Namibia, the standards are developed in line with international practices and stages (such as the Proposal Stage; Preparatory Stage; Committee Stage; Enquiry Stage; Approval Stage; and Publication Stage). These stages are sponsored and administered by the Namibian Standards Institute (NSI) through the appointment of technical committees and working groups. Standards are developed by organizations known as Standards Development Organizations (SDOs) and National Standards Bodies (NSBs),  which  operate  in  several  areas,  notably  the  NSI;  African  Regional  Organization  for

Standardization (ARSO); and the International Organization for Standardisation (ISO) or the International Electro-Technical Commission (IEC). These bodies are tasked by governments with the development of appropriate standards under internationally-accepted norms and following ISO/IEC directives (REEEI, 2013). Also, the norms suggest that the standards shall be developed:

➢  by properly-constituted and representative Technical Committees (TCs);

➢  using  the  principles  of  “Consensus”;  Aligned  with  the  International  Standards,  wherever

possible; and

➢  to comply with WTO/TBT Annex 3 Code of Good Practice (Schultz, et. at., 2006).

2.4.2 Namibia Energy Efficiency Programme in Buildings (NEEP)

The Namibia Energy Efficiency Programme in Buildings (NEEP) is the major programme in the country that aims to promote the use of energy-efficient technologies and practices in Namibia’s commercial and residential building sector. NEEP is co-funded by the GEF and UNDP under the Framework for Promoting Low Greenhouse Gas Buildings. This is a three-year programme and is being implemented by the MME and REEEI at the Namibia University of Science and Technology. The NEEP project’s objective is geared towards the reduction of Namibia’s energy-related GHG emissions through the nationwide adoption of energy-efficient technologies and practices in the commercial and residential building sector, with a focus on government buildings, hospitals, hotels, schools, and possibly a sample of residential buildings. In particular, the activities of NEEP include the following:

❖  Development of improved regulations (standards and labelling of building appliances) and adoption of building codes for energy savings,

❖  Provision of auditing and energy marketing services to stimulate the demand and supply of EE services

and technology, particularly through the introduction of mandatory audits in public and commercial buildings,

❖ Strengthening institutional capacity and awareness of EE in a building that would further contribute to

the adoption of EE technologies and best practices.

2.4.3 NEEP Baseline Study

The NEEP baseline study intended to establish building energy benchmarks in Namibia and recognise and review the current energy efficiency standards to make recommendations on energy efficiency approaches that are appropriate for Namibia. The study included 52 commercial buildings from four localities (Windhoek, Keetmanshoop, Oshkati/Ongwediva, Walvis Bay/Swakopmund).

The buildings selected were based on the building occupancy for large shops, offices, and hotels as defined under SANS 10400. To develop energy benchmarks, a wide variety of data was collected including electricity usage records, floor area, occupancy, and other data including other energy sources where applicable. Energy benchmarks measured comprise of the total annual energy consumption divided by the net square metre area of a building (unit kWh/m2 /annum), as defined by SANS 204 (the South African National Standard governing EE in buildings).

2.5 Forms of Solar Heating and Cooling

2.5.1 Passive solar home system

Passive Solar space heating makes use of the energy from the sun to heat the building. This uses orientation features such as south-facing windows to absorb heat during the day and release it at night when needed. According to Irace, et. al., (2017), Passive solar space heating is designed using direct solar gain and indirect solar gain. The direct solar gain uses the architectural features of buildings such as windows, walls, and floors to collect, store, and distribute energy in the form of heat in the winter and reject heat in the summer (Solar Space, 2017). It is called passive solar because it does not require any material medium for operation. According to Ambuga, (2018), passive buildings use about 60-75% of the solar energy that hits the building to moderate the indoor temperature and can reduce energy cost by 75% as shown in Fig. 2.1.

Figure 2.1 Passive solar space heating design (Irace, et. al, 2017)

2.5.2 Building Orientation

In solar passive design orientation of the building is a major factor to be considered with regards to solar radiation, daylight, and wind. In an arid climate like Namibia, buildings should be oriented toward North-South to take advantage of solar radiation (Wienecke and Mawisa, 2008). This means any deviance from the north-south direction would reduce the effects of solar passive heating and cool in a building. Also, east and west orientation makes buildings receive maximum solar radiation during summer. Apart from that, a report by the Namibia University of Science and Technology (2011) on Energy and Environmental Partnership with Southern and Eastern Africa emphasised having the extended side of a building with most windows positioned to the northern direction because it is the warmer front of the building in the southern hemisphere. Therefore, having most windows on that side can affect the heating and cooling of the building during the winter and summer periods.

In building orientation, the key issue to be considered, especially with performance, is the orientation

of the windows. According to Li, et. al., (2013) Solar energy radiation through large windows in summer can elevate a building´s indoor temperature high above the ambient temperature and thus cause significant thermal stress. In hot arid regions like Namibia, based on a study done by Zalaudek, (2013) orientation according to the sun is most important, and the north-south orientation of the main facades is preferable. East and west oriented buildings possibly will not be able to gain satisfactory solar radiation in winter (Maerefat et al., 2010).

In the cooler season, correctly placed and oriented windows may improve indoor comfort during

winter. If there is a conflict between the wind and the solar consideration, the cross ventilation should be the main factor to study in warm-humid climate (Givoni, 1994). However, the effects of indirect solar gain can be limited by using reflective colour and by shading with plants. Plants can also be used to offer shade for the walls.

2.6 Energy efficient building in Namibia (EEBN) Concept

The Namibia University of Science and Technology (NUST) in close collaboration with the Carinthia University of Applied Sciences, Austria designed the first energy-efficient house in Windhoek using the concept of passive solar design. Also, the EEBN house utilises natural ventilation principles to regulate the indoor temperature in winter and summer seasons without any use of electrical Appliances. Figure

2.2 shows the principle operation of the building that employs a solar chimney to cool the building in summer and an underground heat exchanger to heat the building in winter.

Figure 2.2: Energy-efficient Building of Namibia: (Kamara, 2018)

According to Kamara, (2018), the EEBN design principle in its current form works effectively in winter, while more redesigning needs to be done to ensure ambient and appreciable thermal comfort of building interior in summer. Design concepts and principles used in this are key in developing insulating building materials from agricultural wastes/residues that will be used to ensure energy efficiency in Buildings.

2.6.1 Energy Efficient Building/House

A study carried out by Ambuga, (2018) describes an energy-efficient house as a house with low energy consumption, produces a comfortable indoor climate, has low investment, and running costs, therefore, achieving a sustainable “green building” concept. The study done by Miller et al. (2012) revealed that many features have to be considered when designing and building energy-efficient houses, these are based on social criteria (i.e. thermal comfort, health, and time have taken to build); economic criteria (i.e. material cost); and environmental criteria (i.e. less use of energy and less or zero pollution). The three measures are key in measuring building energy efficiency and sustainability. The current study successfully used the criteria emphasized by Miller et al. (2012) to assess the efficiency of a house built with Agricultural residues and marble dust. Also, recent technology and improvements in the construction industry have made it easy to save money, improve comfort and health which this present study looked at.

Eludoyin, (2014) defines thermal comfort as “a condition of mind that expresses the satisfaction within the thermal environment”. Thermal comfort depends on environmental and personal factors. Environmental factors include; air temperature and velocity, relative humidity, and radiant temperature. Personal factors include; the clothing and level of activity. Also, the environmental conditions may not be similar for everyone as there are disparities physiologically and psychologically, from person to person in space.

According to ASHRAE (2011), occupants will be comfortable when the temperature within the building is between 20° C and 24°C, with an average of 22 °C with relative humidity 50%. Bearing in mind a study by Eludoyin, (2014) study on factors that affects thermal comfort, the thrust in this paper was on how Agricultural residues and marble dust influence thermal comfort.

Additionally, the buildings envelop (walls, windows, and roof) of energy-efficient houses are designed

in a way that they could reduce heat flow into and out of the building. First, the exterior walls should be designed with appropriate insulation to minimize heat transfer and help maintain the right temperature within the building that provides thermal comfort. In normal/conventional designs, windows are the most essential component/element in a building since ensure adequate free movement of air between inside and outside of a building thereby avoiding the trapping of heat (mostly derived from the roofing systems) at the interior of a building (Teles, 2016). Based on building airtightness and the ability to ensure a consistent and smooth conventional flow of air from the outside/exterior to the roof-mounted chimney through underground cooling systems/design, a constant ambient indoor temperature was achieved in both extremely hot (summer) and cold (winter) periods of the year. This forms the basic design concept and principle of the EEBN that was design, constructed, and equipped at the NUST campus.  Preliminary measurements and analyses carried out so far for the past five years (i.e. between 2014 – 2019) revealed results that are following the design concept i.e. ensure appropriate occupancy comfort and building energy efficiency at extremely hot and cold seasons without using conventional heating and cooling devices used in modern buildings. However, almost all materials used in the design of the house are all imported from varying factories and industries in Austria. Such key materials include walls and roof insulating materials; special perforated/air locked bricks; special underground heat exchangers; double-glazed windows, etc. With the design of a weather station and inlet air ducts at the outside compounded with installation of both data logger, humidity and temperature sensors, and outlet chimneys at the interior, the EEBN was

designed and energy performance of the building at both summer and winter were measured at well- defined time intervals throughout the measurement period.

Based on such positive outcome of Austria borrowed design concept and materials, there is a need to develop building materials from locally available agricultural wastes/residues that can give the same/similar positive building energy performance by using less or no energy from the local electricity grid to power generally known heating and cooling devices like air conditioning systems.

This research is a follow up on key conclusions on how energy efficiency /human comfort can be improved, based on the use of appropriate mix design of agricultural residues (Onjefu et. al., 2019).

The objective of this research was to construct design rigs, measuring in-situ the temperature and humidity in the Rigs made from locally available materials that are the residues of Agriculture and marble dust in Namibia. The Temperature conditions and Humidity were monitored and analysed, and the results were compared with the conventional buildings in terms of Energy Efficiency Building of Namibia (EEBN) built with conventional materials.

2.6.2 Energy analysis of buildings

The conventional energy analysis in buildings includes numerous stages. Key among these stages involved the calculation of the heating and cooling loads to be enforced upon the building by the Heating Ventilation and the Air Conditioning (HVAC) systems based on the work done by (Varkie, 2013). The calculations are carried out for a well-defined space at a fixed temperature with time. Hence, how much heat addition or extraction is required to maintain a constant temperature in the given fixed space as the outside weather conditions and internal activities vary in time while the building mass absorbs and releases heat?

Hence, this study assessed all these stages to ascertain whether a building built with materials developed from Agricultural wastes/residues has a better energy performance compared with those built with conventional materials and generally known design concepts.

2.6.3.1 Heating and Cooling Load

Heating and cooling load is one of the measures that are used to assess the energy efficiency of buildings. A study carried out by Matthew (2008) looked at heating load as the quantity of heat that must be added to the room and cooling load as the amount of heat that must be removed from the room to keep constant air temperature that leads to thermal comfort. The concept of heating and

cooling load is significant as it regulates the size of the Heating Ventilation and Air Conditioning (HVAC)

system that under extreme conditions within can afford thermal comfort.

Air conditioners regulate the temperature, humidity, and airflow inside a room or a building for human comfort irrespective of external conditions. HVAC can be classified according to winter air- conditioners that provide heating and humidification and summer air-conditioners provide cooling and dehumidification all year round to maintain thermal comfort (Gupta, 2010). This is an important classification that can be extended to the current study to analyse if the building with agricultural residues will be able to accommodate season in their performances.

In general, heating and cooling load is usually estimated based on four categories, namely heat due to

transmission, solar, infiltration, and internal load (Stoecker & Jonas, 2010).

2.6.3.2 Thermal Transmission

This comprises heat loss and heat gains through the building envelope (walls, windows, floor, and roof) due to temperature differences (Ambuga, 2018). The thermal transmission according to Ambuga, (2018) can be represented as:

Q= UA∆T	(2.1)

Where:

U = overall heat transfer coefficient (W/m2. K) A= surface area

T =temperature difference between the outside and inside (0C)

2.6.3.3 Solar

This involves the heat loss and heat gains due to the transmission of solar energy through the transparent building elements, generally the heat transfers through glasses and depends on the physical characteristics of the surface. Therefore, the solar energy passing through windows according to Ambuga, (2018) is represented as:

Qsg = SHGFmax x SC x A	(2.2 )

Where:

SHGF= Solar Heat Gain Factor

SC= Shading Coefficient

A = Surface area (m2)

2.6.3.4 Infiltrations

These are the heat losses and heat gain due to the diffusion or accumulation of air into and out of the building through cracks in the walls, opening of windows and doors. Stoecker & Jonas, (2010) stated that Infiltration varies with the quality of construction, wind speed, indoor-outdoor temperature difference, and the internal pressure of the building

2.6.3.5 Internal loads

It involves the heat gains due to the discharge of energy within the space and mainly generated by occupants, lights, and equipment operating within the space. According to Ambuga, (2018), the heat generated by the lighting and equipment depends on the rating while heat gain from the occupant depends on the level of activity of a person. Hence according to Ambuga, (2018), heat gain from lighting and equipment is given by:

Q= (rating in watt) (Fu)(CLF).	(2.3)

Where:

Fu    = utilization factor of the installed lamp in use

CLF = cooling load temperature difference

Heat gain from occupants:

Sensible heat load = gain per person x number of people x CLT, hence

Qsensible = Qsensible x N x CLT	(2.4)

Latent heat load = gain per person x number of occupants

Qlatent = Qlatent x N	( 2.5)

2.7 Ventilation systems

2.7.1 Types of Ventilation systems

The ventilation system is made up of two types namely; natural and mechanical. A pure natural ventilation system is one where the ventilation rises from flows through openings in the envelope, which are made by the natural forces due to wind and buoyancy (gravity) (Swenka, 2008). The envelope is the fabric that encloses the air, e.g. external and internal walls. Natural ventilation is the sole means of ventilation for thousands of years in all climates.

On the other hand, a mechanical ventilation system is one where the ventilation is delivered by a

network of ducts, driven by fan/fans. Mechanical ventilation is a recent phenomenon, which is suitable for the particular demands of large non-domestic buildings.   Swenka, (2008) classified mechanical system into three types:

➢  Extract only – the air is extracted through ducts, with openings in the envelope providing the

route for air supply.

➢  Supply only – air is supplied through the ducts, and openings in the envelope provide the exhaust route.

➢  Supply and extract system – separate duct networks perform the supply and extract functions,

which if the mass flow rates are equal, are denoted as a balanced system.

2.8 Low-energy ventilation systems

There is no exact definition of what is meant by a low-energy ventilation system, and even less for what constitutes a ‘sustainable’ or a ‘green’ system. Many factors need to be taken into considerations (Liddament, 1996). In the following, we focus on the more important ways in which the energy consumption directly related to the provision of ventilation can be reduced. it is significant to ponder on heating and cooling separately and in that order.

For a given flow rate of fresh air, Q (m3/s), the heating load, H (W), imposed on a building is:

Hv = ρcpQ(Tin-Tout )	(2.6)

Where ρ denotes density (Kg/m3), Cp the specific heat (J/Kg K), Tin the temperature of the air flowing into the building, and Tout the temperature of the air leaving the envelope.

Low-energy  forms  of  mechanical  ventilation  systems  can  be  attained  by  reducing  fan  energy consumption and the use of heat recovery. The fan energy consumed, E (J), is presented by

EF =100top QF ∆p/ῃ	(2.7) Where top is the operating time (s), QF the fan flow rate (m3 /s), Dp the pressure rise (Pa), and h the overall fan efficiency (%) (CIBSE,2005).

2.8.1 Air quality

A key role of ventilation is to conserve satisfactory air quality inside the building and this is often used for shaping flow rates for design.

Pollutants released inside the building mix with the internal air and are eventually conveyed out of the building. The mixing process is given by the internal air motion and the nature of the emissions. Though, the bulk features of the process can be seen by considering a single space of volume V (m3), in which the concentration is assumed to be unchanging at all times (mixing ventilation), with a steady (constant) ventilation rate, Q (m/s) and a steady emission rate of contaminant qc (m3/s). Under these

conditions, the concentration at time t (s) is given by (CIBSE, 2005):

�

�

C(t) = Cext +

�

��

106 – (Cext – C(0) +

�

106 ) exp ( �

𝑽

�	(2.8)

is the concentration in the external air (ppmv) and C(0) is the concentration at time t = 0 (ppmv). The steady-state concentration, C where C(t) is the volumetric concentration in parts per million (ppmv), Cst, is given by:

����

Cst = Cext +

�

106	(2.9)

For buildings, the fundamental purpose is often to uphold body odours at a suitable level. The CO2 concentration is directly linked to the number of occupants and it can be used as a measure of air quality.

Equation 2.9 can then be used to determine the vital ventilation rate. if space is occupied for a short

period (e.g. a theatre), Eq. 2.8 can be used to give a lower design ventilation rate.  The use of CO2 in the above way is based on the assumption that any other contaminants require lower ventilation rates.

2.9 Psychometrics

2.9.1 State of the air

The air in the atmosphere is a mixture of gases. It comprises 78.08% nitrogen, 20.95% oxygen plus a small number of inert gases such as argon and carbon dioxide, etc. Air also comprises of water vapour. Air that contains no water vapour is called dry air. When the air contains water vapour, humidity is a term that is used to describe the amount of water vapour in it (Swenka, 2008).

Based on the study done by Swenka, (2008), there are two ways to describe how humid the air is: the

quantity of water vapour contained in the air (absolute humidity) and the degree to which the air is close to its saturated state (relative humidity).  Absolute humidity is specified in terms of the mass of water vapour contained in one kilogram of dry air, i.e.

W = ��

��

(Kg water vapour/ Kg dry air)	(2.10)

Here, mw and mg are the quantities of water vapour and dry air, respectively.

Since the water vapour and air can be treated as an ideal gas under the relevant conditions, the absolute humidity can also be represented in the following form:

W = �.𝟔����

�−��

(Kg/Kg)	(2.11)

Here, 𝑝 is the total pressure which equals the sum of the partial pressures of dry air and water vapour

in the air. 𝑝 is water vapour pressure.

The relative humidity is the ratio of the mass of water vapour in the air to the mass of water vapour when the air is in a saturated state, i.e. the maximum amount of water vapour the air can hold under the same temperature and pressure. If the maximum amount of water vapour is denoted as mw, then

its vapour pressure is ��, thus according to the definition, relative humidity can be written as:

ⱷ =  �𝑤

���,�

=  �𝑤

���,�

(2.12)

Absolute humidity and relative humidity have the following relationship according to Eqs 2.11 and 2.12

��

ⱷ =

(0.662+�)�𝑔

(2.13)

Both absolute and relative humidity are of dimensionless units. The relative humidity ranges from 0 to

1 and is usually expressed as a percentage, where 0% indicates that the air is dry and 100% indicates that the air is saturated.

When the humidity of air reaches 100%, water vapour in the air starts to condense. This point is called the dew point. The temperature at which condensation begins as a result of cooling the air (at constant pressure) is called the dew-point temperature.

2.10 Thermal comfort

Thermal comfort is a term that is usually viewed as a desired or positive state of a person. It is used about how warm or cold a person feels and is related to the environment a person occupies.

The concern of whether the concept of thermal comfort is an international phenomenon is of interest if we are to agree that optimal conditions for indoor environments worldwide. Opinions against this assumption have generally pointed to the likelihood, or natural expectation, that people in hot conditions would prefer ‘warm’ or higher temperature conditions for thermal comfort than those that live in temperate or cold climates. Evidence suggests that this is not the case and that although people who live in hot or cold climates are better able to survive heat or cold respectively, conditions for thermal comfort do not vary (Fanger, 1970; Parsons, 2003).

2.10.1 Measurement of thermal comfort

According to Guildford, (1954), stated that the best ways of determining whether a group of people are comfortable are to ask them. Thermal sensation; comfort; pleasure; pain; as well as behavioural responses are all psychological phenomena. There have been many useful studies to ‘correlate’ physical conditions and physiological responses with psychological responses. However, no model provides a more accurate prediction than measuring psychological responses directly.

Methods for measuring psychological responses range from psychophysical techniques (method of

limits, method of magnitude estimation, multidimensional scaling (Guildford, 1954)

2.10.2 The comfort equation

Fanger (1970) defines three conditions for a person to be in (whole-body) thermal comfort:

•	the body is in heat balance;

•	sweat rate is within comfort limits; and

•	mean skin temperature is within comfort limits.

a fourth condition is the absence of local thermal discomfort (e.g. caused by draught). The objective was to produce a comfort equation requiring the input of only the six basic parameters and based on the above three conditions, to calculate conditions for thermal comfort. This was achieved using a rational analysis of heat transfer between the clothed body and the environment and experimental research. Fanger’s original work was not in SI units so the SI version presented below is taken from Olesen et al. (1982), ASHRAE (1989), and ISO 7730 (2005).

2.10.3 Heat balance

Fanger’s conceptual heat balance equation is:

H – Ed – Esw – E – L = K = R + C	(2.14)

where an explanation of the terms used is given in Table 2.4.

Heat is generated in the body and lost at the skin and from the lungs. It is transferred through clothing where it is released to the environment. Logical considerations, reasonable assumptions, and a literature review provide equations for each of the terms such that they can be calculated from the six basic parameters: air temperature (ta); means radiant temperature (t,); partial vapour pressure (Papv); air velocity (v); clothing insulation (I); and metabolic heat production (M–W, where M is the metabolic rate and W is external work). Table 2.5 provides the equations for the components of the heat balance

equation to determine the PMV thermal comfort equations. ts the mean surface temperature of clothing and exposed skin; tcl is mean skin temperature and fcl is a non-dimensional term for the ratio of the surface area of the clothed person to the surface area of the naked person; hc is the convective heat transfer coefficient in Wm-2K-1

Table 2.4 Terms used in the predicted mean vote (PMV) Source: Comfort equation of Fanger (1970)

| H | = | Internal heat production in the human body |
| --- | --- | --- |
| Ed | = | Heat loss by water vapour diffusion through the skin |
| Esw | = | Heat loss by evaporation of sweat from the skin surface |
| Ere | = | Latent respiration heat loss |
| L | = | Dry respiration heat loss |
| K | = | heat transfer from skin to the outer surface of clothing |
| R | = | Heat transfer by radiation from clothing surface |
| C | = | Heat transfer by convection from clothing surface |

Table 2.5 Equations for components of the heat balance equation used by Fanger (1970) in determining the PMV thermal comfort equations (see Table 2.4 for terms)

H	= M- W

Ed	= 3.05 x 10-3 (256ts – 3373 - Pa )

ts	= tsk,req i.e. for thermal comfort

= 35.7 – 0.0275H

Esw = Ersw,req i.e. for thermal comfort

= 0.42(M – W – 58.15) L	= 0.0014M (34 - ta)

Ere = 1.72 x 10-5 M (5867 – Pa)

(��− �𝑐�� )

K	=

0.155 �𝑐𝑙

R  = 3.96 x 10-8 fcl [ ( tcl + 273)4 – ( tr + 273)4] C = fclhc(tcl – ta)

2.11 Computational fluid dynamics

Computational fluid dynamics (CFD) is a tool for simulating and analysing fluid flows numerically using computers. In the ventilation industry, the tool can be used to analyse important factors affecting the thermal and atmospheric environment such as the airflow pattern, pressure, temperature, humidity, and heat distribution. The tool is therefore perfect for design and research of ventilation. According to Kayne, (2012) CFD takes place in three phases: Firstly, a pre-processing application (in the current work, ANSYS WORKBENCH) is used to launch the geometry of the model. Boundaries (such as walls, inlets, and outlets) are also defined in this stage. When the geometry and the boundary conditions for the problem are completed, the computational domain in defining the problem is divided into quadrilateral or triangular cells in 2-D; or hexagonal or tetrahedral cells in 3D, which form a mesh or a grid (Kayne, 2012). The mesh is then imported to ANSYS FLUENT 18.2 for making the flow field solutions at mesh points. Also, proper boundary conditions such as wall temperature, inlet velocity, and gauge pressure are applied in the computational domain.

The CFD Solver FLUENT creates the flow field data at each mesh point after solving the appropriate

governing equations. Once the flow field is made by FLUENT, it is disseminated to a data processor to generate line plots and flow variable contours. The data can also be spread to other software such as Excel to permit comparisons with the other calculations and data in an easy manner.

In recent times, CFD has been contributing clearly to the design of energy-efficient, user- comfortable,

and environmentally friendly buildings (Zhai 2006; van Hooff and Blocken 2010).

2.12 Mesh

The mesh has a great impact on the numerical outcome, accuracy of simulations, and convergence. When generating the mesh, it is vital to have an upper resolution where the gradients are high. Where the mesh is coarser, one must therefore analyse the problem before the simulations are made. It is not obvious how fine the mesh should be and how many cells or nodes your domain should contain. The number of cells/ nodes at the inlet and outlet is important for convergence. If for example, the pressure outlet has a coarse grid, the solution can "jump" between different solutions as the quantities in the coarse cells change.

The mesh quality plays a vital role in the accuracy of CFD. ANSYS Fluent checks important quality

parameters of the elements. Two important indicators are orthogonal quality and skewness. The range for orthogonal quality is 0 to 1 where 0 is the worst and 1 is the best. For the skewness 0 is best and 1

is worst (Hjermann, 2017). For all quality indicators, it is the worst cell that explains the quality, and one should check where these cells are situated to find out whether they affect significant areas of the simulation are as shown in Fig. 2.3.

Figure 2.3: Model computational mesh

2.13 Mathematical model for heat simulation

Srigiriraju, (2015) stated the Navier Stokes Equations in 3D in Cartesian coordinates as

��( ��� + 𝑈�  * 𝜕�� )   = -  𝜕�

+ µ(��2𝑈�/��𝑥�2  ) +  ��𝑔�	(2.15)

��	𝜕𝑋�

𝜕𝑋�

Continuity Equation can be written as

Where,

𝜕𝜌

𝜕�

������

+

����

= 0	(2.16)

Ui represents the velocity vector component in the ith direction,  𝜌 is the density of the fluid, P is the

Pressure, gi is the gravity in the ith direction and µ is the viscosity.

This principle states the rate of increase of fluid mass limited within a given space must be in equilibrium to the difference between the rates of influx into and efflux out of the space (Gdhaidh,

2019).

Figure 2.4: Flow domain of interest

2.13.1 Momentum equations

Newton’s second law of motion states that the rate of change of momentum of a fluid particle is equaled to the sum of the forces on the particle (Shati, 2013). The general form of the momentum equation in the x and y coordinates for a turbulent flow is:

The x-direction of the momentum equation is denoted as,

��(𝜌�)

𝜕�

��(����)

+

𝜕�

��(����)

+

𝜕�

��(�)

= -	+

𝜕�

𝜕

𝜕�

[µ (

𝜕�

𝜕�

𝜕�

+

𝜕�

)]	(2.17)

Where P is the static pressure and µ is the viscosity.

The y- component of the momentum equation is also denoted as follows,

��(𝜌�)

𝜕�

��(����)

+

𝜕�

��(����)

+

𝜕�

��(�)

= -

𝜕�

𝜕

+

𝜕�

[µ(

𝜕�

𝜕�

𝜕�

+

𝜕�

)] +𝜌 𝛽��(T-T0)	(2.18)

Where 𝜌 𝛽��(T-T0) is denoted as the Boussinesq approximation, 𝛽  is the thermal expansion coefficient

and the gravitational acceleration is denoted as g.

2.13.2 Energy equation

The energy equation of heat transfer in a two-dimensional coordinate system is given as:

∂(ρCpT)

∂t

∂(ρuCpT)

+

∂x

∂(ρvCpT)

+

∂y

=  ( ∂  [K

∂x

∂T)] +

∂x

∂ 	∂T

[K (

∂y 	∂y

)]	(2.19)

Multiplying equation 2.18 by

𝜕�

𝜕�

and also equation 2.19 by

𝜕�

𝜕�

, the result will give a single equation as:

( ∂  ( ∂v/ ∂t + u ∂v  + v ∂v

∂ 	∂u 	u ∂u 	∂u 	∂2

) -	(	+	+ v	) = ϑ [∂/ ∂x(

v 	∂2

+

v 	∂2u

) - [∂/ ∂y(	+

∂x

∂2u

∂x 	∂y

∂T

∂y    ∂t 	∂x 	∂y

∂x2

∂y2

∂x2

∂y2 )] +gβ ∂x 	(2.20)

The combined momentum equation controls the flow of air in the enclosure due to the effect of

Buoyancy (Shati, 2013).

2.13.3 Dimensional numbers

The governing equations due to free convection the non-dimensional number and the variables are added to form a reduced number of variables.

2.13.4 Nusselt number

Looking at the heat transfer from a fluid layer of surface area A, a thickness L and a temperature difference between two sides of ΔT = T1 – T2. If the fluid is moving, from the equation (Shati, 2013):

Qconv = h A (Ta- Tb)	(2. 21) Where Qconv is the heat transfers by convection, h is the convection heat transfer coefficient, Ta is the temperature of the surface, Tb is the temperature of the fluid and A is the surface area.

Also, according to Shati, (2013) when a fluid is motionless the heat will be moved by pure conduction

as given by the equation:

Qcond = KA (T1 – T2) / L	(2.22)

By dividing equation (2.21) by equation (2.22):

����� =	{� 𝑨 (�� – ��)}

=  �� = Nu	(2.23)

�����

���(�� – ��) / �	�

The dimensionless number formed is called the Nusselt number (Shati, 2013), which signifies the number of times that the heat transfer is improved by convection relative to that of conduction. This can be said that the larger the Nusselt number, the more effective the convection heat transfer.

2.13.5 Reynolds number

According to Srigiriraju, (2015), Reynolds number is defined as the ratio of inertial forces to viscous forces.

Re =

𝑰�����𝒂� ������

=

𝑽������ ������

��𝑽�

µ

(2.24)

Where 𝜌 is the density of the fluid, V is the velocity of the fluid, L is the characteristics length of the fluid and µ is the viscosity of the fluid.

2.13.6 Grashoff number

The Grashoff number is defined as the ratio of the buoyancy to viscous forces acting on a fluid (Srigiriraju, 2015). Also, the Grashoff number is the magnitude that considers flows to be Laminar or turbulent.

Gr=��( �� − �ø)  L3	(2.25)

𝝑

Where g is the gravity, β is the volumetric thermal expansion coefficient, Ts is the surface temperature,

Tø is the bulk temperature, L is the characteristics length and 𝜗 is the viscosity of the fluid.

According to  Bejan and Kraus, (2003) the product of the Grashoff number and the Prandtl number is

given as the Rayleigh number:

��( �� − �ø)

Ra=GrPr =

L3 * Pr	(2.26)

𝝑

Where Prandtl number is:

Pr =

µ𝑪�	𝝑

=  =

�	�

(2.27)

The Rayleigh number in free convection is similar to the Reynolds number in forced convection and is a degree by which the flow can be solved as laminar or turbulent. Inside enclosures, the transition from

laminar to turbulent flow occurs when the Rayleigh number is more than one million (Holman, 1997: Markatos and Pericleous, 1984).

2.13.7 Dimensionless temperature

Srigiriraju, (2015) define the dimensionless temperature as:

T•= (� – ��)/(L2• �/� )	(2.28)

Where T is the measured temperature, Tm is the ambient temperature, L is the characteristic length,

Q  is the applied heat flux and K is the thermal conductivity.

2.14 Approximating the differential equation by a numerical equation

The purpose of approximating a differential equation that describes a system by an appropriate numerical method is to give a definite numerical algorithm, which allows the effective numerical computation of the solution of the mathematical problem. The differential equation is simply changed into a difference equation, finite difference method (FDM), or finite difference volume (FDV), alternatively calculated by evaluating an equivalent variation problem, finite element method (FEM).

2.14.1 The Finite-Volume Methodology

In this technique, the first phase is the integration of a generic transport equation for quantity ∅ over

a three-dimensional control volume V (Pinho, 2001).

𝝏

∫

� 𝝏��

(������)��� −  ∫�

𝝏

𝝏��

[𝜞

𝝏∅

𝝏��

] ��� =  ∫� �∅ �𝑽

(2.29)

Following, Gauss’ divergence theorem to the left-hand side of Equation (2.29) that is

∫  𝝏∅�

� 𝝏��

��� =  ∫𝑨 ∅����𝑨

(2.30)

Where ni is the unit vector normal to the surface element dA. This theorem transforms volume integrals of divergence terms into surface integrals of fluxes all around the control volume; Gauss' theorem gives integrated conservation equation:

𝑨	(	)	𝑨	𝝏�	�

𝝏∅

∫ ��  ����𝝋 ��� − ∫ ��  [𝜞	] ��� =  ∫ �∅ �𝑽

�

(2.31)

2.14.2 Discretisation

When numerical methods are used to solve partial differential equations (PDE) including boundary and possible initial conditions, in this case, a second-order partial differential equation for steady-state heat conduction in two dimensions, a network of grid points is first established throughout the geometry of concern. The geometry must be divided into small elements as shown in Figures 2.8 (a) and (b).

Figure 2.5- Two-dimensional control volumes in an orthogonal grid. (a) General grid

(b) A control volume and its neighbours.

Figure 2.8-a displays the grid mapping of a specific calculation domain in the x-y plane coordinate, for example, flow in and out of a box. Figure 2.8-b separates a computational molecule of a control volume bounded by its nearest neighbours and gives the resultant notation. The central control volume is signified by its node P, where the fluid and flow quantities are stored and its neighbour nodes are denoted by W, E, S, N for the west, east, south, and north cells, respectively (Pinho, 2001). Nodes are always represented by capital letters and the faces of the control volume P adjacent to a given neighbour cell F= W, E, S, N is identified by the corresponding small letter f= w, e, s, n.

In discretizing Equation (2.22) the following estimates are applied:

i)	The integral of g is estimated in terms of the values of g at numerous positions on the cell face. The simplest estimate accepted here is the midpoint rule, which is of second order, whereby g is the value at the centre of the cell face (represented by crosses in Figure 2.8- b), i.e.

(2.32)

In this integral ḡf may represent a convection flux (ni � ui), or a diffusion flux (ni  Γ

∂ϕ

) f. It is noted that

∂xi

other higher-order approximations could be applied but they lead to an integration rule requiring more

points on the cell face.

ii. The cell face values of the function gf are approximated in terms of the nodal values gF.

2.15 Building materials

Building materials have many purposes, and the most significant concerning energy efficiency is to reduce heat and moisture from the house. The main conditions for choosing the building materials are based on the thermal performance and availability of the materials locally. The ‘’insulation coupled with a reflective coating will reduce heat transfer through walls and roofs; glazing windows and low emissivity; glass will help as well for transparent surfaces’’ (Baeza, 2013). To prevent moisture inside the house a vapour barrier is required. Fire protection and noise insulation are other features of the building that have to be considered.

2.16 Insulation materials

These materials aim to decrease the heat transfer within the environment and the house. According to literature, heat can be transferred by conduction, convection, and radiation. The insulating performance depends on the thermal properties, which depend on several operating conditions as well.  The thermal conductivity k (W/m K) is the one that defines the performance of the material under heat conduction, which is the main heat transfer through the building envelope (Baeza, 2013). Moreover, the author stated that a high k means a low thermal resistance, which indicates a poor thermal insulation performance. Many studies looked at different types of thermal insulation materials and their economic importance in building (Kaynakli, 2012).

A good extent of thermal insulation in the building envelope supports to lessen the cooling and heating

energy usage of a building and its related carbon dioxide (CO2) and sulphur dioxide (SO2) discharges into the atmosphere as validated by Charde, (2013), Comakli and Yuksel (2004), Dombayci (2007), Mahlia and Iqbal (2010). Thermal insulation supports the saving of energy by decreasing the rate of

heat transfer. Several studies have been carried out in diverse climate conditions to evaluate the thermal insulation used in external walls (Kaynakli 2008; Ucar and Balo 2009; Daouas et al., 2010). Some researchers considered both annual heating and cooling loads (Bolatturk 2008; Yu et al. 2009; Ucar and Balo 2010). Sodha et al. (1979), Al-Sallal (2003), Ozel, and Pihtili (2007) examined the most appropriate position for the roof and/or walls insulation. Several works have been done to carry out the properties of thermal insulation materials (Al-Homoud 2005; Papadopoulos and Giama 2007; Anastaselos et al. 2009).

2.17 Building thermal system

According to Risberg, (2018), Indoor climate is classified into four climate factors; which include: thermal climate, indoor air quality, sound, and light. Nilsson et al., (2003) described the indoor air quality as the concentration of polluting gases and particles in the air that is influenced by the polluting sources, outdoor conditions, and the ventilation performance. The thermal climate is referring to the heat balance of the human body. It is influenced by all heat transfer mechanisms that appear against the human skin and the heat generated inside the body to have a stable body core temperature around

37oC  (Prek,  2005).  Also,  Fanger,  (1970)  developed  a  model  from  an  experiment describing  the

statistical number of dissatisfied people, where most of the heat transfer mechanisms that appear are considered. Some Parameters that influence thermal comfort are the metabolic rate, external work, clothing insulation, air temperature, radiation temperature, air velocity, and relative humidity (Lin et al., 2008). The last four parameters are influenced by the envelope surfaces and heating system of the building.

The heat balance of a building consists of four major parts: building component and materials, heat transfer processes, internal heat, and external conditions as presented in Figure 2.6.

External conditions

➢	Outdoor

temperature

➢	Solar Radiation

➢  Wind speed

➢	Relative humidity

➢	Pollution

Building heat balance

Components:

➢  Walls

➢  Ceiling/roof

➢  Foundation

➢  Windows

➢  Doors

➢  Thermal bridges

Internal Heat

➢	HVAC

➢  Equipment

&Appliance load

➢  Occupant load

➢	Lighting load

Heat transfer process

➢  Heat transfer

❖ Convection

❖ Radiation

❖ Conduction

➢  Thermal storage

➢  Ventilation

Material properties

➢  Heat transmition

➢  Heat capacity

➢  Density

➢  Surface

characteristics

➢  Emissivity

Figure2.6 Outline of parts in the building heat balance (Risberg, 2018)

2.18 Building elements and materials

The heat transmission through walls and ceiling results from building elements causing a high heat loss for most houses due to their relatively great area (Risberb, 2018). Hence the energy efficiency of such a building is measured by the extent to which these components and some others are insulated. Their direct contact with outdoor conditions results in a one-dimensional (1D) approach applicable for building simulation of these building components (Martin et al., 2010). Also, the use of overall heat transfer coefficients according to ISO 6946 standard is applicable for heat demand calculations for walls and ceiling constructions.

Also, the largest heat flux in a building is through windows. However, depending on the orientation,

area, and position, windows can be the highest heat loss in a building. Major improvements have been made during the last decades to reduce heat losses. This includes window glazing with improved coatings to reduce the emissivity (Pilkington, 2010).

Heat losses at the foundation are difficult to forecast since numerous disturbing parameters including the high amount of thermal inertia in the soil (Spiga, 2014). Also, in a cold climate, temperatures below zero and snow are parameters that can also disturb the thermal performance.

A thermal bridge, also called a cold bridge, or thermal bypass is an area or component of an object that has higher thermal conductivity than the surrounding materials (Martin et al., 2011) as shown in Figure

2.7. Also, Lorenzati, et al., (2016) stated that the thermal bridge is creating a path of least resistance for heat transfer. Furthermore, thermal bridges result in an overall reduction in thermal resistance of the object. The term is often debated in the context of a building's thermal envelopes where thermal bridges result in heat transfer into or out of conditioned space. Again, Thermal bridges in buildings may impact the amount of energy required to heat and cool a space, causing condensation (moisture) within the building envelope resulting in thermal discomfort (Evola et al., 2011).

Building material is mainly specified by mechanical properties. It is frequently stated in terms of mechanical properties or thermal insulation capabilities. For heat transfer and thermal indoor climate performance, the insulation capabilities have the highest interest. Common insulation materials are well studied by different researchers and specified in the ISO standards (B. ISO, 2007; Papadopoulos, A.M. 2005); BS EN. 2012). Also, Mohammad and Al-Homoud, (2004) have summarized the thermal performance of the most common building insulation materials. Many research studies have been made based on the state of the art material, like phase change materials (Demirbas, 2006), Vacuum insulation panels (VIP) (Baetens, et al., 2009), Gas-filled panels (Baetens et. al., 2010), and aerogels (Baetens, 2011). Also, improvements in commonly used building materials have been studied and developed. These include Mineral wool; expanded polystyrene (EPS); Extruded polystyrene (XPS); and Cellulose and Polyurethane (PUR). Also, new materials like Nano insulation materials and dynamic insulation materials have emerged Jelle, (2011).

Figure 2.7 Thermal bridges at the junction

2.19 Basic Theoretical Information

The following are basic theoretical information that is relevant and key in this research work:

2.19.1   Conduction heat transfer

Heat transfer is the process of thermal exchange between two or more systems. The heat transfer between two regions will be from the hotter to the cooler regions of a system. This is important in building for determining the design of the building fabric.

Conduction is the transfer of heat within a body as a result of the temperature difference across it. It is important in the building where there may be a temperature difference between the inside and the outside of the building. According to Akbari et.al., (2011) heat transfer is a function of temperature.

Q = AKAT/ ΔX = Q / A = KAT/ ΔX	(W/m2)	(2.33)

K = Ko (1+ βt)	(2.34)

Where,

Q = total amount of heat transfer, K = thermal conductivity

Ko = thermal conductivity at 0o C, βt = temperature coefficient of thermal conductivity, A = area of heat transfer, T= temperature.

2.19.2 Heat Conduction in Plane Wall

Akbari et.al., (2011) defined heat conduction as the transfer of energy from a dense substance to a less dense energetic substance due to the interaction of the particles. According to the first laws of Thermodynamics:

Q•	•

in - Q out= dEwall/dt	(2.35)

For a steady operation

Q•	•

in = Q out = constant	(2.36)

Where,

Q•

in = heat transfer inside the wall, Q•in = heat transfer outside the wall,

dE	= change in Energy, dt = temperature difference.

The study by Akbari et.al., (2011) further investigated experimentally that heat conduction through a wall is proportional to the temperature difference across the wall and the heat transfer area, and

inversely proportional to the thickness of the wall.

Q•

cond.= KAΔT / Δx	(2.37)

Where,

K = thermal conductivity of the insulation material, A = area of heat transfer, ΔT = temperature difference, Δx = thickness of the layer.

2.19.3 Heat transfer by convection

Convection is the process by which heat travels through fluids that is liquid and gases. It is important principles in the building where air movement is necessary to moderate the internal temperatures, to reduce the accumulation of moisture, odours, and other gases, and to improve the comfort levels of the occupant in the room.

Veloo, (2013) showed that the convective heat transfer is related to air movement in buildings. The study looked at the convective heat transfer as the difference between the heat flow through the building elements and the longwave radiation.

qc = qcond -  qr	(2.38)

For the absorb solar energy,

qc = qcond - qabs	(2.39)

The convective heat transfer is then calculated as,

hc = qc / (Tref - Tsurface) = qc /ΔT	(2.40)

Where,

qc = convective heat transfer, qcond = conductive heat transfer, qr = longwave radiation, hc = convective heat transfer coefficient,

Tref  = reference temperature, Tsurface = surface temperature.

2.19.4   Heat transfer by radiation

Radiation heat transfer is the interaction of energy between two or more bodies. Heat transfers by radiation in buildings through transparent building envelopes and from internal heat sources to the building envelope. The main source of radiant heat in a building is through windows and glass doors which transmit solar radiation directly to the building (Somayeh, 2003). Almshkawi, (2011) showed that the radiative heat coefficient will only apply to radiation exchange between surfaces with less ambient temperature.

E= αrad. ΔT	(2.41)

Where, E = energy, αrad. =    radioactive heat coefficient,

ΔT. = temperature difference.

2.19.5 Solar Radiation

Namibia has more than 2400 kWh/m² in a year; Namibia is regarded as one of the countries with the highest amount of solar radiation in the world* (Zalaudek, 2013). Figs. 2.8 – 2.9 shows how the intensity is distributed across key regions in the country as well as in Windhoek across the 12 months of the year respectively.

Figure 2.8: Solar Radiation across regions in Namibia (SolarGIS-Solar-map-Namibia, 2017)

Sum of direct horizontal radiation

Sum of diffuse horizontal radiation

Figure 2.9: Monthly solar radiation of Windhoek, Namibia (Zalaudek, 2013)

CHAPTER THREE

LABORATORY SETUP, TEST, AND MEASUREMENT

3.1 Overview

This chapter focuses on the sample collection, preparation, and development of particle boards, bricks, and rigs. The procedures on how the samples were developed and the different equipment used for the developments of the samples are also highlighted. The different mixed compositions of the samples are also shown in the chapter. This chapter agreed with the specific objective of developing affordable and highly thermal efficient insulating materials from millet husks, rice husks, maize husks, and cow dung residue for the design of energy-efficient buildings.

3.2 Sample collection

Samples were collected in the Khomas, Erongo, Kavango, Omusati, and Zambezi regions of Namibia. Cow dungs were collected in the Okapuka meat co farms located 30 kilometres along the Windhoek

and Okahandja road. The Okapuka Feedlot is an intensive animal production system that helps animals below 18 months and weighing more than 280 kilograms to attain the preferred market value requirements.

Marble dust was sourced from the Karibib mines located between Karibib and Swakopmund in the Erongo region while rice husk was collected from the University of Namibia (Unam) rice mill production in the Zambezi region. Moreover, millet husks were sourced from local farms in the Kavango East region while Maize husks were collected from local farms in both the Omusati region and Namib mills in Windhoek. Debris and all other forms of unwanted materials were removed, and samples were carefully categorized for each of the Agricultural residues. Samples were later transported to specific laboratories at the Namibia University of Science and Technology for further analysis. Figures 3.1 shows regions and towns where samples were collected.

Katima Mulilo

Karibib

Figure 3.1 - Regions and Towns Samples Collected

3.3 Sample preparation of Particleboard

3.3.1 Overview

Particle Board (PB) is defined by Wang et al., (2008) as a panel product developed from wood products or other materials having lignocellulose properties attached by urea-formaldehyde or other synthetic resin under high temperature and pressure to produce boards/sheets. The primary lignocellulose materials used in the particleboard industry are wood residues while agro-based residues/wastes from palm stalks, rice straw, rice husks, and other type’s plant were also explored for producing particleboards The use of such agricultural residues for particleboard production is important for reducing the demand of woods and improving the environment (ASTM, 1999). Also, a study carried out by Singh, (2015) stated particleboards as lightweight boards that can be recycled as thermal insulators, ceiling boards, wall partitions, doors, and some other household furniture. Recently, agro- based wastes are being integrated into green buildings designs because they are usually more economical and sustainable. This led to the development of new environmentally friendly building technologies from using agricultural residues like maize cob, rice husk, groundnut shell (Mgbemene et al., 2014 and Sekaluvu, et al., 2014), coconut coir, durian peel (Khedari, et. al., 2004). Some works have been done towards the improvement of composite particle and ceiling boards from both industrial and agricultural wastes/residues in Namibia and other parts of the world (Onjefu et al., 2019). Sawdust, wastepaper, and starch were mixed by weight to produce a ceiling board with good physical, mechanical, and thermal conductivity properties (Obam, 2012).

3.3.2 Preparation of Particleboard/Isolating Material

The laboratory preparation of each of the samples was done in the materials laboratory at the Namibia University of Science and Technology. Residues were washed in water and initially sun-dried for three days. To remove additional moisture, samples were further oven-dried to a temperature of 1100C for

24 hours and ground into smaller particle sizes of 0.1mm using the Retsch SK100 hammer mill shown in Figure 3.8. The final nature of samples is as shown in Figures 3.2 – 3.6. Moreover, to ensure proper binding and compaction, 20% of cement was added in the various percentage samples mixes. The combined mixed were filled into a 220mm X 110mm X 40mm mould, compacted, and cured under the sun  for  7  days  at  an  average  temperature  and  humidity  of  270C  and  79.7%  respectively.  The

particleboard  that  was  developed  from  the  agricultural  waste/residue  was  mixed  in  different percentage composition as shown in Table 3.1 and Figure 3.7.

Table 3.1: Percentage composition of samples

| Samples | Maize | Millet | Rice | Cow dung |
| --- | --- | --- | --- | --- |
|  | % | % | % | % |
| A | 40 | 30 | 10 | 20 |
| B | 10 | 40 | 20 | 30 |
| C | 20 | 10 | 30 | 40 |
| D | 30 | 20 | 40 | 10 |
| E | 25 | 25 | 25 | 25 |
| F | 10 | 25 | 50 | 25 |
| G | 15 | 25 | 10 | 50 |
| H | 20 | 20 | 30 | 30 |
| I | 30 | 30 | 20 | 20 |
| J | 50 | 15 | 25 | 10 |
| K | 25 | 50 | 10 | 15 |

Thermal conductivity and thermal resistivity tests carried out on all samples shown in Table 3.1

revealed samples A and C have the lowest and highest thermal conductivity respectively. To further investigate their behaviour, 5%, 10%, 20%, and 30% by weight of marble dust was introduced in both the best and worst thermal conductivity samples i.e. samples A and C as shown in Table 3.2. This is to ascertain the contribution of marble dust in the thermal conductivity in both samples.

Table 3.2 Percentage composition of samples A and C with Marble dust

| Samples | Marble dust % | Marble dust % | Marble dust % | Marble dust % |
| --- | --- | --- | --- | --- |
| A | 5 | 10 | 20 | 30 |
| C | 5 | 10 | 20 | 30 |

Figure 3.2 – Sample of Cow dung

Figure 3.3 – Sample of marble dust

Figure 3.4 – Sample of ground rice husk

Figure 3.5 – Sample of ground maize husk

Figure 3.6 – Sample of ground millet husk

PERCENTAGES OF SAMPLE MIX

60

50

40

PERCENTAGE

Maize %

30

Millet %

Rice %

20

Cow dung %

10

0

A	B	C	D	E	F	G	H	I	J	K

SAMPLES

Figure 3.7 - Sample mixture for particleboard

3.3.3 Preparation and Production of Bricks

Tables 3.3 – 3.6 show various selected compositions for the various brick types A, B, C, D containing maize, rice, cow dung, and millet respectively. The samples were crushed into smaller particles sizes using the Retsch SK 100 hammer milling machine of 0.1mm sieve diameter size as shown in Figure 3.8

Furthermore, the samples were prepared in various percentages and were also combined with 20%

cement as a binder to ensure proper compaction. The combined mixes were filled into a 230mm X

110mm X 85mm mould as shown in Figure 3.9, compacted with 2.5 kg Rammer at drops 30 cm blow, sun-dried at temperature, and average humidity of 240C and 79.7% respectively for 14 days. A sample of the final brick produced is as shown in Figure 3.10.

Figure 3.8 Retsch SK 100 hammer mill

Figure 3.9 The Brick Making Mould	Figure 3.10 The brick test sample

Table 3.3 Composition of Maize Husk Mix with Sand

Bricks types

Sand (%)

Maize Husk (%)

| A | 80 | 20 |
| --- | --- | --- |
| B | 60 | 40 |
| C | 40 | 60 |
| D | 20 | 80 |

Table3.4 Composition of Rice Husk Mix with Sand

Bricks types

Sand (%)

Rice Husk (%)

| A1 | 80 | 20 |
| --- | --- | --- |
| B1 | 60 | 40 |
| C1 | 40 | 60 |
| D1 | 20 | 80 |

Table 3.5 Composition of Cow Dung Mix with Sand

Bricks types

Sand (%)

Cow dung (%)

| A2 | 80 | 20 |
| --- | --- | --- |
| B2 | 60 | 40 |
| C2 | 40 | 60 |
| D2 | 20 | 80 |

Table 3.6 Composition of Millet Mix with Sand

Bricks types

Sand (%)

Millet Husk (%)

| A3 | 80 | 20 |
| --- | --- | --- |
| B3 | 60 | 40 |
| C3 | 40 | 60 |
| D3 | 20 | 80 |

3.3.4 Preparation of experimental rigs

Three experimental rigs labelled A, B, and C of dimensions 1.5 m (length) x 1.5 m (width) x 1.5 m (height) were constructed as shown in Figure 3.11 using locally produced 201mm x 100mm x 100mm bricks. The three experimental buildings were built using agricultural residues from rice, maize, millet, and cow dung but with the following specifications:

i.	Rig A: Agricultural residues containing 20% maize, 10% millet, 30% rice, and 40% cow dung

(considered as sample C from Table 3.1) as an insulating material between two brick walls, 50 mm apart. Sample C from experimental results shown in Table 4.1 in the next chapter gives the highest thermal resistivity, hence the lowest thermal conductivity)

ii.   Rig B: Agricultural residue containing 20% Marble dust mixed with 40% maize, 30% millet, 10% rice and 20% cow dung (considered as sample A, from Table 3.1)) as insulating material board between two brick walls, 50 mm apart.  Sample A, from experimental results shown in Table

4.1 gives the lowest thermal resistivity, hence the highest thermal conductivity)

iii.  Rig C: Control rig constructed using locally produced 201mm x 100mm x100 fired bricks with

conventional single-layered brickwork with no insulation.

(A)	(B)	(C)

Figure 3.11 Three experimental used in the research

3.4 Laboratory Tests: Tools, Procedures, and Measurements

3.4.1 Overview

Below are details of laboratory tools/machines used to derived at experimental result obtained for thermal conductivity, thermal resistivity, water absorption, and compressive strength on insolating board and bricks

3.4.1.1 Thermal Conductivity Test Tool (EP500e)

Figures 3.12 and 3.13 show the principal characteristics of a guarded hot plate device (GHPA) used in this research and which is usually accepted as a significant method for evaluating the thermal conductivity and thermal resistivity of insulating materials. The apparatus measures the thermal conductivity, thermal resistance as well as the k-value and U-value respectively of an insulating material (Onjefu, et al., 2019).

The EP500 lambda machine is specifically designed for testing insulation and construction materials

under ISO 8302, ASTM C177, EN 1946-2, EN 12664, EN12667, EN 12939, DIN 52612. Namibia also adopts this standard for energy-efficient insulating materials for building and SANS 204 as well.

Figure 3.12:  EP500 lambda machine

Fig.3.13 Set up for Thermal Conductivity Measurement

3.4.1.2 Water Absorption Test

Water absorption tests were conducted for different samples of brick types. The water absorption (WA) test was used to determine the amount of water each brick can absorb after 24 hours of soaking. The samples were formed using the mould size in Figure 3.9 that produced a brick size of 230 mm X

110 mm X 85 mm according to ASTM C 62 (2007).

In the water absorption test, samples were first weighed in a weight balancing device before immersed in water and the initial weight noted. Brick samples were then horizontally placed in a large container of water for 24 hours at a temperature of 200C and again weighed. The water absorption for each brick composite was determined by using the formula:

Water Absorption % = Final weight –  Initial weight x 100	(3.1) Initial weight

3.4.1.3 Compressive Test

Two bricks from each sample type were collected, and the detailed finishing of brick edges was done to ensure a perfectly regular rectangular shape. Bricks samples were then horizontally between the two plates of the uni-axial compression testing machine shown in Figure 3.14. The constant load was applied axially at a uniform rate of 14 N/mm2 per minute till failure/crushing occurred and the maximum load at failure was recorded. The load at failure is the maximum load at which the specimen fails to produce any further increase in the indicator reading on the testing machine. The crushing strength was then calculated as the ratio of crushing load to the area of brick loaded. The average crushing strengths of two specimens were taken by (Venkatesan, et al., 2015).

3.4.1.4 Density

The densities of the bricks were determined under the American Society for Testing and Materials (ASTM) C303-02 (Standard test method for dimensions and density of preformed block and board type thermal insulation) (ASTM, 2004). From each of the produced bricks, two (2) specimens of 230 mm x

110 mm X 85 mm were cut. The thickness, length, and width were measured, with the thickness measured and the average of each was determined and recorded. The volume of each specimen was then calculated.

Each specimen was weighed using a digital weighing balance and the mass recorded. The density of each specimen was then calculated using equation (3.2)

�𝑎��  �𝑔

Density =

������  �3

(3.2)

Figure 3.14: Uniaxial Compressive Test Machine Used

3.4.1.5 Experimental Rigs

Three rigs carried out for this research were constructed using 201 mm (length) by 100 mm (width) by

100 mm (height) bricks with a 7 MPa compressive strength. The design specifications of each of the rigs are as follows:

Rig A: made of double-layered brick walls on all 4 sides separated by 50 mm thick cavity with sample C mix design that is 20% (by weight) maize husks, 10% (by weight) millet Husks, 30% (by weight) rice husks and 40% (by weight) cow dung.   The insulation material (i.e. sample C) was mixed with 3% Powafix creosote insecticides to prevent insect attack on the building. Two windows, 40 cm height by

50 cm width (i.e. one at both east and west) were placed in this Rig to give adequate light during the

day.

Rig B: Built with the same brick dimension, strength, and cavity thickness but insulating material i.e. sample C mixed with 20% (by weight) of marble dust Like Rig A, the insulating material was also treated with 3% insecticide to prevent insect attack to the Rig.

Rig C: Built with the same brick dimension and strength but with no cavity walls and insulation. This is considered as the control Rig representing conventional single-layered brickwork.

A door (120 cm height by 60 cm width) on the north wall was placed in the Rigs as shown in Fig.3.11. The 50 mm cavity thickness was chosen as the minimum thickness in compliance with the building code for Namibia and South Africa (REEEI, 2013).

The thermal performances of the three Rigs shown in Figure 3.11 were evaluated based on the internal ambient temperature and humidity at a height of 1.5m. The external temperature and humidity were also measured. The temperature and the humidity data were recorded with the data logger at 15 minutes’ intervals.

3.4.2 Sensors: Types, application, and measurement

3.4.2.1 Temperature sensors

Thermo wire NiCr-Ni:

Thermocouples used to consist of two spot-welded wires of different metals or alloys. The thermoelectric effect at the contact surface is used to measure temperatures. A relatively small thermoelectric voltage was produced since it depends on the temperature difference between the measuring point and the connecting terminal (Zalaudek, 2013). The technical specification and nature of the thermos wires used are as shown in Table 3.7 and Figure 3.17 respectively.

Table 3.7: Technical data of thermo wires

| Technical data of thermos wires |  |
| --- | --- |
| Manufacturer and probe | Symmetron Stylitis 101 |
| Specification | Thermowire: NiCr-Ni (Typ K), class 2, welded tip Insulation: PVC (wires and sheath) |

| Tolerances | ±0,5 °C |
| --- | --- |
| Operating temp. | -10 °C … +105 °C |
| External diameter | Ca. 2,2 x 3,4 mm |

Fig. 3.15: Thermowire NiCr-Ni

3.4.2.2 Digital humidity and temperature sensors

Digital Humidity and temperature sensors were used. This means all key sensor characteristics and settings data are stored in the sensor element itself and supplies calibrated data for temperature in degree [°C] and relative humidity in percentage [%]. Data received/measured were then transfers and stored in a Symmetron Stylitis 101 data logger shown in Figure 3.18. Technical specification and nature of the digital humidity and temperature sensors are as shown in Table 3.8 and Figure 3.16 respectively

Table 3.8: Technical data of digital humidity and temperature sensors

| Technical data of digital humidity and temperature sensors |  |
| --- | --- |
| Manufacturer and probe | Symmetron Stylitis 101 digital humidity and temperature sensors, the slotted sensor cover |
| Specification | Insulation: PVC (wires and sheath) Symmetron Stylitis 101 Sensor cover Ø 8 mm, length 36 mm Plug connection Ø ca. 9 mm Extension tube: Ø 8 mm, Länge 97 mm |
| Relative humidity |  |
| Tolerances | 0,0% … 98,0% RH |
| Operating temp. | ±1,8% RH |

| Temperat |  |
| --- | --- |
| Tolerances | -20 °C … +60 °C |
| Operating temp. | ±1,0 K |

Fig. 3.16: Digital humidity and temperature sensors

3.4.2.3 Meteorological Station

A meteorological weather station shown in Figure 3.17 was built at the EEBN house at Namibia University of Science and Technology (NUST) campus. It contains a data logger and several sensors to record the following variables:

❖ Air temperature in degrees Celsius [°C]

❖ Relative humidity in percentage [% RH]

❖ Precipitation (rain and hail) in millimetres per hour [mm/h]

❖ Wind velocity in meters per second [m/s]

❖ The wind direction in degree [°]

❖ Global radiation in watts per square meter [W/m²]

Fig. 3.17: Weather Station and Symmetron data logger

3.4.2.4 Symmetron stylitis 101

Symmetron Stylitis-101 shown in Figure 3.18 and used in this research was a complete, sealed, portable data acquisition device that was designed to record in a broad range of applications in Industrial, Meteorological, and Laboratory fields. The Stylitis-101 measured voltage, current, frequency, and pulses. With suitable sensors, it is also capable of measuring: Wind speed, direction, and wind-turbine power curves, Temperature, humidity, pressure, solar radiation, rain height, and water speed. The sensors’ output was within –50 ~ +50V, -20 ~ +20mAand 0 ~ 3 kHz. It has up to 18 analogue inputs using optional CARD approximately 11 to 16 and 2, 4, and 6 configuration modules.

Also, the device can be integrated into a computer network to assess the collected data remotely. Also, a data logger shown in Figure 19 was fitted out with a display, with illuminated graphics, and a control panel which allows checking out the whole system and sensors, or for functional check of the device and the connected sensors. It is easy and convenient to operate by soft-keys and cursor block.

Figure 3.18 Symmetron stylitis 101

3.4.2.5 Data measurement and data collection methods

Data used in the research were recorded using the Symmetron data logger shown in Fig. 3.19. Data instrument was used to measure temperature and humidity both inside and outside of any close system (mostly buildings) at periodic intervals. The symmetron data logger was equipped with a USB- interface port for easy transfer of collected data to the personal high-speed computer with the appropriate software. The weather station built shown in Fig. 3.17 was used the measured the external air temperature, humidity, and air velocity.

The Symmetron data logger was placed in the middle Rig (i.e. Rig B) and temperature and humidity sensors were connected to the other two rigs (i.e. Rigs A and C). All temperature sensors used were PT100 DIN B probes, calibrated to maximum error, ±0.3 ºC. The air humidity sensors were ELEKTRONIK EE21FT6AA21 type with an accuracy of ± 2% (Castell et. al, 2010).  The winter and the summer temperature were recorded at every 15 minutes’ time intervals. The raw data were downloaded to the computer with the Option 4 software application. The collected results were tabulated and further

analysed in a statistical form with Microsoft excel thereafter, tables and graphs are used to present the data for visualization and professional purposes.

Figure 3.19 Symmetron data logger connected with sensors

CHAPTER FOUR

EXPERIMENTAL RESULTS

4.1 Overview

The  objective of  this  chapter is  to  present  the  experimental results obtained  in  the  laboratory concerning the different categories highlighted in chapter three.

Results of the thermal conductivity, thermal resistivity, water absorption, compressive strength of different categories from the agricultural residues are shown in this chapter.

4.2 Results

4.2.1 Thermal Conductivity and Resistivity of Insulation / Particleboards

Laboratory results of thermal conductivity and thermal resistivity of selected samples of the particle board as prepared in chapter three are shown in Table 4.1, Figures 4.1, and Figure 4.2 respectively.

Table 4.1: Thermal Conductivity and Resistivity of insulation boards of Samples considered

| SAMPLES | THERMAL CONDUCTIVITY (k) mW/(m*K) | THERMAL RESISTIVITY (r) m2K/W | RAW DENSITY Kg/m3 |
| --- | --- | --- | --- |
| A B C D | 100.71 66.79 54.65 76.12 | 0.4002 0.5150 0.6935 0.4769 | 935.10 845.70 849.30 899.30 |

| E F G H I J K | 60.79 56.50 55.88 57.50 58.74 57.27 63.07 | 0.5922 0.6584 0.6890 0.6696 0.6554 0.6723 0.6009 | 865.20 850.10 849.40 855.30 870.20 855.10 900.10 |
| --- | --- | --- | --- |

THERMAL CONDUCTIVITY mW/m*K

120

100

100.71

80

66.79

60

54.65

76.12

60.79	56.5	55.88	57.5	58.74	57.27

63.07

40

20

0

A	B	C	D	E	F	G	H	I	J	K

SAMPLES

Figure 4.1: Bar Chart of Sample Thermal Conductivity of Samples Considered

0.8

0.7

THERMAL RESISTIVITY m2K/W

0.6

0.5

0.4

0.4002

0.515

0.6935

THERMAL RESISTIVTY

0.6584    0.689    0.6696

0.5922

0.4769

0.6554   0.6723

0.6009

0.3

0.2

0.1

0

A	B	C	D	E	F	G	H	I	J	K

SAMPLE

Figure 4.2: Bar Chart of Thermal Resistivity of Samples Considered

4.2.2 Thermal Conductivity of Samples Mixed with Marble Dust

Results of thermal conductivities obtained by mixing samples having the best (i.e. sample C) and worst (i.e. sample A) thermal conductivities from Table 3.2 i.e. 5%, 10%, 20%, and 30% by weight of marble dust to form particle /Insolating boards are as shown in Table 4.2. The uniqueness and contribution of the marble dust to the agricultural residues act as a binder and also decrease the thermal conductivity of the best and the worst samples.

Table 4.2: Results of Thermal Conductivities of Samples from Table 3.2 when varying percentage of Marble Dust

| Percentage mix | Thermal conductivity for sample C + Marble dust (k) mW/(m*K) | Thermal conductivity for sample A + Marble dust mW/(m*K) |
| --- | --- | --- |
| 5 | 78.08 | 71.99 |
| 10 | 77.00 | 67.12 |
| 20 | 62.63 | 65.91 |
| 30 | 60.18 | 62.93 |

4.2.3 Thermal conductivity of the brick types

Tables 4.3 – 4.6 shows the results of thermal conductivity and thermal resistivity of the different mix design of the various bricks types as per Tables 4.3 – 4.6 in chapter three. Figs. 4.3 – 4.6 shows the regression analyses of thermal conductivity versus time for 60% maize husks, rice husks, cow dung, and millet husks.

Table 4.3: Bricks Thermal conductivity and resistivity results for Maize Husk Bricks

| Percentage Mix | THERMAL CONDUCTIVITY (k) mW/(m*K) | THERMAL RESISTIVITY (r) m2K/W | RAW DENSITY Kg/m3 |
| --- | --- | --- | --- |
| 20 40 60 80 | 175.04 153.42 127.24 184.09 | 0.4439 0.4393 0.6051 0.5640 | 1708.00 1675.00 1655.00 1548.00 |

145

Thermal Conductivity

140

135

130

125

120

115

y = -8E-05x2 + 0.0574x + 125.41

R² = 0.8684

1

18

35

52

69

86

103

120

137

154

171

188

205

222

239

256

273

290

307

324

341

358

375

392

409

426

443

460

Time (Minutes)

Raw data	moving average	Poly. (moving average)

Figure 4.3: Thermal Conductivity versus Time for 60% Maize husk brick

Table 4.4: Results of thermal conductivity and resistivity for Rice Husks brick

| Percentage mix | THERMAL CONDUCTIVITY (k) mW/(m*K) | THERMAL RESISTIVITY (r) m2K/W | RAW DENSITY Kg/m3 |
| --- | --- | --- | --- |
| 20 40 60 80 | 161.54 185.73 130.27 147.78 | 0.3522 0.3979 0.5910 0.5210 | 1750.00 1665.00 1600.00 1550.00 |

134

133

132

Thermal conductivity

mW/m*K

131

130

129

128

127

126

125

124

60% Rice husk

y = -2E-05x2 - 0.0769x + 133.37

R² = 0.9905

1    4    7   10  13  16  19  22  25  28  31  34  37  40  43  46  49  52  55  58  61  64  67  70  73  76

Time (Minutes)

Actual	Forecast	Poly. (Forecast)

Figure4.4: Thermal Conductivity versus Time for 60% Rice husk brick

Table 4.5: Results of thermal conductivity and resistivity for Cow dung brick

| Percentage mix | THERMAL CONDUCTIVITY (k) mW/(m*K) | THERMAL RESISTIVITY (r) m2K/W | RAW DENSITY Kg/m3 |
| --- | --- | --- | --- |
| 20 40 60 80 | 202.22 132.11 128.46 220.60 | 0.3807 0.5526 0.5994 0.3490 | 1800.00 1765.00 1660.00 1505.00 |

145

Thermal conductivity

mW/m*K

140

60 % Cow dung

y = 0.0004x2 - 0.1523x + 139.42

R² = 0.9433

135

130

125

120

1

10

19

28

37

46

55

64

73

82

91

100

109

118

127

136

145

154

163

172

181

190

199

208

217

226

235

115

Time (Minutes)

Actual	Forecast	Poly. (Forecast)

Figure 4.5: Thermal Conductivity versus Time for 60% Cow dung brick

Table 4.6:  Results of thermal conductivity and resistivity for Millet Husks bricks

| Percentage Mix | THERMAL CONDUCTIVITY (k) mW/(m*K) | THERMAL RESISTIVITY (r) m2K/W | RAW DENSITY Kg/m3 |
| --- | --- | --- | --- |
| 20 40 60 80 | 171.95 154.26 143.72 187.24 | 0.4478 0.4991 0.5357 0.4165 | 1700.00 1665.00 1600.00 1555.00 |

165

Thermal conductivity

mW/m*K

160

155

150

145

140

135

60% Millet husk brick

y = 0.0007x2 - 0.2197x + 160.55

R² = 0.9868

1

6

11

16

21

26

31

36

41

46

51

56

61

66

71

76

81

86

91

96

101

106

111

116

121

126

131

Time (Minutes)

Actual	Forecast	Poly. (Forecast)

Figure 4.6: Thermal Conductivity versus Time for 60% Millet husk bricks

4.2.4 Physical and mechanical properties of the brick types

4.2.4.1 Water Absorption Results of Bricks

Results of water absorption of bricks for 20%, 40%, 60%, and 80% sample mixes of maize husks, rice husks, millet husks, and cow dung are as shown in Table 4.7 and Figs. 4.7 – 4.10 respectively.

Table 4.7: Water Absorption of Bricks with varying percentage mixes

| Percentage of Samples (%) | Maize husk | Rice hulls | Millet husk | Cow dung |
| --- | --- | --- | --- | --- |
| 20 | 4.65 | 3.25 | 5.24 | 3.47 |
| 40 | 8.78 | 4.26 | 5.25 | 5.42 |
| 60 | 9.84 | 5.49 | 12.76 | 14.03 |
| 80 | 13.26 | 8.42 | 14.62 | 22.15 |

Maize husk bricks

14

Water Absorption

12

10

8

6

4

2

0

0	20	40	60	80	100

% of Maize husk

Figure 4.7: Water absorption of Maize Husk Bricks

Rice husk bricks

9

8

7

Water Absorption

6

5

4

3

2

1

0

0	10	20	30	40	50	60	70	80	90

% of Rice husks

Figure 4.8: Water absorption of Rice Husk Bricks

Millet husk brick

16

14

12

Water Absorption

10

8

6

4

2

0

0	10	20	30	40	50	60	70	80	90

% of Millet husk

Figure 4.9: Water absorption of Millet Husk Bricks

Cow dung Brick

Water Absorption %

25

20

15

10

5

0

0	10	20	30	40	50	60	70	80	90

% of Cow dung

Figure 4.10: Water absorption of Cow Dung Bricks

4.2. Compressive Strength Results of Bricks

Results of compressive strength of bricks for 20%, 40%, 60%, and 80% sample mixes of maize husks, rice husks, millet husks, and cow dung are as shown in Table 4.8 and Figs. 4.11 – 4.14 respectively.

Table 4.8:  Compressive Strength of Bricks

| Percentage of Samples (%) | Maize husk | Rice hulls | Millet husk | Cow dung |
| --- | --- | --- | --- | --- |
|  | Compressive Strength N/mm2 |  |  |  |
| 20 | 12.50 | 23.50 | 13.70 | 9.72 |
| 40 | 10.90 | 20.20 | 11.60 | 8.80 |
| 60 | 9.70 | 16.80 | 10.70 | 8.30 |
| 80 | 8.50 | 10.40 | 9.50 | 5.5 |

Maize husk brick

Compressive strength

N/mm2

14

12

10

8

6

4

2

0

0	10	20	30	40	50	60	70	80	90

% of husk Maize

Figure 4.11: Compressive Strength of Maize Brick

Rice husk brick

compressive strength

N/mm2

25

20

15

10

5

0

0	10	20	30	40	50	60	70	80	90

% of Rice husk

Figure 4.12: Compressive Strength of Rice Brick

Millet husk brick

compressive strength

N/mm2

15

10

5

0

0	10	20	30	40	50	60	70	80	90

% of millet husk

Figure 4.13: Compressive Strength of Millet Brick

Cow dung brick

12

compressive strength

N/mm2

10

8

6

4

2

0

0	10	20	30	40	50	60	70	80	90

% of cow dung

Figure 4.14: Compressive Strength of Cow Dung Brick

4.2.5 Results on Experimental Rigs

Results from the experimental rigs measured during winter and summer of 2018 and 2019 seasons are shown in Tables 4.9 – 4.19. This is accompanied by their respective graphs each month for both the

2018 and 2019 winter and summer seasons as shown in Figs. 4.15 – 4.25 respectively. The following terminologies as used in this research are shown

TAR1	Temperature of agricultural residue for rig A,

TMAB2 Temperature of agricultural residue and marble dust for rig B TNO3	Temperature for rig C without insulation

RHA1	Relative humidity for rig A RHExt.	External Relative humidity

RHMB2 Relative humidity for rig B containing Marble dust

RHNo3  Relative humidity for rig C with no insulation

TAR1, 19 Temperature of agricultural residue for rig A for data collection in 2019

TMAB,19 Temperature of agricultural residue and marble dust for rig B for data in 2019

TAN19 Temperature for rig C without insulation for data collection in 2019

EXT.19 External temperature for 2019

Table 4.9: Average quarterly indoor air temperature in rig TAR1, TAMB2, TNo3 and outdoor temperature for July 2018

| Time | TAR1 | TMAB2 | TNo3 | Ext. Air temp. |
| --- | --- | --- | --- | --- |
| 0:15 | 25.3 | 25.9 | 24.3 | 17.3 |
| 0:30 | 25.5 | 26.2 | 24.7 | 17.4 |
| 0:45 | 25.6 | 25.5 | 24.5 | 17.4 |
| 1:00 | 26 | 25.6 | 24.9 | 17.3 |
| 1:15 | 27.2 | 25.4 | 25 | 17.1 |
| 1:30 | 26.4 | 25.8 | 25 | 16.9 |
| 1:45 | 26.8 | 25.5 | 25 | 16.9 |
| 2:00 | 27.4 | 25.7 | 25.2 | 16.9 |

| 2:15 | 27.8 | 25.2 | 25.3 | 16.8 |
| --- | --- | --- | --- | --- |
| 2:30 | 27.8 | 26.5 | 24.7 | 16.6 |
| 2:45 | 27.9 | 25.2 | 25 | 16.8 |
| 3:00 | 27.9 | 25.5 | 24.8 | 16.7 |
| 3:15 | 25.6 | 26.3 | 25 | 16.8 |
| 3:30 | 27.4 | 25.8 | 24.8 | 16.6 |
| 3:45 | 28.4 | 26.2 | 24.6 | 16.6 |
| 4:00 | 28.1 | 26.2 | 24.8 | 16.5 |
| 4:15 | 28.7 | 26.4 | 24.6 | 16.5 |
| 4:30 | 27.9 | 26.3 | 24.8 | 16.5 |
| 4:45 | 27.4 | 27.2 | 25.3 | 16.5 |
| 5:00 | 27.5 | 27.9 | 25.6 | 16.2 |
| 5:15 | 28.6 | 26.9 | 25.4 | 16 |
| 5:30 | 27.7 | 27.6 | 25.5 | 15.9 |
| 5:45 | 29.1 | 27.5 | 24.9 | 15.8 |
| 6:00 | 28.3 | 27.6 | 24.3 | 15.9 |
| 6:15 | 28.4 | 27.5 | 25.5 | 15.9 |
| 6:30 | 28.7 | 26.8 | 25.4 | 15.8 |
| 6:45 | 29.3 | 27.3 | 25.3 | 15.6 |
| 7:00 | 28.7 | 27.4 | 25.4 | 15.4 |
| 7:15 | 27 | 27.7 | 25.3 | 15.7 |
| 7:30 | 28.1 | 26.8 | 25.6 | 16 |
| 7:45 | 28 | 26.7 | 25.6 | 16.3 |
| 8:00 | 27.3 | 25.9 | 25 | 16.8 |
| 8:15 | 26.7 | 25.5 | 24.4 | 17.4 |
| 8:30 | 26 | 25.1 | 24.2 | 17.7 |
| 8:45 | 25.8 | 24.8 | 23.9 | 18.6 |
| 9:00 | 25.6 | 24.5 | 23.6 | 18.9 |
| 9:15 | 25.4 | 24.5 | 23.5 | 19.5 |
| 9:30 | 25.4 | 24.4 | 23.4 | 20.2 |
| 9:45 | 25.4 | 24.4 | 23.3 | 21 |
| 10:00 | 25.4 | 24.4 | 23.4 | 21.8 |
| 10:15 | 25.3 | 24.3 | 23.4 | 22.4 |
| 10:30 | 25.3 | 24.4 | 23.1 | 23.7 |
| 10:45 | 25.2 | 24.4 | 23.1 | 24.2 |

| 11:00 | 25.1 | 24.3 | 22.9 | 24.3 |
| --- | --- | --- | --- | --- |
| 11:15 | 25.1 | 24.3 | 22.9 | 24 |
| 11:30 | 25.1 | 24.3 | 23.1 | 24 |
| 11:45 | 25.1 | 24.3 | 22.8 | 24.3 |
| 12:00 | 25.1 | 24.1 | 22.8 | 23.7 |
| 12:15 | 25 | 24.2 | 22.8 | 23.2 |
| 12:30 | 25 | 24.2 | 22.8 | 23.2 |
| 12:45 | 25 | 24.2 | 22.8 | 23.3 |
| 13:00 | 25 | 24.1 | 22.8 | 23.7 |
| 13:15 | 24.9 | 24.1 | 22.6 | 24.5 |
| 13:30 | 24.9 | 24.2 | 22.9 | 24.1 |
| 13:45 | 24.9 | 24.1 | 22.7 | 23.5 |
| 14:00 | 24.9 | 24.2 | 22.8 | 23.7 |
| 14:15 | 24.9 | 24.2 | 22.8 | 23.9 |
| 14:30 | 24.9 | 24.2 | 22.6 | 24.1 |
| 14:45 | 24.9 | 24 | 22.6 | 23.4 |
| 15:00 | 24.9 | 24.1 | 22.7 | 23.4 |
| 15:15 | 24.8 | 24.1 | 22.4 | 23 |
| 15:30 | 24.9 | 24.4 | 23.2 | 22.9 |
| 15:45 | 25.1 | 24.5 | 23.9 | 22.9 |
| 16:00 | 24.9 | 24.7 | 23.9 | 22.6 |
| 16:15 | 25.1 | 24.4 | 24 | 22.4 |
| 16:30 | 25 | 24.5 | 23.9 | 21.9 |
| 16:45 | 24.9 | 25.1 | 23.5 | 21.7 |
| 17:00 | 24.9 | 24.5 | 23.6 | 21.2 |
| 17:15 | 25 | 24.5 | 23.6 | 20.7 |
| 17:30 | 25 | 24.4 | 23.8 | 20.1 |
| 17:45 | 25.1 | 24.3 | 24.1 | 19.9 |
| 18:00 | 25.1 | 24.4 | 23.7 | 19.8 |
| 18:15 | 24.9 | 24.2 | 23.4 | 19.7 |
| 18:30 | 24.9 | 24.3 | 23.8 | 19.6 |
| 18:45 | 24.9 | 24.4 | 23.3 | 19.5 |
| 19:00 | 25 | 24.6 | 23 | 19.5 |
| 19:15 | 24.9 | 24.3 | 23 | 19.4 |
| 19:30 | 24.7 | 24.2 | 23.2 | 19.2 |

| 19:45 | 24.7 | 24.1 | 22.5 | 19.1 |
| --- | --- | --- | --- | --- |
| 20:00 | 24.7 | 24.2 | 22.6 | 19.1 |
| 20:15 | 24.6 | 24.1 | 22.7 | 19 |
| 20:30 | 24.5 | 24 | 22.2 | 18.9 |
| 20:45 | 24.6 | 24 | 22.4 | 19 |
| 21:00 | 24.5 | 23.9 | 22.2 | 19 |
| 21:15 | 24.5 | 24 | 22.5 | 18.8 |
| 21:30 | 24.5 | 24 | 22.3 | 18.7 |
| 21:45 | 24.5 | 24 | 22 | 18.6 |
| 22:00 | 24.5 | 23.9 | 22.5 | 18.5 |
| 22:15 | 24.5 | 24 | 22.5 | 18.4 |
| 22:30 | 24.6 | 24.2 | 22.6 | 18.3 |
| 22:45 | 24.5 | 24.4 | 22.3 | 18.3 |
| 23:00 | 24.7 | 24.3 | 23.4 | 18.3 |
| 23:15 | 24.8 | 24.7 | 23.6 | 18.3 |
| 23:30 | 25 | 24.7 | 23.8 | 18.3 |
| 23:45 | 25 | 25.1 | 23.7 | 18.1 |
| 24:00 | 25.1 | 25.7 | 24.5 | 18 |

Figure 4.15: Temperature quarterly Profile on 03-07-2018

Table 4.10: Average monthly indoor air temperature in rig TAR1, TAMB2, TNo3 and outdoor temperature in July

2018

| Date | TAR1 | TMAB2 | TNo3 | Air temp. (average) |
| --- | --- | --- | --- | --- |
| 1 Jul 2018 | 27.3 | 26.2 | 24.7 | 12.5 |
| 2 Jul 2018 | 25.6 | 25.5 | 24.5 | 8.1 |
| 3 Jul 2018 | 26 | 25.6 | 24.9 | 7.9 |
| 4 Jul 2018 | 27.2 | 25.4 | 25 | 8.5 |
| 5 Jul 2018 | 26.4 | 25.8 | 25 | 11.5 |
| 6 Jul 2018 | 26.8 | 25.5 | 25 | 11.49 |
| 7 Jul 2018 | 27.4 | 25.7 | 25.2 | 11.65 |
| 8 Jul 2018 | 27.8 | 25.2 | 25.3 | 12.14 |
| 9 Jul 2018 | 27.8 | 26.5 | 24.7 | 13.33 |
| 10 Jul 2018 | 27.9 | 25.2 | 25 | 13.68 |
| 11 Jul 2018 | 27.9 | 25.5 | 24.8 | 13.34 |
| 12 Jul 2018 | 25.6 | 26.3 | 25 | 12.48 |
| 13 Jul 2018 | 27.4 | 25.8 | 24.8 | 13.24 |
| 14 Jul 2018 | 28.4 | 26.2 | 24.6 | 11.3 |
| 15 Jul 2018 | 28.1 | 26.2 | 24.8 | 10.52 |
| 16 Jul 2018 | 28.7 | 26.4 | 24.6 | 14.2 |
| 17 Jul 2018 | 27.9 | 26.3 | 24.8 | 13.28 |
| 18 Jul 2018 | 27.4 | 27.2 | 25.3 | 11.35 |
| 19 Jul 2018 | 27.5 | 27.9 | 25.6 | 12.09 |
| 20 Jul 2018 | 28.6 | 26.9 | 25.4 | 10.97 |
| 21 Jul 2018 | 27.7 | 27.6 | 25.5 | 14.19 |
| 22 Jul 2018 | 29.1 | 27.5 | 24.9 | 13.48 |
| 23 Jul 2018 | 28.3 | 27.6 | 24.3 | 15.04 |
| 24 Jul 2018 | 28.4 | 27.5 | 25.5 | 13.85 |
| 25 Jul 2018 | 28.7 | 26.8 | 25.4 | 14.41 |
| 26 Jul 2018 | 29.3 | 27.3 | 25.3 | 14.47 |
| 27 Jul 2018 | 28.7 | 27.4 | 25.4 | 12.09 |
| 28 Jul 2018 | 27 | 27.7 | 25.3 | 12.72 |
| 29 Jul 2018 | 28.1 | 26.8 | 25.6 | 13.77 |
| 30 Jul 2018 | 28 | 26.7 | 25.6 | 14.68 |
| 31 Jul 2018 | 27.3 | 25.9 | 25 | 13.8 |

TAR1	TMAB2	TNo3	Air temp. (avg)

35

30

Temperature

25

20

15

10

5

1 Jul 2018

2 Jul 2018

3 Jul 2018

4 Jul 2018

5 Jul 2018

6 Jul 2018

7 Jul 2018

8 Jul 2018

9 Jul 2018

10 Jul 2018

11 Jul 2018

12 Jul 2018

13 Jul 2018

14 Jul 2018

15 Jul 2018

16 Jul 2018

17 Jul 2018

18 Jul 2018

19 Jul 2018

20 Jul 2018

21 Jul 2018

22 Jul 2018

23 Jul 2018

24 Jul 2018

25 Jul 2018

26 Jul 2018

27 Jul 2018

28 Jul 2018

29 Jul 2018

30 Jul 2018

31 Jul 2018

0

DAY

Figure 4.16: Temperature profile for July 2018

Table 4.11: Average monthly indoor humidity in rig TAR1, TAMB2, TNo3 and outdoor humidity in July 2018

| Date | RHA1 | RHMB2 | RHNo3 | Humidity |
| --- | --- | --- | --- | --- |
| 1 Jul 2018 | 24 | 26.4 | 27.4 | 36.3 |
| 2 Jul 2018 | 24 | 26.4 | 27.4 | 31.5 |
| 3 Jul 2018 | 23.9 | 26.4 | 27.4 | 26.2 |
| 4 Jul 2018 | 23.8 | 26.4 | 27.4 | 28.1 |
| 5 Jul 2018 | 23.9 | 26.4 | 27.4 | 44.93 |
| 6 Jul 2018 | 23.9 | 26.4 | 27.5 | 59.74 |
| 7 Jul 2018 | 23.9 | 26.4 | 27.5 | 63.27 |
| 8 Jul 2018 | 23.8 | 26.5 | 27.5 | 54.53 |
| 9 Jul 2018 | 23.9 | 26.4 | 27.5 | 51.31 |
| 10 Jul 2018 | 23.9 | 26.5 | 27.5 | 47.33 |
| 11 Jul 2018 | 24 | 26.5 | 27.5 | 45.23 |
| 12 Jul 2018 | 24 | 26.5 | 27.5 | 52.01 |
| 13 Jul 2018 | 24 | 26.5 | 27.5 | 46.85 |
| 14 Jul 2018 | 23.9 | 26.5 | 27.5 | 55.13 |
| 15 Jul 2018 | 24 | 26.5 | 27.6 | 64.24 |
| 16 Jul 2018 | 24 | 26.5 | 27.6 | 51.7 |

Humidity in %H

|  | 17 Jul 2018 | 24 | 26.5 | 27.6 | 45.08 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 18 Jul 2018 | 24 | 26.6 | 27.6 | 43.33 |  |
|  | 19 Jul 2018 | 24 | 26.6 | 27.6 | 46.02 |  |
|  | 20 Jul 2018 | 24.1 | 26.6 | 27.7 | 52.92 |  |
|  | 21 Jul 2018 | 24.1 | 26.6 | 27.7 | 42.45 |  |
|  | 22 Jul 2018 | 24 | 26.6 | 27.7 | 45.94 |  |
|  | 23 Jul 2018 | 23.9 | 26.6 | 27.7 | 38.35 |  |
|  | 24 Jul 2018 | 23.9 | 26.6 | 27.7 | 42.66 |  |
|  | 25 Jul 2018 | 23.9 | 26.6 | 27.7 | 39.33 |  |
|  | 26 Jul 2018 | 23.9 | 26.6 | 27.7 | 39.24 |  |
|  | 27 Jul 2018 | 23.8 | 26.6 | 27.7 | 41.87 |  |
|  | 28 Jul 2018 | 23.9 | 26.5 | 27.7 | 37.84 |  |
|  | 29 Jul 2018 | 23.9 | 26.5 | 27.7 | 32.9 |  |
|  | 30 Jul 2018 | 24 | 26.4 | 27.7 | 29.82 |  |
|  | 31 Jul 2018 | 24.2 | 26.6 | 27.7 | 33.5 |  |
| 70 60 50 40 30 20 10 0 Days RHA1 RHMB2 RHNo3 Humidity |  |  |  |  |  |  |

1 Jul 2018

2 Jul 2018

3 Jul 2018

4 Jul 2018

5 Jul 2018

6 Jul 2018

7 Jul 2018

8 Jul 2018

9 Jul 2018

10 Jul 2018

11 Jul 2018

12 Jul 2018

13 Jul 2018

14 Jul 2018

15 Jul 2018

16 Jul 2018

17 Jul 2018

18 Jul 2018

19 Jul 2018

20 Jul 2018

21 Jul 2018

22 Jul 2018

23 Jul 2018

24 Jul 2018

25 Jul 2018

26 Jul 2018

27 Jul 2018

28 Jul 2018

29 Jul 2018

30 Jul 2018

31 Jul 2018

Figure 4.17: Humidity profile for July 2018

Table 4.12: Average quarterly indoor air temperature in rig TAR1, TAMB2, TNo3 and outdoor temperature for October

2018

| Time | TAR1 | TANo3 | TAMB2 | Air Temp average. |
| --- | --- | --- | --- | --- |
| 15:30 | 25.345 | 26.098 | 27.829 | 29.9 |
| 15:45 | 24.955 | 26.27 | 26.197 | 28.7 |
| 16:00 | 24.797 | 26.468 | 25.794 | 27.2 |
| 16:15 | 24.988 | 26.799 | 25.814 | 26.4 |
| 16:30 | 25.253 | 26.931 | 25.907 | 26.9 |
| 16:45 | 25.457 | 26.97 | 26.138 | 28.4 |
| 17:00 | 25.438 | 27.136 | 25.887 | 29.2 |
| 17:15 | 25.88 | 27.169 | 26.369 | 29.3 |
| 17:30 | 25.57 | 27.195 | 25.715 | 29.7 |
| 17:45 | 25.702 | 27.056 | 25.907 | 28.4 |
| 18:00 | 25.649 | 26.779 | 25.642 | 30.1 |
| 18:15 | 25.464 | 26.713 | 25.345 | 30.2 |
| 18:30 | 25.504 | 26.567 | 25.702 | 26.3 |
| 18:45 | 25.167 | 26.277 | 25.517 | 30.4 |
| 19:00 | 25.061 | 25.999 | 25.12 | 28.8 |
| 19:15 | 25.153 | 25.662 | 24.929 | 27.5 |
| 19:30 | 24.896 | 25.087 | 24.513 | 27.4 |
| 19:45 | 24.228 | 24.559 | 24.017 | 29 |
| 20:00 | 23.561 | 24.176 | 23.706 | 28.7 |
| 20:15 | 23.416 | 23.958 | 23.581 | 28 |
| 20:30 | 23.112 | 23.786 | 23.455 | 28 |
| 20:45 | 22.795 | 23.66 | 23.303 | 28.5 |
| 21:00 | 22.577 | 23.554 | 23.184 | 28.2 |
| 21:15 | 22.193 | 23.409 | 23.079 | 28.1 |
| 21:30 | 22.022 | 23.323 | 22.953 | 28.3 |
| 21:45 | 21.962 | 23.244 | 22.887 | 28.7 |
| 22:00 | 21.817 | 23.165 | 22.841 | 26.9 |
| 22:15 | 21.619 | 23.125 | 22.762 | 27.6 |
| 22:30 | 21.348 | 23.092 | 22.696 | 26.3 |
| 22:45 | 21.11 | 22.999 | 22.583 | 26.8 |

| 23:00 | 20.885 | 22.94 | 22.458 | 26 |
| --- | --- | --- | --- | --- |
| 23:15 | 20.727 | 22.867 | 22.359 | 28 |
| 23:30 | 20.555 | 22.762 | 22.193 | 27.9 |
| 23:45 | 20.178 | 22.669 | 22.074 | 28.3 |
| 0:00 | 20.079 | 22.563 | 21.936 | 26 |
| 0:15 | 19.94 | 22.458 | 21.81 | 27.6 |
| 0:30 | 19.874 | 22.345 | 21.685 | 26.8 |
| 0:45 | 19.755 | 22.253 | 21.586 | 29.4 |
| 1:00 | 19.471 | 22.18 | 21.5 | 28.4 |
| 1:15 | 19.24 | 22.048 | 21.374 | 29.7 |
| 1:30 | 19.048 | 21.949 | 21.275 | 29.8 |
| 1:45 | 18.863 | 21.83 | 21.103 | 29.6 |
| 2:00 | 18.698 | 21.731 | 21.011 | 30.7 |
| 2:15 | 18.48 | 21.638 | 20.918 | 30.6 |
| 2:30 | 18.249 | 21.506 | 20.753 | 30.2 |
| 2:45 | 18.203 | 21.407 | 20.647 | 30.2 |
| 3:00 | 17.978 | 21.295 | 20.469 | 30 |
| 3:15 | 17.714 | 21.176 | 20.409 | 30 |
| 3:30 | 17.542 | 21.097 | 20.238 | 29.9 |
| 3:45 | 17.456 | 20.918 | 20.165 | 29.7 |
| 4:00 | 17.304 | 20.865 | 20.02 | 30.3 |
| 4:15 | 17.231 | 20.72 | 19.907 | 30 |
| 4:30 | 17.033 | 20.608 | 19.788 | 30.4 |
| 4:45 | 16.994 | 20.515 | 19.689 | 29.6 |
| 5:00 | 16.776 | 20.416 | 19.544 | 30.1 |
| 5:15 | 16.736 | 20.297 | 19.385 | 29.3 |
| 5:30 | 16.558 | 20.185 | 19.333 | 29.9 |
| 5:45 | 16.353 | 20.053 | 19.273 | 29.9 |
| 6:00 | 16.207 | 19.947 | 19.128 | 30.3 |
| 6:15 | 16.075 | 19.828 | 18.982 | 30.1 |
| 6:30 | 15.923 | 19.709 | 18.877 | 30.8 |
| 6:45 | 15.738 | 19.59 | 18.731 | 30.1 |
| 7:00 | 15.633 | 19.458 | 18.639 | 30.8 |
| 7:15 | 15.494 | 19.359 | 18.526 | 29.6 |
| 7:30 | 15.342 | 19.247 | 18.381 | 29.6 |

| 7:45 | 15.177 | 19.095 | 18.315 | 30.7 |
| --- | --- | --- | --- | --- |
| 8:00 | 15.177 | 19.022 | 18.17 | 30.8 |
| 8:15 | 15.223 | 18.916 | 18.071 | 30.7 |
| 8:30 | 15.362 | 18.877 | 18.09 | 29.9 |
| 8:45 | 15.699 | 18.837 | 18.11 | 30.3 |
| 9:00 | 15.989 | 18.863 | 18.183 | 30.3 |
| 9:15 | 16.108 | 18.943 | 18.355 | 30.6 |
| 9:30 | 16.201 | 19.2 | 18.467 | 30.4 |
| 9:45 | 16.392 | 19.359 | 18.586 | 30.8 |
| 10:00 | 16.604 | 19.405 | 18.83 | 30.4 |
| 10:15 | 16.809 | 19.669 | 19.128 | 30.5 |
| 10:30 | 17.027 | 20.224 | 19.399 | 30.7 |
| 1045 | 17.231 | 20.594 | 19.788 | 30.8 |
| 1100 | 17.562 | 21.037 | 20.205 | 30.5 |
| 1115 | 18.262 | 21.592 | 21.011 | 30.6 |
| 11:30 | 18.751 | 22.061 | 21.46 | 30.4 |
| 11:45 | 19.557 | 22.55 | 22.213 | 29.9 |
| 12:00 | 20.079 | 22.881 | 22.557 | 29.5 |
| 1215 | 20.191 | 23.409 | 22.768 | 29.2 |
| 1230 | 21.07 | 23.66 | 23.488 | 30.2 |
| 12::45 | 20.945 | 24.037 | 23.363 | 29.5 |
| 1300 | 21.348 | 24.4 | 23.64 | 29.9 |
| 1315 | 22.378 | 24.612 | 24.407 | 30.4 |
| 1330 | 23.171 | 25.001 | 25.193 | 29.6 |
| 13:45 | 23.561 | 25.127 | 25.286 | 29.9 |
| 14:00 | 23.026 | 25.371 | 24.479 | 29.9 |
| 14:15 | 24.552 | 25.887 | 26.019 | 29.8 |
| 14:30 | 24.493 | 25.973 | 25.774 | 29.9 |
| 14:45 | 24.334 | 26.125 | 25.702 | 29.4 |
| 15:00 | 25.127 | 26.475 | 26.336 | 27.1 |
| 15::15 | 25.319 | 26.614 | 26.554 | 28.4 |
| 15:30 | 25.636 | 26.832 | 26.686 | 26.7 |

30

Temperature in degree celcius

25

20

15

10

5

1 Oct 2018

2 Oct 2018

3 Oct 2018

4 Oct 2018

5 Oct 2018

6 Oct 2018

7 Oct 2018

8 Oct 2018

9 Oct 2018

10 Oct 2018

11 Oct 2018

12 Oct 2018

13 Oct 2018

14 Oct 2018

15 Oct 2018

16 Oct 2018

17 Oct 2018

18 Oct 2018

19 Oct 2018

20 Oct 2018

21 Oct 2018

22 Oct 2018

23 Oct 2018

24 Oct 2018

25 Oct 2018

26 Oct 2018

27 Oct 2018

28 Oct 2018

29 Oct 2018

30 Oct 2018

31 Oct 2018

0

days

sTAR1	Air temp. (avg)

Figure 4.18 Summer Temperature Profile for October 2018

Table 4.13: Average quarterly indoor air humidity in rig TAR1, TAMB2, TNo3 and outdoor humidity for 15th October

2018

| Time | RH1 | RH2 |  | RH3 |  | RH4 |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 00:00 | 23.1 | 22.7 |  | 22.2 |  | 25.6 |  |
| 00:15 | 23.1 | 22.8 |  | 22.2 |  | 26.2 |  |
| 00:30 | 23.09 | 22.8 |  | 22.1 |  | 26.4 |  |
| 00:45 | 23.1 |  | 23 | 22.2 |  | 26.6 |  |
| 01:00 | 23.1 | 22.9 |  | 22.2 |  | 26.8 |  |
| 01:15 | 23.12 |  | 23 | 22.2 |  | 27.1 |  |
| 01:30 | 23.14 | 23.2 |  | 22.7 |  |  | 26 |
| 01:45 | 23.13 | 23.4 |  | 22.9 |  | 25.9 |  |
| 02:00 | 23.17 | 23.2 |  |  | 23 | 26.1 |  |
| 02:15 | 23.18 | 23.2 |  |  | 23 | 26.3 |  |
| 02:30 | 23.21 | 23.2 |  | 22.9 |  | 26.3 |  |
| 02:45 | 23.22 | 23.4 |  | 22.9 |  | 26.4 |  |
| 03:00 | 23.24 | 23.1 |  | 22.8 |  | 26.4 |  |
| 03:15 | 23.28 | 23.1 |  | 22.7 |  | 26.3 |  |
| 03:30 | 23.3 | 23.1 |  | 22.6 |  | 26.4 |  |
| 03:45 | 23.31 | 23.1 |  | 22.5 |  | 26.3 |  |
| 04:00 | 23.32 | 23.2 |  | 22.8 |  | 26.6 |  |

| 04:15 | 23.37 | 23.3 | 22.7 | 26.6 |
| --- | --- | --- | --- | --- |
| 04:30 | 23.39 | 23.3 | 22.7 | 26.5 |
| 04:45 | 23.44 | 23.2 | 22.6 | 26.5 |
| 05:00 | 23.45 | 23.3 | 22.7 | 26.5 |
| 05:15 | 23.51 | 23.4 | 22.5 | 26.4 |
| 05:30 | 23.53 | 23.3 | 22.5 | 26.4 |
| 05:45 | 23.56 | 23.4 | 22.6 | 26.4 |
| 06:00 | 23.58 | 23.3 | 22.6 | 26.4 |
| 06:15 | 23.62 | 23.5 | 22.6 | 26.2 |
| 06:30 | 23.63 | 23.8 | 22.6 | 26.3 |
| 06:45 | 23.63 | 23.7 | 22.7 | 26.3 |
| 07:00 | 23.66 | 23.9 | 22.8 | 26.1 |
| 07:15 | 23.66 | 24 | 22.6 | 26.5 |
| 07:30 | 23.65 | 23.7 | 22.5 | 26.8 |
| 07:45 | 23.64 | 23.9 | 22.5 | 26.9 |
| 08:00 | 23.64 | 23.9 | 22.5 | 27 |
| 08:15 | 23.64 | 23.9 | 22.5 | 27.3 |
| 08:30 | 23.62 | 24 | 22.6 | 27.5 |
| 08:45 | 23.62 | 23.8 | 22.6 | 27.7 |
| 09:00 | 23.62 | 24 | 22.5 | 27.9 |
| 09:15 | 23.62 | 23.9 | 22.6 | 28.1 |
| 09:30 | 23.62 | 23.9 | 22.6 | 28.2 |
| 09:45 | 23.6 | 23.9 | 22.6 | 28.3 |
| 10:00 | 23.6 | 23.8 | 22.6 | 28.5 |
| 10:15 | 23.58 | 23.8 | 22.6 | 28.6 |
| 10:30 | 23.58 | 23.9 | 22.6 | 28.6 |
| 10:45 | 23.56 | 24 | 22.6 | 28.7 |
| 11:00 | 23.55 | 24.1 | 22.6 | 28.8 |
| 11:15 | 23.54 | 24 | 22.7 | 28.8 |
| 11:30 | 23.54 | 24.1 | 22.6 | 28.9 |
| 11:45 | 23.53 | 23.9 | 22.7 | 28.8 |
| 12:00 | 23.53 | 23.9 | 22.7 | 29 |
| 12:15 | 23.5 | 23.9 | 22.7 | 28.9 |
| 12:30 | 23.49 | 23.9 | 22.6 | 28.9 |
| 12:45 | 23.46 | 23.9 | 22.6 | 28.9 |

| 13:00 | 23.44 | 23.9 | 22.6 | 28.9 |
| --- | --- | --- | --- | --- |
| 13:15 | 23.43 | 23.9 | 22.6 | 28.9 |
| 13:30 | 23.43 | 23.8 | 22.5 | 28.8 |
| 13:45 | 23.42 | 23.7 | 22.5 | 28.8 |
| 14:00 | 23.39 | 23.9 | 22.4 | 28.7 |
| 14:15 | 23.4 | 23.9 | 22.3 | 28.7 |
| 14:30 | 23.4 | 23.9 | 22.3 | 28.7 |
| 14:45 | 23.38 | 23.9 | 22.3 | 28.7 |
| 15:00 | 23.37 | 23.8 | 22.2 | 28.7 |
| 15:15 | 23.34 | 23.9 | 22.1 | 28.7 |
| 15:30 | 23.37 | 24 | 22.1 | 28.9 |
| 15:45 | 23.34 | 23.9 | 22.1 | 28.9 |
| 16:00 | 23.35 | 23.8 | 22.1 | 29.1 |
| 16:15 | 23.34 | 23.7 | 22.1 | 29.1 |
| 16:30 | 23.34 | 23.7 | 22 | 29 |
| 16:45 | 23.32 | 23.8 | 22 | 28.9 |
| 17:00 | 23.3 | 23.8 | 21.9 | 28.9 |
| 17:15 | 23.3 | 23.7 | 21.9 | 28.9 |
| 17:30 | 23.28 | 23.7 | 21.9 | 29.1 |
| 17:45 | 23.29 | 23.7 | 21.9 | 29.1 |
| 18:00 | 23.28 | 23.7 | 21.9 | 29.1 |
| 18:15 | 23.28 | 23.6 | 21.9 | 29.1 |
| 18:30 | 23.26 | 23.7 | 21.9 | 28.9 |
| 18:45 | 23.24 | 23.6 | 21.8 | 28.9 |
| 19:00 | 23.24 | 23.8 | 21.8 | 28.8 |
| 19:15 | 23.22 | 23.7 | 21.8 | 28.7 |
| 19:30 | 23.22 | 23.8 | 21.7 | 28.5 |
| 19:45 | 23.2 | 23.7 | 21.7 | 28.5 |
| 20:00 | 23.19 | 23.8 | 21.7 | 28.4 |
| 20:15 | 23.16 | 23.8 | 21.7 | 28.3 |
| 20:30 | 23.17 | 23.7 | 21.7 | 28.3 |
| 20:45 | 23.13 | 23.8 | 21.7 | 28.4 |
| 21:00 | 23.13 | 23.7 | 21.7 | 28.3 |
| 21:15 | 23.12 | 23.7 | 21.8 | 28.4 |
| 21:30 | 23.09 | 23.8 | 21.8 | 28.6 |

| 21:45 | 23.09 | 23.7 | 21.8 | 28.5 |
| --- | --- | --- | --- | --- |
| 22:00 | 23.09 | 23.8 | 21.8 | 28.5 |
| 22:15 | 23.12 | 23.7 | 21.8 | 28.4 |
| 22:30 | 23.13 | 23.7 | 21.8 | 28.6 |
| 22:45 | 23.14 | 23.6 | 21.8 | 28.5 |
| 23:00 | 23.14 | 23.3 | 21.8 | 28.7 |
| 23:15 | 23.14 | 23.2 | 21.8 | 28.7 |
| 23:30 | 23.15 | 23 | 21.8 | 28.7 |
| 23:45 | 23.17 | 23.1 | 21.8 | 29 |
| 00:00 | 23.17 | 23.1 | 21.9 | 28.9 |

70

60

50

HUMIDITY %

40

RH1

30	RHM2

20	RHA3

RHEXT.

10

0:00

1:00

2:00

3:00

4:00

5:00

6:00

7:00

8:00

9:00

10:00

11:00

12:00

13:00

14:00

15:00

16:00

17:00

18:00

19:00

20:00

21:00

22:00

23:00

0

TIME (hour)

Figure 4.19 Hourly Summer Humidity Profile 15th October 2018

Table 4.14: Average quarterly indoor air temperature in rig TAR1,19, TAMB19, TAN19 and outdoor temperature for

June 2019

| TIME | TAR1,19 | TAMB19 | TAN19 | EXT 19 |
| --- | --- | --- | --- | --- |
| 0:15 | 25.4 | 25 | 23.4 | 9.3 |
| 0:30 | 25.2 | 24.9 | 23.1 | 9.2 |
| 0:45 | 25.2 | 24.8 | 23.1 | 8.9 |
| 1:00 | 25.1 | 24.8 | 23.2 | 8.2 |
| 1:15 | 25.1 | 24.8 | 22.9 | 8.2 |
| 1:30 | 25.1 | 24.9 | 23.2 | 8.7 |
| 1:45 | 25.1 | 24.8 | 23.5 | 8.7 |
| 2:00 | 25.1 | 24.8 | 23.2 | 8.7 |
| 2:15 | 25.1 | 24.8 | 23.7 | 8.7 |
| 2:30 | 25.1 | 24.8 | 23.4 | 8.7 |
| 2:45 | 25.2 | 24.8 | 23.2 | 9 |
| 3:00 | 25 | 24.8 | 22.9 | 8 |
| 3:15 | 25 | 24.7 | 23.7 | 8.5 |
| 3:30 | 25 | 24.8 | 23.2 | 8.6 |
| 3:45 | 25.4 | 24.8 | 23.1 | 8.7 |
| 4:00 | 25.2 | 24.8 | 22.9 | 8.6 |
| 4:15 | 25.1 | 24.7 | 23.2 | 8.5 |
| 4:30 | 24.9 | 24.7 | 22.5 | 7.5 |
| 4:45 | 24.9 | 24.6 | 22.6 | 7.2 |
| 5:00 | 24.9 | 24.7 | 22.6 | 6.9 |
| 5:15 | 25.1 | 24.5 | 22.9 | 7.8 |
| 5:30 | 25 | 24.6 | 22.8 | 7.7 |
| 5:45 | 25 | 24.7 | 23.3 | 7.8 |
| 6:00 | 25 | 24.7 | 22.6 | 7.8 |
| 6:15 | 24.9 | 24.6 | 22.6 | 7.7 |
| 6:30 | 25.1 | 24.5 | 22.6 | 8.6 |
| 6:45 | 25.1 | 24.6 | 23.4 | 9.3 |
| 7:00 | 25.4 | 24.8 | 23.7 | 10.4 |
| 7:15 | 25.5 | 24.8 | 23.9 | 11.6 |
| 7:30 | 25.9 | 24.9 | 24.7 | 13.4 |
| 7:45 | 26 | 24.9 | 24.3 | 16.9 |
| 8:00 | 26.6 | 24.9 | 24.7 | 20.2 |
| 8:15 | 27.2 | 24.9 | 25 | 21.9 |
| 8:30 | 26.7 | 24.7 | 25.4 | 21.1 |
| 8:45 | 26.5 | 24.8 | 25.4 | 19.4 |
| 9:00 | 26.8 | 24.8 | 25.3 | 19 |
| 9:15 | 26.8 | 24.7 | 25.6 | 18.4 |
| 9:30 | 27 | 24.8 | 25.3 | 18.5 |
| 9:45 | 27.6 | 24.8 | 25 | 18.3 |
| 10:00 | 27.3 | 24.9 | 25.6 | 18.7 |
| 10:15 | 27.3 | 25 | 24.7 | 18.2 |

| 10:30 | 27.8 | 25.3 | 25.3 | 19.4 |
| --- | --- | --- | --- | --- |
| 10:45 | 26.7 | 25.2 | 24.9 | 19.9 |
| 11:00 | 27.4 | 25.6 | 25.2 | 20.3 |
| 11:15 | 27.6 | 25.7 | 23.9 | 19.5 |
| 11:30 | 27.2 | 25.8 | 24.4 | 20.9 |
| 11:45 | 28.1 | 26 | 24.4 | 20.1 |
| 12:00 | 28 | 26.3 | 24.9 | 21.3 |
| 12:15 | 28 | 26.3 | 23.8 | 20.4 |
| 12:30 | 27.1 | 26.4 | 25.7 | 25.9 |
| 12:45 | 28.7 | 26.6 | 24.1 | 25.1 |
| 13:00 | 28.6 | 26.6 | 25.5 | 26.6 |
| 13:15 | 28.9 | 26.6 | 23.5 | 22.4 |
| 13:30 | 29.1 | 26.7 | 24.9 | 23.9 |
| 13:45 | 28.5 | 26.6 | 24.1 | 26.9 |
| 14:00 | 28.4 | 26.7 | 23.6 | 24.4 |
| 14:15 | 28.4 | 26.6 | 24.4 | 25.8 |
| 14:30 | 29.4 | 26.4 | 24.5 | 21.4 |
| 14:45 | 29.2 | 26.5 | 25.2 | 23.5 |
| 15:00 | 29.1 | 26.3 | 25 | 24.9 |
| 15:15 | 28.9 | 26.4 | 25.7 | 27.7 |
| 15:30 | 28.5 | 26.4 | 26.1 | 26.7 |
| 15:45 | 29.1 | 26.4 | 25.5 | 25 |
| 16:00 | 28.2 | 26.3 | 26.2 | 22.4 |
| 16:15 | 27.7 | 26.2 | 26.4 | 20.8 |
| 16:30 | 27.2 | 26.2 | 25.7 | 19 |
| 16:45 | 26.8 | 26.1 | 25.2 | 17.8 |
| 17:00 | 26.6 | 26 | 24.8 | 16.6 |
| 17:15 | 26.4 | 25.9 | 24.8 | 15.9 |
| 17:30 | 26.3 | 25.9 | 24.6 | 15.3 |
| 17:45 | 26.1 | 25.9 | 24.4 | 14.6 |
| 18:00 | 26 | 25.8 | 24.2 | 14.1 |
| 18:15 | 26.3 | 25.8 | 24.5 | 14.5 |
| 18:30 | 25.9 | 25.7 | 24.1 | 13.4 |
| 18:45 | 25.9 | 25.7 | 24 | 13.3 |
| 19:00 | 25.9 | 25.7 | 24 | 12.7 |
| 19:15 | 25.9 | 25.7 | 23.9 | 12.8 |
| 19:30 | 25.8 | 25.6 | 23.7 | 12.4 |
| 19:45 | 25.9 | 25.6 | 24.2 | 12.4 |
| 20:00 | 25.7 | 25.5 | 23.7 | 11.9 |
| 20:15 | 25.7 | 25.5 | 23.5 | 11.6 |
| 20:30 | 25.7 | 25.5 | 23.7 | 11.6 |
| 20:45 | 25.7 | 25.5 | 23.7 | 11.3 |
| 21:00 | 25.6 | 25.4 | 23.5 | 10.9 |
| 21:15 | 25.5 | 25.4 | 23.4 | 10.9 |

Temperature ̊C

|  | 21:30 | 25.5 | 25.3 | 23.8 | 10.4 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 21:45 | 25.3 | 25.3 | 23.5 | 10.1 |  |
|  | 22:00 | 25.3 | 25.3 | 23.6 | 10.1 |  |
|  | 22:15 | 25.4 | 25.3 | 23.5 | 9.9 |  |
|  | 22:30 | 25.4 | 25.2 | 23.2 | 9.9 |  |
|  | 22:45 | 25.4 | 25.2 | 23.1 | 9.6 |  |
|  | 23:00 | 25.3 | 25.2 | 23.2 | 9.5 |  |
|  | 23:15 | 25.4 | 25.3 | 23.3 | 9.6 |  |
|  | 23:30 | 25.3 | 25.1 | 23.3 | 9.5 |  |
|  | 23:45 | 25.3 | 25.2 | 23.3 | 9.5 |  |
|  | 24:00:00 | 25.5 | 25.1 | 23.3 | 9.4 |  |
| TEMPERATURE 01.06. 2019 35 30 25 20 15 10 5 0 Time TAR1,19 TAMB19 TAN19 EXT19 |  |  |  |  |  |  |

00:15

01:00

01:45

02:30

03:15

04:00

04:45

05:30

06:15

07:00

07:45

08:30

09:15

10:00

10:45

11:30

12:15

13:00

13:45

14:30

15:15

16:00

16:45

17:30

18:15

19:00

19:45

20:30

21:15

22:00

22:45

23:30

Figure 4.20 Winter quarterly Temperature Profile for 1st June 2019

Table 4.15: Average monthly indoor air temperature in rig TAR1,19 TAMB19, TAN19 and outdoor temperature in June

2019

| Date | TAR1,19 | TAMB19 | TAN19 | EXT19 |
| --- | --- | --- | --- | --- |
| 1-Jun- 19 | 26.8 | 25.7 | 25.2 | 14.5 |
| 2-Jun- 19 | 26.6 | 25.7 | 25 | 10.1 |
| 3-Jun- 19 | 26.5 | 26 | 25.2 | 8.3 |
| 4-Jun- 19 | 26.3 | 25.7 | 24.7 | 9.5 |
| 5-Jun- 19 | 26.1 | 25.5 | 24.5 | 12.5 |
| 6-Jun- 19 | 26.1 | 25.4 | 24.2 | 12.31 |

| 7-Jun- 19 | 26 | 25.3 | 24 | 12.45 |
| --- | --- | --- | --- | --- |
| 8-Jun- 19 | 26 | 25.3 | 23.9 | 13.16 |
| 9-Jun- 19 | 26 | 25.4 | 23.9 | 14.33 |
| 10-Jun- 19 | 25.9 | 25.2 | 23.7 | 14.68 |
| 11-Jun- 19 | 25.9 | 25.3 | 23.7 | 14.54 |
| 12-Jun- 19 | 25.9 | 25.3 | 23.7 | 13.48 |
| 13-Jun- 19 | 25.8 | 25.3 | 23.6 | 14.54 |
| 14-Jun- 19 | 25.8 | 25.3 | 23.7 | 12.48 |
| 15-Jun- 19 | 25.9 | 25.3 | 23.6 | 11.32 |
| 16-Jun- 19 | 25.9 | 25.4 | 23.7 | 15.2 |
| 17-Jun- 19 | 25.8 | 25.3 | 23.7 | 14.28 |
| 18-Jun- 19 | 25.8 | 25.3 | 23.7 | 13.35 |
| 19-Jun- 19 | 25.9 | 25.4 | 24 | 13.09 |
| 20-Jun- 19 | 25.9 | 25.4 | 24.6 | 12.97 |
| 21-Jun- 19 | 26 | 25.4 | 24 | 15.19 |
| 22-Jun- 19 | 25.8 | 25.5 | 24.3 | 14.68 |
| 23-Jun- 19 | 25.8 | 25.4 | 24 | 16.54 |
| 24-Jun- 19 | 25.8 | 25.3 | 24.2 | 14.55 |
| 25-Jun- 19 | 25.8 | 25.3 | 23.7 | 15.31 |
| 26-Jun- 19 | 25.8 | 25.3 | 23.8 | 14.57 |
| 27-Jun- 19 | 25.7 | 25.2 | 23.5 | 13.19 |
| 28-Jun- 19 | 25.8 | 25.2 | 23.7 | 13.75 |
| 29-Jun- 19 | 25.7 | 25.1 | 23.5 | 14.47 |
| 30-Jun- 19 | 25.7 | 25.3 | 23.5 | 15.48 |

01-Jun-19

02-Jun-19

03-Jun-19

04-Jun-19

05-Jun-19

06-Jun-19

07-Jun-19

08-Jun-19

09-Jun-19

10-Jun-19

11-Jun-19

12-Jun-19

13-Jun-19

14-Jun-19

15-Jun-19

16-Jun-19

17-Jun-19

18-Jun-19

19-Jun-19

20-Jun-19

21-Jun-19

22-Jun-19

23-Jun-19

24-Jun-19

25-Jun-19

26-Jun-19

27-Jun-19

28-Jun-19

29-Jun-19

30-Jun-19

Monthly Temperature June 2019

Temperature (degree Cel.)

30

25

20

15

10

5

0

Day

TAR1,19	TAMB19	TAN19	EXT19

Figure 4.21 Winter Temperature Profile for June 2019

Table 4.16: Average monthly indoor humidity in rig TAR1, TAMB2, TNo3 and outdoor humidity in June 2019

| Date | RHA19 Relative humidity for Rig A 2019 | RHMB19 Relative humidity for Rig B 2019 | RHNO19 Relative humidity for Rig C 2019 | EXT RH Ext. Relative humidity 2019 |
| --- | --- | --- | --- | --- |
| 1-Jun-19 | 22.40 | 24.90 | 26.70 | 38.3 |
| 2-Jun-19 | 21.80 | 24.90 | 26.80 | 33.2 |
| 3-Jun-19 | 20.20 | 25.00 | 26.80 | 28.3 |
| 4-Jun-19 | 21.90 | 25.00 | 26.90 | 30.1 |
| 5-Jun-19 | 22.20 | 25.10 | 26.90 | 46.23 |
| 6-Jun-19 | 23.10 | 25.00 | 26.80 | 62.24 |
| 7-Jun-19 | 23.40 | 25.10 | 26.80 | 65.21 |
| 8-Jun-19 | 23.70 | 25.10 | 26.60 | 56.53 |
| 9-Jun-19 | 21.70 | 25.10 | 26.70 | 54.31 |
| 10-Jun-19 | 23.50 | 25.20 | 26.70 | 50.32 |
| 11-Jun-19 | 23.90 | 25.20 | 26.70 | 47.23 |
| 12-Jun-19 | 22.60 | 25.20 | 26.60 | 55.01 |
| 13-Jun-19 | 24.20 | 25.20 | 26.50 | 48.05 |
| 14-Jun-19 | 22.90 | 25.20 | 26.50 | 57.43 |
| 15-Jun-19 | 22.40 | 25.20 | 26.40 | 66.24 |
| 16-Jun-19 | 23.00 | 25.30 | 26.30 | 53.72 |
| 17-Jun-19 | 22.30 | 25.20 | 26.30 | 47.18 |
| 18-Jun-19 | 23.40 | 25.20 | 26.30 | 45.23 |

Humidity (%)

|  | 19-Jun-19 | 25.10 | 25.30 | 26.20 | 48.22 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 20-Jun-19 | 24.80 | 25.20 | 26.00 | 53.62 |  |
|  | 21-Jun-19 | 23.10 | 25.20 | 25.90 | 43.25 |  |
|  | 22-Jun-19 | 24.80 | 25.20 | 25.90 | 48.94 |  |
|  | 23-Jun-19 | 23.80 | 25.30 | 25.80 | 40.35 |  |
|  | 24-Jun-19 | 24.20 | 25.20 | 25.60 | 44.66 |  |
|  | 25-Jun-19 | 23.40 | 25.30 | 25.60 | 41.03 |  |
|  | 26-Jun-19 | 22.60 | 25.30 | 25.50 | 41.24 |  |
|  | 27-Jun-19 | 22.00 | 25.20 | 25.50 | 43.87 |  |
|  | 28-Jun-19 | 21.40 | 25.30 | 25.50 | 40.22 |  |
|  | 29-Jun-19 | 21.10 | 25.20 | 25.50 | 34.19 |  |
|  | 30-Jun-19 | 21.00 | 25.20 | 25.50 | 31.32 |  |
| Winter Humidity June 2019 70.00 60.00 50.00 40.00 30.00 20.00 10.00 0.00 Day RHA19 RHMB19 RHNO19 EXT RH |  |  |  |  |  |  |

01-Jun-19

02-Jun-19

03-Jun-19

04-Jun-19

05-Jun-19

06-Jun-19

07-Jun-19

08-Jun-19

09-Jun-19

10-Jun-19

11-Jun-19

12-Jun-19

13-Jun-19

14-Jun-19

15-Jun-19

16-Jun-19

17-Jun-19

18-Jun-19

19-Jun-19

20-Jun-19

21-Jun-19

22-Jun-19

23-Jun-19

24-Jun-19

25-Jun-19

26-Jun-19

27-Jun-19

28-Jun-19

29-Jun-19

30-Jun-19

Figure 4.22 Winter Humidity Profile for June 2019

Table 4.17: Average quarterly Temperature in rig A, B, C and outdoor Temperature on 17th September 2019

| TIME | TAR2,19 | TAMB2,19 | TANO2,19 | EXT2,19 |
| --- | --- | --- | --- | --- |
| 0:00 | 20.291 | 22.24 | 22.94 | 25.8 |
| 0:15 | 20.092 | 22.167 | 22.848 | 25.5 |
| 0:30 | 19.868 | 22.035 | 22.755 | 25.6 |
| 0:45 | 19.663 | 21.909 | 22.656 | 25.4 |
| 1:00 | 19.478 | 21.817 | 22.524 | 26 |
| 1:15 | 19.372 | 21.678 | 22.425 | 26.3 |
| 1:30 | 19.214 | 21.579 | 22.312 | 26.4 |
| 1:45 | 19.002 | 21.486 | 22.22 | 26.4 |
| 2:00 | 18.804 | 21.354 | 22.108 | 26.2 |
| 2:15 | 18.573 | 21.222 | 21.975 | 26.8 |
| 2:30 | 18.348 | 21.057 | 21.85 | 27.1 |

| 2:45 | 18.17 | 20.938 | 21.757 | 27.4 |
| --- | --- | --- | --- | --- |
| 3:00 | 18.024 | 20.832 | 21.625 | 27.8 |
| 3:15 | 17.813 | 20.7 | 21.5 | 28.7 |
| 3:30 | 17.648 | 20.568 | 21.368 | 29.9 |
| 3:45 | 17.496 | 20.449 | 21.209 | 28.7 |
| 4:00 | 17.449 | 20.337 | 21.116 | 27.2 |
| 4:15 | 17.245 | 20.218 | 21.004 | 26.4 |
| 4:30 | 17.04 | 20.119 | 20.885 | 26.9 |
| 4:45 | 16.934 | 20.006 | 20.753 | 28.4 |
| 5:00 | 16.795 | 19.888 | 20.634 | 29.2 |
| 5:15 | 16.637 | 19.775 | 20.509 | 29.3 |
| 5:30 | 16.531 | 19.636 | 20.443 | 29.7 |
| 5:45 | 16.313 | 19.511 | 20.324 | 28.4 |
| 6:00 | 16.273 | 19.425 | 20.158 | 30.1 |
| 6:15 | 16.082 | 19.273 | 20.092 | 30.2 |
| 6:30 | 16.009 | 19.181 | 19.967 | 26.3 |
| 6:45 | 15.91 | 19.088 | 19.848 | 30.4 |
| 7:00 | 15.804 | 18.982 | 19.762 | 28.8 |
| 7:15 | 15.672 | 18.883 | 19.63 | 27.5 |
| 7:30 | 15.586 | 18.804 | 19.577 | 27.4 |
| 7:45 | 15.5 | 18.718 | 19.504 | 29 |
| 8:00 | 15.58 | 18.659 | 19.425 | 28.7 |
| 8:15 | 15.765 | 18.626 | 19.392 | 28 |
| 8:30 | 16.062 | 18.632 | 19.372 | 28 |
| 8:45 | 16.366 | 18.778 | 19.405 | 28.5 |
| 9:00 | 16.558 | 18.903 | 19.385 | 28.2 |
| 9:15 | 16.551 | 19.015 | 19.484 | 28.1 |
| 9:30 | 16.723 | 18.989 | 19.61 | 28.3 |
| 9:45 | 16.934 | 19.068 | 19.696 | 28.7 |
| 10:00 | 17.146 | 19.273 | 19.967 | 26.9 |
| 10:15 | 17.357 | 19.465 | 20.165 | 27.6 |
| 10:30 | 17.516 | 19.623 | 20.376 | 26.3 |
| 10:45 | 17.747 | 19.861 | 20.601 | 26.8 |
| 11:00 | 17.991 | 20.119 | 20.912 | 26 |
| 11:15 | 18.262 | 20.383 | 21.288 | 28 |
| 11:30 | 18.606 | 20.634 | 21.87 | 27.9 |
| 11:45 | 19.035 | 20.978 | 22.266 | 28.3 |
| 12:00 | 19.451 | 21.295 | 22.795 | 26 |
| 12:15 | 19.61 | 21.467 | 23.165 | 27.5 |
| 12:30 | 20.178 | 21.85 | 23.554 | 28.3 |
| 12:45 | 20.277 | 21.903 | 23.832 | 29.2 |
| 13:00 | 20.614 | 22.253 | 23.984 | 30.4 |
| 13:15 | 21.07 | 22.557 | 24.38 | 30.7 |

| 13:30 | 21.519 | 22.881 | 24.638 | 30.9 |
| --- | --- | --- | --- | --- |
| 13:45 | 21.982 | 23.396 | 24.698 | 31.2 |
| 14:00 | 22.022 | 23.231 | 25.087 | 31.3 |
| 14:15 | 22.841 | 24.076 | 25.101 | 31.6 |
| 14:30 | 23.118 | 24.42 | 25.305 | 31.7 |
| 14:45 | 22.999 | 23.799 | 25.774 | 30.6 |
| 15:00 | 23.363 | 24.182 | 26.092 | 30.8 |
| 15:15 | 24.162 | 24.803 | 26.415 | 30.4 |
| 15:30 | 24.169 | 24.678 | 26.475 | 29.9 |
| 15:45 | 24.572 | 24.916 | 26.594 | 30.6 |
| 16:00 | 24.764 | 25.2 | 26.759 | 27.4 |
| 16:15 | 24.863 | 25.411 | 27.076 | 27.8 |
| 16:30 | 25.239 | 25.517 | 27.043 | 27.9 |
| 16:45 | 25.028 | 25.279 | 27.003 | 27.7 |
| 17:00 | 25.385 | 25.51 | 27.155 | 27.5 |
| 17:15 | 24.876 | 24.83 | 26.363 | 26.8 |
| 17:30 | 24.724 | 24.565 | 25.874 | 26.6 |
| 17:45 | 24.764 | 24.493 | 25.623 | 26.6 |
| 18:00 | 24.81 | 24.592 | 25.477 | 26.4 |
| 18:15 | 24.532 | 24.321 | 25.18 | 26.3 |
| 18:30 | 24.479 | 24.156 | 24.869 | 26.1 |
| 18:45 | 24.261 | 23.898 | 24.539 | 25.8 |
| 19:00 | 24.083 | 23.753 | 24.268 | 25.5 |
| 19:15 | 23.799 | 23.594 | 24.063 | 25.3 |
| 19:30 | 23.363 | 23.409 | 23.799 | 25.1 |
| 19:45 | 23.006 | 23.204 | 23.601 | 24.8 |
| 20:00 | 22.841 | 23.072 | 23.469 | 24.6 |
| 20:15 | 22.629 | 22.953 | 23.343 | 24.5 |
| 20:30 | 22.411 | 22.821 | 23.204 | 24.5 |
| 20:45 | 22.2 | 22.676 | 23.066 | 24.3 |
| 21:00 | 21.962 | 22.596 | 23.026 | 24.3 |
| 21:15 | 21.777 | 22.491 | 22.973 | 24.3 |
| 21:30 | 21.599 | 22.464 | 22.947 | 24.2 |
| 21:45 | 21.407 | 22.418 | 22.9 | 24.2 |
| 22:00 | 21.196 | 22.411 | 22.914 | 24.1 |
| 22:15 | 21.057 | 22.233 | 22.781 | 24.1 |
| 22:30 | 20.964 | 22.108 | 22.656 | 24.1 |
| 22:45 | 20.813 | 22.035 | 22.616 | 23.9 |
| 23:00 | 20.634 | 21.916 | 22.57 | 23.7 |
| 23:15 | 20.482 | 21.863 | 22.511 | 23.7 |
| 23:30 | 20.304 | 21.804 | 22.464 | 23.6 |
| 23:45 | 20.092 | 21.645 | 22.345 | 23.4 |
| 0:00 | 19.888 | 21.519 | 22.226 | 23.2 |

00:00

00:45

01:30

02:15

03:00

03:45

04:30

05:15

06:00

06:45

07:30

08:15

09:00

09:45

10:30

11:15

12:00

12:45

13:30

14:15

15:00

15:45

16:30

17:15

18:00

18:45

19:30

20:15

21:00

21:45

22:30

23:15

00:00

Summer Temperature 17th September,2019

Temperature (degree Cel.

35

30

25

20

15

10

5

0

TIME

TAR2,19	TAMB2,19	TANO2,19	EXT2,19

Figure 4.23 Summer quarterly Temperature Profile for 17th September 2019

Table 4.18: Average daily Temperature in rig A, B, C and outdoor Temperature in September 2019

| DATE | TAR2,19 | TAMB2,19 | TANO2,19 | EXT2,19 |
| --- | --- | --- | --- | --- |
| 1-Sept. 2019 | 21.209 | 22.537 | 23.257 | 14 |
| 2-Sept.2019 | 20.971 | 22.464 | 23.257 | 19.5 |
| 3-Sept.2019 | 20.879 | 22.339 | 23.151 | 20.9 |
| 4-Sept.2019 | 21.235 | 22.226 | 23.046 | 22.6 |
| 5-Sept.2019 | 21.301 | 22.286 | 23.151 | 21.6 |
| 6-Sept.2019 | 21.255 | 22.319 | 23.046 | 23.5 |
| 7-Sept.2019 | 20.746 | 22.326 | 23.046 | 22.6 |
| 8-Sept.2019 | 20.522 | 22.187 | 22.94 | 18.9 |
| 9-Sept.2019 | 20.383 | 22.074 | 22.834 | 18 |
| 10-Sept.2019 | 20.185 | 21.956 | 22.729 | 19.3 |
| 11-Sept.2019 | 20.079 | 21.863 | 22.729 | 20.3 |
| 12-Sept.2019 | 20 | 21.764 | 22.623 | 19 |
| 13-Sept.2019 | 19.815 | 21.691 | 22.517 | 19.2 |
| 14-Sept.2019 | 19.716 | 21.586 | 22.411 | 21.3 |
| 15-Sept.2019 | 19.65 | 21.48 | 22.411 | 23.3 |
| 16-Sept.2019 | 19.518 | 21.387 | 22.306 | 25 |
| 17-Sept.2019 | 19.458 | 21.229 | 22.2 | 25 |
| 18-Sept.2019 | 19.418 | 21.13 | 22.094 | 25 |
| 19-Sept.2019 | 19.379 | 21.037 | 21.989 | 24.9 |
| 20-Sept.2019 | 19.266 | 21.024 | 21.989 | 24.9 |
| 21-Sept.2019 | 19.088 | 21.017 | 22.094 | 21.5 |
| 22-Sept.2019 | 18.824 | 20.991 | 21.883 | 18.5 |
| 23-Sept.2019 | 18.778 | 20.879 | 21.777 | 20.7 |
| 24-Sept.2019 | 18.83 | 20.667 | 21.777 | 21.4 |

|  | 25-Sept.2019 | 18.857 | 20.614 | 21.671 | 19.5 |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 26-Sept.2019 | 18.586 | 20.68 | 21.566 | 19.1 |  |
|  | 27-Sept.2019 | 18.388 | 20.621 | 21.46 | 20.5 |  |
|  | 28-Sept.2019 | 18.203 | 20.482 | 21.46 | 19.4 |  |
|  | 29-Sept.2019 | 18.018 | 20.423 | 21.46 | 19.4 |  |
|  | 30-Sept. 2019 | 17.965 | 20.251 | 21.249 | 15.8 |  |
| DAILY TEMPERATURE PROFILE FOR SEPTEMBER 2019 30 25 20 15 10 5 0 Day TAR2,19 TAMB2,19 TANO2,19 EXT2,19 |  |  |  |  |  |  |

Temperature in degree Cel.

1-Sept. 2019

2-Sept.2019

3-Sept.2019

4-Sept.2019

5-Sept.2019

6-Sept.2019

7-Sept.2019

8-Sept.2019

9-Sept.2019

10-Sept.2019

11-Sept.2019

12-Sept.2019

13-Sept.2019

14-Sept.2019

15-Sept.2019

16-Sept.2019

17-Sept.2019

18-Sept.2019

19-Sept.2019

20-Sept.2019

21-Sept.2019

22-Sept.2019

23-Sept.2019

24-Sept.2019

25-Sept.2019

26-Sept.2019

27-Sept.2019

28-Sept.2019

29-Sept.2019

30-Sept.2019

Figure 4.24 Summer daily Temperature Profile for September 2019

Table 4.19: Average daily Humidity in rig A, B, C and outdoor humidity in September 2019

| DATE | HTAR2,19 | HTAMB2,19 | HTANO2,19 | RHEXT2,19 |
| --- | --- | --- | --- | --- |
| 1-Sept. 2019 | 19.618 | 15.926 | 15 | 10.3 |
| 2-Sept.2019 | 19.658 | 15.904 | 15.113 | 5.1 |
| 3-Sept.2019 | 19.708 | 15.887 | 15.102 | 8.3 |
| 4-Sept.2019 | 19.78 | 15.954 | 15.246 | 8 |
| 5-Sept.2019 | 19.71 | 15.847 | 15.201 | 9.5 |
| 6-Sept.2019 | 19.696 | 15.919 | 15.023 | 11 |
| 7-Sept.2019 | 19.675 | 15.905 | 15.073 | 18.5 |
| 8-Sept.2019 | 19.634 | 15.936 | 14.968 | 25.4 |
| 9-Sept.2019 | 19.451 | 15.94 | 14.976 | 13.2 |
| 10-Sept.2019 | 19.426 | 15.879 | 14.805 | 5.6 |
| 11-Sept.2019 | 19.316 | 15.929 | 14.637 | 5.8 |
| 12-Sept.2019 | 19.145 | 15.789 | 14.391 | 13.3 |
| 13-Sept.2019 | 18.938 | 15.762 | 14.248 | 17.3 |
| 14-Sept.2019 | 18.877 | 15.759 | 14.376 | 10.4 |
| 15-Sept.2019 | 18.851 | 15.786 | 14.383 | 9.4 |
| 16-Sept.2019 | 18.744 | 15.893 | 14.417 | 6.4 |
| 17-Sept.2019 | 18.724 | 15.992 | 14.457 | 8.6 |
| 18-Sept.2019 | 18.771 | 16.02 | 14.243 | 10.6 |

1-Sept. 2019

2-Sept.2019

3-Sept.2019

4-Sept.2019

5-Sept.2019

6-Sept.2019

7-Sept.2019

8-Sept.2019

9-Sept.2019

10-Sept.2019

11-Sept.2019

12-Sept.2019

13-Sept.2019

14-Sept.2019

15-Sept.2019

16-Sept.2019

17-Sept.2019

18-Sept.2019

19-Sept.2019

20-Sept.2019

21-Sept.2019

22-Sept.2019

23-Sept.2019

24-Sept.2019

25-Sept.2019

26-Sept.2019

27-Sept.2019

28-Sept.2019

29-Sept.2019

30-Sept.2019

| 19-Sept.2019 | 18.849 | 16.027 | 14.212 | 9.3 |
| --- | --- | --- | --- | --- |
| 20-Sept.2019 | 18.817 | 16.128 | 14.483 | 7.5 |
| 21-Sept.2019 | 18.62 | 16.163 | 14.56 | 9.7 |
| 22-Sept.2019 | 18.632 | 16.223 | 14.441 | 18.7 |
| 23-Sept.2019 | 18.81 | 16.288 | 14.417 | 8.6 |
| 24-Sept.2019 | 18.77 | 16.346 | 14.693 | 9.2 |
| 25-Sept.2019 | 18.822 | 16.537 | 14.919 | 8.8 |
| 26-Sept.2019 | 18.86 | 16.651 | 14.956 | 26.7 |
| 27-Sept.2019 | 18.745 | 16.644 | 14.77 | 10 |
| 28-Sept.2019 | 18.951 | 16.703 | 14.721 | 7.5 |
| 29-Sept.2019 | 19.003 | 16.816 | 14.814 | 19.1 |
| 30-Sept.2019 | 19.086 | 16.947 | 14.89 | 21.5 |

Humidity Profile for September

Average daily humidity (%)

30

25

20

15

10

5

0

Days

HTAR2,19	HTAMB2,19	HTANO2,19	RHEXT2,19

Figure 4.25 Summer daily Humidity Profile for September 2019

CHAPTER FIVE

ANALYSIS AND DISCUSSION OF RESULTS

5.1 Overview

This chapter focused on the analysis and discussion of the results obtained from all categories of experimental tasks mentioned in Chapter Four. Results obtained in this research that is highlighted in chapter four are in line with key elements of the approved research topic and specific objectives. Hence, as reflected in laboratory results obtained, the aim to determine the appropriateness of using producing Energy Efficient Materials produced using carefully selected agricultural wastes/residues in Namibia has been achieved. Results obtained in this research agreed with similar studies carried out in other countries (Akinyemi, et al., 2016).

Accuracy of experimental results obtained from bricks and insulating sheets were used to compare the

indoor temperature behaviour of three self-developed experimental rigs that are explained in chapter four. Results (i.e. indoor temperature, humidity, etc.) obtained from these rigs at both summer and winter of 2018 and 2019 clearly showed that bricks and insulating board developed from the selected agricultural residues/waste can lead to the design of a high Energy Efficient residential building/housing.

5.2 Analysis and Discussion

5.2.1 Results of Thermal Conductivity of Insulating Board

From the different mix designs presented in chapter three for agricultural residues of Maize Husks, Millet Husks, Rice Husks, and Cow Dung, various graphs were plotted to show their thermal properties. Based on Figures 5.1 and 5.2, sample C (comprising of 20% (wt.) of Maize Husks, 10% (wt.) of Millet

Husks, 30% (wt.) of Rice Husks, and 40% (wt.) of cow dung) displayed the lowest thermal conductivity of 54.65 mW/(m*K) and the highest thermal resistivity of 0.6935 m2K/W and density of 849 kg/ m3. Sample A on the other hand (composing of 40% (wt.) of maize, 30% (wt.) of millet, 10% (wt.) of rice husks, and 20% (wt.) of cow dung) had the highest thermal conductivity (i.e. 100.71 mW/(m*K) and the lowest thermal resistivity (i.e. 0.4002 m2K/W) and density of 935.10 kg/ m3.

This revealed that sample C has the greatest insulation properties while sample A has the minimum thermal conductivity properties. Therefore, sample C is considered the best thermal efficient insulating material as compared to the rest been investigated since the extent of thermal insulation effectiveness is measured by how low the thermal resistivity and how high the thermal conductivity is. These two parameters measure the suitability of any material concerning the design of energy-efficient buildings or infrastructure. Also, values of thermal conductivity and thermal resistivity obtained for sample C fall within the generally recognized values for a good thermal efficient material as published by Kyauta, et al. (2014) that revealed the following thermal conductivities of good insulating material: Asbestos cement sheet - 0.319 W-1mK; brick building - 0.600 W-1m K; pine wood - 0.138 W-1mK and oak wood -

0.160 W1mK.

Furthermore, regression analyses of thermal conductivity against time for the conditions of the worst and best sample (i.e. samples A and C) as shown in Figures 5.1 and 5.2 revealed that the R2 value of samples A and C are 91% and 95% respectively. This proved that sample C has a good R2  value as compared with sample A, therefore, exhibiting good thermal insulating properties. This is shown in Figures 5.1 (for sample A) and 5.2 (for sample C) respectively.

112

SAMPLE A

110

THERMAL CONDUCTIVITY mW/(m*K)

108

106

y = 0.0001x2 - 0.0489x + 107.9

R² = 0.9149

104

102

100

98

1	51	101	151	201

TIME (Minutes)

RAW THERMAL CONDUCTIVITY DATA	MOVING AVERAGE	Poly. (MOVING AVERAGE)

Figure 5.1: Sample A Thermal Conductivity versus Time

Sample C

60

THERMAL CONDUCTIVITY

50

40

30

20	y = -0.0007x2 + 0.254x + 25.939

R² = 0.9505

10

0

0	50	100	150	200	250	300

Time (Minutes)

RAW DATA VALUE	MOVING AVERAGE	Poly. (MOVING AVERAGE)

Figure 5.2: Sample C Thermal Conductivity versus Time

5.2.2 Results of Thermal Conductivity of Bricks

Results of Thermal Conductivity (hence thermal Resistivity) of bricks of sand mixed with varying percentages of maize husks, rice husks, cow dung, and millet husks respectively are shown in Tables

4.3 – 4.6. This table provides results of thermal conductivity and thermal resistivity of bricks tested using the EPe 500 Lambda machine. From these results, it can be deduced that the percentage mix of

60 % (wt) and 40% of sand has favourable thermal conductivity and thermal resistivity for all bricks.

The thermal conductivity and thermal resistivity of Brick C were determined as 127.24 mW/m*K and

0.6051 m2K/W respectively as shown in Figures 4.3.

Figure 4.5 also shows that the thermal conductivity and thermal resistivity against time for brick type C2 (comprising of 60% (wt.) of cow dung and 40% sand are 128.46 mW/m*K and 0.5994m2K/W respectively. Also, from Figure 4.4 the thermal conductivity and thermal conductivity of brick C1 versus time for brick C1 (comprising of 60% rice husks and 40% sand) are 130.27 mW/m*K and 0.5910 m2K/W respectively.

Figure 4.6 shows that the thermal conductivity and resistivity of the brick C3 (comprises of 60% millet husks and 40% sand are 143.72 mW/m*K and 0.5357 m2K/W respectively.

It can be deduced therefore that brick C (made of 60% maize and 40% sand) has the best thermal conductivity because of its high thermal resistivity 0.6051 m2K/W.

Also, it can be seen from Fig.5.3 that 80% of Agricultural residues lead to an increase in thermal conductivity which shows that from 20% to 60% from Fig.5.3 exhibits a linear relationship that is K = (1

+��𝑚���.)K0   in most cases when K0  = thermal Conductivity at zero temperature. When the effect of

��

temperature on thermal conductivity is considered, the Fourier’s equation,  Q= -kA

��

is written as:

��

Q= -k0(1 + 𝛽��)

.A	5.1

��

�

.dx = - K0 (1 +𝛽��)dt	5.2

𝐴

�    �	�2

∫  𝑑𝑥 = −�0 ∫   ( (1 + 𝛽��)dt.	5.3

𝐴   0 	�1

�� = −�

[(𝑡

− 𝑡 ) + 𝛽

(��2 −  ��2 )]	5.4

𝐴	0 	2 	1 	2 	2 	1

�� =  �

[(𝑡

− 𝑡

) + 𝛽 ( (𝑡

− 𝑡

)(𝑡

+ 𝑡

)]	5.5

𝐴	0 	1 	2

2 	1 	2 	1 	2

= �0 [ 1 +

𝛽  (𝑡  + 𝑡 )] (𝑡  − 𝑡 )	5.6

1 	2 	1 	2

2

= �0 [ 1 + ����� ] (��1 − ��2)	 5.7

where tm =

(�1+�2)

2

Q = �0 ( 1 +  ����� ). 𝐴

(�1−�2)	 5.8

�

It can be seen from Fig.5.3 that the thermal conductivity of rice increases as the percentage mix of

agricultural residue increase from 20% to 40% because the equation K = (1 +��𝑚���)K0  it shows that the value of the coefficient of thermal conductivity 𝛽 < 0 therefore, the thermal conductivity will increase from 20% to 40 %. From 40% to 60% there is a decrease in thermal conductivity which shows the 𝛽 >0, and from 60% to 80% the thermal conductivity rises that shows that 𝛽 < 0.

From Fig.5.3 the thermal conductivity for maize husk, cow dung, and millet shows a similar trend from

20% to 60% which linear i.e K = (1 +��𝑚���)K0  for the value of 𝛽 = 0. Again, from 60% to 80% there is a change in the thermal conductivity which shows that 𝛽 > 0. This indicates that the thermal conductivity

is a function of the mix ratio which shows that from 80% is not linear as depicted in Fig. 5.3, therefore,

the thermal conductivity k = K0 f(mix) and

�    �	�2

∫  𝑑𝑥 = ∫   [�0 f(mix)dt.

𝐴   0 	�1

Thermal conductivity

250

200

150

100

50

0

Thermal Conductivity/Percentage Mix

0	10	20	30	40	50	60	70	80	90

Percentage mix

Thermal Conductivity of Rice husk	Thermal Conductivity of Maize husk

Thermal Conductivity of Cow dung	Thermal Conductivity of Millet husk

Fig. 5.3. Thermal conductivity versus percentage mix of Agricultural residues

5.2.3 Results of Marble Dust mixed with Agricultural Residues

From results in Table 4.2, samples A and C mixed with marble dust at various percentages of 5%, 10%,

20%, and 30% revealed that sample A thermal conductivity decreases (with an initial of 100.71 mW/m*K) with a percentage increase in marble dust (i.e. from 5% to 30%). Also, sample C shows a similar trend as sample A, from 5% to 30% with marble dust.

5.2.4 Results on Physical and Mechanical Properties of Brick Type

water absorption test results for the different brick samples were also presented in chapter four. After

24 hours’ immersion of the samples in water, it was revealed that the sample with 20% rice husk has the least value of water absorption followed by the sample with 20% cow dung, 40% rice, and 20 % millet husk respectively. Also, a sample with 80% rice husk has 8.42% water absorption as shown in Table 5.6. From these test results, therefore, 20 % rice husk which is a combination of 20% rice husk and 80% sand had a better performance when compared with 40% rice husk, 20 % millet husk, and

80% rice husk performances after 24 h of  immersion in  water. A  significant  decrease in  water

absorption was also noticed. Therefore, an increase in water absorption can be explained by the increase in the agricultural residue of the brick samples.

The successive rise in water absorption as a result of an increase in the agricultural residue (shown in Figures 4.7 - 4.10) can be attributed to the fact that the capability of the binder that binds particles decreases as the agricultural residue increases. Scatolino et al. (2015) and Akinyemi, et al. (2016) also detected a similar increase in water absorption with an increase in agricultural residues.

Also, the compressive strength of the sample type bricks was seen to decrease with the addition of

agricultural residues for each brick type as shown in Table 4.8. Brick A1 had the highest value of compressive strength while D2 had the least value as shown in Fig. 4.11.

The compressive strength also showed a similar trend in the rise of agricultural residue leading to a declining pattern of compressive strength values as shown in Figures 4.11 – 4.14. Hence, the D2 had the least value of compressive strength of 5.50 N/mm2 and A1 had the highest value of compressive strength of 23.50 N/mm2.

5.2.5 Results of Experimental Rigs

5.2.5.1 Winter period

Figure 4.15 shows the temperature profiles for winter July of 2018 having the highest recorded indoor temperatures of 29.30C. It can be seen that the indoor temperatures for Rig TAR1 recorded higher temperatures than that of Rigs B and C. From Fig. 4.15, it can be seen that the temperature profiles of Rig A or TAR1 range between a comfort level of 20 -24 °C from midnight till midday when the External Air Temperature (Ext.AT) was relatively low. Likewise, as from midday, the indoor temperatures decrease as the external temperatures increase. Conversely, the external temperature did not have much effect on the indoor temperatures as shown in Fig. 4.15. Also, from Fig. 4.15, it can be seen that the indoor temperatures were high while the external temperatures were low and vice-versa. This revealed that Rig A or TAR1 had a better insulating property than the other rigs (i.e. Rigs B and C) that comprise marble dust mix and that with no insulation respectively.

Figure 4.16 shows the monthly temperature for winter in July of 2018. It can be seen from the Figure that as the outer door temperature decreased the indoor temperature increased. Also, Rig A (or TAR1) exhibited the best insulating property since the rig maintained warmer indoor temperature as the outdoor temperature changed on any given day.

Figure 4.17 shows the monthly humidity for winter July of 2018. It can be seen that Rig C (or RHNo3) had the highest humidity followed by Rig B (i.e. mix with 20% marble dust, labelled RHMB2), and lastly Rig A (or RHA1). It can be presumed that the outside humidity does not have much influence on the inside humidity since the increase in humidity outside caused the inside humidity to increase by a very small or negligible amount. Similarly, by matching Figures 4.16 and 4.17, it can be said that the increase in temperature drops the humidity and vice versa.

5.2.5.2 Summer period

Figure 4.18 illustrates the monthly temperature profiles for October of 2018. The average indoor temperature for STAR1 (i.e. Rig A) was 23.4°C and the average outdoor temperature was 23.4 °C, resulting in a difference approximately equal to zero. Likewise, the indoor temperatures range between 21.3°C and 25.50C with many days out of the thermal comfort range of 200C to 24°C thereby

leading to the possible use of an air conditioning system. From Fig. 4.18 however, it can deduce that there are no significant changes between indoor and external air temperatures.

Figure 4.19 shows the humidity in the summer period for the 3rd of October 2018 for Rigs A (represented with humidity RHA3); marble dust Rig B (represented with humidity RHM2); and Rig C (represented with humidity by RH1). The external humidity is represented as RHExt. It can be understood from Figure 4.19 that RHA3 or Rig C has high humidity when compared with Rigs B and A. It can therefore be concluded from Fig. 4.18 that lower temperatures lead to high humidity as shown in Fig. 4.19.

Furthermore, data were analysed for both winter and summer sessions in 2019 as shown in Figures

4.20 – 4.25. It can be seen from Fig. 4.20 that the indoor temperatures for Rig TAR1 on 19 June 2019 recorded high temperatures than rigs B and C. From Fig. 4.20 i.e. temperature profiles of Rig A or TAR1,19 can be observed that the thermal comfort ranges between 20 -23.4 °C from midnight till midday while the External Air Temperature (Ext.AT) was comparatively little. Likewise, as from noontime i.e. between 12:00 – 14:30, the indoor temperatures decrease as the external temperatures rise. On the contrary, the external ambient temperature did not have much consequence on the indoor temperatures as shown in Fig. 4.20. Similarly, Fig. 4.20, clearly shows that the indoor temperatures were high as the external ambient temperatures were low and vice-versa. This can therefore be concluded that Rig A or TAR1,19 had better insulation than the other rigs (i.e. Rigs B and C) including marble dust mix and the rig without any insulation.

Also, Figure 4.21 displays the monthly temperature for the winter of June 2019. It can be noticed from the plot that as the outer door temperature decreases the indoor temperature increased. Also, Rig A (or TAR1, 19) showed the highest insulation since the rig conserved warmer indoor comfort as the outdoor temperature altered in a given day.

From Figure 4.22 that shows the monthly humidity for winter of June 2019, it can be seen that Rig C (or RHTANO19) had the highest humidity followed by Rig B (i.e. mix with 20% marble dust, labelled RHMB2, 19) and lastly Rig A (or TAR1, 19). It also showed that the outside humidity does not have much influence on the inside humidity since the increase in humidity outside causes the inside humidity to increase by a very small or negligible amount. Similarly, by comparing Figures 4.21 and

4.22, it can be observed that the increase in temperature decreases the humidity and vice versa as in the case of July 2018.

Also, the plots of Figures 4.23-4.25 revealed the temperature and humidity of data collected from rig A, B, and C for the summer session in 2019. Figure 4.23 showed the temperature profile for 15th September 2019. It can be seen from the plots that rig A has the lowest temperature than the other two rigs.

Figure 4.24 illustrates the monthly temperature profiles for September 2019. The average indoor temperature for TAR1, 19 (i.e. Rig A) was 22°C and the average outdoor temperature was 22 °C, resulting in a difference of approximately zero. Likewise, the indoor temperatures range between

19.2°C and 21.90C. From Fig. 4.18, it can be seen that there are no significant variations between indoor

and external air temperatures.

Furthermore, Figure 4.25 shows the humidity in the summer period for September 2019 for Rigs A (represented with humidity RHTAR1, 19); marble dust Rig B (represented with humidity HTAMB2 19); Rig C (represented with humidity by HTANO2,19) and the outer humidity represented as RHEXT2,19. It can be understood from Figure 4.25 that Rig C has high humidity when compared with Rigs B and A. It can therefore be concluded that this was due to the lower temperature (from Fig. 4.24), which lead to the high humidity as shown in Fig. 4.25.

5.3 Thermal performance on the experimental rig

5.3.1 Winter condition

Results obtained from this study revealed that the thermal comforts range obtained are better when compared with those obtained by Andre (2011) that ranged from 15.8°C to 12°C.

In this study, the indoor temperatures of the house with agricultural residues recorded a maximum temperature of 20.4 °C and minimum temperature of 13.5 °C which are higher than the temperatures of the study conducted by Andre (2011) in South Africa. Also, as from 12:15 AM - 10:45 AM, the recorded indoor temperatures were higher than the outdoor temperatures thus heat was being lost from the house to the outdoor. The question has been why were high temperatures being recorded at night? This could be as a result of the building envelope storing the solar energy and uses the thermal mass concept, to distribute it. That is by the heat absorbed during the day gets circulated via buoyancy phenomena.

The performances of the three rig systems were related considering the average daily temperatures. Rig A (with the agricultural residues from maize, millet, rice, and cow dung as the insulating material in the middle of two brick walls) recorded 18 days out of 31 with an average temperature of 22.4°C which is within thermal comfort temperature while Rig B (Marble dust mixed with agricultural residue from maize, millet, rice, and cow dung as insulating material sandwiched between two brick walls with cavity 50mm) recorded 14 and Rig C (which served as Control design rig i.e. conventional single-layered brickwork with no insulation) recorded 10 days with an average temperature of 22.4°C (Onjefu et al.,

2019).

Calculating the efficiency of the three systems;

18

ŊrigA =

31

X 100 = 58.06 %.........................................................................................5.9

ŊrigB =

14

X 100 = 45.16 %.............................................................................................510

31

10

ŊrigC =

31

X 100 = 32.25 %.........................................................................................5.11

These results show that Rig A (with the agricultural residues from maize, millet, rice, and cow dung)

will use less energy (therefore higher efficiency) than the other two rigs B and C.

5.3.2 Summer condition

Results from this research as reflected in chapter four show that high indoor temperatures recorded in Rig C (or TAN03) were above the comfort temperature range. The highest indoor temperature recorded was 300C at midday, when the outside air temperature was relatively high. It can therefore be concluded that the rig without insulation (i.e. Rig C), when compared with that of Rig A had a higher temperature.

This finding answers/addresses the specific objective that requires conducting a comparative thermal behaviour assessment with conventional insulating materials.

5.4 Summary of Key Results

The results of this research also revealed that it is possible to develop particleboards from agricultural residues of maize, millet, and rice and cow dung still obtain reasonable/acceptable physical properties. From the results obtained from the eleven samples tested labelled A to K, Sample C (composed of 10% maize, 10% millet, 30% rice, and 40% cow dung) offers the lowest thermal conductivity of 54.65 mW/ (m*K) and the highest thermal resistivity 0.6935 m2K/W, whereas sample A (composed of 40% maize,

30% millet, 10% rice and 20% cow dung) gave the highest thermal conductivity and lowest thermal

resistivity, hence considered poor thermal efficiency.

However, with a mix ratio of 5%, 10%, 20%, and 30% marble dust added to sample A and C showed that with 5% addition of marble dust to sample A (of compositions 40% maize, 30% millet, 10% rice and 20% cow dung) gave a thermal conductivity of 71.99 mW/ (m*K) and thermal resistivity of 0.9136 m2K/W. Furthermore, with 5% addition of marble dust to sample C (made of varying ratio of 10% maize, 10% millet, 30% rice, and 40% cow dung) gave a high thermal conductivity and low thermal resistivity, hence considered poor thermal efficient with the addition of marble dust.

Furthermore, for Brick C, the thermal conductivity and thermal resistivity were observed as 127.24 mW/m*K and 0.6051 m2K/W respectively which makes brick C (comprises of 60% maize and 40% sand) the best in terms of lower thermal conductivity and high thermal resistivity.

From the experimental rigs A, B, and C, the following can be concluded: In winter, Rig A accomplishes better performance in terms of temperature and humidity followed by Rig B and Rig C as control. The same applies in summer irrespective of an increase in external temperature, the indoor temperature is maintained at ambient at the constant condition. This means in summer Rig C due to high temperature will need the use of an HVAC unit for cooling.

It can be seen from Table 4.9- 4.19 that the temperature and humidity collected is relatively small when compared with both inside and outside of the rigs. This might be attributed to inadequate air tightness and less/no insulation at the doors and windows of the rigs.

CHAPTER SIX

VALIDATION OF RESULTS

6.1 Overview

This chapter focuses on appropriate tools used to validate results obtained from laboratory results especially those related to Rig A.

The tools were then used to check the accuracy of results and conclusions obtained from the major category.

6.2 Validation Tools Used for thermal conductivity

The guarded hot plate apparatus (GHPA) is widely accepted as a primary apparatus to determine the apparent thermal conductivity of insulating materials. The hot and cold plate keeps the boundary conditions constants (temperature) in the superior and inferior surfaces of the specimen. In the ideal case, the plates are in perfect thermal contact with the specimen, and the heat flow through it is one- dimensional and independent of time. The specification for the thermal conductivity tool Meter EP 500 can be seen in Table 6.1.

The guarded hot plate apparatus k-Meter EP 500 can automatically complete three subsequent tests

on one specimen at different temperatures between 10 and 40 0C, the average measuring temperature was 10, 25, 40 0C. The difference between cool and heat plate was 5 0C for all test sequents. The average temperature was calculated from the cold and heating plates.

Table 6.1 Specifications for thermal conductivity equipment. Source (Ashour, 2010)

6.3 Validation Tools Used for Experimental Rigs

The software ANSYS and the design tools ANSYS Fluent will be used. The modelling will include the temperature and velocity distribution of the rigs. The ANSYS Fluent tool comprises the broad physical modelling abilities needed to model airflow, heat transfer, in the rigs.

Figure 6.1 fluent simulation convergences

Fig. 6.1 shows the Reynolds Averaged Navier Stokes (RANS) equations and turbulence models which create a system of equations that is essential to be resolved numerically. An analytical solution for

these equations is difficult; therefore, an iterative numerical solution method is employed on a mesh to estimate the partial differential equations into estimated algebraic equations. The linearized algebraic equations iteratively converge to the nonlinear solutions by employing a suitable algorithm built-in FLUENT. A convergence criterion is specified to attain a suitable accuracy. When all the flow properties in all cells of the mesh reach the convergence criteria, the solution is considered “converged” and the iterative process ends (Kayne, 2012).

Figure 6.2 Temperature (in Kelvin) plot

Figure 6.2 shows the contour of temperature distribution on the walls and the air inside rig A made with maize husks, rice husks, and millet husk, and cow dung. The temperature distribution for the air is taken at a height of 1.5 m from the ground. It can be seen that the average air temperature of about

281.3K (8.3°C) on the wall is almost uniform. The average air temperature is a little higher than inside the rig at about 283.8K (10.8°C). This is due to a high heat loss from the rig to the outdoors during the winter season.

Figure 6.3 Velocity plot

Figure 6.3 shows the distribution of air velocity from the CFD simulation. With free convection, the air is seen to flow in a streamlined condition from the door towards the top side of the rig on the central wall, with increasing velocity toward the top. It can be seen that air circulation also occurs in the middle of the rig but there is almost no airflow around the edges of the walls.

Figure6.4 Temperature (in Kelvin) plot winter

From Figure 6.4, it can be seen that the average air temperature distribution during winter results revealed that there is a significant temperature variation on the front wall surface toward the top of the rig with the highest temperature of about 284.2K (11.2°C), it can be seen from Figure 6.4 that the lowest temperature is 280.9K (8.1°C).

Figure 6.5 Velocity plot for winter

Also, Fig. 6.5 shows the air velocity distribution with free convection. The air is seen to flow in a streamlined condition from the door towards the top side of the rig, with increased velocity toward the top. It can also be seen that the air velocity is more towards the two adjacent windows.

Figure6.6 Temperature (in Kelvin) plot summer

From Figure 6.6, it can be seen that the air temperature distribution during summer revealed that there is a significant temperature variation on the front wall surface toward the top of the rig with the highest temperature of 303K (30°C). Specifically, temperatures remain low near the floor and increase with height.

6.4 Validation Model for thermal conductivity of particleboard

Thermal conductivity determinations are subject to several equations. The data were taken from the data logger and thermal conductivity was calculated through software related to the k instrument.

Thermal conductivity was calculated using the following equation.

Λ10 =   Φc. L/ 2A (Th - Tc)	(6.1)

where, Λ10 is the thermal conductivity at 10 0C (W/mK), Φc the heat flow, which flows under stationary conditions perpendicularly to the sample surface through the sample (W), The heating plate area (m2), L the thickness of the samples (m), Th  the temperature at the heating plate surface (K), and TC is the temperature at the surface of the cooling plate (K)

6.5 Validation Model for Bricks

T1

H	T2

x

L

Figure 6.7 Fourier Law with constant thermal conductivity

However, the equation for one-dimensional steady heat conduction in a slab, according to the Fourier law (Fig. 6.7) is:

−�𝐴∆�

Q =	6.2

𝑋

Where,

Q= Heat transfer rate [W].

A = Area, L x H, in heat flow direction [m2]. k = Material thermal conductivity [W/m K] ΔT = T1-T2, Temperature [K]

x = Brick Thickness [m

Generally, the thermal conductivity value deduced is related to the average temperature of the tests

Tm = (Th + Tc)/ 2	6.3

The thermal conductivity is computed for each time step using Equation 6.2. The measurement area

used has a side of 150.4mm, which corresponds to the optimal area obtained by numerical simulation. This experimental validation will thus also confirm this area choice. The moving averaged thermal

conductivity �̅ 720(𝑡�) is then evaluated as in Equation 6.4, with ��� > 720. At each time step, it agrees with

the mean of the thermal conductivity measured.

6.4

The moving standard deviation of the thermal conductivity is defined by Equation 6.5. At a given time step, it defines the variations of measured thermal conductivity around the average on the time

interval [��(�−720), ���]   (Dubois et.al., 2015).

6.5

In conclusion, the moving variation coefficient at time ��� is the ratio of the moving standard deviation of  thermal conductivity on  its moving average. The measurement terminates when  the  moving

variation coefficient falls below 0.4%, which is defined as the stability threshold.

6.6 Validation Model for Experimental Rig

Results obtained by the CFD model were matched with the real corresponding experimental data using the normalized mean square error (NMSE).

NMSE = ( VCFD  - Vm )2 / (VCFD x Vm )	(6.3)

Where,

VCFD = Simulated value of CFD Vm    = measured value obtained

Table 6.2: Normalized Mean Square Error (NMSE) between the winter temperature values obtained in the simulation and experimentally

| Average Measured temperature | Average Simulated Value | NMSE |
| --- | --- | --- |
| 8.10 C | 110 C | 0.09 |
| 7.90 C | 10.60 C | 0.08 |

Table 6.3: Normalized Mean Square Error (NMSE) between the summer temperature values obtained in the simulation and experimentally.

| Average Measured temperature | Average Simulated Value | NMSE |
| --- | --- | --- |
| 310 C | 220 C | 0.12 |
| 290 C | 200 C | 0.14 |
| 270 C | 21.40 C | 0.05 |

Based on the work of Mostafa et al., (2012) stated that NMSE values below 0.25 are considered a good indicator of agreement between simulated and measured values. It is observed from Table 6.2 and Table

6.2 that the NMSE found shows agreement between the values simulated and measured experimentally

for both winter and summer season. The findings confirm with the work of, Vilela et al., (2019), that NMSE

of 0.2, signifying a good acceptance of simulated results with measurements.

6.6.1 Validation of CFD data for winter and summer in 2019

The comparison between measured and simulated temperature gradients is presented in Figures 6.8 –

6.9. The temperature gradients from the CFD model agree well with the measured temperatures. On average, the difference between simulated and measured data was 0.2°C for the values of Rig A in the winter season of June 2019 at different days in the month as given in Table 6.4. Also, Table 6.5 shows the measured and simulated temperatures for the summer season in 2019.

Table 6.4: Measured and Simulated data for June 2019

| June 2019 | Average Measured Temperature | Average Simulated Temperature |
| --- | --- | --- |
| 2nd June | 10.1 | 12.8 |
| 3rd June | 8.3 | 11.8 |
| 4th June | 9.5 | 10.7 |
| 5th June | 12.5 | 15.3 |
| 10th June | 14.7 | 16.8 |
| 23rd June | 16.5 | 17.6 |

June 2019

Temperature in degree Ce

20

15

10

Measured Data

5	Simulated Data

0

0	5	10	15	20	25

Days of the Month

Figure 6.8 Validation of CFD Simulation for Rig A

Table 6.5 : Measured and Simulated data for September 2019

| September 2019 |  | Average Measured Temperature | Average Simulated Temperature |  |
| --- | --- | --- | --- | --- |
| 1st June |  | 31 | 23 |  |
| 4th June |  | 30 | 22 |  |
| 10th June |  | 29 | 21.7 |  |
| 12th June |  | 28 | 20 |  |
| 16th June |  | 27 | 21.4 |  |
| 22nd June |  | 26 | 20.3 |  |
|  | Month of September 2019 35 30 25 20 15 Measurement Data 10 Simulated Data 5 0 0 5 10 15 20 25 Days of the Month |  |  |  |

Temperature in degree Cel.

Figure 6.9 Validation of CFD Simulation for Rig A

Simulation of Rig A was validated at six different days (i.e. 1st, 4th, 10th, 12th, 16th, and 22nd) in September

2019. The temperatures in rig A are presented in Figure 6.9. Results obtained by the CFD model in 2019 were also matched with the real corresponding experimental data using the normalized mean square error (NMSE) given in equation 6.3. The error from the NMSE equation is 0.25 which is relatively small. The general agreement between the CFD simulation and the experimental measurement was satisfactory.

CHAPTER SEVEN

CONCLUSION AND RECOMMENDATION

7.1 Overview

This Chapter provides concluding remarks for the solution for material investigation. This encompasses the thermal conductivity of the insulating board; thermal conductivity test on the different brick samples; the thermal conductivity of marble mix with the agricultural particle board ratio; the physical and mechanical properties of the type of the brick used in the research; and the experimental rig used. Also, some recommendations for further research are included in this Chapter.

7.2 Key Research Findings

In Namibia and most developing African countries, most agricultural wastes add no value to human advancement. They are mostly either allowed to rot or burnt thereby contributing to environmental degradation and pollution. The novelty of this research in terms of environmental benefit aimed at converting this negative environmental impact to developing building materials that will lead to the design of energy-efficient housing that eliminates the use of conventional electricity-driven devices for heating and cooling during cool and hot seasons.

Due to the large volume produced every year and the extent of their environmental degradation

observed in Namibia and most African countries, key building materials were developed and tested from the following agricultural wastes/residues: maize husk, millet husk, rice husk, and cow dung. Based on the well-selected proportionate mixed design of these materials, the research was able to develop the following key findings in each of the categories considered.

7.2.1 Thermal Conductivity Test of Insulating Board

The findings clearly showed that with suitable mixed ratios and methods, agricultural residues can be used to develop insulating materials that contribute to thermal efficiency and increased human comfort without the use of conventional heating and cooling devices like air conditioning systems that

are usually powered by machines that pollutes the environment. Insulating boards were produced from a well-selected combination of agricultural residues of maize, millet, rice husks, and cow dung. Laboratory results obtained give better thermal resistivity values when compared with existing literature and materials. This makes it appropriate for the design and construction of energy-efficient buildings. Very few existing literature looks into this aspect of research.

7.2.2 Thermal Conductivity Test of Bricks

Thermal Conductivity and resistivity results revealed that materials developed from the residues of maize, millet, maize, and cow have good energy efficiency in building. Laboratory results obtained in this research concludes that bricks with the percentage composition of 60% maize and 40 sand produced the lowest thermal conductivity of 127.24 mW/(m*K) and the highest thermal resistivity of

0.6051 m2K/W. This makes such bricks suitable in the design of affordable, sustainable, and energy-

efficient housing infrastructure, especially for low-income individuals.

7.2.3 Marble Dust mixed with Agricultural Residues

The usefulness of marble dust is tested by adding certain percentages of it in the best and worst samples that measure thermal conductivity and thermal resistivity. Results revealed that there was a decrease in thermal conductivity hence an increase of thermal resistivity for samples A and a decrease in thermal conductivity with an increase in resistivity of sample C. This showed that also of marble dust there was a decrease in thermal conductivity for both samples A and C.

This research, therefore, concludes that the use of marble dust in the mixed design serves as a binder, raw material for energy-efficient building, improved/increased the thermal resistivity of the material, improved building thermal efficiency, occupants’ comfort, and reduction in energy consumption.

7.2.4 Physical and Mechanical Properties of Brick Type

Laboratory investigations were carried out on the thermal, physical, and mechanical properties of materials developed from agricultural wastes/residues developed from Maize husk, Rice husk, Millet husk, and cow dungs. Results revealed that water absorption for all bricks increases with a percentage increase of 20%, 40%, 60% & 80% of agricultural residues/wastes.  Also, the compressive strengths of all bricks decrease with a percentage increase of agricultural residues of 20%, 40%, 60%, and 80%. However, with  the  addition  of  cement and  sand  in  the  agricultural  residues/wastes, the  water

absorption increases with an increase in the agricultural residues. Also, the compressive strength of bricks decreases and water absorption increases for all the sample bricks.

This finding further revealed how carefully selected mixed design in agricultural residues/wastes can lead to the development of bricks that are strong and suitable for use in a sustainable, affordable, and environmentally friendly energy-efficient building.

7.2.5 Experimental Rigs

To further prove the authenticity of results obtained, 3 rigs of varying designs were built from materials developed to which temperature and humidity measurements were taken at both hot (summer) and cold (winter) periods in Namibia. Their thermal efficiencies were then compared with that of a normal residential building. Results showed that the indoor temperature and humidity of rigs made from agricultural residues (with and without marble dust and insulation) compared with outside temperature during summer and winter in Namibia correlated sustainable green buildings.

In winter, the Rig made from the agricultural residues (i.e. Rig A), used as insulation, performs better

than the Rig with marble mix (i.e. Rig B) in terms of temperature and humidity taking the third Rig (i.e. Rig C) without any form of insulation as reference. In summer irrespective of the increase in outside temperature, the indoor temperature remains at the ambient and constant condition.

The once again showed the good thermal resistivity behaviour of material developed in this research when appropriate design concepts are followed. Hence using locally available agricultural wastes/residues under carefully selected mixed proportions can lead to addressing emerging social, economic, and environmental challenges that are linked to climate changes.

7.3 Key Recommendations

The following are key recommendations to be made for each of the following categories considered in this research.

7.3.1 Recommendations of Thermal Conductivity Tests for particle Boards

In other to see how the mix ratio performs concerning microstructure when using the Section Electron Microscope (SEM), varying tests in varied testing environments including those in humid/tropical environments have to be conducted for a period longer than six months. This was not this case in this research since Namibia is a semi-arid country. However, results obtained so far in semi-arid environments comply with existing literature.

7.3.2 Recommendations Thermal Conductivity Test of Bricks

The current research does not consider analyses/studies linked to the stress-strain behaviour of bricks with the time it takes for the sample to fail. Also, a thickness swelling test to determine the change in the thickness of a sample after it has been immersed in water for a given period was not done. This test will show the effect of water on the thickness of the bricks by using a digital veneer calliper to measure the changes before and after water immersion. Performing such studies and tests will provide more information that will complement the results obtained in this research.

7.3.3 Recommendations Marble Dust mixed with Agricultural Residues

The results obtained for this category was based on an optimum temperature of 40oC. This research recommends further studies based on a range of temperatures up to collapse or failure stage be conducted. Also, information related to the mineral composition of marble dust should be obtained to ascertain their contribution to the positive behaviour of marble dust to the thermal behaviour of samples considered.

Due to its positive viability to improve thermal resistivity marble dust should be exploring for energy- efficient materials to be used for building in energy performance.

7.3.4 Recommendations Physical and Mechanical Properties of Brick Type

Since the soil sample and agricultural residues/wastes used had a lot of fines particles, wide-ranging tests including permeability and shear box tests need to be performed to understand how the samples

perform under shear forces. There is a need for further study to look at Possible approaches to improve the workability (i.e. Permeability test, relative density, Soundness test Hardness test, Efflorescence test to know the presence of soluble salt in the sample, etc.) of bricks.

7.3.5 Recommendations Experimental Rigs

Comparative studies on rigs behaviour under changes in climatic conditions especially under extremely hot and dry, hot and wet environments need to be conducted. This study is only limited to the moderately cold and hot environment in assessing the performance of material developed.  This will lead to detailed and wide-ranging assessment results that capture wide-ranging environmental and climatic conditions of rig performance. Also, the In-situ performance measurement should be done under a closed airtightness with adequate insulation of the doors and windows of the rigs to give good readings of temperature and humidity in the rigs.

LIST OF REFERENCES

Akbari, M., Sinton, D., & Bahrami, M. (2011). Geometrical effects on the temperature distribution in a half-space due to a moving heat source. Journal of heat transfer, 133(6).

Akinyemi, A. B., Afolayan, J. O., & Oluwatobi, E. O. (2016). Some properties of composite corn cob and sawdust particle boards. Construction and building materials, 127, 436-441.

Al-Homoud, M. S., (2005). Performance characteristics and practical applications of common building thermal insulation materials, Building and Environment 40, 353–366.

Al-Juruf, R.S., Ahmed, F.A., Alam, I.A., Abdel-Rahman, H.H. (1988). Development of heat-insulating materials using date palm leaves. Journal of Building Physics, 6(3), 158-164.

Almshkawi, M. J. (2011). Modelling and Assessing an Efficient Building with Absorption Chillier for Two Different   Climates   in   the   MENA   Region. Master's   thesis,   Kassel   University,   Kassel, Germany.https://www.uni-Kassel. de/EECS/file admin/groups/w_460600/thesis/batch1/Master_Thesis_-_Jihad_Mishkawi. pdf.

Al-Sallal, K. A., 2003. Comparison between polystyrene and fiberglass roof insulation in warm and cold climates, Renewable Energy 28, 603–611.

Anas, Z., & AL-Hafzan, A. (2010). Efficiency towards Building envelope an Analysis study between the main Library of University Malaya Building of UiTM Perak Building. Efficiency towards Building envelope an Analysis study between the main Library of University of Malaya Building of UiTM Perak. Journal of Environmental Science and Development., 264-270.

Anastaselos, D., Giama, E., Papadopoulos, A. M., (2009). An assessment tool for the energy, economic and environmental evaluation of thermal insulation solutions, Energy and Buildings 41,

1165–1171.

Ashour, T. (2010). The Influence of Natural Reinforcement Fibres on Insulation values of Earth Plaster for Straw Bale Buildings. Materials and Design, 4676-4685.

ASHRAE. (2011). Energy Benchmarking and Benchmarking Tools. In ASHRAE, American Society of Heating, Refrigerating, and Air-Conditioning Engineers. https://www.pnnl.gov/main/publications/external/technical_reports/PNNL-20956.pdf.

ASHRAE (1997), Thermal comfort. ASHRAE Handbook of Fundamentals, Chapter 8, Atlanta, USA.

Ambuga, J. N. (2018).   Investigation of Energy Efficiency as a result of a House Built with Geoplast Modulo Foundation System (GMFS), A Case study of Mariental Residential Area. Final year project of Bachelor of Engineering submitted in the Department of Mechanical and Marine Engineering, Namibia University of Science and Technology.

American Society for Testing and Materials (ASTM) Standard ASTM international,100 Barr Harbor

Drive, West Conshohocken, United States. Retrieved from www.astm.org, 2004.

American Society of Testing and Materials, (1999). Standard Test Method for Evaluating Properties of Wood-Base Fiber and Particle Panel Materials. Designation: D1037- 99. West Conshohocken, PA, pp. 142–171.

ASTM C 62, (2007). Technical Note on Bricks Construction: Specifications for and Classification of Brick.

Brick Industry Association, Reston, Virginia.  www.gobrick.com

Baetens, R. Jelle, B.P. Thue, J.V. Tenpierik, M.J. Grynning, S. Uvsløkk, S. Gustavsen, A. (2009). Vacuum insulation panels for building applications: A review and beyond, Energy Build. 42 (2010) 147–

172. DOI:10.1016/J.ENBUILD.2009.09.005.

Baetens, R., Jelle, B. P., Gustavsen, A., & Grynning, S. (2010). Gas-filled panels for building applications: A state-of-the-art review. Energy and Buildings, 42(11), 1969-1975.

Baetens, R. Jelle, B.P. Gustavsen, A. (2010). Aerogel insulation for building applications: A state-of-the- art review, Energy Build. 43 (2011) 761–769.

Baeza, A. (2013). A zero-energy house for UAE. Retrieved from MSc thesis from KTH School of Industrial

Engineering and Management.

B. ISO, 6946: (2007). Building components and building elements—Thermal resistance and thermal transmittance—Calculation method.

Bal, H., Jannot, Y., Quenette, N., Chenu, A., & Gaye, S. (2013). Water content dependence of the porosity, density, and thermal capacity of the laterite based on millet waste additive. International Journal of Construction and Building Materials., 141-151.

Bejan, A. Kraus, A.D (2003). Heat transfer handbook. Hoboken, New Jersey: JOHN WILEY & SONS, INC.

Binici, H. K. (2015). The production of thermal insulation by waste animal and vegetable fibers. Journal of Science and Engineering, 4(5), 140-148.

Blocken, B., Stathopoulos, T., Carmeliet, J., and Hensen, J. L. M. (2010). Application of computational fluid dynamics in building performance simulation for the outdoor environment: an overview. Journal of Building Performance Simulation

Bolatturk, A., (2008). Optimum insulation thicknesses for building walls concerning cooling and heating degree-hours in the warmest zone of Turkey, Building and Environment 43, 1055–1064.

"BoN	and	IMF	(2018).	Forecast	a	recovery	for	the	Namibian	economy".	AgriForum.

https://en.wikipedia.org/wiki/Agriculture_in_Namibia

B.S. EN, 13163: (2012) Thermal insulation products for buildings, Fact. Made Prod. Expand. Polystyrene

Specified.

Building Research Energy Conservation Research Unit (BRECSU) (1997) Passive Solar House Design: Barrat Study', General Information leaflet 22, Best Practice Programme, Energy Efficiency Office,

Department of the Environment.

Bahrami, S. (2008). Energy-efficient buildings in warm climates of the Middle East.

Bwayo, E., & Obwoya, S. K. (2014). Coefficient of thermal diffusivity of insulation brick developed from sawdust and clays. Journal of ceramics, 2014.

Cabeza, L., Castell, A., Medrano, M., Pereza, G., & Fernandez, I. (2010). Experimental study on the performance of insulation materials in Mediterranean construction. Energy and Building; Vol

42(5), 630-636.

Castell, A., Medrano, M., Martorell, I., & Cabeza, L. F., (2010). Experimental study on the performance of buildings with different insulation materials. https://www.hindawi.com/journals/amse/2014/809595/.

CIBSE, Natural ventilation in non-domestic buildings. Applications Manual AM10:2005, London, CIBSE,

2005.

Charde, M. S. (2013). Experimental study of designed passive elements for energy efficiency in buildings in composite climate.

Choi, N. W., Mori, I., & Ohama, Y. (2006). Development of rice husks–plastics composites for building materials. Waste Management, 26(2), 189-194.

Chow, P. (1974). Dry formed composite board-formed selected agricultural residues, in world insulation on wood-based panels. Food and Agricultural Organisation of the United Nations: New Delhi, India., Chow, P. (1974). Dry formed composite board-formed selected agricultural residues, in world insulation on wood base 24(1) 41-44.

Comakli, K., Yuksel, B., (2004). Environmental impact of thermal insulation thickness in buildings.

Applied Thermal Engineering 24, 933–940.

Daouas, N., Hassen, Z., Aissia, H. B., 2010. Analytical periodic solution for the study of thermal performance and the optimum insulation thickness of building walls in Tunisia, Applied Thermal Engineering 30, 319–326.

Dubois, S., & Lebeau, F. (2015). Design, construction, and validation of a guarded hot plate apparatus

for thermal conductivity measurement of high thickness crop-based specimens. Materials and Structures, 48(1-2), 407-421.

Demirbas, M. F. (2006). Thermal energy storage and phase change materials: an overview. Energy

Sources, Part B: Economics, Planning, and Policy, 1(1), 85-95.

Dombayci, O. A., (2007). The environmental impact of optimum insulation thickness for external walls of buildings. Building and Environment 42, 3855–3859.

Domingue, E. C., Cline, E. K., Cline, J. G., & Villar Martin, M. A. (2012). SUSTAINABLE PAPER INSULATION FOR KAMBASHUS IN INFORMAL SETTLEMENTS OF NAMIBIA.

EEA. (2006). Agricultural waste management. Center on Resources and Waste Management.

https://www.eea.europa.eu/publications/material-resources-and-waste-2014/download

Ekoja, M., Edeoja AO., Nwankwo K. (2016). Thermal characteristics of oil palm fibre treated with cassava starch solution for possible use as insulation material. International Journal of Academic Research and Development ISSN: 2455-4197; Impact Factor: RJIF 5.22. www.newresearchjournal.com/academic Volume 1; Issue 4; April 2016; Page No. 20-23.

Elias-Ozkan, S. T., Summers, F., Surmeli, N., & Yannas, S. (2006, September). A comparative study of the thermal performance of building materials. In PLEA2006 Conference (pp. 6-8).

Els Sweeney-B. (2011). Housing Policy and Delivery in Namibia. Institute for Public Policy Research. A report Funded by the Netherlands Embassy in Pretoria through the Netherlands Consulate in Windhoek.

Eludoyin, O. M., Adelekan, I. O., Webster, R., & Eludoyin, A. O. (2014). Air temperature, relative humidity, climate regionalization, and thermal comfort of Nigeria. International Journal of Climatology, 34(6), 2000-2018.

Eskin, N., & Turkmen, H. (2008). Analysis of annual heating and cooling energy requirements for office buildings in different climates in Turkey. Journal of Energy and Building.vol 40, 763-773.

Evola, G.; Margani, G.; Marletta, L. (2011). Energy and cost evaluation of thermal bridge correction in the Mediterranean climate. Journal Energy Build. 43, 2385–2393.

Fanger P O (1970), Thermal Comfort, Copenhagen, Danish Technical Press.

Fanger P O, Melikov A K, Hanzawa H and Ring J (1989), Turbulence and draught, ASHRAE Journal, April.

FAO. (2004.). Statics Division. Food and Agriculture Organization of the United Nations.

www.fao.org/statistics/en/

Fraes, R.C., (1994). Environmental uses – flue gas desulfuration. Industrial Minerals and Rocks 6th edition. D.D.Carr., edition. SME, Littleton, CO, pp. 453-457.

Gdhaidh, F.A.S. (2019). Heat Transfer Characteristics of Natural Convection within an Enclosure Using

Liquid Cooling System. Retrieved from Ph.D. The Thesis University of Bradford.

Givoni,   B.   (1994).  Passive  and   low   energy  cooling  of   buildings.   New  York:   Van   Nostrand Reinhold.www.worldcat.org/title/passive-and-low-energy-cooling-of- buildings/oclc/30319234?.

Gupta, J. (2010). Refrigeration and Air Conditioning. (Revised, Edition) New Delhi, India.

Guildford J P (1954), Psychometric Methods, 2nd edition, New York, McGraw-Hill. Hoffmann, J. (2006). Greening the Namibian Desert: African Success Story.

Holman, J.P. (1997). Heat transfer handbook. Eight editions, International Edition: McGraw-Hill.

http://solargis.info/doc/_pics/freemaps/1000px/ghi/SolarGIS-Solar-map-Namibia-en.png

Hjermann, T. (2017). CFD simulation of active displacement ventilation (Master's thesis, NTNU). Irace, P., & Brandon, H. (2017). Solar Heating in Commercial Buildings.

Jelle, B. P. (2011). Traditional, state-of-the-art, and future thermal building insulation materials and solutions–Properties, requirements, and possibilities. Energy and Buildings, 43(10), 2549-

2563.

Judkoff,  R.  (2008).  Increasing  building  energy  efficiency  through  advances  in  materials. MRS Bulletin, 33(4), 449-454.

Kamara, V.S. (2018). Research Focus: Namibia University of Science and Technology Research day.

fe.nust.na/.../NUST%20FoE%20Research%20Day%202018%20-%20Dr%20Victor%2.

Katale, D.P. Kamara, V.S. Adedeji, A.A. (2014). Investigation on the use of Clay soil mixed with Cow dung to produce Sustainable Bricks. The trend in Applied Science Research 9 (8): 406- 424, ISSN. Academic Journals Inc.

Kaynakli, O., (2008). A study on residential heating energy requirement and optimum insulation thickness, Renewable Energy 33, 1164–1172.

Kaynakli, O., (2012). A review of the economical and optimum thermal insulation thickness for building applications, Renewable and Sustainable Energy Reviews 16, 415– 425.

Kayne, A. (2012). Computational Fluid Dynamics (CFD) Modelling of Mixed Convection Flows in Building

Enclosures. Retrieved from MSc Thesis of Washington University in St. Louis.

Kgabi, N. A., Uugwanga, M., & Ithindi, J. (2016). Atmospheric Conditions and Precipitation in Arid

Environments: A Case of Namibia. International Journal, 6(1), 148-159.

Khedari, J., Nankongnab, N., Hirunlabh, J., & Teekasap, S. (2004). New low-cost insulation particleboards   from   a   mixture   of   durian   peel   and   coconut   coir. Building   and Environment, 39(1), 59-65.

Khomenko, A.I. (1974). Elektrotekhnicheskii Spravochnik, fifth edition. 1, Moscow.

Kyauta, E. E., Dauda, D. M., & Justin, E. (2014). Investigation on thermal properties of a composite of rice  husk,  corncob,  and  bagasse  for  building  thermal  insulation. American Journal  of Engineering Research (AJER), 3(12), 34-40.

Laser Comp FOX 304 (2006). Heat flow meter thermal conductivity instrument. Information Sheet, Laser Comp, Wakefield, MA, USA.

Li, H., Yu, Y., Niu, F., Shafik, M., & Chen, B. (2014). Performance of a coupled cooling system with earth- to-air heat exchanger and a solar chimney. Renewable Energy, 62, 468-477.

Liang, H., & Ho, M. (2007). Toxicity characteristics of commercially manufactured insulation materials for building applications in Taiwan. Journal of Construction Building Materials,21., 1254-

1261.

Liddament M, A guide to Energy Efficient Ventilation. Coventry, AIVC, 1996.

Lin, Z. Deng, S. (2008). A study on the thermal comfort in sleeping environments in the subtropics— developing a thermal comfort model for sleeping environments, Build. Environ. 43:70–81. doi:10.1016/J. BUILDENV.2006.11.026.

Lorenzati, A.; Fantucci, S.; Capozzoli, A.; Perino, M. (2016). Experimental and numerical investigation

of thermal bridging effects of joint Vacuum Insulation Panels. Energy Build. 111, 164–175. Luamkanchanaphan, T., Chotikaprakhan, S., & Jarusombati, S. (2012). A study of physical, mechanical, and thermal properties for thermal insulation from narrow-leaved cattail fibers. APCBEE

Procedia, 1, 46-52.

Maerefat, M. Haghighi, A.P. (2010).  “Passive cooling of buildings by using integrated earth to an air

heat exchanger and solar chimney”, Renewable Energy, Volume 35, Issue 10, October

2010, Pages 2316-2324, ISSN 0960-1481, URL:http://www.sciencedirect.com/science/article/pii/S0960148110001059

Meatco,(2017). The importance of Agriculture in Namibia. https://www.meatco.com.na › news

Mostafa, E., Lee, I. B., Song, S. H., Kwon, K. S., Seo, I. H., Hong, S. W., ... & Han, H. T. (2012).

Computational fluid dynamics simulation of air temperature distribution inside broiler building fitted with a duct ventilation system. Biosystems Engineering, 112(4), 293-303.

Mahamat, A. D., Khayal, M. Y., Thiam M., Abdelakh, A. O. Menguy, G. & Gaye, S. (2008, June). Thermo- physical characterization of clay Bricks mixed with Agricultural waste: case millet's pod. . International Journal of Emerging Technology and Advance Engineering., 225-232.

Mahlia, T. M. I., & Iqbal, A. (2010). Cost benefits analysis and emission reductions of optimum thickness and air gaps for selected insulation materials for building walls in the Maldives. Energy, 35(5),

2242-2250.

Manohar, K., Yarbrough, D.W. (2003). A comparison of Biodegradable Fibre Insulation with Conventional Fibrous Insulation, Proceedings of the International Conference on Thermal Insulation, Volume 18, January 13–15, White Sulphur Springs, West Virginia, The U.S.A., Product Safety Corporation, 133-140.

Markatos, N.C. Pericleous, K.A. (1984) Laminar and Turbulent Natural- Convection in an Enclosed

Cavity. International Journal of Heat and Mass Transfer, 1984. 27(5): p. 755-772.

Martin, K., Erkoreka, A., Flores, I., Odriozola, M., & Sala, J. M. (2011). Problems in the calculation of thermal bridges in dynamic conditions. Energy and Buildings, 43(2-3), 529-535

.

METEOTEST: Meteonorm Software Version 7.0. URL:http://www.meteonorm.com.

Mgbemene, C., Rosenkranz, A., Pichelin, F., Lehmann, M., Job, C., Kimeng, H., ... & Nduka, O. (2014).

Feasibility study on the production of particleboard from maize cobs, rice husks, and groundnut shells using acacia mimosa tannin extract as the bonding adhesive. Journal of Architectural Engineering, 20(1), 04013006.

Miller, W., Buys, L., & Bell, J. (2012). Performance evaluation of eight contemporary passive solar homes in subtropical Australia. Building and Environment, 56, 57-68.

Millogo, Y., Morel, J. C., Aubert, J. E., & Ghavami, K. (2014). Experimental analysis of Pressed Adobe

Blocks reinforced with Hibiscus cannabinus fibers. Construction and Building Materials, 52,

71-78.

Misra, A., Gupta, R., & Gupta, R. C. (2008). Utilization of marble slurry in construction materials.

In Workshop on gainful utilization of Marble Slurry and other stone waste. Murtorwa, J. (2015). Kalimbeza rice goes commercial. New Era Bulletin.

NAB. (2008). Cropnprospect and food security. Namibian Agronomic Board Situation Report Statistics.

husks-plastics composites for building materials. Waste Management 26(2):189-94.DOI:

Nina, M. (2006). Energy efficiency in building. National Renewable Workshop, Harmony Centre, 1-7

Windhoek.

Olesen B W, Sliwinska E, Madsen T L, and Fanger P O (1982), Effects of body posture and activity on the thermal insulation of clothing: measurements by a movable thermal manikin, ASHRAE Transactions, 88(2), 791–805.

Onjefu, LA., Kamara, VS., Chisale, P., Kgabi, NA., Zulu, A. (2019). Thermal Efficient Isolating Materials from Agricultural Residues to Improve Energy Efficiency in Buildings. International Journal of Civil Engineering and Technology (IJCIET) Volume 10, Issue 02, February 2019, pp. 2067–

2074, Article ID: IJCIET_10_02_206

Ozel, M., & Pihtili, K. (2007). Investigation of the most suitable location of insulation applying on building roof from maximum load levelling point of view. building and environment, 42(6),

2360-2368.

Panyakaew, S., & Fotios, S. (2008, October). 321: agricultural waste materials as thermal insulation for dwellings in Thailand: preliminary results. In 25 Conference on Passive and Low Energy Architecture, Dublin.

Panyakaew, S., & Fotios, S. (2011). New thermal insulation boards are made from coconut husk and bagasse. Energy and Buildings, 43(7), 1732-1739.

Papadopoulos, A. M., Giama, E., (2007). Environmental performance evaluation of thermal insulation materials and their impact on the building, Building Environment 42, 2178–2187.

Patnaik, A., Mvubu, M., Muniyasamy, S., Botha, A., & Anandjiwala, R. D. (2015). Thermal and sound insulation materials from waste wool and recycled polyester fibers and their

biodegradation studies. Energy and Buildings, 92, 161-169.

Pilkington, (2010). NSG Group Flat Glass Business, Pilkington Glass Handbook 2010, 200 pages.

Pincomb, A.C., Shapiro, A.R., (1994). Environmental uses – Neutralization.

Industrial Minerals and Rocks 6th ed., D.D.Carr., ed. SME, Littleton, CO, pp. 459-463.

Pinho, F. T. (2001). The Finite-volume Method Applied to Computational Rheology: II-Fundamentals for Stress-explicit Fluids. University of Porto, 1, 63-100.

Piva, A. M., Steudner, S. H., & Wiebeck, H. (2004). physicomechanical properties of rice husk powder filled polypropylene composites with coupling agent study. In Proceedings of the Fifth International Symposium on Natural Polymer and Composites.

Polytechnic of Namibia. (2011). Energy and Environment Partnership Programme With Southern and

Eastern Africa. Windhoek, Namibia.

www.nust.na/sites/default/files/documents/Annual-Report-2011.pdf

Punturo, R., Ricchiuti, C., Rizzo, M., & Marrocchino, E. (2019). Mineralogical and Microstructural Features of Namibia Marbles: Insights about Tremolite Related to Natural Asbestos Occurrences. Fibers, 7(4), 31.

Radhi, H. (2009). Evaluating the potential impact of global warming on the UAE residential buildings–

A contribution to reducing CO2 emissions. Building and Environment, 44(12), 2451-2462.

Ranum, P., Peña‐Rosas, J. P., & Garcia‐Casal, M. N. (2014). Global maize production, utilization, and

consumption. Annals of the New York Academy of Sciences, 1312(1), 105-112.

Rowell, R. M., & Rowell, J. (1996). Paper and composites from agro-based resources. CRC press.

REEEI, (2013). Revision of National Building Codes to Incorporate Renewable Energy Technologies and

Energy Efficiency Principles. A Background Review Building Code.

Rodríguez, N. J., Yáñez-Limón, M., Gutiérrez-Miceli, F. A., Gomez-Guzman, O., Matadamas-Ortiz, T. P., Lagunez-Rivera, L., & Feijoo, J. V. (2011). Assessment of coconut fibre insulation characteristics and its use to modulate temperatures in concrete slabs with the aid of a finite element methodology. Energy and Buildings, 43(6), 1264-1272.

Rosenlund, H. (2000). Climatic Design of Buildings using Passive Techniques, Building Issues 2000, Volume 10, Number 1, URL:http://www.heatinghelp.com/files/articles/721/29.pdf.

Sanoussi, N. S. (2012, November). Numerical analysis to identify the quantity of heat flow through the building  floor  with  outer  horizontal  edge  insulation.  In 2012  International  Conference  on Renewable Energies for Developing Countries (REDEC) (pp. 1-8). IEEE.

Scatolino, M.V.,  Silva, D.W.,  Mendes, R.F., Mendes, L.M. (2015), Use of maize cob for production of particleboard, Retrieved from doi: 10.1590/S1413- 70542013000400006.

Schneiderat, (2011). Communal rangelands in northern and central Namibia: The grazing and browsing resources and their users. Retrieved from Master’s Thesis Justus-Liebig Universitat Giessen.

Schultz, R., Heita, M., and Schumann, C. (2006). Strategic Action plan for the implementation of renewable energy policies as outlined in the Namibia white paper on energy policy. A report was released as part of the Barrier Removal to Namibian Energy Programme. Pgs

81.

Sekaluvu, L., Tumutegyereize, P., & Kiggundu, N. (2014). Investigation of factors affecting the production and properties of maize cob-particleboards. Waste and biomass valorization, 5(1), 27-32.

Singh, T. (2010) Corn Waste Transformed Into Versatile Building Material, Retrieved January 30, 2015, from <http://inhabitat.com/corn-waste-transformed-intoversatile- building-aterial/>, 2010.

Shati, A. (2013). The Interaction between Radiation and Turbulent natural convection in Square Rectangular Enclosures. Retrieved from Ph.D. thesis from the Department of Mechanical Engineering. The University of Sheffield Mappin Street, Sheffield, S1 3JD United Kingdom.

Shifiona, T. K., Dongyang, W., & Zhiguan, H. (2016). Analysis of Namibian Main Grain Crops Annual Production,   Consumption   and   Trade—Maize   and   Pearl   Millet. Journal   of   Agricultural Science, 8(3), 70-77.

Sodha, M. S., Singh, U., Kumar, A., & Tiwari, G. N. (1981). Effect of using a reflecting sheet in an air gap on the thermal performance of hollow walls and roofs. Applied Energy, 8(1), 67-78.

Solar Space Heating and Cooling." Goldkamp Heating & Cooling. U.S. Depart of Energy, n.d. Web. 05

June	2017.	<http://www.goldkamphvac.com/webapp/p/338/solar-space-heating-and- cooling>.

Spiga, M. Vocale, P. (2014). Effect of floor geometry on building heat loss via the ground, Heat Transfer.

Eng. 35:1520–1527. doi:10.1080/01457632.2014.897560.

Srigiriraju,  C.  S.  (2015). Numerical  modelling  of  forced  convection  in  a  cavity  due  to  finite  heat sources (Doctoral dissertation, Rutgers University-Graduate School-New Brunswick).

Stoecker, W., & Jonas, J. (2010). Refrigeration and Air Conditioning (2nd ed.). New York: McGraw-Hill

Inc.

Sun.Y., & Xiao, H. (2014). Use of energy-efficient materials and sustainable design strategy for large sport architectural in Beijing. 30th International PLEA Conference 16th-18th December, CEPT University, Ahmedabad.

Swenka, M. J. (2008). An energy and cost analysis of residential ground-source heat pumps in Iowa.

Obam, S. O. (2012). Properties of saw-dust, paper, and starch composite ceiling board. Am. J. Sci. Ind.

Res, 3(5), 300-304.

Tangjuank, S. (2011). Thermal insulation and physical properties of particleboards from pineapple leaves. . International Journal of Physical Sciences, 6(19), 4528-4532.

Teles, D. S. S. (2016). Energy performance for a residential building: comparison between seasonal method (national) and monthly method (PHPP) (Master's thesis).

Trenberth, K.E. (2011). Changes in Precipitation with Climate change, contribution to CR Special 25

‘Climate Services for Sustainable Development’, Climate Research, 47, 123- 138.

Ucar, A., Balo, F.,(2009). Effect of fuel type on the optimum thickness of selected insulation materials for the four different climatic regions of Turkey, Applied Energy 86, 730–736.

Ucar, A., Balo, F., (2010). Determination of the energy savings and the optimum insulation thickness in the four different insulated exterior walls, Renewable Energy 35, 88–94.

Van Hooff, T., and Blocken, B. (2010). Coupled urban wind flow and indoor natural ventilation modelling on a high-resolution grid: A case study for the Amsterdam Arena stadium. Environmental Modelling & Software 25(1): 51-65.

Vilela, M.O., Gates, R.S, Martins, M.A, Barbari, M., Conti, L. Rossi, G. Zolnier, S., Teles Jr. C.G.S. Zanetoni, H.H.R. Andrade, R.R. Tinôco, I.F.F. (2019). Computational fluids dynamics (CFD) in the spatial distribution of air velocity in a prototype designed for animal experimentation in controlled environments. Agronomy Research 17(3) 890-899.

Varkie, C. T. (2013). Energy Model: Instruction and Discussion for Energy Modelers. Retrieved 12 28,

2017,	from	Energy	Model.Com:	http://energy-models.com/energy-usage-analysis- buildings

Veloo, P. S., & Quintiere, J. G. (2013). Convective heat transfer coefficient in compartment fires. Journal of fire sciences, 31(5), 410-423.

Venkatesan, A. Anand, G. George Fernandez, A. Thillai Natarajan, V. Alex, A. (2015). Compressive strength and Water absorption test on Bricks made of Wood ash, Charcoal with Clay Bricks: A comparative study. The International Journal of Science & Technology (ISSN 2321 – 919X). Volume 3. www.theijst.com.

United States Department of State, (2016). U.S. Relations with Namibia. Retrieved, from Bureau of

African Affairs.

Wan, D.C. Patnak, B.S.V. Wei, G.W. (2001). A new Benchmark Quality Solution for the Buoyancy- driven

Cavity by Discrete Singular Convolution. Numerical Heat Transfer, part B,40: 199- 228.

Wang, D., & Sun, X. S. (2002). Low-density particleboard from wheat straw and corn pith. Industrial crops and products, 15(1), 43-50.

Wienecke,  M., &  Mawisa, M. (2008). Guidelines for Building in Energy Efficient Manner. Windhoek, Namibia:	Renewable	Energy	and	Energy	Efficiency	Institute. https://www.researchgate.net/.../224830397_Renewable_Energy_for_Rural_Developmen t.

Weidlich,  Brigitte (2010). "Land  ministry tests new farm acquisition  model".  Retrieved from the

Namibian.

Yarbrough, D. W., Wilkes, K. E., Olivier, P. A., Graves, R. S., & Vohra, A. (2005). Apparent thermal conductivity data and related information for rice hulls and crushed pecan shells. Thermal Conductivity, 27, 222-230.

Yu, J., Yang, C., Tian, L., & Liao, D. (2009). A study on optimum insulation thicknesses of external walls in hot summer and cold winter zone of China. applied energy, 86(11), 2520-2529.

Zalaudek. (2013). Passive Energy Concept, Energy Performance & Measurement.  E E B N – ENERGY EFFICIENT BUILDING IN NAMIBIA. Retrieved from Master’s Thesis: Carinthia University of Applied Sciences Fachhochschule Kärnten.

Zhai, Z. J., and Chen, Q. Y. (2006). Sensitivity analysis and application guides for integrated building energy and CFD simulation. Energy and Buildings 38(9): 1060-1068.

Zhou, X. Y., Zheng, F., Li, H. G., & Lu, C. L. (2010). An environment-friendly thermal insulation material from cotton stalk fibers. Energy and Buildings, 42(7), 1070-1074.

Zulkifli, R., Nor, M. M., Ismail, A. R., Nuawi, M. Z., Abdullah, S., Tahir, M. M., & Rahman, M. A. (2009).

Comparison of acoustic properties between coir fibre and oil palm fibre. European Journal of Scientific Research, 33(1), 144-152.

List of publications

The following are peered reviewed articles published from this research. Reports of editors for each of the said publications are also shown. More publications are also expected from this research.

1.	Onjefu, LA., Kamara, VS., Chisale, P., Kgabi, NA., Zulu A. (2019): Thermal Efficient Isolating Materials from Agricultural Residues to Improve Energy Efficiency in Buildings. International Journal of Civil Engineering and Technology (IJCIET) Volume 10, Issue 02, February 2019, pp. 2067–2074, Article ID: IJCIET_10_02_206.

2.	Onjefu, LA., Kamara, VS., Chisale (2019): In-Situ Performance Measurements in Buildings

Made from Agricultural Waste Materials. International Journal of Civil Engineering and

Technology 10(6), 2019, pp. 615-626. http://www.iaeme.com/IJCIET/issues.asp?

3.	Kamara, VS., Onjefu, LA., Chisale (2019): Thermal, water absorption, and compressive behaviour of energy-efficient bricks from agricultural residues in Namibia. International Journal of Civil Engineering and Technology (IJCIET) Volume 10, Issue 09, September

2019, pp. 90-101, Article ID: IJCIET_10_09_010 http://www.iaeme.com/ijciet/issues.asp?JType=IJCIET&VType=10&IType=9 ISSN Print:

0976-6308 and ISSN Online: 0976-6316 © IAEME Publication

APPENDICES

A.1 Acceptance and editors report from publications

INTERNATIONAL .JOURNAL OF CIVIL ENGINEERING AND TECHNOLOGY (I.JCIET)

www.iaeme.com/ijciet/index.asp SCOPUS INDEXED JOURNAL http://iaeme.com/IJCIET Scopus.asp

.Journal Impact Factor (2016):9.7820 Calculated by CISI (www.jifactor.com)

ISSX Print:0976 - 6308	ISS:"Online: 0976 - 6316

Official Acceptance of Research Paper

Paper ID: UCIET/10102/2019/IJCIET_41879	Date: 13-Feb-2019

Dear Onjefu, LA., Kamara, VS., Chisale, P., Kgabi, NA  and Zulu, A

We would like to inform you that your paper titled "Thermal  Efficient Isolating  Nlaterials from Agricultural Residues to Improve Energy Efficiency in Buildings'"' has been accepted for publication in International  Journal  of Civil Engineering  and Technology (IJCIEl), Volume 10, Issue 02, (February 2019) issue of the journal based on  the  Recommendation of the Editorial Board without any major corrections in  the content submitted by the researcher.

This letter is the official confirmation of acceptance of your research paper.

Your research work is licensed under a Creative Commons Attribution 4.0 (International) License.(CC BY-NC 4.0). Hen ce no n eed to submit the Copy right form.

Your research paper will be appearing in UCIET, Volwne 10, Issue 02, February 2019. International.Journal of Civil Engineering and Technology (I.JCIET)

.Journal Impact Factor (2016):9.7820 Calc ulated by GISI

ISSN Print:0976 - 6308

http://iaeme.com/IJCIET  Scopus.asp

.Jour nal Im pact  Factor (2016): 9.7820 Calculated by G ISI (www.jifactor.com)

ISSN  Print: 0976 - 6308 	ISSN Online: 0976 - 6316

Review  Report

Date:	13-February-2019

Title:	Thermal Efficient Isolating Materials  from Agricultural Residues to Improve

Energy Efficiency in Buildings

Authors: 	Onjefu, LA., Kamara, VS.., Chisale, P., Kgabi, NA and  Zulu, A

|  | Evaluation | Poor | Fair | Good | Very Good | Outstanding |
| --- | --- | --- | --- | --- | --- | --- |
|  | 0riginality |  |  |  |  | ..J |
|  | Innovation |  |  |  | ..J |  |
|  | Teclmical merit |  |  |  |  | ..J |
|  | Applicability |  |  |  |  | ..J |
|  | Presentation and English |  |  |  |  | ..J |
|  | Match to Journal Topic |  |  |  |  | ..J |
|  | Recomm endation to Chief Editors |  |  |  |  |  |
|  |  | Strongly Reject | Reject | Marginally Accept | Accept | Strongly Acc.ept |
|  | Recomm endation |  |  |  |  | ..J |
|  | Review Comments:In tlus study clearly showed that with appropriate mixed design and techniques, such agricultural residues can be used to develop engineered insulating materials that contribute to thermal efficiency, increased human comfort w itl10ut the use of conventional heating and cooling devices like air conditioning system, and low risk of environmental poUution. Thermal conductivity and thermal resistivity values were developed. Analytical study. Paper Accepted For Publication In IJCIET. |  |  |  |  |  |

INTERNATIONAL .JOURNAL OF CIVIL ENGINEERING AND TECHNOLOGY (I.JCIET)

www.iaeme.com/i jciet/index.asp

Journal I mpact Factor (2019): 10.7810 Calculated by CISI (www.jifactor.com)

ISSN P•·int: 0976 - 6308                                                                      ISSN Online: 0976 - 6316

Official Acceptance of Research Paper

Paper ID: UCIET!l0105120 19/UCIET_43797                                        Date:05-June-20 19

Dear On jef u, LA, Ka mara, VS and Chisale, P

We    would   like    to   inform  you    that    your    paper  titled     "IN-SIT U    PERFORMANCE MEASUREMENTS   IN     BUI LDINGS   MADE   FROM   AGRICULTURAL   WASTE MATERIALS"   has    been    accepted  for  publication    in  Internatio nal   Journal  of   Civil Engineering and  Technology (IJCIET), Volume I0, Issue 05, (May 2019) issue of the journal based on   the  Recommendation of  the  Editorial  Board  without any   major corrections in  the content submitted by the researcher.

This letter is the official confirmation of acceptance of your research paper.

Your resea rch work Llicensed under a C reative Commons Attribution 4.0 (I nternation al) License. (CC BY-NC 4.0). Hence n o need to submit th e Copy rigbt form.

Your research paper will be appearing in UCIET, Volume 10, Issue 05, May  2019. Intern ational .Jo urnal of Civil Engin eering and Technology (IJCIET)

Journal Impact Factor (2019):10.7810 Calculated by GISI

ISSN Print: 0976 - 6308

ISSN Online:0976 - 6316

.Journal Impact  Factor  (2019): 10.7810  Calculated  by GISI (www.jifactor.com)

ISSN Print: 0976 - 6308	ISSN Online: 0976 - 6316

Review Report

Date: 	05-.June-2019

Title:	IN-SITU  PERFORMANCE  M.EASUREMENTS IN  B UI LDINGS MADE  FROM AG RICULTURAL WASTE MATERIALS

Authors: 	On jefu, LA, Kamara,VS and Chisale, P

| Evaluation | Poor | Fair | Good | Very Good | Outstandin |
| --- | --- | --- | --- | --- | --- |
| Originality |  |  |  |  | ..j |
| I nnovation |  |  |  | ..j |  |
| Technical merit |  |  |  |  | ..j |
| Applicability |  |  |  |  | ..j |
| Presentation and English |  |  |  |  | ..j |
| M atch to .Journal Topic |  |  |  |  | ..j |
| Recommendation to Chief Editors |  |  |  |  |  |
|  | Strongly Reject | Reject | Marginally Accept | Accept | Strongly Accept |
| Recommendation |  |  |  |  | ..j |
| Review Comments: The st ud y aimed at comparing them1al efficiency of residential bui ldings varying designs using material from Agricultural residues and marble dust in Namibia. The indc temperature and humidity of rigs made from agricultural resid ues (with and without marble dust a insulation) and com pare that with outside temperat ure d uring swnmer and winter in Namibia, showe< correlation of sustainable green buildings. Using locally available agricultural wastes/resid ues c therefore address emerging social, economic and environmental challenges linked to climate chan Ex perimental and Analytical studl:. Pa er Acceted For Pu blication In UCI ET. |  |  |  |  |  |

INTERNATIONAL .JOURNAL OF CIVIL ENGINEERDJG AND TECHNOLOGY (I.JCIET)

www.iaeme.com/ijciet/index.asp

Journal Impact Factor (2019):10.7810 Calculated by G ISI (www.jifactor.com )

ISSN Print: 0976 - 6308                                                                  ISSN Online: 0976 - 6316

Official Acceptance of  Research Paper

Paper ID: UCIET/ 10/08/2019/UCIET_75089                                       Date: 08-August-2019

Dear Kamara, VS, Onjef u , LA and Chisale, P

We would like to inform you that your paper titled "THERMAL, \.VATER ABSORPTION AND COMPRESSIVE    BE HAVIOUR   OF    ENERGY    E FFICI ENT    BRICKS    FROM AGRICULTURAL  RESID UES  IN  NA!\1IBIA"   has  been  accepted  for  publication  in International Journal of  Civil Engineering and Tech n ology (IJCIEn, Volume 10, Issue 08, (August 2019) issue of the journal based on the Recommendation of the Editorial Board without any major corrections in  the content submitted by  the researcher.

This letter is the official confirmation of acceptance of your research paper.

You r research work is licensed un der a Creative Commons Attribution 4.0 (International) License.(CC BY-NC 4.0). Hence no need to su bmit the Copyright form.

Your research paper will be appearing in UCIET, Volume 10, Issue 08, August 2019. International .Journal of  Civil En gineerin g and Technology (IJCIET)

Journal Impact Factor (2019): 10.7810 Calculated by GISI

ISSN Print: 0976 - 6308

ISSN Online: 0976- 6316

A1.1 Thermal conductivity raw data for sample A

t/[min] lambda/[mW/(m*K)]

1	106.800003051758

2	107.019996643066

3	106.949996948242

4	107.180000305176

5	107.459999084473

6	107.959999084473

7	108.559997558594

8	109.150001525879

9	109.589996337891

10	109.559997558594

11	109.319999694824

12	109.23999786377

13	109

14	108.860000610352

15	108.650001525879

16	108.389999389648

17	108.25

18	108.050003051758

19	107.699996948242

20	107.23999786377

| 21 | 106.919998168945 |
| --- | --- |
| 22 | 106.470001220703 |
| 23 | 106.230003356934 |
| 24 | 105.870002746582 |
| 25 | 105.660003662109 |
| 26 | 105.620002746582 |
| 27 | 105.309997558594 |
| 28 | 104.940002441406 |
| 29 | 104.5 |
| 30 | 104.349998474121 |
| 31 | 104.230003356934 |
| 32 | 104.230003356934 |
| 33 | 104.400001525879 |
| 34 | 104.569999694824 |
| 35 | 104.769996643066 |
| 36 | 104.959999084473 |
| 37 | 105.129997253418 |
| 38 | 105.459999084473 |
| 39 | 105.809997558594 |
| 40 | 106.029998779297 |
| 41 | 106.23999786377 |
| 42 | 106.360000610352 |

| 43 | 106.230003356934 |
| --- | --- |
| 44 | 106.160003662109 |
| 45 | 105.959999084473 |
| 46 | 105.800003051758 |
| 47 | 105.769996643066 |
| 48 | 105.75 |
| 49 | 105.709999084473 |
| 50 | 105.559997558594 |
| 51 | 105.389999389648 |
| 52 | 105.169998168945 |
| 53 | 104.800003051758 |
| 54 | 104.519996643066 |
| 55 | 104.220001220703 |
| 56 | 103.779998779297 |
| 57 | 103.089996337891 |
| 58 | 103.120002746582 |
| 59 | 103.169998168945 |
| 60 | 103.190002441406 |
| 61 | 103.230003356934 |
| 62 | 103.26000213623 |
| 63 | 103.330001831055 |
| 64 | 103.410003662109 |

| 65 | 103.5 |
| --- | --- |
| 66 | 103.599998474121 |
| 67 | 103.720001220703 |
| 68 | 103.849998474121 |
| 69 | 104 |
| 70 | 104.120002746582 |
| 71 | 104.26000213623 |
| 72 | 104.400001525879 |
| 73 | 104.529998779297 |
| 74 | 104.629997253418 |
| 75 | 104.709999084473 |
| 76 | 104.730003356934 |
| 77 | 104.75 |
| 78 | 104.76000213623 |
| 79 | 104.75 |
| 80 | 104.690002441406 |
| 81 | 104.610000610352 |
| 82 | 104.529998779297 |
| 83 | 104.410003662109 |
| 84 | 104.309997558594 |
| 85 | 104.199996948242 |
| 86 | 104.110000610352 |

| 87 | 104.040000915527 |
| --- | --- |
| 88 | 103.970001220703 |
| 89 | 103.919998168945 |
| 90 | 103.900001525879 |
| 91 | 103.889999389648 |
| 92 | 103.900001525879 |
| 93 | 103.930000305176 |
| 94 | 104 |
| 95 | 104.069999694824 |
| 96 | 104.139999389648 |
| 97 | 104.209999084473 |
| 98 | 104.26000213623 |
| 99 | 104.279998779297 |
| 100 | 104.300003051758 |
| 101 | 104.290000915527 |
| 102 | 104.290000915527 |
| 103 | 104.279998779297 |
| 104 | 104.26000213623 |
| 105 | 104.220001220703 |
| 106 | 104.169998168945 |
| 107 | 104.080001831055 |
| 108 | 103.980003356934 |

| 109 | 103.879997253418 |
| --- | --- |
| 110 | 103.779998779297 |
| 111 | 103.709999084473 |
| 112 | 103.720001220703 |
| 113 | 104.529998779297 |
| 114 | 104.459999084473 |
| 115 | 104.23999786377 |
| 116 | 104.160003662109 |
| 117 | 104.110000610352 |
| 118 | 104.120002746582 |
| 119 | 104.080001831055 |
| 120 | 103.98999786377 |
| 121 | 103.980003356934 |
| 122 | 104.050003051758 |
| 123 | 103.959999084473 |
| 124 | 103.849998474121 |
| 125 | 103.650001525879 |
| 126 | 103.480003356934 |
| 127 | 103.379997253418 |
| 128 | 103.370002746582 |
| 129 | 103.180000305176 |
| 130 | 103.150001525879 |

| 131 | 103.139999389648 |
| --- | --- |
| 132 | 103.129997253418 |
| 133 | 103.069999694824 |
| 134 | 103.01000213623 |
| 135 | 102.930000305176 |
| 136 | 102.860000610352 |
| 137 | 102.790000915527 |
| 138 | 102.730003356934 |
| 139 | 102.669998168945 |
| 140 | 102.629997253418 |
| 141 | 102.589996337891 |
| 142 | 102.589996337891 |
| 143 | 102.620002746582 |
| 144 | 102.680000305176 |
| 145 | 102.769996643066 |
| 146 | 102.879997253418 |
| 147 | 102.949996948242 |
| 148 | 103.069999694824 |
| 149 | 103.190002441406 |
| 150 | 103.319999694824 |
| 151 | 103.430000305176 |
| 152 | 103.51000213623 |

| 153 | 103.620002746582 |
| --- | --- |
| 154 | 103.660003662109 |
| 155 | 103.669998168945 |
| 156 | 103.669998168945 |
| 157 | 103.680000305176 |
| 158 | 103.650001525879 |
| 159 | 103.589996337891 |
| 160 | 103.480003356934 |
| 161 | 103.379997253418 |
| 162 | 103.25 |
| 163 | 103.139999389648 |
| 164 | 103.01000213623 |
| 165 | 102.889999389648 |
| 166 | 102.779998779297 |
| 167 | 102.669998168945 |
| 168 | 102.599998474121 |
| 169 | 102.529998779297 |
| 170 | 102.5 |
| 171 | 102.5 |
| 172 | 102.51000213623 |
| 173 | 102.519996643066 |
| 174 | 102.589996337891 |

| 175 | 102.660003662109 |
| --- | --- |
| 176 | 102.720001220703 |
| 177 | 102.790000915527 |
| 178 | 102.830001831055 |
| 179 | 102.870002746582 |
| 180 | 102.919998168945 |
| 181 | 102.930000305176 |
| 182 | 102.930000305176 |
| 183 | 102.940002441406 |
| 184 | 102.930000305176 |
| 185 | 102.889999389648 |
| 186 | 102.849998474121 |
| 187 | 102.769996643066 |
| 188 | 102.730003356934 |
| 189 | 102.720001220703 |
| 190 | 102.730003356934 |
| 191 | 102.919998168945 |
| 192 | 103.25 |
| 193 | 103.309997558594 |
| 194 | 103.410003662109 |
| 195 | 103.540000915527 |
| 196 | 103.639999389648 |

| 197 | 103.680000305176 |
| --- | --- |
| 198 | 103.779998779297 |
| 199 | 103.809997558594 |
| 200 | 103.779998779297 |
| 201 | 103.75 |
| 202 | 103.620002746582 |

A1.2. Thermal conductivity raw data for sample C

t/[min] lambda/[mW/(m*K)]

1	17.2099990844727

2	17.7800006866455

3	18.4599990844727

4	19.25

5	20.1299991607666

6	21.1399993896484

7	22.25

8	23.4200000762939

9	24.5499992370605

10	25.5699996948242

11	26.4699993133545

12	27.2999992370605

13	28.0400009155273

14	28.7199993133545

15	29.2999992370605

16	29.7600002288818

17	30.1200008392334

18	30.4599990844727

19	30.7900009155273

20	31.1200008392334

| 21 | 31.5 |
| --- | --- |
| 22 | 31.9400005340576 |
| 23 | 32.3899993896484 |
| 24 | 32.8199996948242 |
| 25 | 33.2400016784668 |
| 26 | 33.689998626709 |
| 27 | 34.1399993896484 |
| 28 | 34.5800018310547 |
| 29 | 35.0200004577637 |
| 30 | 35.3499984741211 |
| 31 | 35.5200004577637 |
| 32 | 35.6100006103516 |
| 33 | 35.6800003051758 |
| 34 | 35.810001373291 |
| 35 | 35.9300003051758 |
| 36 | 36.0499992370605 |
| 37 | 36.1599998474121 |
| 38 | 36.2700004577637 |
| 39 | 36.4199981689453 |
| 40 | 36.6399993896484 |
| 41 | 36.9199981689453 |
| 42 | 37.2200012207031 |

| 43 | 37.5200004577637 |
| --- | --- |
| 44 | 37.8199996948242 |
| 45 | 38.1399993896484 |
| 46 | 38.4500007629395 |
| 47 | 38.7799987792969 |
| 48 | 39.0999984741211 |
| 49 | 39.4199981689453 |
| 50 | 39.7400016784668 |
| 51 | 40.0400009155273 |
| 52 | 40.3300018310547 |
| 53 | 40.5800018310547 |
| 54 | 40.7900009155273 |
| 55 | 40.9900016784668 |
| 56 | 41.1399993896484 |
| 57 | 41.2400016784668 |
| 58 | 41.3300018310547 |
| 59 | 41.3899993896484 |
| 60 | 41.4300003051758 |
| 61 | 41.4799995422363 |
| 62 | 41.5299987792969 |
| 63 | 41.6300010681152 |
| 64 | 41.75 |

| 65 | 41.8800010681152 |
| --- | --- |
| 66 | 42.0800018310547 |
| 67 | 42.3499984741211 |
| 68 | 42.689998626709 |
| 69 | 43.0699996948242 |
| 70 | 43.4199981689453 |
| 71 | 43.7599983215332 |
| 72 | 44.0499992370605 |
| 73 | 44.3199996948242 |
| 74 | 44.5699996948242 |
| 75 | 44.7700004577637 |
| 76 | 44.8699989318848 |
| 77 | 44.9000015258789 |
| 78 | 44.8600006103516 |
| 79 | 44.7900009155273 |
| 80 | 44.7299995422363 |
| 81 | 44.689998626709 |
| 82 | 44.6599998474121 |
| 83 | 44.6199989318848 |
| 84 | 44.5800018310547 |
| 85 | 44.5699996948242 |
| 86 | 44.5499992370605 |

| 87 | 44.560001373291 |
| --- | --- |
| 88 | 44.5999984741211 |
| 89 | 44.6500015258789 |
| 90 | 44.7299995422363 |
| 91 | 44.810001373291 |
| 92 | 44.9000015258789 |
| 93 | 45 |
| 94 | 45.1100006103516 |
| 95 | 45.2000007629395 |
| 96 | 45.2999992370605 |
| 97 | 45.3699989318848 |
| 98 | 45.439998626709 |
| 99 | 45.4799995422363 |
| 100 | 45.5200004577637 |
| 101 | 45.560001373291 |
| 102 | 45.5999984741211 |
| 103 | 45.6399993896484 |
| 104 | 45.7400016784668 |
| 105 | 45.9099998474121 |
| 106 | 46.1399993896484 |
| 107 | 46.4700012207031 |
| 108 | 46.8899993896484 |

| 109 | 47.3499984741211 |
| --- | --- |
| 110 | 47.810001373291 |
| 111 | 48.2299995422363 |
| 112 | 48.5999984741211 |
| 113 | 48.9500007629395 |
| 114 | 49.2400016784668 |
| 115 | 49.439998626709 |
| 116 | 49.5400009155273 |
| 117 | 49.5400009155273 |
| 118 | 49.4300003051758 |
| 119 | 49.2599983215332 |
| 120 | 49.0900001525879 |
| 121 | 48.9300003051758 |
| 122 | 48.7700004577637 |
| 123 | 48.5699996948242 |
| 124 | 48.3199996948242 |
| 125 | 48.0800018310547 |
| 126 | 47.8400001525879 |
| 127 | 47.5200004577637 |
| 128 | 47.310001373291 |
| 129 | 47.1199989318848 |
| 130 | 46.9599990844727 |

| 131 | 46.8600006103516 |
| --- | --- |
| 132 | 46.8300018310547 |
| 133 | 46.8300018310547 |
| 134 | 46.8400001525879 |
| 135 | 46.8600006103516 |
| 136 | 46.8699989318848 |
| 137 | 46.8899993896484 |
| 138 | 46.9199981689453 |
| 139 | 46.9799995422363 |
| 140 | 47.0900001525879 |
| 141 | 47.189998626709 |
| 142 | 47.4199981689453 |
| 143 | 47.7200012207031 |
| 144 | 48.060001373291 |
| 145 | 48.3600006103516 |
| 146 | 48.6199989318848 |
| 147 | 48.8600006103516 |
| 148 | 49.1199989318848 |
| 149 | 49.3699989318848 |
| 150 | 49.5900001525879 |
| 151 | 49.7000007629395 |
| 152 | 49.689998626709 |

| 153 | 49.5699996948242 |
| --- | --- |
| 154 | 49.4300003051758 |
| 155 | 49.3199996948242 |
| 156 | 49.2400016784668 |
| 157 | 49.1199989318848 |
| 158 | 48.9700012207031 |
| 159 | 48.7999992370605 |
| 160 | 48.6300010681152 |
| 161 | 48.4599990844727 |
| 162 | 48.3300018310547 |
| 163 | 48.1800003051758 |
| 164 | 48.0499992370605 |
| 165 | 47.9500007629395 |
| 166 | 47.8699989318848 |
| 167 | 47.8499984741211 |
| 168 | 47.8499984741211 |
| 169 | 47.8400001525879 |
| 170 | 47.8199996948242 |
| 171 | 47.810001373291 |
| 172 | 47.8199996948242 |
| 173 | 47.8499984741211 |
| 174 | 47.9099998474121 |

| 175 | 47.9799995422363 |
| --- | --- |
| 176 | 48.0200004577637 |
| 177 | 48.0800018310547 |
| 178 | 48.1199989318848 |
| 179 | 48.1800003051758 |
| 180 | 48.2400016784668 |
| 181 | 48.3199996948242 |
| 182 | 48.4199981689453 |
| 183 | 48.4599990844727 |
| 184 | 48.4700012207031 |
| 185 | 48.4700012207031 |
| 186 | 48.4900016784668 |
| 187 | 48.5299987792969 |
| 188 | 48.5900001525879 |
| 189 | 48.6300010681152 |
| 190 | 48.6699981689453 |
| 191 | 48.7099990844727 |
| 192 | 48.7299995422363 |
| 193 | 48.7400016784668 |
| 194 | 48.7599983215332 |
| 195 | 48.7700004577637 |
| 196 | 48.7700004577637 |

| 197 | 48.7700004577637 |
| --- | --- |
| 198 | 48.7700004577637 |
| 199 | 48.75 |
| 200 | 48.7200012207031 |
| 201 | 48.6599998474121 |
| 202 | 48.5999984741211 |

A1.3. Thermal conductivity raw data for marble mix at 20 %

t/[min] lambda/[mW/(m*K)]

1	21.8600006103516

2	22.9799995422363

3	24.1200008392334

4	25.3099994659424

5	26.5100002288818

6	27.6399993896484

7	28.6499996185303

8	29.4599990844727

9	30.1399993896484

10	30.7600002288818

11	31.3500003814697

12	31.8999996185303

13	32.4199981689453

14	32.9099998474121

15	33.3800010681152

16	33.810001373291

17	34.2400016784668

18	34.6599998474121

19	35.0699996948242

20	35.4900016784668

| 21 | 35.9099998474121 |
| --- | --- |
| 22 | 36.3400001525879 |
| 23 | 36.7400016784668 |
| 24 | 37.1500015258789 |
| 25 | 37.5800018310547 |
| 26 | 38.0200004577637 |
| 27 | 38.4500007629395 |
| 28 | 38.9000015258789 |
| 29 | 39.3300018310547 |
| 30 | 39.7400016784668 |
| 31 | 40.1199989318848 |
| 32 | 40.4799995422363 |
| 33 | 40.8600006103516 |
| 34 | 41.2299995422363 |
| 35 | 41.5900001525879 |
| 36 | 41.9099998474121 |
| 37 | 42.2099990844727 |
| 38 | 42.5099983215332 |
| 39 | 42.810001373291 |
| 40 | 43.1100006103516 |
| 41 | 43.4099998474121 |
| 42 | 43.7099990844727 |

| 43 | 44 |
| --- | --- |
| 44 | 44.2900009155273 |
| 45 | 44.5699996948242 |
| 46 | 44.8600006103516 |
| 47 | 45.1699981689453 |
| 48 | 45.4700012207031 |
| 49 | 45.7900009155273 |
| 50 | 46.1100006103516 |
| 51 | 46.4199981689453 |
| 52 | 46.7200012207031 |
| 53 | 47.0200004577637 |
| 54 | 47.310001373291 |
| 55 | 47.5999984741211 |
| 56 | 47.8899993896484 |
| 57 | 48.1800003051758 |
| 58 | 48.4700012207031 |
| 59 | 48.75 |
| 60 | 49.0200004577637 |
| 61 | 49.2900009155273 |
| 62 | 49.5400009155273 |
| 63 | 49.7999992370605 |
| 64 | 50.0299987792969 |

| 65 | 50.2400016784668 |
| --- | --- |
| 66 | 50.4599990844727 |
| 67 | 50.6500015258789 |
| 68 | 50.8499984741211 |
| 69 | 51.0299987792969 |
| 70 | 51.2099990844727 |
| 71 | 51.3699989318848 |
| 72 | 51.5299987792969 |
| 73 | 51.7000007629395 |
| 74 | 51.8699989318848 |
| 75 | 52.0400009155273 |
| 76 | 52.2099990844727 |
| 77 | 52.3800010681152 |
| 78 | 52.5499992370605 |
| 79 | 52.7200012207031 |
| 80 | 52.9000015258789 |
| 81 | 53.0900001525879 |
| 82 | 53.2700004577637 |
| 83 | 53.4599990844727 |
| 84 | 53.6500015258789 |
| 85 | 53.8300018310547 |
| 86 | 54.0099983215332 |

| 87 | 54.1599998474121 |
| --- | --- |
| 88 | 54.310001373291 |
| 89 | 54.4599990844727 |
| 90 | 54.5900001525879 |
| 91 | 54.7299995422363 |
| 92 | 54.8499984741211 |
| 93 | 54.9700012207031 |
| 94 | 55.0999984741211 |
| 95 | 55.2200012207031 |
| 96 | 55.3400001525879 |
| 97 | 55.4599990844727 |
| 98 | 55.5999984741211 |
| 99 | 55.7299995422363 |
| 100 | 55.8499984741211 |
| 101 | 55.9799995422363 |
| 102 | 56.1199989318848 |
| 103 | 56.2599983215332 |
| 104 | 56.3899993896484 |
| 105 | 56.5099983215332 |
| 106 | 56.6300010681152 |
| 107 | 56.7400016784668 |
| 108 | 56.8600006103516 |

| 109 | 56.9700012207031 |
| --- | --- |
| 110 | 57.0800018310547 |
| 111 | 57.1800003051758 |
| 112 | 57.2700004577637 |
| 113 | 57.3600006103516 |
| 114 | 57.4599990844727 |
| 115 | 57.5499992370605 |
| 116 | 57.6399993896484 |
| 117 | 57.7400016784668 |
| 118 | 57.8300018310547 |
| 119 | 57.9099998474121 |
| 120 | 57.9900016784668 |
| 121 | 58.0800018310547 |
| 122 | 58.1599998474121 |
| 123 | 58.2400016784668 |
| 124 | 58.3300018310547 |
| 125 | 58.4000015258789 |
| 126 | 58.4700012207031 |
| 127 | 58.5400009155273 |
| 128 | 58.6199989318848 |
| 129 | 58.7000007629395 |
| 130 | 58.7799987792969 |

| 131 | 58.8699989318848 |
| --- | --- |
| 132 | 58.939998626709 |
| 133 | 59.0099983215332 |
| 134 | 59.0900001525879 |
| 135 | 59.1599998474121 |
| 136 | 59.2099990844727 |
| 137 | 59.2700004577637 |
| 138 | 59.310001373291 |
| 139 | 59.3499984741211 |
| 140 | 59.3800010681152 |
| 141 | 59.4199981689453 |
| 142 | 59.4500007629395 |
| 143 | 59.4799995422363 |
| 144 | 59.5099983215332 |
| 145 | 59.5299987792969 |
| 146 | 59.5699996948242 |
| 147 | 59.6100006103516 |
| 148 | 59.6500015258789 |
| 149 | 59.7000007629395 |
| 150 | 59.7299995422363 |
| 151 | 59.7799987792969 |
| 152 | 59.8199996948242 |

| 153 | 59.8600006103516 |
| --- | --- |
| 154 | 59.9099998474121 |
| 155 | 59.9799995422363 |
| 156 | 60.0400009155273 |
| 157 | 60.0999984741211 |
| 158 | 60.1599998474121 |
| 159 | 60.2200012207031 |
| 160 | 60.2999992370605 |
| 161 | 60.3600006103516 |
| 162 | 60.4300003051758 |
| 163 | 60.5 |
| 164 | 60.5699996948242 |
| 165 | 60.5999984741211 |
| 166 | 60.6500015258789 |
| 167 | 60.689998626709 |
| 168 | 60.7400016784668 |
| 169 | 60.7700004577637 |
| 170 | 60.7999992370605 |
| 171 | 60.8300018310547 |
| 172 | 60.8499984741211 |
| 173 | 60.8899993896484 |
| 174 | 60.9199981689453 |

| 175 | 60.9599990844727 |
| --- | --- |
| 176 | 61.0099983215332 |
| 177 | 61.0400009155273 |
| 178 | 61.0900001525879 |
| 179 | 61.1399993896484 |
| 180 | 61.1800003051758 |
| 181 | 61.2200012207031 |
| 182 | 61.2599983215332 |
| 183 | 61.2900009155273 |
| 184 | 61.3199996948242 |
| 185 | 61.3499984741211 |
| 186 | 61.3699989318848 |
| 187 | 61.4000015258789 |
| 188 | 61.4099998474121 |
| 189 | 61.4300003051758 |
| 190 | 61.4500007629395 |
| 191 | 61.4799995422363 |
| 192 | 61.5 |
| 193 | 61.5299987792969 |
| 194 | 61.5499992370605 |
| 195 | 61.5699996948242 |
| 196 | 61.5900001525879 |

| 197 | 61.6300010681152 |
| --- | --- |
| 198 | 61.6500015258789 |
| 199 | 61.6800003051758 |
| 200 | 61.7099990844727 |
| 201 | 61.7299995422363 |
| 202 | 61.7400016784668 |

A1.4. Thermal conductivity raw data for 60 % maize husk

t/[min] lambda/[mW/(m*K)]

1	131.229995727539

2	130.809997558594

3	130.330001831055

4	129.860000610352

5	129.490005493164

6	129.190002441406

7	128.970001220703

8	128.830001831055

9	128.729995727539

10	128.679992675781

11	128.679992675781

12	128.75

13	128.899993896484

14	129.050003051758

15	129.119995117188

16	129.160003662109

17	129.119995117188

18	129.070007324219

19	128.940002441406

20	128.779998779297

| 21 | 128.580001831055 |
| --- | --- |
| 22 | 128.360000610352 |
| 23 | 128.110000610352 |
| 24 | 127.849998474121 |
| 25 | 127.610000610352 |
| 26 | 127.430000305176 |
| 27 | 127.26000213623 |
| 28 | 127.180000305176 |
| 29 | 127.059997558594 |
| 30 | 127.019996643066 |
| 31 | 127 |
| 32 | 127.029998779297 |
| 33 | 127.120002746582 |
| 34 | 127.230003356934 |
| 35 | 127.379997253418 |
| 36 | 127.519996643066 |
| 37 | 127.669998168945 |
| 38 | 127.870002746582 |
| 39 | 128.070007324219 |
| 40 | 128.369995117188 |
| 41 | 128.740005493164 |
| 42 | 129.179992675781 |

| 43 | 129.690002441406 |
| --- | --- |
| 44 | 130.240005493164 |
| 45 | 130.809997558594 |
| 46 | 131.320007324219 |
| 47 | 131.779998779297 |
| 48 | 132.190002441406 |
| 49 | 132.479995727539 |
| 50 | 132.660003662109 |
| 51 | 132.740005493164 |
| 52 | 132.669998168945 |
| 53 | 132.479995727539 |
| 54 | 132.190002441406 |
| 55 | 131.809997558594 |
| 56 | 131.589996337891 |
| 57 | 131.080001831055 |
| 58 | 130.5 |
| 59 | 129.860000610352 |
| 60 | 129.220001220703 |
| 61 | 128.580001831055 |
| 62 | 127.980003356934 |
| 63 | 127.430000305176 |
| 64 | 126.949996948242 |

| 65 | 126.639999389648 |
| --- | --- |
| 66 | 126.480003356934 |
| 67 | 126.459999084473 |
| 68 | 126.589996337891 |
| 69 | 126.800003051758 |
| 70 | 127.129997253418 |
| 71 | 127.5 |
| 72 | 127.940002441406 |
| 73 | 128.360000610352 |
| 74 | 128.779998779297 |
| 75 | 129.130004882813 |
| 76 | 129.429992675781 |
| 77 | 129.699996948242 |
| 78 | 129.899993896484 |
| 79 | 130.009994506836 |
| 80 | 130.029998779297 |
| 81 | 130 |
| 82 | 129.910003662109 |
| 83 | 129.800003051758 |
| 84 | 129.669998168945 |
| 85 | 129.529998779297 |
| 86 | 129.449996948242 |

| 87 | 129.360000610352 |
| --- | --- |
| 88 | 129.279998779297 |
| 89 | 129.229995727539 |
| 90 | 129.229995727539 |
| 91 | 129.210006713867 |
| 92 | 129.210006713867 |
| 93 | 129.190002441406 |
| 94 | 129.190002441406 |
| 95 | 129.210006713867 |
| 96 | 129.259994506836 |
| 97 | 129.279998779297 |
| 98 | 129.300003051758 |
| 99 | 129.279998779297 |
| 100 | 129.25 |
| 101 | 129.190002441406 |
| 102 | 129.139999389648 |
| 103 | 129.070007324219 |
| 104 | 128.979995727539 |
| 105 | 128.919998168945 |
| 106 | 128.869995117188 |
| 107 | 128.839996337891 |
| 108 | 128.880004882813 |

| 109 | 128.910003662109 |
| --- | --- |
| 110 | 129.020004272461 |
| 111 | 129.149993896484 |
| 112 | 129.350006103516 |
| 113 | 129.449996948242 |
| 114 | 129.729995727539 |
| 115 | 130.080001831055 |
| 116 | 130.419998168945 |
| 117 | 130.789993286133 |
| 118 | 131.119995117188 |
| 119 | 131.380004882813 |
| 120 | 131.619995117188 |
| 121 | 131.770004272461 |
| 122 | 131.880004882813 |
| 123 | 131.910003662109 |
| 124 | 131.899993896484 |
| 125 | 131.820007324219 |
| 126 | 131.720001220703 |
| 127 | 131.619995117188 |
| 128 | 131.529998779297 |
| 129 | 131.460006713867 |
| 130 | 131.380004882813 |

| 131 | 131.350006103516 |
| --- | --- |
| 132 | 131.330001831055 |
| 133 | 131.360000610352 |
| 134 | 131.410003662109 |
| 135 | 131.509994506836 |
| 136 | 131.630004882813 |
| 137 | 131.800003051758 |
| 138 | 131.889999389648 |
| 139 | 132.070007324219 |
| 140 | 132.270004272461 |
| 141 | 132.479995727539 |
| 142 | 132.660003662109 |
| 143 | 132.820007324219 |
| 144 | 132.929992675781 |
| 145 | 133.009994506836 |
| 146 | 133.029998779297 |
| 147 | 132.990005493164 |
| 148 | 132.940002441406 |
| 149 | 132.880004882813 |
| 150 | 132.720001220703 |
| 151 | 132.570007324219 |
| 152 | 132.460006713867 |

| 153 | 132.369995117188 |
| --- | --- |
| 154 | 132.330001831055 |
| 155 | 132.309997558594 |
| 156 | 132.279998779297 |
| 157 | 132.259994506836 |
| 158 | 132.240005493164 |
| 159 | 132.279998779297 |
| 160 | 132.309997558594 |
| 161 | 132.350006103516 |
| 162 | 132.419998168945 |
| 163 | 132.479995727539 |
| 164 | 132.520004272461 |
| 165 | 132.5 |
| 166 | 132.479995727539 |
| 167 | 132.460006713867 |
| 168 | 132.410003662109 |
| 169 | 132.339996337891 |
| 170 | 132.259994506836 |
| 171 | 132.190002441406 |
| 172 | 132.119995117188 |
| 173 | 132.080001831055 |
| 174 | 132.110000610352 |

| 175 | 132.130004882813 |
| --- | --- |
| 176 | 132.149993896484 |
| 177 | 132.240005493164 |
| 178 | 132.270004272461 |
| 179 | 132.369995117188 |
| 180 | 132.479995727539 |
| 181 | 132.589996337891 |
| 182 | 132.710006713867 |
| 183 | 132.809997558594 |
| 184 | 132.899993896484 |
| 185 | 132.949996948242 |
| 186 | 132.970001220703 |
| 187 | 132.970001220703 |
| 188 | 132.940002441406 |
| 189 | 132.899993896484 |
| 190 | 132.880004882813 |
| 191 | 132.860000610352 |
| 192 | 132.860000610352 |
| 193 | 132.899993896484 |
| 194 | 132.929992675781 |
| 195 | 133.020004272461 |
| 196 | 133.119995117188 |

| 197 | 133.229995727539 |
| --- | --- |
| 198 | 133.339996337891 |
| 199 | 133.429992675781 |
| 200 | 133.539993286133 |
| 201 | 133.649993896484 |
| 202 | 133.740005493164 |
| 203 | 133.809997558594 |

A1.5. Thermal conductivity raw data for 60 % cow dung

t/[min] lambda/[mW/(m*K)]

1	131.089996337891

2	130.559997558594

3	130.419998168945

4	130.429992675781

5	130.059997558594

6	129.929992675781

7	129.929992675781

8	129.869995117188

9	129.860000610352

10	129.490005493164

11	129.449996948242

12	129.429992675781

13	129.300003051758

14	128.850006103516

15	128.729995727539

16	128.610000610352

17	128.229995727539

18	128.210006713867

19	128.110000610352

20	127.650001525879

| 21 | 127.550003051758 |
| --- | --- |
| 22 | 127.51000213623 |
| 23 | 127.120002746582 |
| 24 | 127.029998779297 |
| 25 | 126.980003356934 |
| 26 | 126.949996948242 |
| 27 | 126.910003662109 |
| 28 | 126.830001831055 |
| 29 | 126.419998168945 |
| 30 | 126.330001831055 |
| 31 | 126.25 |
| 32 | 125.910003662109 |
| 33 | 125.860000610352 |
| 34 | 125.819999694824 |
| 35 | 125.779998779297 |
| 36 | 125.430000305176 |
| 37 | 125.339996337891 |
| 38 | 125.300003051758 |
| 39 | 125.279998779297 |
| 40 | 125.26000213623 |
| 41 | 125.279998779297 |
| 42 | 125.230003356934 |

| 43 | 125.150001525879 |
| --- | --- |
| 44 | 124.819999694824 |
| 45 | 124.76000213623 |
| 46 | 124.730003356934 |
| 47 | 124.669998168945 |
| 48 | 124.650001525879 |
| 49 | 124.360000610352 |
| 50 | 124.330001831055 |
| 51 | 124.309997558594 |
| 52 | 124.269996643066 |
| 53 | 124.209999084473 |
| 54 | 124.199996948242 |
| 55 | 124.190002441406 |
| 56 | 124.129997253418 |
| 57 | 123.800003051758 |
| 58 | 123.75 |
| 59 | 123.720001220703 |
| 60 | 123.690002441406 |
| 61 | 123.680000305176 |
| 62 | 123.669998168945 |
| 63 | 123.650001525879 |
| 64 | 123.620002746582 |

| 65 | 123.580001831055 |
| --- | --- |
| 66 | 123.559997558594 |
| 67 | 123.550003051758 |
| 68 | 123.230003356934 |
| 69 | 123.230003356934 |
| 70 | 123.209999084473 |
| 71 | 123.169998168945 |
| 72 | 123.139999389648 |
| 73 | 123.110000610352 |
| 74 | 123.110000610352 |
| 75 | 123.110000610352 |
| 76 | 123.089996337891 |
| 77 | 123.089996337891 |
| 78 | 123.099998474121 |
| 79 | 123.089996337891 |
| 80 | 123.089996337891 |
| 81 | 123.089996337891 |
| 82 | 123.069999694824 |
| 83 | 123.050003051758 |
| 84 | 123.029998779297 |
| 85 | 123.01000213623 |
| 86 | 122.709999084473 |

| 87 | 122.650001525879 |
| --- | --- |
| 88 | 122.629997253418 |
| 89 | 122.599998474121 |
| 90 | 122.569999694824 |
| 91 | 122.559997558594 |
| 92 | 122.550003051758 |
| 93 | 122.550003051758 |
| 94 | 122.550003051758 |
| 95 | 122.51000213623 |
| 96 | 122.48999786377 |
| 97 | 122.51000213623 |
| 98 | 122.519996643066 |
| 99 | 122.5 |
| 100 | 122.48999786377 |
| 101 | 122.5 |
| 102 | 122.48999786377 |
| 103 | 122.48999786377 |
| 104 | 122.48999786377 |
| 105 | 122.48999786377 |
| 106 | 122.480003356934 |
| 107 | 122.48999786377 |
| 108 | 122.220001220703 |

| 109 | 122.470001220703 |
| --- | --- |
| 110 | 122.459999084473 |
| 111 | 122.190002441406 |
| 112 | 122.180000305176 |
| 113 | 122.160003662109 |
| 114 | 122.139999389648 |
| 115 | 122.129997253418 |
| 116 | 122.120002746582 |
| 117 | 122.110000610352 |
| 118 | 122.120002746582 |
| 119 | 122.089996337891 |
| 120 | 122.069999694824 |
| 121 | 122.120002746582 |
| 122 | 122.129997253418 |
| 123 | 122.120002746582 |
| 124 | 122.099998474121 |
| 125 | 122.089996337891 |
| 126 | 122.069999694824 |
| 127 | 122.099998474121 |
| 128 | 122.129997253418 |
| 129 | 122.080001831055 |
| 130 | 122.040000915527 |

| 131 | 122.029998779297 |
| --- | --- |
| 132 | 122.040000915527 |
| 133 | 122.029998779297 |
| 134 | 122.019996643066 |
| 135 | 122 |
| 136 | 121.980003356934 |
| 137 | 121.980003356934 |
| 138 | 121.970001220703 |
| 139 | 121.980003356934 |
| 140 | 121.970001220703 |
| 141 | 121.980003356934 |
| 142 | 121.980003356934 |
| 143 | 121.980003356934 |
| 144 | 121.980003356934 |
| 145 | 121.970001220703 |
| 146 | 121.970001220703 |
| 147 | 121.980003356934 |
| 148 | 121.970001220703 |
| 149 | 121.970001220703 |
| 150 | 121.970001220703 |
| 151 | 121.970001220703 |
| 152 | 121.959999084473 |

| 153 | 121.959999084473 |
| --- | --- |
| 154 | 121.959999084473 |
| 155 | 121.940002441406 |
| 156 | 121.680000305176 |
| 157 | 121.680000305176 |
| 158 | 121.930000305176 |
| 159 | 121.660003662109 |
| 160 | 121.660003662109 |
| 161 | 121.650001525879 |
| 162 | 121.629997253418 |
| 163 | 121.620002746582 |
| 164 | 121.620002746582 |
| 165 | 121.620002746582 |
| 166 | 121.620002746582 |
| 167 | 121.620002746582 |
| 168 | 121.620002746582 |
| 169 | 121.639999389648 |
| 170 | 121.629997253418 |
| 171 | 121.650001525879 |
| 172 | 121.660003662109 |
| 173 | 121.660003662109 |
| 174 | 121.660003662109 |

| 175 | 121.650001525879 |
| --- | --- |
| 176 | 121.650001525879 |
| 177 | 121.650001525879 |
| 178 | 121.660003662109 |
| 179 | 121.650001525879 |
| 180 | 121.639999389648 |
| 181 | 121.620002746582 |
| 182 | 121.629997253418 |
| 183 | 121.650001525879 |
| 184 | 121.650001525879 |
| 185 | 121.639999389648 |
| 186 | 121.650001525879 |
| 187 | 121.620002746582 |
| 188 | 121.610000610352 |
| 189 | 121.629997253418 |
| 190 | 121.629997253418 |
| 191 | 121.629997253418 |
| 192 | 121.629997253418 |
| 193 | 121.629997253418 |
| 194 | 121.629997253418 |
| 195 | 121.629997253418 |
| 196 | 121.629997253418 |

| 197 | 121.639999389648 |
| --- | --- |
| 198 | 121.629997253418 |
| 199 | 121.629997253418 |
| 200 | 121.629997253418 |
| 201 | 121.639999389648 |
| 202 | 121.639999389648 |
| 203 | 121.620002746582 |
| 204 | 121.639999389648 |

A1.6. Thermal conductivity raw data for 60 % millet

t/[min] lambda/[mW/(m*K)]

1	142.679992675781

2	142.149993896484

3	141.600006103516

4	141.160003662109

5	141.059997558594

6	140.710006713867

7	140.270004272461

8	139.869995117188

9	139.789993286133

10	139.490005493164

11	139.399993896484

12	139.029998779297

13	138.919998168945

14	138.589996337891

15	138.190002441406

16	138.050003051758

17	137.729995727539

18	137.589996337891

19	137.229995727539

20	136.880004882813

| 21 | 136.740005493164 |
| --- | --- |
| 22 | 136.449996948242 |
| 23 | 136.350006103516 |
| 24 | 136.029998779297 |
| 25 | 135.889999389648 |
| 26 | 135.559997558594 |
| 27 | 135.210006713867 |
| 28 | 134.830001831055 |
| 29 | 134.779998779297 |
| 30 | 134.509994506836 |
| 31 | 134.460006713867 |
| 32 | 134.169998168945 |
| 33 | 134.050003051758 |
| 34 | 133.800003051758 |
| 35 | 133.740005493164 |
| 36 | 133.470001220703 |
| 37 | 133.369995117188 |
| 38 | 133.339996337891 |
| 39 | 133.080001831055 |
| 40 | 133.020004272461 |
| 41 | 132.729995727539 |
| 42 | 132.630004882813 |

| 43 | 132.580001831055 |
| --- | --- |
| 44 | 132.320007324219 |
| 45 | 132.240005493164 |
| 46 | 132.009994506836 |
| 47 | 131.759994506836 |
| 48 | 131.660003662109 |
| 49 | 131.399993896484 |
| 50 | 131.330001831055 |
| 51 | 131.110000610352 |
| 52 | 131.089996337891 |
| 53 | 131.050003051758 |
| 54 | 131.020004272461 |
| 55 | 130.830001831055 |
| 56 | 130.800003051758 |
| 57 | 130.740005493164 |
| 58 | 130.529998779297 |
| 59 | 130.490005493164 |
| 60 | 130.440002441406 |
| 61 | 130.419998168945 |
| 62 | 130.240005493164 |
| 63 | 130.199996948242 |
| 64 | 129.990005493164 |

| 65 | 129.919998168945 |
| --- | --- |
| 66 | 129.899993896484 |
| 67 | 129.690002441406 |
| 68 | 129.619995117188 |
| 69 | 129.570007324219 |
| 70 | 129.380004882813 |
| 71 | 129.330001831055 |
| 72 | 129.149993896484 |
| 73 | 129.119995117188 |
| 74 | 129.100006103516 |
| 75 | 129.089996337891 |
| 76 | 129.089996337891 |
| 77 | 128.919998168945 |
| 78 | 128.880004882813 |
| 79 | 128.850006103516 |
| 80 | 128.830001831055 |
| 81 | 128.669998168945 |
| 82 | 128.630004882813 |
| 83 | 128.589996337891 |
| 84 | 128.559997558594 |
| 85 | 128.410003662109 |
| 86 | 128.369995117188 |

| 87 | 128.350006103516 |
| --- | --- |
| 88 | 128.300003051758 |
| 89 | 128.139999389648 |
| 90 | 128.089996337891 |
| 91 | 127.940002441406 |
| 92 | 127.930000305176 |
| 93 | 127.940002441406 |
| 94 | 127.970001220703 |
| 95 | 127.98999786377 |
| 96 | 128.139999389648 |
| 97 | 128.160003662109 |
| 98 | 128.179992675781 |
| 99 | 128.199996948242 |
| 100 | 128.229995727539 |
| 101 | 128.25 |
| 102 | 128.279998779297 |
| 103 | 128.440002441406 |
| 104 | 128.490005493164 |
| 105 | 128.649993896484 |
| 106 | 128.669998168945 |
| 107 | 128.639999389648 |
| 108 | 128.639999389648 |

| 109 | 128.660003662109 |
| --- | --- |
| 110 | 128.639999389648 |
| 111 | 128.449996948242 |
| 112 | 128.449996948242 |
| 113 | 128.419998168945 |
| 114 | 128.399993896484 |
| 115 | 128.360000610352 |
| 116 | 128.330001831055 |
| 117 | 128.149993896484 |
| 118 | 127.959999084473 |
| 119 | 127.910003662109 |
| 120 | 127.870002746582 |
| 121 | 127.839996337891 |
| 122 | 127.699996948242 |
| 123 | 127.669998168945 |
| 124 | 127.650001525879 |
| 125 | 127.650001525879 |
| 126 | 127.620002746582 |
| 127 | 127.480003356934 |
| 128 | 127.459999084473 |
| 129 | 127.440002441406 |
| 130 | 127.440002441406 |

| 131 | 127.330001831055 |
| --- | --- |
| 132 | 127.290000915527 |
| 133 | 127.290000915527 |
| 134 | 127.25 |
| 135 | 127.220001220703 |
| 136 | 127.080001831055 |
| 137 | 127.069999694824 |
| 138 | 127.059997558594 |
| 139 | 127.080001831055 |
| 140 | 127.069999694824 |
| 141 | 127.050003051758 |
| 142 | 127.050003051758 |
| 143 | 127.069999694824 |
| 144 | 127.059997558594 |
| 145 | 127.059997558594 |
| 146 | 127.059997558594 |
| 147 | 127.069999694824 |
| 148 | 127.080001831055 |
| 149 | 127.080001831055 |
| 150 | 127.059997558594 |
| 151 | 127.050003051758 |
| 152 | 127.029998779297 |

| 153 | 127.029998779297 |
| --- | --- |
| 154 | 127.019996643066 |
| 155 | 126.919998168945 |
| 156 | 126.910003662109 |
| 157 | 126.910003662109 |
| 158 | 126.900001525879 |
| 159 | 126.889999389648 |
| 160 | 126.889999389648 |
| 161 | 126.879997253418 |
| 162 | 126.879997253418 |
| 163 | 126.870002746582 |
| 164 | 126.849998474121 |
| 165 | 126.849998474121 |
| 166 | 126.849998474121 |
| 167 | 126.849998474121 |
| 168 | 126.819999694824 |
| 169 | 126.830001831055 |
| 170 | 126.709999084473 |
| 171 | 126.709999084473 |
| 172 | 126.709999084473 |
| 173 | 126.709999084473 |
| 174 | 126.720001220703 |

| 175 | 126.709999084473 |
| --- | --- |
| 176 | 126.699996948242 |
| 177 | 126.709999084473 |
| 178 | 126.709999084473 |
| 179 | 126.720001220703 |
| 180 | 126.709999084473 |
| 181 | 126.720001220703 |
| 182 | 126.720001220703 |
| 183 | 126.709999084473 |
| 184 | 126.720001220703 |
| 185 | 126.730003356934 |
| 186 | 126.720001220703 |
| 187 | 126.720001220703 |
| 188 | 126.709999084473 |
| 189 | 126.699996948242 |
| 190 | 126.709999084473 |
| 191 | 126.709999084473 |
| 192 | 126.720001220703 |
| 193 | 126.720001220703 |
| 194 | 126.720001220703 |
| 195 | 126.699996948242 |
| 196 | 126.709999084473 |

| 197 | 126.699996948242 |
| --- | --- |
| 198 | 126.699996948242 |
| 199 | 126.709999084473 |
| 200 | 126.709999084473 |
| 201 | 126.709999084473 |
| 202 | 126.699996948242 |

A2.1 Raw data of Marble dust at 5% for Sample A

t/[min] lambda/[mW/(m*K)]

| 1 | 51.4799995422363 |
| --- | --- |
| 2 | 51.6800003051758 |
| 3 | 51.9199981689453 |
| 4 | 52.2400016784668 |
| 5 | 52.6199989318848 |
| 6 | 53.0499992370605 |
| 7 | 53.5200004577637 |
| 8 | 54 |
| 9 | 54.4900016784668 |
| 10 | 55.0200004577637 |
| 11 | 55.5800018310547 |
| 12 | 56.1800003051758 |
| 13 | 56.7299995422363 |
| 14 | 57.2299995422363 |
| 15 | 57.689998626709 |
| 16 | 58.1199989318848 |
| 17 | 58.5200004577637 |
| 18 | 58.9000015258789 |
| 19 | 59.2700004577637 |
| 20 | 59.5999984741211 |
| 21 | 59.9000015258789 |
| 22 | 60.1599998474121 |
| 23 | 60.4300003051758 |
| 24 | 60.6399993896484 |
| 25 | 60.8499984741211 |
| 26 | 61.0499992370605 |
| 27 | 61.2400016784668 |
| 28 | 61.4099998474121 |

| 29 | 61.5699996948242 |
| --- | --- |
| 30 | 61.7200012207031 |
| 31 | 61.8800010681152 |
| 32 | 62.0200004577637 |
| 33 | 62.1699981689453 |
| 34 | 62.310001373291 |
| 35 | 62.4500007629395 |
| 36 | 62.5900001525879 |
| 37 | 62.7400016784668 |
| 38 | 62.8699989318848 |
| 39 | 63.0200004577637 |
| 40 | 63.1599998474121 |
| 41 | 63.310001373291 |
| 42 | 63.4500007629395 |
| 43 | 63.5900001525879 |
| 44 | 63.7299995422363 |
| 45 | 63.8699989318848 |
| 46 | 64.0100021362305 |
| 47 | 64.1699981689453 |
| 48 | 64.3199996948242 |
| 49 | 64.4800033569336 |
| 50 | 64.6600036621094 |
| 51 | 64.8199996948242 |
| 52 | 65 |

| 61 | 66.4199981689453 |
| --- | --- |
| 62 | 66.5400009155273 |
| 63 | 66.6399993896484 |
| 64 | 66.75 |
| 65 | 66.8399963378906 |
| 66 | 66.9400024414063 |
| 67 | 67.0599975585938 |
| 68 | 67.1699981689453 |
| 69 | 67.2900009155273 |
| 70 | 67.4000015258789 |
| 71 | 67.5 |
| 72 | 67.5999984741211 |
| 73 | 67.7099990844727 |
| 74 | 67.8000030517578 |
| 75 | 67.9000015258789 |
| 76 | 67.9700012207031 |
| 77 | 68.0400009155273 |
| 78 | 68.120002746582 |
| 79 | 68.1900024414063 |
| 80 | 68.2600021362305 |
| 81 | 68.3300018310547 |
| 82 | 68.4100036621094 |
| 83 | 68.4700012207031 |
| 84 | 68.5599975585938 |

| 93 | 69.25 |
| --- | --- |
| 94 | 69.3199996948242 |
| 95 | 69.3899993896484 |
| 96 | 69.4599990844727 |
| 97 | 69.5500030517578 |
| 98 | 69.6500015258789 |
| 99 | 69.7699966430664 |
| 100 | 69.879997253418 |
| 101 | 69.9899978637695 |
| 102 | 70.1100006103516 |
| 103 | 70.2200012207031 |
| 104 | 70.3300018310547 |
| 105 | 70.4199981689453 |
| 106 | 70.5299987792969 |
| 107 | 70.5999984741211 |
| 108 | 70.6600036621094 |
| 109 | 70.7099990844727 |
| 110 | 70.7699966430664 |
| 111 | 70.8000030517578 |
| 112 | 70.8399963378906 |
| 113 | 70.9000015258789 |
| 114 | 70.9599990844727 |
| 115 | 71.0100021362305 |
| 116 | 71.0699996948242 |

| 125 | 71.6600036621094 |
| --- | --- |
| 126 | 71.7099990844727 |
| 127 | 71.75 |
| 128 | 71.7900009155273 |
| 129 | 71.8399963378906 |
| 130 | 71.8899993896484 |
| 131 | 71.9300003051758 |
| 132 | 71.9899978637695 |
| 133 | 72.0599975585938 |
| 134 | 72.129997253418 |
| 135 | 72.1999969482422 |
| 136 | 72.2600021362305 |
| 137 | 72.3300018310547 |
| 138 | 72.3899993896484 |
| 139 | 72.4499969482422 |
| 140 | 72.5 |
| 141 | 72.5299987792969 |
| 142 | 72.5699996948242 |
| 143 | 72.6100006103516 |
| 144 | 72.620002746582 |
| 145 | 72.6399993896484 |
| 146 | 72.6800003051758 |
| 147 | 72.7099990844727 |
| 148 | 72.75 |

| 157 | 73.120002746582 |
| --- | --- |
| 158 | 73.1500015258789 |
| 159 | 73.1800003051758 |
| 160 | 73.2200012207031 |
| 161 | 73.2399978637695 |
| 162 | 73.2699966430664 |
| 163 | 73.2799987792969 |
| 164 | 73.3000030517578 |
| 165 | 73.3099975585938 |
| 166 | 73.3199996948242 |
| 167 | 73.3199996948242 |
| 168 | 73.3199996948242 |
| 169 | 73.3300018310547 |
| 170 | 73.3300018310547 |
| 171 | 73.3399963378906 |
| 172 | 73.3499984741211 |
| 173 | 73.3300018310547 |
| 174 | 73.3099975585938 |
| 175 | 73.2900009155273 |
| 176 | 73.2699966430664 |
| 177 | 73.2399978637695 |
| 178 | 73.2099990844727 |
| 179 | 73.1600036621094 |
| 180 | 73.120002746582 |

| 189 | 72.5800018310547 |
| --- | --- |
| 190 | 72.5199966430664 |
| 191 | 72.4300003051758 |
| 192 | 72.3600006103516 |
| 193 | 72.2699966430664 |
| 194 | 72.1900024414063 |
| 195 | 72.0999984741211 |
| 196 | 72.0199966430664 |
| 197 | 71.9599990844727 |
| 198 | 71.9100036621094 |
| 199 | 71.8600006103516 |
| 200 | 71.8199996948242 |
| 201 | 71.7900009155273 |
| 202 | 71.75 |

A2.2 Raw data of Marble dust at 5% for Sample C

t/[min] lambda/[mW/(m*K)]

| 1 | 68.3499984741211 |
| --- | --- |
| 2 | 68.5500030517578 |
| 3 | 68.7699966430664 |
| 4 | 68.9899978637695 |
| 5 | 69.2300033569336 |
| 6 | 69.4599990844727 |
| 7 | 69.6800003051758 |
| 8 | 69.8899993896484 |
| 9 | 70.0999984741211 |
| 10 | 70.2900009155273 |
| 11 | 70.4499969482422 |
| 12 | 70.5999984741211 |
| 13 | 70.7300033569336 |
| 14 | 70.8499984741211 |
| 15 | 70.9599990844727 |
| 16 | 71.0699996948242 |
| 17 | 71.1500015258789 |
| 18 | 71.25 |
| 19 | 71.3399963378906 |
| 20 | 71.4300003051758 |
| 21 | 71.5199966430664 |
| 22 | 71.620002746582 |
| 23 | 71.7099990844727 |
| 24 | 71.7900009155273 |
| 25 | 71.879997253418 |
| 26 | 71.9800033569336 |
| 27 | 72.0599975585938 |
| 28 | 72.1399993896484 |

| 29 | 72.2200012207031 |
| --- | --- |
| 30 | 72.3000030517578 |
| 31 | 72.370002746582 |
| 32 | 72.4499969482422 |
| 33 | 72.5100021362305 |
| 34 | 72.5899963378906 |
| 35 | 72.6500015258789 |
| 36 | 72.7200012207031 |
| 37 | 72.7900009155273 |
| 38 | 72.8499984741211 |
| 39 | 72.9300003051758 |
| 40 | 73 |
| 41 | 73.0699996948242 |
| 42 | 73.1399993896484 |
| 43 | 73.1999969482422 |
| 44 | 73.2799987792969 |
| 45 | 73.3399963378906 |
| 46 | 73.3899993896484 |
| 47 | 73.4599990844727 |
| 48 | 73.5100021362305 |
| 49 | 73.5599975585938 |
| 50 | 73.5999984741211 |
| 51 | 73.6500015258789 |
| 52 | 73.6900024414063 |
| 53 | 73.7399978637695 |
| 54 | 73.7699966430664 |
| 55 | 73.8099975585938 |
| 56 | 73.8600006103516 |
| 57 | 73.9000015258789 |
| 58 | 73.9499969482422 |
| 59 | 74 |
| 60 | 74.0500030517578 |

| 61 | 74.1100006103516 |
| --- | --- |
| 62 | 74.1800003051758 |
| 63 | 74.2300033569336 |
| 64 | 74.2900009155273 |
| 65 | 74.3399963378906 |
| 66 | 74.4000015258789 |
| 67 | 74.4499969482422 |
| 68 | 74.4899978637695 |
| 69 | 74.5299987792969 |
| 70 | 74.5800018310547 |
| 71 | 74.620002746582 |
| 72 | 74.6600036621094 |
| 73 | 74.6999969482422 |
| 74 | 74.7399978637695 |
| 75 | 74.7699966430664 |
| 76 | 74.8199996948242 |
| 77 | 74.8600006103516 |
| 78 | 74.9000015258789 |
| 79 | 74.9300003051758 |
| 80 | 74.9700012207031 |
| 81 | 75 |
| 82 | 75.0400009155273 |
| 83 | 75.0699996948242 |
| 84 | 75.0999984741211 |

| 93 | 75.3300018310547 |
| --- | --- |
| 94 | 75.3499984741211 |
| 95 | 75.370002746582 |
| 96 | 75.3899993896484 |
| 97 | 75.4100036621094 |
| 98 | 75.4300003051758 |
| 99 | 75.4499969482422 |
| 100 | 75.4800033569336 |
| 101 | 75.4899978637695 |
| 102 | 75.5199966430664 |
| 103 | 75.5400009155273 |
| 104 | 75.5699996948242 |
| 105 | 75.5899963378906 |
| 106 | 75.6100006103516 |
| 107 | 75.629997253418 |
| 108 | 75.6600036621094 |
| 109 | 75.6900024414063 |
| 110 | 75.7200012207031 |
| 111 | 75.7399978637695 |
| 112 | 75.7600021362305 |
| 113 | 75.7799987792969 |
| 114 | 75.8099975585938 |
| 115 | 75.8399963378906 |
| 116 | 75.870002746582 |

| 125 | 76.2200012207031 |
| --- | --- |
| 126 | 76.25 |
| 127 | 76.2799987792969 |
| 128 | 76.3099975585938 |
| 129 | 76.3300018310547 |
| 130 | 76.3600006103516 |
| 131 | 76.370002746582 |
| 132 | 76.4000015258789 |
| 133 | 76.4199981689453 |
| 134 | 76.4300003051758 |
| 135 | 76.4499969482422 |
| 136 | 76.4599990844727 |
| 137 | 76.4800033569336 |
| 138 | 76.4899978637695 |
| 139 | 76.5 |
| 140 | 76.5100021362305 |
| 141 | 76.5299987792969 |
| 142 | 76.5299987792969 |
| 143 | 76.5400009155273 |
| 144 | 76.5500030517578 |
| 145 | 76.5500030517578 |
| 146 | 76.5599975585938 |
| 147 | 76.5699996948242 |
| 148 | 76.5800018310547 |

| 157 | 76.6399993896484 |
| --- | --- |
| 158 | 76.6500015258789 |
| 159 | 76.6699981689453 |
| 160 | 76.6900024414063 |
| 161 | 76.7099990844727 |
| 162 | 76.7300033569336 |
| 163 | 76.75 |
| 164 | 76.7799987792969 |
| 165 | 76.8000030517578 |
| 166 | 76.8300018310547 |
| 167 | 76.8499984741211 |
| 168 | 76.879997253418 |
| 169 | 76.9000015258789 |
| 170 | 76.9300003051758 |
| 171 | 76.9499969482422 |
| 172 | 76.9899978637695 |
| 173 | 77.0199966430664 |
| 174 | 77.0400009155273 |
| 175 | 77.0800018310547 |
| 176 | 77.1100006103516 |
| 177 | 77.1399993896484 |
| 178 | 77.1600036621094 |
| 179 | 77.1900024414063 |
| 180 | 77.2200012207031 |

| 189 | 77.4000015258789 |
| --- | --- |
| 190 | 77.4199981689453 |
| 191 | 77.4300003051758 |
| 192 | 77.4599990844727 |
| 193 | 77.4700012207031 |
| 194 | 77.4899978637695 |
| 195 | 77.5100021362305 |
| 196 | 77.5100021362305 |
| 197 | 77.5199966430664 |
| 198 | 77.5299987792969 |
| 199 | 77.5500030517578 |
| 200 | 77.5500030517578 |
| 201 | 77.5699996948242 |
| 202 | 77.5899963378906 |

B.1 Welcome to ANSYS Fluent Release 18.2

Copyright 2017 SAS IP, Inc. All Rights Reserved. Unauthorized use, distribution or duplication is prohibited.

This product is subject to U.S. laws governing export and re-export. For full Legal Notice, see documentation.

Build Time: Jul 25 2017 20:05:41 Build Id: 10098

--------------------------------------------------------------

This is an academic version of ANSYS FLUENT. Usage of this product License is limited to the terms and conditions specified in your ANSYS License form, additional terms section.

--------------------------------------------------------------

Host spawning Node 0 on machine "Onjefu-PC" (win64). WARNING: No cached password or password provided. use '-pass' or '-cache' to provide password

mpid: mpid IP address 0.0.0.0, changed to IP address 127.0.0.1

Host 0 -- ip 127.0.0.1 -- ranks 0

host | 0

======|======

0 : SHM

Prot - All Intra-node communication is: SHM

------------------------------------------------------------------------------- ID Hostname Core O.S. PID Vendor

-------------------------------------------------------------------------------

n0 Onjefu-PC 1/4 Windows-x64 5264 Intel(R) Core(TM) i5-2450M

host Onjefu-PC Windows-x64 2788 Intel(R) Core(TM) i5-2450M

MPI Option Selected: ibmmpi

-------------------------------------------------------------------------------

The cleanup script file is C:\Users\Onjefu\cleanup-fluent-Onjefu-PC-2788.bat

Posting ANSYS Product Improvement Program startup data

Done.

> Multicore SMT processors were detected. Processor affinity set!

Reading	"C:\Users\Onjefu\AppData\Local\Temp\WB_ONJEFU- PC_Onjefu_1080_2\unsaved_project_files\dp0\FFF\MECH\FFF.msh"...

Buffering for file scan...

39777 nodes, binary.

36657 nodes, binary.

264 triangular wall faces, zone 1, binary.

7498 triangular wall faces, zone 2, binary.

136 quadrilateral interior faces, zone 3, binary.

136 quadrilateral interior faces, zone 4, binary.

12877 triangular interior faces, zone 5, binary.

97396 triangular interior faces, zone 6, binary.

546126 triangular interior faces, zone 7, binary.

3144 triangular wall faces, zone 15, binary.

2934 triangular wall faces, zone 16, binary.

2920 triangular wall faces, zone 17, binary.

3030 triangular wall faces, zone 18, binary.

3638 triangular wall faces, zone 19, binary.

3044 triangular wall faces, zone 20, binary.

44 triangular wall faces, zone 21, binary.

36 quadrilateral interface faces, zone 22, binary.

72 triangular interface faces, zone 23, binary.

190 quadrilateral interface faces, zone 24, binary.

154 quadrilateral interface faces, zone 25, binary.

1694 triangular interface faces, zone 26, binary.

21130 triangular interface faces, zone 27, binary.

186 triangular interface faces, zone 28, binary.

22810 triangular interface faces, zone 29, binary.

150 triangular interface faces, zone 30, binary.

77 hexahedral cells, zone 8, binary.

77 hexahedral cells, zone 9, binary.

6928 tetrahedral cells, zone 10, binary.

54045 tetrahedral cells, zone 11, binary.

285366 tetrahedral cells, zone 12, binary. Building...

mesh materials, interface, domains, zones,

Door-contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4-

contact_region_7-contact_region_5-contact_region_6-trg

Contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-trg-part_5

Contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-trg-part_4

Contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4-

contact_region_7-contact_region_5-contact_region_6-src-part_4

Contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_3

Contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_2

Contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_1

Contact_region_3-trg Contact_region_3-src window

Insulation north side east_side top

Southern side

Heated side part_5 part_4 part_3 part_2 part_1

interior-part_5

interior-part_4 interior-part_3 interior-part_2 interior-part_1 wall-part_5 wall-part_3 interior-14

wall-31 wall-32 interior-33 interior-34 interior-35 interior-36 interior-37 interior-38

interior-39 interior-40 interior-41 interior-42 interior-43 interior-44 wall-45 wall-46 wall-47 wall-48 wall-49 wall-50 wall-51

mesh interfaces,

parallel, Done.

Preparing mesh for display...

Note: zone-surface: cannot create a surface from the sliding interface zone. Creating empty surface.

Note: zone-surface: cannot create surface from sliding interface zone. Creating empty surface.

Note: zone-surface: cannot create surface from sliding interface zone. Creating empty surface.

Note: zone-surface: cannot create surface from sliding interface zone. Creating empty surface.

Note: zone-surface: cannot create surface from sliding interface zone. Creating empty surface.

Note: zone-surface: cannot create surface from sliding interface zone. Creating empty surface.

Note: zone-surface: cannot create surface from sliding interface zone. Creating an empty surface.

Note: zone-surface: cannot create a surface from the sliding interface zone. Creating an empty surface.

Note: zone-surface: cannot create a surface from the sliding interface zone. Creating an empty surface.

Done.

Writing	Settings	file	"C:\Users\Onjefu\AppData\Local\Temp\WB_ONJEFU- PC_Onjefu_1080_2\unsaved_project_files\dp0\FFF\Fluent\FFF.set"...

writing rp variables ... Done. writing domain variables ... Done.

writing part_1 (type fluid) (mixture) ... Done. writing part_2 (type fluid) (mixture) ... Done. writing part_3 (type fluid) (mixture) ... Done. writing part_4 (type fluid) (mixture) ... Done. writing part_5 (type fluid) (mixture) ... Done. writing wall-51 (type wall) (mixture) ... Done. writing wall-50 (type wall) (mixture) ... Done. writing wall-49 (type wall) (mixture) ... Done. writing wall-48 (type wall) (mixture) ... Done. writing wall-47 (type wall) (mixture) ... Done. writing wall-46 (type wall) (mixture) ... Done. writing wall-45 (type wall) (mixture) ... Done.

writing interior-44 (type interior) (mixture) ... Done.

writing interior-43 (type interior) (mixture) ... Done. writing interior-42 (type interior) (mixture) ... Done. writing interior-41 (type interior) (mixture) ... Done. writing interior-40 (type interior) (mixture) ... Done. writing interior-39 (type interior) (mixture) ... Done. writing interior-38 (type interior) (mixture) ... Done. writing interior-37 (type interior) (mixture) ... Done. writing interior-36 (type interior) (mixture) ... Done. writing interior-35 (type interior) (mixture) ... Done.

writing interior-34 (type interior) (mixture) ... Done. writing interior-33 (type interior) (mixture) ... Done. writing wall-32 (type wall) (mixture) ... Done.

writing wall-31 (type wall) (mixture) ... Done.

writing interior-14 (type interior) (mixture) ... Done. writing wall-part_3 (type wall) (mixture) ... Done. writing wall-part_5 (type wall) (mixture) ... Done.

writing interior-part_1 (type interior) (mixture) ... Done.

writing interior-part_2 (type interior) (mixture) ... Done. writing interior-part_3 (type interior) (mixture) ... Done. writing interior-part_4 (type interior) (mixture) ... Done. writing interior-part_5 (type interior) (mixture) ... Done. writing heated_side (type wall) (mixture) ... Done. writing southern_side (type wall) (mixture) ... Done. writing top (type wall) (mixture) ... Done.

writing east_side (type wall) (mixture) ... Done. writing north_side (type wall) (mixture) ... Done. writing insulation (type wall) (mixture) ... Done. writing window (type wall) (mixture) ... Done.

writing contact_region_3-src (type interface) (mixture) ... Done. writing contact_region_3-trg (type interface) (mixture) ... Done.

writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_1 (type interface) (mixture) ... Done. writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_2 (type interface) (mixture) ... Done. writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_3 (type interface) (mixture) ... Done. writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_4 (type interface) (mixture) ... Done. writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-trg-part_4 (type interface) (mixture) ... Done.

writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-trg-part_5 (type interface) (mixture) ... Done. writing		door-contact_region-contact_region_2-contact_region_4-contact_region_7- contact_region_4-contact_region_7-contact_region_5-contact_region_6-trg	(type	interface) (mixture) ... Done.

writing sliding-interface contact_region_3 ... Done

writing	sliding-interface	contact_region-contact_region_2-contact_region_4-contact_region_7- contact_region_4-contact_region_7-contact_region_5-contact_region_6 ... Done

writing zones map name-id ... Done.

Creating intersection zones for non-conformal interfaces ...done. Creating Surface Cluster...

Total Faces 30115, 30115 Surface Clusters created.

The number of surface clusters in the compute-node 0 is

30115

Writing "C:/Users/Onjefu/Desktop/27summer1.s2s"...

15494 nodes.

1637 mixed wall faces, zone 50.

150 mixed wall faces, zone 49.

154 mixed wall faces, zone 48.

154 mixed wall faces, zone 47.

1504 mixed wall faces, zone 46.

264 triangular wall faces, zone 1.

7498 triangular wall faces, zone 2.

3144 triangular wall faces, zone 15.

2934 triangular wall faces, zone 16.

2920 triangular wall faces, zone 17.

3030 triangular wall faces, zone 18.

3638 triangular wall faces, zone 19.

3044 triangular wall faces, zone 20.

44 triangular wall faces, zone 21.

1637 mixed wall faces, zone 50.

150 mixed wall faces, zone 49.

154 mixed wall faces, zone 48.

154 mixed wall faces, zone 47.

1504 mixed wall faces, zone 46.

264 triangular wall faces, zone 1.

7498 triangular wall faces, zone 2.

3144 triangular wall faces, zone 15.

2934 triangular wall faces, zone 16.

2920 triangular wall faces, zone 17.

3030 triangular wall faces, zone 18.

3638 triangular wall faces, zone 19.

3044 triangular wall faces, zone 20.

44 triangular wall faces, zone 21.

The number of radiating faces and radiating clusters in compute node 0 is

30115,30115

Done.

# Using MPI with 1 process...

# Using OpenMP with 1 thread per MPI process...

# 0 Onjefu-PC

# Read parameter section...

# Create BSP tree...

# Maximum tree depth = 19

# Calculate and write view factors...

# 100% done! Opening library "C:\PROGRA~1\ANSYSS~1\v182\fluent\fluent18.2.0/utility/raytracing/win64/librtp"... done. Linking to library symbols ...# CPU time: 28.249 (s)

# Wall time: 28 (s)

Reading "C:/Users/Onjefu/Desktop/27summer1.s2s"...

Reading radiating clusters (30115) and view factor values from

C:/Users/Onjefu/Desktop/27summer1.s2s...

Done.

The number of radiating surface clusters in the compute-node 0 is

30115

Initialized VF Storage

Completed 100% reading of view factors

The mesh has been modified.

Previously saved S2S files are incompatible and cannot be read.

warning: for compressible (ideal and real) gas models with buoyancy, it is recommended to use a specified operating density value of zero. GUI access: Cell Zone/Boundary Conditions -> Operating Conditions... TUI access: define operating-conditions operating-density?

warning: for compressible (ideal and real) gas models with buoyancy, it is recommended to use a specified operating density value of zero.

warning: for compressible (ideal and real) gas models with buoyancy, it is recommended to use a specified operating density value of zero.

Changing smoother type to ilu, post-sweeps to 3, coarsening group size to 8, max number of fixed cycles to 30 for scalar parameters.

Initialize using the hybrid initialization method.

Checking case topology...

-This case has no inlets & no outlets

-Case will be initialized with constant parameters

hybrid initialization is done.

Registering S2s, ("C:/Users/Onjefu/Desktop/27summer1.s2s")

Writing	Settings	file	"C:\Users\Onjefu\AppData\Local\Temp\WB_ONJEFU- PC_Onjefu_1080_2\unsaved_project_files\dp0\FFF\Fluent\FFF.set"...

writing rp variables ... Done. writing domain variables ... Done.

writing part_1 (type fluid) (mixture) ... Done. writing part_2 (type fluid) (mixture) ... Done. writing part_3 (type fluid) (mixture) ... Done. writing part_4 (type fluid) (mixture) ... Done. writing part_5 (type fluid) (mixture) ... Done. writing wall-51 (type wall) (mixture) ... Done. writing wall-50 (type wall) (mixture) ... Done. writing wall-49 (type wall) (mixture) ... Done. writing wall-48 (type wall) (mixture) ... Done. writing wall-47 (type wall) (mixture) ... Done. writing wall-46 (type wall) (mixture) ... Done. writing wall-45 (type wall) (mixture) ... Done.

writing interior-44 (type interior) (mixture) ... Done.

writing interior-43 (type interior) (mixture) ... Done. writing interior-42 (type interior) (mixture) ... Done. writing interior-41 (type interior) (mixture) ... Done. writing interior-40 (type interior) (mixture) ... Done. writing interior-39 (type interior) (mixture) ... Done. writing interior-38 (type interior) (mixture) ... Done. writing interior-37 (type interior) (mixture) ... Done. writing interior-36 (type interior) (mixture) ... Done. writing interior-35 (type interior) (mixture) ... Done. writing interior-34 (type interior) (mixture) ... Done. writing interior-33 (type interior) (mixture) ... Done. writing wall-32 (type wall) (mixture) ... Done.

writing wall-31 (type wall) (mixture) ... Done.

writing interior-14 (type interior) (mixture) ... Done. writing wall-part_3 (type wall) (mixture) ... Done.

writing wall-part_5 (type wall) (mixture) ... Done.

writing interior-part_1 (type interior) (mixture) ... Done. writing interior-part_2 (type interior) (mixture) ... Done. writing interior-part_3 (type interior) (mixture) ... Done. writing interior-part_4 (type interior) (mixture) ... Done. writing interior-part_5 (type interior) (mixture) ... Done. writing heated_side (type wall) (mixture) ... Done. writing southern_side (type wall) (mixture) ... Done. writing top (type wall) (mixture) ... Done.

writing east_side (type wall) (mixture) ... Done.

writing north_side (type wall) (mixture) ... Done. Writing insulation (type wall) (mixture) ... Done. Writing window (type wall) (mixture) ... Done.

writing contact_region_3-src (type interface) (mixture) ... Done. writing contact_region_3-trg (type interface) (mixture) ... Done.

writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_1 (type interface) (mixture) ... Done. writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_2 (type interface) (mixture) ... Done. writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_3 (type interface) (mixture) ... Done. writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-src-part_4 (type interface) (mixture) ... Done. writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-trg-part_4 (type interface) (mixture) ... Done. writing	contact_region-contact_region_2-contact_region_4-contact_region_7-contact_region_4- contact_region_7-contact_region_5-contact_region_6-trg-part_5 (type interface) (mixture) ... Done. writing		door-contact_region-contact_region_2-contact_region_4-contact_region_7- contact_region_4-contact_region_7-contact_region_5-contact_region_6-trg	(type	interface) (mixture) ... Done.

writing sliding-interface contact_region_3 ... Done

writing	sliding-interface	contact_region-contact_region_2-contact_region_4-contact_region_7- contact_region_4-contact_region_7-contact_region_5-contact_region_6 ... Done

writing zones map name-id ... Done.

Writing "| gzip -2cf > FFF-Setup-Output.cas.gz"...

Writing temporary file C:\Users\Onjefu\AppData\Local\Temp\flntgz-27882 ...

77 hexahedral cells, zone 8, binary.

77 hexahedral cells, zone 9, binary.

6928 tetrahedral cells, zone 10, binary.

54045 tetrahedral cells, zone 11, binary.

285366 tetrahedral cells, zone 12, binary.

1637 mixed wall faces, zone 50, binary.

150 mixed wall faces, zone 49, binary.

154 mixed wall faces, zone 48, binary.

154 mixed wall faces, zone 47, binary.

1504 mixed wall faces, zone 46, binary.

72 mixed interior faces, zone 44, binary.

302 mixed interior faces, zone 38, binary.

117 mixed interior faces, zone 37, binary.

65783 mixed interior faces, zone 34, binary.

72 mixed interior faces, zone 14, binary.

264 triangular wall faces, zone 1, binary.

7498 triangular wall faces, zone 2, binary.

136 quadrilateral interior faces, zone 3, binary.

136 quadrilateral interior faces, zone 4, binary.

12877 triangular interior faces, zone 5, binary.

97396 triangular interior faces, zone 6, binary.

546126 triangular interior faces, zone 7, binary.

3144 triangular wall faces, zone 15, binary.

2934 triangular wall faces, zone 16, binary.

2920 triangular wall faces, zone 17, binary.

3030 triangular wall faces, zone 18, binary.

3638 triangular wall faces, zone 19, binary.

3044 triangular wall faces, zone 20, binary.

44 triangular wall faces, zone 21, binary.

36 quadrilateral interface faces, zone 22, binary.

72 triangular interface faces, zone 23, binary.

190 quadrilateral interface faces, zone 24, binary.

154 quadrilateral interface faces, zone 25, binary.

1694 triangular interface faces, zone 26, binary.

21130 triangular interface faces, zone 27, binary.

186 triangular interface faces, zone 28, binary.

22810 triangular interface faces, zone 29, binary.

150 triangular interface faces, zone 30, binary.

1637 wall parent pointers, zone 50, binary.

150 wall parent pointers, zone 49, binary.

154 wall parent pointers, zone 48, binary.

154 wall parent pointers, zone 47, binary.

1504 wall parent pointers, zone 46, binary.

72 interior parent pointers, zone 44, binary.

302 interior parent pointers, zone 38, binary.

117 interior parent pointers, zone 37, binary.

65783 interior parent pointers, zone 34, binary.

72 interior parent pointers, zone 14, binary.

1637 interface metric data, zone 50, binary.

150 interface metric data, zone 49, binary.

154 interface metric data, zone 48, binary.

154 interface metric data, zone 47, binary.

1504 interface metric data, zone 46, binary.

72 interface metric data, zone 44, binary.

302 interface metric data, zone 38, binary.

117 interface metric data, zone 37, binary.

65783 interface metric data, zone 34, binary.

76434 nodes, binary.

76434 node flags, binary. Done.

iter continuity x-velocity y-velocity z-velocity energy time/iter

Radiosity converged after 3 iterations

Final radiosity residual = 1.595955e-06

1 0.0000e+00 0.0000e+00 4.3387e+01 0.0000e+00 4.0808e-06 0:59:51 399

2 1.0000e+00 1.0599e-01 1.4324e-01 1.0689e-01 1.3416e-05 0:53:04 398

3 6.2110e-01 9.2433e-02 1.4214e-01 9.3105e-02 1.5556e-05 0:47:38 397

4 4.6572e-01 6.6966e-02 8.2626e-02 6.7458e-02 2.1843e-05 0:43:18 396

5 3.7651e-01 6.7218e-02 7.9117e-02 6.7805e-02 2.2825e-05 0:39:49 395

6 2.6507e-01 5.0599e-02 6.8906e-02 5.0949e-02 2.5789e-05 0:35:43 394

7 2.1907e-01 4.9799e-02 9.3087e-02 5.0377e-02 3.3300e-05 0:33:44 393

8 2.1823e-01 6.8412e-02 1.7702e-01 6.9467e-02 5.2123e-05 0:32:09 392

9 2.3429e-01 1.2909e-01 3.6885e-01 1.3156e-01 6.4248e-05 0:30:52 391

Radiosity converged after 3 iterations

Final radiosity residual = 1.536456e-06

10 1.9785e-01 2.0556e-01 5.6568e-01 2.1000e-01 5.8566e-05 0:28:32 390

11 1.4875e-01 1.9709e-01 5.3856e-01 2.0266e-01 5.4944e-05 0:27:57 389 iter continuity x-velocity y-velocity z-velocity energy time/iter

12 1.1428e-01 1.0957e-01 3.0656e-01 1.1392e-01 4.9198e-05 0:27:29 388

13 8.7156e-02 6.7949e-02 2.0332e-01 7.2944e-02 4.4858e-05 0:27:05 387

14 6.8992e-02 5.0298e-02 1.2868e-01 5.4351e-02 4.1740e-05 0:26:46 386

15 5.5552e-02 4.1176e-02 8.0271e-02 4.3674e-02 4.1165e-05 0:26:29 385

16 4.5847e-02 3.7646e-02 5.2542e-02 3.8697e-02 4.2370e-05 0:26:15 384

17 3.8369e-02 3.6257e-02 5.0932e-02 3.6086e-02 4.6380e-05 0:26:03 383

18 3.2681e-02 3.7408e-02 7.8842e-02 3.6859e-02 4.7957e-05 0:25:53 382

19 2.6634e-02 3.6683e-02 1.0030e-01 3.5972e-02 5.3349e-05 0:25:44 381

Radiosity converged after 3 iterations

Final radiosity residual = 1.579984e-06

21 1.8760e-02 4.3596e-02 1.6745e-01 4.5166e-02 6.7760e-05 0:24:13 379

22 1.5949e-02 4.8227e-02 2.0125e-01 5.2168e-02 6.9444e-05 0:24:22 378 iter continuity x-velocity y-velocity z-velocity energy time/iter

23 1.3582e-02 5.0658e-02 2.2145e-01 5.7126e-02 6.7327e-05 0:24:28 377

24 1.1365e-02 4.7898e-02 2.1380e-01 5.6884e-02 6.2956e-05 0:24:32 376

25 9.5575e-03 4.2197e-02 1.8081e-01 5.0821e-02 5.8583e-05 0:25:49 375

26 8.4979e-03 3.7813e-02 1.3863e-01 4.3290e-02 5.5490e-05 0:26:50 374

27 7.8321e-03 3.4672e-02 1.0290e-01 3.6827e-02 5.2704e-05 0:27:38 373

28 7.3354e-03 3.1978e-02 7.4118e-02 3.1570e-02 5.0219e-05 0:28:15 372

29 6.8406e-03 2.8730e-02 5.5127e-02 2.7380e-02 4.8676e-05 0:27:29 371

Radiosity converged after 3 iterations

Final radiosity residual = 1.556837e-06

30 6.1944e-03 2.5768e-02 4.7242e-02 2.3994e-02 4.8343e-05 0:28:06 370

31 5.6682e-03 2.3121e-02 4.4430e-02 2.1463e-02 4.8763e-05 0:27:20 369

32 5.1107e-03 2.0726e-02 4.2863e-02 1.9292e-02 4.6550e-05 0:26:43 368

33 4.6857e-03 1.8718e-02 4.1789e-02 1.7686e-02 4.5550e-05 0:26:12 367 iter continuity x-velocity y-velocity z-velocity energy time/iter

34 4.3259e-03 1.6973e-02 4.0576e-02 1.6375e-02 4.4893e-05 0:25:47 366

35 4.0511e-03 1.5478e-02 3.9317e-02 1.5352e-02 4.4350e-05 0:25:26 365

36 3.8083e-03 1.4181e-02 3.7696e-02 1.4429e-02 4.3938e-05 0:25:09 364

37 3.6072e-03 1.3111e-02 3.5829e-02 1.3609e-02 4.3610e-05 0:24:54 363

38 3.4422e-03 1.2227e-02 3.3759e-02 1.2869e-02 4.3413e-05 0:24:42 362

39 3.3169e-03 1.1506e-02 3.1619e-02 1.2202e-02 4.3304e-05 0:25:43 361

Radiosity converged after 3 iterations

Final radiosity residual = 1.648286e-06

40 3.2265e-03 1.0914e-02 2.9474e-02 1.1595e-02 4.3532e-05 0:25:19 360

41 3.1649e-03 1.0411e-02 2.7445e-02 1.1053e-02 4.4846e-05 0:24:59 359

42 3.1242e-03 9.9764e-03 2.5560e-02 1.0570e-02 4.3854e-05 0:24:42 358

43 3.0940e-03 9.6106e-03 2.3875e-02 1.0142e-02 4.3668e-05 0:24:28 357

44 3.0745e-03 9.2975e-03 2.2406e-02 9.7720e-03 4.3703e-05 0:24:16 356 iter continuity x-velocity y-velocity z-velocity energy time/iter

46 3.0554e-03 8.8099e-03 2.0122e-02 9.1998e-03 4.3921e-05 0:23:56 354

47 3.0545e-03 8.6357e-03 1.9274e-02 8.9909e-03 4.4061e-05 0:23:48 353

48 3.0503e-03 8.4958e-03 1.8594e-02 8.8161e-03 4.4169e-05 0:23:41 352

49 3.0499e-03 8.3890e-03 1.8049e-02 8.6839e-03 4.4264e-05 0:23:34 351

Radiosity converged after 3 iterations

Final radiosity residual = 1.648502e-06

50 3.0515e-03 8.3173e-03 1.7619e-02 8.5877e-03 4.4432e-05 0:23:28 350

51 3.0582e-03 8.2715e-03 1.7294e-02 8.5174e-03 4.5488e-05 0:23:23 349

52 3.0709e-03 8.2459e-03 1.7033e-02 8.4694e-03 4.4897e-05 0:23:17 348

53 3.0872e-03 8.2363e-03 1.6837e-02 8.4345e-03 4.4810e-05 0:24:22 347

54 3.1057e-03 8.2436e-03 1.6672e-02 8.4110e-03 4.4846e-05 0:24:03 346

55 3.1253e-03 8.2585e-03 1.6529e-02 8.3990e-03 4.4934e-05 0:23:47 345 iter continuity x-velocity y-velocity z-velocity energy time/iter

56 3.1483e-03 8.2823e-03 1.6425e-02 8.3920e-03 4.5019e-05 0:23:33 344

57 3.1675e-03 8.3156e-03 1.6353e-02 8.3919e-03 4.5081e-05 0:23:22 343

58 3.1866e-03 8.3559e-03 1.6313e-02 8.4020e-03 4.5116e-05 0:23:12 342

59 3.2092e-03 8.4104e-03 1.6302e-02 8.4191e-03 4.5106e-05 0:23:03 341

Radiosity converged after 3 iterations

Final radiosity residual = 1.535961e-06

60 3.2356e-03 8.4700e-03 1.6311e-02 8.4374e-03 4.5072e-05 0:22:55 340

61 3.2649e-03 8.5370e-03 1.6340e-02 8.4617e-03 4.5532e-05 0:22:48 339

62 3.2930e-03 8.6061e-03 1.6379e-02 8.4813e-03 4.5050e-05 0:22:42 338

63 3.3185e-03 8.6775e-03 1.6437e-02 8.4987e-03 4.4839e-05 0:22:36 337

64 3.3496e-03 8.7548e-03 1.6495e-02 8.5156e-03 4.4693e-05 0:22:30 336

65 3.3791e-03 8.8311e-03 1.6564e-02 8.5470e-03 4.4541e-05 0:22:25 335

66 3.4014e-03 8.9080e-03 1.6634e-02 8.5893e-03 4.4375e-05 0:22:20 334 iter continuity x-velocity y-velocity z-velocity energy time/iter

67 3.4259e-03 8.9818e-03 1.6691e-02 8.6356e-03 4.4182e-05 0:22:15 333

68 3.4523e-03 9.0491e-03 1.6741e-02 8.6906e-03 4.3972e-05 0:23:17 332

69 3.4781e-03 9.1104e-03 1.6781e-02 8.7564e-03 4.3740e-05 0:22:59 331

Radiosity converged after 3 iterations

Final radiosity residual = 1.638689e-06

70 3.5018e-03 9.1692e-03 1.6822e-02 8.8292e-03 4.3492e-05 0:22:44 330

71 3.5212e-03 9.2241e-03 1.6854e-02 8.9025e-03 4.3373e-05 0:22:31 329

72 3.5369e-03 9.2817e-03 1.6881e-02 8.9794e-03 4.2935e-05 0:22:20 328

73 3.5546e-03 9.3390e-03 1.6898e-02 9.0601e-03 4.2645e-05 0:22:10 327

74 3.5689e-03 9.4001e-03 1.6910e-02 9.1439e-03 4.2336e-05 0:22:02 326

75 3.5802e-03 9.4649e-03 1.6914e-02 9.2284e-03 4.1988e-05 0:21:54 325

76 3.5863e-03 9.5322e-03 1.6931e-02 9.3116e-03 4.1642e-05 0:21:47 324

77 3.5896e-03 9.5995e-03 1.6954e-02 9.3933e-03 4.1289e-05 0:21:41 323 iter continuity x-velocity y-velocity z-velocity energy time/iter

78 3.5953e-03 9.6675e-03 1.6977e-02 9.4753e-03 4.0946e-05 0:21:35 322

79 3.5984e-03 9.7365e-03 1.7006e-02 9.5545e-03 4.0590e-05 0:21:30 321

Radiosity converged after 3 iterations

Final radiosity residual = 1.602222e-06

80 3.5980e-03 9.8054e-03 1.7042e-02 9.6377e-03 4.0253e-05 0:21:25 320

81 3.5970e-03 9.8756e-03 1.7082e-02 9.7254e-03 3.9855e-05 0:22:23 319

82 3.5973e-03 9.9502e-03 1.7119e-02 9.8086e-03 3.9489e-05 0:22:06 318

83 3.5992e-03 1.0022e-02 1.7153e-02 9.8934e-03 3.9129e-05 0:21:51 317

84 3.5994e-03 1.0091e-02 1.7178e-02 9.9755e-03 3.8796e-05 0:21:38 316

85 3.5952e-03 1.0159e-02 1.7196e-02 1.0052e-02 3.8450e-05 0:21:27 315

86 3.5916e-03 1.0231e-02 1.7212e-02 1.0130e-02 3.8114e-05 0:21:18 314

87 3.5830e-03 1.0301e-02 1.7225e-02 1.0207e-02 3.7776e-05 0:21:09 313

88 3.5761e-03 1.0376e-02 1.7235e-02 1.0285e-02 3.7469e-05 0:21:02 312 iter continuity x-velocity y-velocity z-velocity energy time/iter

89 3.5686e-03 1.0443e-02 1.7239e-02 1.0361e-02 3.7173e-05 0:20:55 311

Radiosity converged after 3 iterations

Final radiosity residual = 1.596996e-06

90 3.5550e-03 1.0500e-02 1.7246e-02 1.0431e-02 3.6863e-05 0:20:49 310

91 3.5478e-03 1.0555e-02 1.7254e-02 1.0496e-02 3.6569e-05 0:20:43 309

92 3.5403e-03 1.0607e-02 1.7253e-02 1.0561e-02 3.6278e-05 0:20:38 308

93 3.5291e-03 1.0647e-02 1.7252e-02 1.0613e-02 3.5999e-05 0:21:34 307

94 3.5175e-03 1.0692e-02 1.7259e-02 1.0651e-02 3.5715e-05 0:21:17 306

95 3.5039e-03 1.0731e-02 1.7262e-02 1.0683e-02 3.5455e-05 0:21:02 305

96 3.4870e-03 1.0759e-02 1.7277e-02 1.0711e-02 3.5219e-05 0:20:49 304

97 3.4700e-03 1.0784e-02 1.7296e-02 1.0733e-02 3.4992e-05 0:20:39 303

98 3.4515e-03 1.0807e-02 1.7314e-02 1.0752e-02 3.4753e-05 0:20:29 302

99 3.4331e-03 1.0826e-02 1.7337e-02 1.0768e-02 3.4488e-05 0:20:21 301

Radiosity converged after 3 iterations

Final radiosity residual = 1.732350e-06

iter continuity x-velocity y-velocity z-velocity energy time/iter

100 3.4163e-03 1.0836e-02 1.7378e-02 1.0786e-02 3.4247e-05 0:20:13 300

101 3.4012e-03 1.0852e-02 1.7415e-02 1.0803e-02 3.3986e-05 0:20:07 299

102 3.3830e-03 1.0875e-02 1.7457e-02 1.0824e-02 3.3811e-05 0:20:01 298

103 3.3627e-03 1.0901e-02 1.7489e-02 1.0840e-02 3.3632e-05 0:19:55 297

104 3.3423e-03 1.0933e-02 1.7514e-02 1.0858e-02 3.3457e-05 0:19:49 296

105 3.3205e-03 1.0962e-02 1.7540e-02 1.0876e-02 3.3321e-05 0:19:44 295

106 3.3015e-03 1.0992e-02 1.7569e-02 1.0899e-02 3.3209e-05 0:19:39 294

107 3.2830e-03 1.1029e-02 1.7602e-02 1.0920e-02 3.3079e-05 0:20:33 293

108 3.2660e-03 1.1066e-02 1.7640e-02 1.0944e-02 3.2949e-05 0:20:17 292

109 3.2494e-03 1.1103e-02 1.7686e-02 1.0966e-02 3.2842e-05 0:20:03 291

Radiosity converged after 3 iterations

Final radiosity residual = 1.641389e-06

110 3.2304e-03 1.1146e-02 1.7733e-02 1.0987e-02 3.2773e-05 0:19:51 290 iter continuity x-velocity y-velocity z-velocity energy time/iter

111 3.2099e-03 1.1183e-02 1.7784e-02 1.1015e-02 3.2673e-05 0:19:41 289

112 3.1870e-03 1.1221e-02 1.7840e-02 1.1048e-02 3.2626e-05 0:19:32 288

113 3.1672e-03 1.1258e-02 1.7896e-02 1.1086e-02 3.2594e-05 0:19:24 287

114 3.1495e-03 1.1297e-02 1.7953e-02 1.1129e-02 3.2557e-05 0:19:17 286

115 3.1298e-03 1.1338e-02 1.8014e-02 1.1177e-02 3.2510e-05 0:19:10 285

116 3.1133e-03 1.1380e-02 1.8076e-02 1.1230e-02 3.2435e-05 0:19:04 284

117 3.1010e-03 1.1420e-02 1.8141e-02 1.1283e-02 3.2353e-05 0:18:58 283

118 3.0871e-03 1.1463e-02 1.8216e-02 1.1337e-02 3.2282e-05 0:18:53 282

119 3.0688e-03 1.1503e-02 1.8293e-02 1.1400e-02 3.2233e-05 0:18:48 281

Radiosity converged after 3 iterations

Final radiosity residual = 1.663552e-06

120 3.0516e-03 1.1539e-02 1.8370e-02 1.1466e-02 3.2236e-05 0:19:39 280

121 3.0362e-03 1.1579e-02 1.8450e-02 1.1534e-02 3.2188e-05 0:19:23 279 iter continuity x-velocity y-velocity z-velocity energy time/iter

122 3.0227e-03 1.1625e-02 1.8537e-02 1.1606e-02 3.2083e-05 0:19:10 278

123 3.0154e-03 1.1674e-02 1.8625e-02 1.1689e-02 3.2033e-05 0:18:58 277

124 3.0061e-03 1.1723e-02 1.8702e-02 1.1771e-02 3.2024e-05 0:18:48 276

125 2.9939e-03 1.1777e-02 1.8780e-02 1.1849e-02 3.1994e-05 0:18:39 275

126 2.9822e-03 1.1826e-02 1.8862e-02 1.1923e-02 3.1965e-05 0:18:31 274

127 2.9674e-03 1.1883e-02 1.8940e-02 1.1994e-02 3.1924e-05 0:18:24 273

128 2.9530e-03 1.1939e-02 1.9027e-02 1.2060e-02 3.1902e-05 0:18:18 272

129 2.9404e-03 1.1992e-02 1.9096e-02 1.2130e-02 3.1901e-05 0:18:12 271

Radiosity converged after 3 iterations

Final radiosity residual = 1.636573e-06

130 2.9301e-03 1.2048e-02 1.9156e-02 1.2195e-02 3.1960e-05 0:18:06 270

131 2.9202e-03 1.2104e-02 1.9196e-02 1.2263e-02 3.1948e-05 0:18:01 269

132 2.9103e-03 1.2161e-02 1.9250e-02 1.2328e-02 3.1847e-05 0:17:56 268 iter continuity x-velocity y-velocity z-velocity energy time/iter

133 2.9000e-03 1.2219e-02 1.9303e-02 1.2388e-02 3.1830e-05 0:17:51 267

134 2.8872e-03 1.2269e-02 1.9346e-02 1.2442e-02 3.1829e-05 0:17:46 266

135 2.8749e-03 1.2312e-02 1.9377e-02 1.2494e-02 3.1823e-05 0:18:35 265

136 2.8644e-03 1.2352e-02 1.9402e-02 1.2542e-02 3.1812e-05 0:18:20 264

137 2.8520e-03 1.2386e-02 1.9416e-02 1.2591e-02 3.1815e-05 0:18:07 263

138 2.8408e-03 1.2413e-02 1.9415e-02 1.2626e-02 3.1824e-05 0:17:56 262

139 2.8291e-03 1.2430e-02 1.9410e-02 1.2653e-02 3.1838e-05 0:17:46 261

Radiosity converged after 3 iterations

Final radiosity residual = 1.614257e-06

140 2.8165e-03 1.2445e-02 1.9415e-02 1.2672e-02 3.1900e-05 0:17:38 260

141 2.8039e-03 1.2457e-02 1.9410e-02 1.2688e-02 3.1884e-05 0:17:30 259

142 2.7883e-03 1.2465e-02 1.9408e-02 1.2692e-02 3.1881e-05 0:17:23 258

143 2.7717e-03 1.2464e-02 1.9404e-02 1.2689e-02 3.1892e-05 0:17:17 257 iter continuity x-velocity y-velocity z-velocity energy time/iter

144 2.7560e-03 1.2463e-02 1.9392e-02 1.2692e-02 3.1892e-05 0:17:11 256

145 2.7402e-03 1.2458e-02 1.9365e-02 1.2694e-02 3.1889e-05 0:17:06 255

146 2.7217e-03 1.2442e-02 1.9336e-02 1.2693e-02 3.1871e-05 0:17:51 254

147 2.7026e-03 1.2429e-02 1.9303e-02 1.2692e-02 3.1853e-05 0:17:36 253

148 2.6838e-03 1.2413e-02 1.9269e-02 1.2690e-02 3.1842e-05 0:17:23 252

149 2.6658e-03 1.2391e-02 1.9233e-02 1.2684e-02 3.1815e-05 0:17:12 251

Radiosity converged after 3 iterations

Final radiosity residual = 1.661784e-06

150 2.6519e-03 1.2368e-02 1.9200e-02 1.2675e-02 3.1831e-05 0:17:02 250

151 2.6405e-03 1.2348e-02 1.9167e-02 1.2662e-02 3.1810e-05 0:16:54 249

152 2.6257e-03 1.2327e-02 1.9145e-02 1.2648e-02 3.1724e-05 0:16:46 248

153 2.6114e-03 1.2307e-02 1.9130e-02 1.2632e-02 3.1683e-05 0:16:39 247

154 2.6009e-03 1.2291e-02 1.9120e-02 1.2615e-02 3.1680e-05 0:16:33 246 iter continuity x-velocity y-velocity z-velocity energy time/iter

155 2.5918e-03 1.2276e-02 1.9111e-02 1.2591e-02 3.1660e-05 0:16:27 245

156 2.5780e-03 1.2259e-02 1.9099e-02 1.2563e-02 3.1623e-05 0:16:22 244

157 2.5683e-03 1.2244e-02 1.9092e-02 1.2537e-02 3.1557e-05 0:16:17 243

158 2.5586e-03 1.2228e-02 1.9077e-02 1.2512e-02 3.1504e-05 0:17:00 242

159 2.5473e-03 1.2211e-02 1.9069e-02 1.2477e-02 3.1456e-05 0:16:45 241

Radiosity converged after 3 iterations

Final radiosity residual = 1.649527e-06

160 2.5352e-03 1.2191e-02 1.9055e-02 1.2442e-02 3.1455e-05 0:16:33 240

161 2.5241e-03 1.2167e-02 1.9045e-02 1.2406e-02 3.1397e-05 0:16:22 239

162 2.5097e-03 1.2143e-02 1.9038e-02 1.2373e-02 3.1271e-05 0:16:13 238

163 2.4931e-03 1.2113e-02 1.9029e-02 1.2338e-02 3.1195e-05 0:16:05 237

164 2.4753e-03 1.2085e-02 1.9022e-02 1.2296e-02 3.1118e-05 0:15:57 236

165 2.4569e-03 1.2061e-02 1.9012e-02 1.2252e-02 3.1033e-05 0:15:51 235 iter continuity x-velocity y-velocity z-velocity energy time/iter

Final radiosity residual = 1.601468e-06

170 2.3874e-03 1.1946e-02 1.8912e-02 1.2038e-02 3.0494e-05 0:16:00 230

171 2.3735e-03 1.1929e-02 1.8888e-02 1.1988e-02 3.0307e-05 0:15:48 229

172 2.3576e-03 1.1909e-02 1.8873e-02 1.1940e-02 3.0116e-05 0:15:38 228

173 2.3435e-03 1.1888e-02 1.8856e-02 1.1903e-02 2.9953e-05 0:15:28 227

174 2.3282e-03 1.1871e-02 1.8832e-02 1.1869e-02 2.9785e-05 0:15:20 226

175 2.3127e-03 1.1851e-02 1.8811e-02 1.1840e-02 2.9609e-05 0:15:13 225

176 2.2971e-03 1.1840e-02 1.8798e-02 1.1819e-02 2.9434e-05 0:15:06 224 iter continuity x-velocity y-velocity z-velocity energy time/iter

177 2.2820e-03 1.1829e-02 1.8781e-02 1.1793e-02 2.9255e-05 0:15:00 223

178 2.2694e-03 1.1824e-02 1.8758e-02 1.1773e-02 2.9074e-05 0:14:55 222

179 2.2558e-03 1.1819e-02 1.8748e-02 1.1752e-02 2.8900e-05 0:14:49 221

Radiosity converged after 3 iterations

Final radiosity residual = 1.597548e-06

180 2.2427e-03 1.1821e-02 1.8735e-02 1.1731e-02 2.8784e-05 0:14:44 220

181 2.2304e-03 1.1820e-02 1.8727e-02 1.1706e-02 2.8609e-05 0:14:39 219

182 2.2211e-03 1.1818e-02 1.8706e-02 1.1678e-02 2.8429e-05 0:14:35 218

183 2.2109e-03 1.1809e-02 1.8687e-02 1.1647e-02 2.8296e-05 0:15:13 217

184 2.2000e-03 1.1800e-02 1.8670e-02 1.1613e-02 2.8145e-05 0:15:00 216

185 2.1906e-03 1.1791e-02 1.8646e-02 1.1578e-02 2.7995e-05 0:14:49 215

186 2.1811e-03 1.1776e-02 1.8628e-02 1.1536e-02 2.7849e-05 0:14:39 214

187 2.1715e-03 1.1756e-02 1.8615e-02 1.1496e-02 2.7707e-05 0:14:30 213 iter continuity x-velocity y-velocity z-velocity energy time/iter

188 2.1600e-03 1.1729e-02 1.8592e-02 1.1462e-02 2.7562e-05 0:14:23 212

189 2.1459e-03 1.1703e-02 1.8563e-02 1.1427e-02 2.7433e-05 0:14:16 211

Radiosity converged after 3 iterations

Final radiosity residual = 1.632020e-06

195 2.0766e-03 1.1488e-02 1.8293e-02 1.1240e-02 2.6673e-05 0:13:43 205

196 2.0638e-03 1.1450e-02 1.8261e-02 1.1209e-02 2.6538e-05 0:14:19 204

197 2.0527e-03 1.1413e-02 1.8231e-02 1.1180e-02 2.6408e-05 0:14:06 203

198 2.0426e-03 1.1371e-02 1.8199e-02 1.1150e-02 2.6216e-05 0:13:15 202 iter continuity x-velocity y-velocity z-velocity energy time/iter

199 2.0413e-03 1.1300e-02 1.8206e-02 1.1098e-02 2.6104e-05 0:13:14 201

Radiosity converged after 3 iterations

Final radiosity residual = 1.617127e-06

200 2.0221e-03 1.1275e-02 1.8134e-02 1.1093e-02 2.6058e-05 0:13:12 200

201 2.0130e-03 1.1234e-02 1.8076e-02 1.1075e-02 2.5965e-05 0:13:49 199

202 2.0025e-03 1.1196e-02 1.8028e-02 1.1059e-02 2.5820e-05 0:13:38 198

203 1.9922e-03 1.1161e-02 1.7974e-02 1.1043e-02 2.5740e-05 0:13:29 197

204 1.9792e-03 1.1132e-02 1.7912e-02 1.1025e-02 2.5664e-05 0:13:21 196

205 1.9684e-03 1.1102e-02 1.7843e-02 1.1005e-02 2.5509e-05 0:12:34 195

206 1.9659e-03 1.1048e-02 1.7831e-02 1.0963e-02 2.5452e-05 0:12:36 194

207 1.9462e-03 1.1036e-02 1.7746e-02 1.0967e-02 2.5396e-05 0:13:14 193

208 1.9357e-03 1.1010e-02 1.7685e-02 1.0951e-02 2.5326e-05 0:13:06 192

209 1.9266e-03 1.0989e-02 1.7629e-02 1.0931e-02 2.5259e-05 0:12:58 191

Radiosity converged after 3 iterations

Final radiosity residual = 1.580432e-06

iter continuity x-velocity y-velocity z-velocity energy time/iter

210 1.9152e-03 1.0974e-02 1.7581e-02 1.0913e-02 2.5249e-05 0:12:51 190

211 1.9018e-03 1.0956e-02 1.7546e-02 1.0894e-02 2.5113e-05 0:12:45 189

212 1.9009e-03 1.0919e-02 1.7565e-02 1.0848e-02 2.5035e-05 0:12:39 188

213 1.8825e-03 1.0916e-02 1.7503e-02 1.0845e-02 2.4984e-05 0:12:34 187

214 1.8714e-03 1.0895e-02 1.7450e-02 1.0825e-02 2.4855e-05 0:11:51 186

215 1.8673e-03 1.0852e-02 1.7458e-02 1.0776e-02 2.4815e-05 0:11:54 185

Final radiosity residual = 1.584302e-06

220 1.8091e-03 1.0797e-02 1.7238e-02 1.0655e-02 2.4570e-05 0:11:52 180 iter continuity x-velocity y-velocity z-velocity energy time/iter

221 1.7995e-03 1.0781e-02 1.7201e-02 1.0631e-02 2.4440e-05 0:11:49 179

222 1.7987e-03 1.0749e-02 1.7223e-02 1.0585e-02 2.4341e-05 0:11:47 178

223 1.7826e-03 1.0759e-02 1.7172e-02 1.0588e-02 2.4275e-05 0:11:44 177

224 1.7752e-03 1.0753e-02 1.7146e-02 1.0577e-02 2.4223e-05 0:11:41 176

225 1.7650e-03 1.0741e-02 1.7130e-02 1.0562e-02 2.4113e-05 0:11:37 175

226 1.7645e-03 1.0714e-02 1.7164e-02 1.0528e-02 2.4084e-05 0:11:34 174

227 1.7501e-03 1.0718e-02 1.7125e-02 1.0541e-02 2.4052e-05 0:11:30 173

228 1.7432e-03 1.0704e-02 1.7104e-02 1.0536e-02 2.4035e-05 0:11:27 172

229 1.7371e-03 1.0686e-02 1.7089e-02 1.0528e-02 2.4023e-05 0:11:23 171

Radiosity converged after 3 iterations

Final radiosity residual = 1.676636e-06

230 1.7331e-03 1.0672e-02 1.7066e-02 1.0523e-02 2.3995e-05 0:11:19 170

231 1.7344e-03 1.0637e-02 1.7092e-02 1.0495e-02 2.3994e-05 0:11:15 169 iter continuity x-velocity y-velocity z-velocity energy time/iter

232 1.7203e-03 1.0636e-02 1.7045e-02 1.0510e-02 2.3922e-05 0:11:11 168

233 1.7145e-03 1.0622e-02 1.7016e-02 1.0509e-02 2.3792e-05 0:11:08 167

234 1.7143e-03 1.0589e-02 1.7053e-02 1.0478e-02 2.3776e-05 0:11:04 166

235 1.7014e-03 1.0594e-02 1.7009e-02 1.0485e-02 2.3740e-05 0:11:00 165

236 1.6940e-03 1.0583e-02 1.6976e-02 1.0472e-02 2.3599e-05 0:10:56 164

237 1.6936e-03 1.0551e-02 1.7008e-02 1.0432e-02 2.3557e-05 0:10:52 163

238 1.6775e-03 1.0558e-02 1.6946e-02 1.0431e-02 2.3417e-05 0:10:15 162

239 1.6749e-03 1.0535e-02 1.6974e-02 1.0389e-02 2.3358e-05 0:10:18 161

Radiosity converged after 3 iterations

Final radiosity residual = 1.649814e-06

244 1.6339e-03 1.0530e-02 1.6773e-02 1.0307e-02 2.2971e-05 0:10:16 156

245 1.6269e-03 1.0515e-02 1.6730e-02 1.0292e-02 2.2806e-05 0:10:13 155

246 1.6272e-03 1.0479e-02 1.6745e-02 1.0259e-02 2.2744e-05 0:10:11 154

247 1.6143e-03 1.0482e-02 1.6681e-02 1.0266e-02 2.2681e-05 0:10:08 153

248 1.6093e-03 1.0464e-02 1.6641e-02 1.0261e-02 2.2601e-05 0:10:05 152

249 1.6024e-03 1.0449e-02 1.6610e-02 1.0253e-02 2.2452e-05 0:10:01 151

Radiosity converged after 3 iterations

Final radiosity residual = 1.488330e-06

250 1.5996e-03 1.0414e-02 1.6623e-02 1.0216e-02 2.2449e-05 0:09:58 150

251 1.5850e-03 1.0418e-02 1.6558e-02 1.0219e-02 2.2371e-05 0:09:54 149

252 1.5788e-03 1.0409e-02 1.6505e-02 1.0213e-02 2.2265e-05 0:09:51 148

253 1.5716e-03 1.0394e-02 1.6461e-02 1.0204e-02 2.2116e-05 0:09:47 147 iter continuity x-velocity y-velocity z-velocity energy time/iter

254 1.5716e-03 1.0359e-02 1.6464e-02 1.0175e-02 2.2062e-05 0:09:43 146

255 1.5581e-03 1.0364e-02 1.6395e-02 1.0181e-02 2.1981e-05 0:09:39 145

256 1.5519e-03 1.0353e-02 1.6343e-02 1.0171e-02 2.1813e-05 0:09:35 144

257 1.5533e-03 1.0319e-02 1.6349e-02 1.0136e-02 2.1750e-05 0:09:32 143

258 1.5414e-03 1.0318e-02 1.6283e-02 1.0135e-02 2.1659e-05 0:09:28 142

259 1.5369e-03 1.0305e-02 1.6223e-02 1.0114e-02 2.1477e-05 0:08:56 141

Radiosity converged after 3 iterations

Final radiosity residual = 1.646943e-06

260 1.5359e-03 1.0269e-02 1.6220e-02 1.0074e-02 2.1465e-05 0:08:57 140

261 1.5236e-03 1.0269e-02 1.6143e-02 1.0066e-02 2.1363e-05 0:09:26 139

262 1.5169e-03 1.0248e-02 1.6079e-02 1.0047e-02 2.1163e-05 0:08:52 138

263 1.5165e-03 1.0207e-02 1.6083e-02 1.0006e-02 2.1108e-05 0:08:52 137

264 1.5064e-03 1.0196e-02 1.6006e-02 9.9921e-03 2.1022e-05 0:08:52 136 iter continuity x-velocity y-velocity z-velocity energy time/iter

Radiosity converged after 3 iterations

Final radiosity residual = 1.671688e-06

270 1.4652e-03 1.0019e-02 1.5654e-02 9.8260e-03 2.0387e-05 0:08:37 130

271 1.4601e-03 9.9855e-03 1.5573e-02 9.7939e-03 2.0213e-05 0:08:34 129

272 1.4587e-03 9.9359e-03 1.5559e-02 9.7378e-03 2.0129e-05 0:08:30 128

273 1.4445e-03 9.9209e-03 1.5452e-02 9.7198e-03 2.0053e-05 0:08:26 127

274 1.4364e-03 9.8917e-03 1.5376e-02 9.6892e-03 1.9893e-05 0:08:23 126

275 1.4347e-03 9.8401e-03 1.5361e-02 9.6355e-03 1.9833e-05 0:08:19 125 iter continuity x-velocity y-velocity z-velocity energy time/iter

276 1.4230e-03 9.8209e-03 1.5262e-02 9.6088e-03 1.9738e-05 0:08:15 124

277 1.4162e-03 9.7827e-03 1.5185e-02 9.5704e-03 1.9576e-05 0:08:11 123

278 1.4143e-03 9.7251e-03 1.5166e-02 9.5145e-03 1.9526e-05 0:08:08 122

279 1.4024e-03 9.7002e-03 1.5065e-02 9.4876e-03 1.9448e-05 0:08:04 121

Radiosity converged after 3 iterations

Final radiosity residual = 1.567103e-06

280 1.3947e-03 9.6605e-03 1.4993e-02 9.4439e-03 1.9360e-05 0:07:36 120

281 1.3921e-03 9.6016e-03 1.4992e-02 9.3798e-03 1.9309e-05 0:08:01 119

282 1.3803e-03 9.5749e-03 1.4906e-02 9.3496e-03 1.9182e-05 0:07:56 118

283 1.3745e-03 9.5340e-03 1.4848e-02 9.3093e-03 1.9030e-05 0:07:27 117

284 1.3739e-03 9.4768e-03 1.4856e-02 9.2484e-03 1.8993e-05 0:07:28 116

285 1.3615e-03 9.4530e-03 1.4773e-02 9.2224e-03 1.8855e-05 0:08:36 115

286 1.3599e-03 9.3969e-03 1.4781e-02 9.1687e-03 1.8801e-05 0:10:14 114 iter continuity x-velocity y-velocity z-velocity energy time/iter

287 1.3486e-03 9.3747e-03 1.4704e-02 9.1467e-03 1.8728e-05 0:11:08 113

288 1.3430e-03 9.3438e-03 1.4642e-02 9.1143e-03 1.8585e-05 0:11:49 112

289 1.3398e-03 9.2939e-03 1.4645e-02 9.0613e-03 1.8544e-05 0:12:42 111

Radiosity converged after 3 iterations

Final radiosity residual = 1.617653e-06

294 1.3116e-03 9.1296e-03 1.4441e-02 8.9072e-03 1.8160e-05 0:14:01 106

295 1.3015e-03 9.1146e-03 1.4358e-02 8.8987e-03 1.8035e-05 0:13:54 105

296 1.3001e-03 9.0703e-03 1.4361e-02 8.8619e-03 1.7990e-05 0:13:47 104

297 1.2902e-03 9.0606e-03 1.4276e-02 8.8568e-03 1.7920e-05 0:14:01 103 iter continuity x-velocity y-velocity z-velocity energy time/iter

298 1.2845e-03 9.0390e-03 1.4221e-02 8.8383e-03 1.7782e-05 0:13:49 102

299 1.2827e-03 9.0043e-03 1.4240e-02 8.7951e-03 1.7748e-05 0:13:39 101

Radiosity converged after 3 iterations

Final radiosity residual = 1.518614e-06

300 1.2723e-03 9.0049e-03 1.4169e-02 8.7854e-03 1.7695e-05 0:13:28 100

301 1.2704e-03 8.9737e-03 1.4198e-02 8.7447e-03 1.7673e-05 0:13:38 99

302 1.2602e-03 8.9757e-03 1.4131e-02 8.7401e-03 1.7571e-05 0:13:45 98

303 1.2554e-03 8.9645e-03 1.4094e-02 8.7268e-03 1.7442e-05 0:13:09 97

304 1.2534e-03 8.9348e-03 1.4126e-02 8.6970e-03 1.7424e-05 0:13:17 96

305 1.2434e-03 8.9365e-03 1.4057e-02 8.6990e-03 1.7391e-05 0:13:22 95

306 1.2400e-03 8.9246e-03 1.4004e-02 8.6876e-03 1.7276e-05 0:13:05 94

307 1.2397e-03 8.8986e-03 1.4033e-02 8.6583e-03 1.7263e-05 0:12:50 93

308 1.2309e-03 8.9018e-03 1.3975e-02 8.6585e-03 1.7157e-05 0:12:37 92 iter continuity x-velocity y-velocity z-velocity energy time/iter

309 1.2310e-03 8.8780e-03 1.4013e-02 8.6287e-03 1.7144e-05 0:12:43 91

Radiosity converged after 3 iterations

Final radiosity residual = 1.570796e-06

310 1.2237e-03 8.8807e-03 1.3965e-02 8.6320e-03 1.7177e-05 0:12:45 90

311 1.2210e-03 8.8665e-03 1.3939e-02 8.6256e-03 1.7072e-05 0:12:10 89

312 1.2208e-03 8.8381e-03 1.3991e-02 8.6027e-03 1.7032e-05 0:12:16 88

313 1.2124e-03 8.8332e-03 1.3947e-02 8.6114e-03 1.6931e-05 0:12:01 87

314 1.2108e-03 8.8036e-03 1.3997e-02 8.5946e-03 1.6941e-05 0:12:05 86

315 1.2019e-03 8.8033e-03 1.3951e-02 8.6093e-03 1.6867e-05 0:11:32 85

Radiosity converged after 3 iterations

Final radiosity residual = 1.524001e-06

iter continuity x-velocity y-velocity z-velocity energy time/iter

320 1.1916e-03 8.7352e-03 1.4036e-02 8.5784e-03 1.6825e-05 0:09:21 80

321 1.1856e-03 8.7402e-03 1.3998e-02 8.5947e-03 1.6823e-05 0:08:26 79

322 1.1845e-03 8.7366e-03 1.3981e-02 8.5945e-03 1.6722e-05 0:07:42 78

323 1.1845e-03 8.7138e-03 1.4033e-02 8.5761e-03 1.6728e-05 0:07:07 77

324 1.1761e-03 8.7167e-03 1.3997e-02 8.5867e-03 1.6643e-05 0:06:38 76

325 1.1750e-03 8.7004e-03 1.4035e-02 8.5694e-03 1.6650e-05 0:06:14 75

326 1.1676e-03 8.7079e-03 1.3983e-02 8.5811e-03 1.6571e-05 0:05:40 74

327 1.1684e-03 8.6914e-03 1.4016e-02 8.5629e-03 1.6572e-05 0:05:26 73

328 1.1622e-03 8.6995e-03 1.3963e-02 8.5730e-03 1.6544e-05 0:05:30 72

329 1.1602e-03 8.6976e-03 1.3924e-02 8.5678e-03 1.6441e-05 0:05:03 71

Radiosity converged after 3 iterations

Final radiosity residual = 1.595295e-06

330 1.1601e-03 8.6789e-03 1.3952e-02 8.5439e-03 1.6497e-05 0:04:55 70 iter continuity x-velocity y-velocity z-velocity energy time/iter

331 1.1523e-03 8.6891e-03 1.3895e-02 8.5505e-03 1.6404e-05 0:04:48 69

332 1.1533e-03 8.6704e-03 1.3925e-02 8.5303e-03 1.6388e-05 0:04:41 68

333 1.1464e-03 8.6766e-03 1.3865e-02 8.5407e-03 1.6305e-05 0:04:35 67

334 1.1462e-03 8.6586e-03 1.3895e-02 8.5230e-03 1.6309e-05 0:04:30 66

335 1.1389e-03 8.6683e-03 1.3839e-02 8.5348e-03 1.6233e-05 0:04:24 65

336 1.1396e-03 8.6482e-03 1.3872e-02 8.5186e-03 1.6249e-05 0:04:20 64

337 1.1336e-03 8.6609e-03 1.3808e-02 8.5327e-03 1.6162e-05 0:04:02 63

338 1.1333e-03 8.6442e-03 1.3832e-02 8.5127e-03 1.6169e-05 0:04:00 62

339 1.1278e-03 8.6576e-03 1.3766e-02 8.5172e-03 1.6081e-05 0:03:58 61

Radiosity converged after 3 iterations

Final radiosity residual = 1.578897e-06

343 1.1163e-03 8.6741e-03 1.3717e-02 8.4880e-03 1.5928e-05 0:03:34 57

344 1.1164e-03 8.6638e-03 1.3753e-02 8.4730e-03 1.5939e-05 0:03:44 56

345 1.1109e-03 8.6812e-03 1.3708e-02 8.4862e-03 1.5918e-05 0:03:40 55

346 1.1081e-03 8.6834e-03 1.3693e-02 8.4878e-03 1.5826e-05 0:03:25 54

347 1.1078e-03 8.6690e-03 1.3736e-02 8.4739e-03 1.5826e-05 0:03:34 53

348 1.1015e-03 8.6838e-03 1.3697e-02 8.4915e-03 1.5734e-05 0:03:19 52

349 1.1016e-03 8.6674e-03 1.3736e-02 8.4780e-03 1.5733e-05 0:03:17 51

Radiosity converged after 3 iterations

Final radiosity residual = 1.635765e-06

350 1.0951e-03 8.6788e-03 1.3699e-02 8.4933e-03 1.5764e-05 0:03:15 50

351 1.0924e-03 8.6750e-03 1.3678e-02 8.4921e-03 1.5669e-05 0:03:12 49

352 1.0929e-03 8.6490e-03 1.3719e-02 8.4760e-03 1.5663e-05 0:03:09 48 iter continuity x-velocity y-velocity z-velocity energy time/iter

353 1.0871e-03 8.6530e-03 1.3696e-02 8.4854e-03 1.5589e-05 0:03:05 47

354 1.0887e-03 8.6316e-03 1.3745e-02 8.4674e-03 1.5599e-05 0:03:02 46

355 1.0831e-03 8.6335e-03 1.3711e-02 8.4731e-03 1.5516e-05 0:02:58 45

356 1.0850e-03 8.6089e-03 1.3755e-02 8.4502e-03 1.5526e-05 0:02:55 44

357 1.0796e-03 8.6083e-03 1.3713e-02 8.4550e-03 1.5511e-05 0:02:51 43

358 1.0779e-03 8.5989e-03 1.3684e-02 8.4456e-03 1.5414e-05 0:02:39 42

359 1.0779e-03 8.5720e-03 1.3729e-02 8.4197e-03 1.5417e-05 0:02:37 41

Radiosity converged after 3 iterations

Final radiosity residual = 1.579390e-06

360 1.0731e-03 8.5725e-03 1.3692e-02 8.4218e-03 1.5391e-05 0:02:34 40

361 1.0754e-03 8.5458e-03 1.3734e-02 8.3978e-03 1.5403e-05 0:02:32 39

362 1.0697e-03 8.5469e-03 1.3682e-02 8.4015e-03 1.5287e-05 0:02:29 38

363 1.0700e-03 8.5215e-03 1.3719e-02 8.3804e-03 1.5283e-05 0:02:25 37 iter continuity x-velocity y-velocity z-velocity energy time/iter

364 1.0639e-03 8.5220e-03 1.3656e-02 8.3869e-03 1.5268e-05 0:02:22 36

369 1.0516e-03 8.4815e-03 1.3553e-02 8.3603e-03 1.4987e-05 0:01:59 31

Radiosity converged after 3 iterations

Final radiosity residual = 1.644234e-06

370 1.0534e-03 8.4612e-03 1.3586e-02 8.3431e-03 1.5052e-05 0:01:56 30

371 1.0475e-03 8.4706e-03 1.3512e-02 8.3526e-03 1.4969e-05 0:01:53 29

372 1.0494e-03 8.4494e-03 1.3533e-02 8.3334e-03 1.4938e-05 0:01:50 28

373 1.0434e-03 8.4568e-03 1.3452e-02 8.3401e-03 1.4851e-05 0:01:46 27

374 1.0441e-03 8.4305e-03 1.3474e-02 8.3169e-03 1.4856e-05 0:01:43 26 iter continuity x-velocity y-velocity z-velocity energy time/iter

375 1.0380e-03 8.4302e-03 1.3390e-02 8.3220e-03 1.4761e-05 0:01:39 25

376 1.0373e-03 8.4009e-03 1.3407e-02 8.2971e-03 1.4744e-05 0:01:35 24

377 1.0304e-03 8.3993e-03 1.3327e-02 8.2994e-03 1.4646e-05 0:01:27 23

378 1.0311e-03 8.3722e-03 1.3347e-02 8.2708e-03 1.4632e-05 0:01:24 22

379 1.0249e-03 8.3739e-03 1.3280e-02 8.2671e-03 1.4542e-05 0:01:21 21

Radiosity converged after 3 iterations

Final radiosity residual = 1.550098e-06

380 1.0252e-03 8.3428e-03 1.3308e-02 8.2338e-03 1.4595e-05 0:01:18 20

381 1.0175e-03 8.3410e-03 1.3240e-02 8.2275e-03 1.4512e-05 0:01:14 19

382 1.0176e-03 8.3102e-03 1.3266e-02 8.1930e-03 1.4468e-05 0:01:11 18

383 1.0130e-03 8.3030e-03 1.3181e-02 8.1879e-03 1.4370e-05 0:01:04 17

384 1.0141e-03 8.2687e-03 1.3204e-02 8.1553e-03 1.4369e-05 0:01:04 16

385 1.0085e-03 8.2646e-03 1.3129e-02 8.1508e-03 1.4290e-05 0:00:57 15 iter continuity x-velocity y-velocity z-velocity energy time/iter

386 1.0077e-03 8.2302e-03 1.3146e-02 8.1127e-03 1.4281e-05 0:00:54 14

387 1.0018e-03 8.2205e-03 1.3069e-02 8.1033e-03 1.4191e-05 0:00:50 13

388 1.0023e-03 8.1867e-03 1.3086e-02 8.0700e-03 1.4180e-05 0:00:47 12

389 9.9527e-04 8.1804e-03 1.3015e-02 8.0678e-03 1.4090e-05 0:00:43 11

Radiosity converged after 3 iterations

Final radiosity residual = 1.545309e-06

390 9.9368e-04 8.1484e-03 1.3040e-02 8.0375e-03 1.4134e-05 0:00:39 10

391 9.8673e-04 8.1406e-03 1.2976e-02 8.0378e-03 1.4050e-05 0:00:34 9

392 9.8668e-04 8.1048e-03 1.2998e-02 8.0112e-03 1.4014e-05 0:00:30 8

393 9.7965e-04 8.0925e-03 1.2939e-02 8.0149e-03 1.3932e-05 0:00:27 7

394 9.7909e-04 8.0602e-03 1.2968e-02 7.9872e-03 1.3934e-05 0:00:23 6

395 9.7377e-04 8.0562e-03 1.2916e-02 7.9891e-03 1.3860e-05 0:00:19 5

396 9.7415e-04 8.0314e-03 1.2954e-02 7.9658e-03 1.3847e-05 0:00:16 4 iter continuity x-velocity y-velocity z-velocity energy time/iter

397 9.6822e-04 8.0300e-03 1.2901e-02 7.9755e-03 1.3766e-05 0:00:12 3

398 9.6961e-04 8.0069e-03 1.2938e-02 7.9557e-03 1.3761e-05 0:00:08 2

399 9.6417e-04 8.0123e-03 1.2880e-02 7.9689e-03 1.3689e-05 0:00:04 1

Radiosity converged after 3 iterations

Final radiosity residual = 1.683581e-06

400 9.6343e-04 7.9918e-03 1.2915e-02 7.9527e-03 1.3728e-05 0:00:00 0

Registering S2s, ("C:\Users\Onjefu\Desktop\27summer1.s2s")

Writing	data	to	C:\Users\Onjefu\AppData\Local\Temp\WB_ONJEFU- PC_Onjefu_1080_2\unsaved_project_files\dp0\FFF\Fluent\FFF.ip ...

x-coord y-coord z-coord

pressure

x-velocity y-velocity z-velocity

temperature hyb_init-0 hyb_init-1

Done.

Calculation complete.

4%

SIMILARITY INDEX	INTERNET SOURCES	PUBLICATIONS	STUDENT PAPERS

PRIMARY SOURCES

2%

Submitted to Swinburne University of

Technology

Student Paper

1%

D. W. Etheridge. "Ventilation, air quality and airtightness in buildings", Materials for energy

efficiency and thermal comfort in buildings, 2010

Publication

II	1%

S. Wu. "Heat energy storage and cooling in buildings", Materials for energy efficiency and thermal comfort in buildings, 2010

Publication

II www.cfd-online.com	19'

Date Report no. Test owner Test tool

Test arrangement

Standards

Tester

l

Test report

Test report ace.EN 12667 and EN12664 paragraph 9

2017/09115

40percentage fine rice-G061

Lambda-Messtechnik GmbH Dresden

Thermal Conductivity Meter 'lambda-Meier EP500e' ace.lo EN 1946-2 by Lambda-Messlechnik GmbH Dresden

Sensor plales horizonta,l hot plale onlop

Measurement with sensor films and compensation pads of ...m theckness

Thickness measurement ace. to EN 823

Thermal conductivity measurement ace. to ISO 8302 and EN 12667

->onjefu Leonard

Specimen designation Origin of specimen Date of manufact. Materialname Materialdescription

40percentage fine rice

German manufacturer

agric resdi ue

PS 30 SE according to EN 13 163

Specimen dimension

Area

Thickness

Nomni al thickness

Specimen mass

Raw density

100 mm x 220 mm

73.9 mm

75 mm

2707 00 g

1665.00 kglm'

Spec.pre-conditoi ning	Stored al...%air humidity and ...'C for ... days before lesting

ChangeIn mass during:

drying test

n •t.

Date Report no. Test owner Test tool

Test arrangement

Standards

Tester

l

Test report

Test report ace.EN 12667 and EN12664 paragraph 9

2018/02/27

sample new c-G022

Lambda-Messtechnlk GmbH Dresden

Thermal Conductivity Meter 'lambda-Meter EP500e' ace. to EN 1946-2 by Lambda-Messtechnlk GmbH Dresden

Sensor plates horizontal,hot plate on top Measurement with sensor films and compensation pads of ...m theckness

Thickness measurement ace. to EN 823

Thermal conductivity measurement ace. toISO 8302 and EN 12667

·>onjefu Leonard

Specimen designation Origin of specimen Date of manufact. Materialname

Material description

sample newc

German manufacturer

agrlc residue

PS 30 SE according to EN 13 163

Specimen dimension

Area Thickness Nominalthickness

Specimen mass

Raw denstiy

110 mm x 220 mm

37.9 mm

40 mm

779.00 g

849.30 kg/m'

Spec.pre-conditioning	Stored at ... % air humidity and ... ' C for ...days before testing

Change in mass during:

drying

sample new c - G022 at 1o·c

C:UI sersiStudenN...ambda Messtechnik\UserDataiMJster_ENG.DBF

2018/02/14 06:07:01 PM

Po = 17.49s c Pu = 2.5oo c

58·--g	.r	I rv 	.. i\4-J\

., '"

lnJ\ \.

56

54

E

52	I

(\

k  ll

r"v"·''

"

"''"

YJ\h

I l.	n \ 	....

3

.Sso

(I)

:g 48

.ft.I

U,Jl' •

I U\1 	1\1 	.........

'

E   ·-§	IV

.!!l 46

]

44·'Z

;

•	I	•	I	I	I

t [min]

1. Test

Test no.	G022_10

Meas.temp.in•c	10

Dfif.temp.inK	15

Lambda In mWfm•K    50.71

R In m2KIW	0.7474

iC) 2004-2016 Lamllda-MmlechnlGmbHDr

Lambda-10

R-10

TC

54.65 mW/(m•K)

0.6935 m••KfW

2.2660 mW/(m'K)'

2018/02127

signature

Date Report no. Test owner Test tool

Test arrangement

Standards

Tester

1

Test report

Test report ace.EN 12667 and EN12664 paragraph 9

2018/02127 sample A·G061

Lambda·Messtechnlk GmbH Dresden

Thermal ConducUvlty Meier 'lambda-Meter EP500e' ace. to EN 1946-2 by Lambda-Messtechnlk GmbH Dresden

Sensor plates horizontal, hot plate on top

Measurement with sensor films and compensaUon pads of ...m theckness

ThiCkness measurement ace. to EN 823

Thermal conductivity measurement  ace. to ISO 8302 and EN 12667

->onjefu Leonard

Specimen designation Origin of specimen Date of manufact. Materialname

Material description

sample A

German manufacturer

agric residue

PS 30 SE according to EN 13 163

Specimen dimension

Area Thickness Nominalthickness

Specimen mass

Raw density

110 mm x 220 mm

40.3 mm

40 mm

912.00 g

935.10 kglm'

Spec.preo(;ondltlonlng	Stored at ...% air humidity and ... ' C for ...days before testing

Change In mass during:

drying test

Humidity before test	0 %

Pressure	500 Pa

-------------------------------------------------

sample A - G061_2017-11-19_001 a123•c

C:lllsets\SIUdenN..ambda Messtechnlk\UserOata\MJster_ENG.DBF

2017/11/19 01:33:14 PM

Po = 3o.soo c Pu = 1s.s2s•c lambda= 103.62 mWI(m•K)

105.5

""105

:' 104.5;:1

I 	\	I	1 \ 	I

' 	v-	I	:_	\

I	I	I

E 	.00

II	\ 	"\.	/\.	I

I

104.<!0'

.s 103.5	r

1"0'3     -

\... 	\

E 102.5,:1

I	......    ./	\.

/'-

102	I 	I

0 	10	20 	30	40 	50	60	70	80 	90    100  110  120  130  140  150  160  170  180  190  200

t(mln)

1. Test

Test no. 	G061_2017-11-19_001_23

Meas.temp.In •c 	23

Dlff.temp. In K	15

Lambda In mWJm•K 	100.71

R In m'KJW	0.4002

Lambda-10 	    0.00 mW/(m·K) R-10	0.0000  m.,KIW

TC	0.0000  mW/(m.K')

2018/02127

signature

NAMIBIA UNIVERSITY OF SCIENCE AND TECHNOLOGY

FACULTY OF ENGINEERING

DEPARTMENT OF CIVIL & ENVIRONMENTAL ENGINEERING Ph.D. (ENG) IN STRUCTURAL ENGINEERING

CANDIDATE’S RESPONSES TO QUESTIONS FROM EXAMINERS DURING ORAL PRESENTATION

| S/ N | Examiner’ s name | Examiner’s comment | Candidate’s response/approa ch | Relevant section response captured | Candidate’s comment |
| --- | --- | --- | --- | --- | --- |
| 1. | Prof. Schneide r (External Examiner 1) | Possible contact with local, regional, and international industries to test and commercialize your findings in thermal resistivity of insulating boards from agricultural residues/wast es | Yes, since this will contribute to the design and construction of affordable energy-efficient housing. | This is captured in chapter 2, section 2.3.5, and paragraph 3 i.e. page 21 of the thesis work. Also section 7.3.3 paragraph 2 page 132 | Examiner’s comment is adequately addressed and captured in the final research work |

| 2. | Prof. Schneide r (External Examiner 1) | What do you think might be the reason for relatively small temperature differences between the inside and outside of the rigs | This might be attributed to inadequate air tightness and less/no insulation at the doors and windows of the rigs. | This is captured in the discussion and recommendation sections i.e. Chapter 5, section 5.4, page 117. Also, section 7.3.5 page 133 of the thesis | This is a very important aspect that will be recommend ed if the findings in this research are to be expanded in the future. |
| --- | --- | --- | --- | --- | --- |
| 3. | Prof. Schneide r (External Examiner 1) | What are the uniqueness and contribution of marble dust in your sample results | Percentage increase in marble dust in samples with best and worst thermal resistivity revealed the usefulness of marble dust in the mixed design | This was already adequately explained and concluded in the current version of the thesis work. Chapter 4 subsection 4.2.2 page 73. The uniqueness and contribution are concluded in Chapters 7 section 7.2.3 paragraph 2 page 130. | This result is key in achieving a key specific objective of this research that was adequately achieved. |
| 4. |  | Possible approaches to improve the workability (i.e. water absorption, relative density, etc.) of bricks produced | This is a valid point that will be investigated in future researches | This is mentioned in the recommendation section i.e. chapter 7, subsection 7.3.4 page 133 of the final version. | This will form part of any future researches on this topic |
| b. | Prof. Inambao (External examiner 2) | Any locally accepted insulating material standards in Namibia and to what degree are they been implemented | Yes, Such facts are indicated in the findings of the National Building Code in the literature of this thesis | This is captured in my literature i.e. chapter 2 of section 2.4.3 pages 21 to 23. Also, section 3.4.1.1 page 62 of the thesis that gives the relevant standard for insulating materials. | A piece of important information that will inform researchers on the developmen t and application of insulating materials in civil engineering buildings |
| 2. |  | To explain the indoor comfort / | Such temperatures are 200C and | This is adequately captured and explained in chapter 2, sections 2.6.1 of pages 26. | Such information is critical in |

|  |  | optimum temperature in building in old and hot seasons in Namibia | 240C in winter and summer respectively for building made of conventional materials ASHRAE (2011 |  | motivating the rationale of this research, hence forms part of my introductory statements in earlier chapter two of my research. |
| --- | --- | --- | --- | --- | --- |
| 3. |  | Briefly highlight your major contribution to such researches | Developing appropriate thermal insulating boards and bricks from local agricultural residues/waste s that are widely available, and in-situ measurements performed to measure their effectiveness by constructing rigs of varying design parameters | This is captured in chapter 7 section 7.2, pages 129 -131 of the final thesis work | This answer a fundamental question in any Ph.D. research |
|  | Others Evaluato rs |  |  |  |  |
| 1 | Others | Why is there inconsistent changes in thermal Conductivity between 60% - 80% mixture | Table 4.3 - 4.6 of my thesis section 4.2.3 shows different mix designs with Agricultural residues. | It can be seen from Fig.5.3 that with 80% of Agricultural residues lead to an increase in thermal conductivity which shows that from 20% to 60% from Fig.5.3 exhibits a linear relationship that is K = (1 +𝛽��)K0 in most cases when K0 = thermal Conductivity at zero temperature. When the effect of temperature on thermal conductivity is | Examiner’s comment is adequately addressed and captured in the final research work of my thesis on page 110 - 111, subsection 5.2.2, |

considered, the Fourier’s equation	Q=

��

paragraph 4, page 110

-kA

��

is written as:

��

Q= -k0(1 + 𝛽��)	.A

��

Thermal conductivity

300

Thermal

Conductivity/Percentage mix

200

100

0

0	20	40	60	80	10

Percentage mix

Thermal Conductivity of Rice husk Thermal Conductivity of Maize husk Thermal Conductivity of Cow dung Thermal Conductivity of Millet husk

Fig. 5.3. Thermal conductivity versus percentage mix of Agricultural residues

It can be seen from Fig.5.3 that the thermal conductivity of rice increases as the percentage mix of agricultural residue increase  from  20%  to  40%  because  the

equation K = (1 +��𝑚���)K0  it shows that the

value    of    the    coefficient    of    thermal

conductivity 𝛽 < 0 therefore, the  thermal

conductivity will increase from 20% to 40 %.

From 40% to 60% there is a decrease in

thermal conductivity which shows the 𝛽 >0,

and   from   60%   to   80%   the   thermal

conductivity rises that shows that 𝛽 < 0.

2	What is the Fundamental law of Conduction

The equation to measure conduction   is

This law is sated as:	This is captured in Chapter 6, sections 6.5, Fig. 6.7,

the	Fourier law

page 124 of the final thesis work.

T1

H	T2

L	x

−�𝐴∆�

Q =

𝑋

Where,

Q= Heat transfer rate [W].

A = Area, L x H, in heat flow direction [m2]. k = Material thermal conductivity [W/m K] ΔT = T1-T2, Temperature [K]

x = Brick Thickness [m

3	Others	What is the state of air inside a building

4	Others	What is the novelty of your research work in terms of environmenta l benefits?

5	Others	Are you sure the number of tons of millet, maize, and

Inside a building, the state of air is free

convection

Agricultural residues	 and marble		dust for	energy- efficient housing

Yes, Such facts are indicated in the  findings  of

The Rayleigh number and the Grashoff number are required to determine convection. The relevant equations for Rayleigh number, Grashoff number, the Prandtl number, and Nusselt number are captured in the thesis work.

This was already adequately explained and concluded in the current version of the thesis work. This is reflected in chapter 7, section 7.2 of the final version paragraph 1 page 129.

This is captured in my literature i.e. chapter 2 of section 2.2 pages 15 to 20

Examiner’s comment is adequately addressed and captured in the final research work Chapter 2 section

2.13.4 -

2.13.6  page

39-40. Evaluator’s comment is adequately addressed and captured in the final research work.

Key information that will inform

|  |  | rice produced in Namibia is that big? | my Literature in Chapter 2. |  | researchers on the Importance of Agriculture in Namibia. |
| --- | --- | --- | --- | --- | --- |

Verified by:

……………………………………………….	…………………………………………………

Prof. Victor Kamara	Prof. Paul Chisale

(Main Supervisor)	(Co-Supervisor)

Verified by:

……………………………………………….	…………………………………………………

Prof. Victor Kamara	Prof. Paul Chisale

(Main Supervisor)	(Co-Supervisor)